## Slide 1: Semi-conductor Detectors HEP and Accelerators
Geoffrey Taylor
ARC Centre for Particle Physics at the Terascale (CoEPP)
The University of Melbourne

## Slide 2: Outline
Semiconductor Detectors
  A Brief Overview
  Radiation Damage
Silicon Strip Detectors
Pixel Detectors
  Hydrid Pixel Detectors
  Integrated Devices
    MAPS
    DEPFET
    HV-CMOS and HR-CMOS
  3D geometry
Diamond Detectors
LHC
SuperKEKB
Outlook

## Slide 3: Basics
Kemmer Process (eg. NIM 226 (1984) 89-93)
Basic Semiconductor materials:
  Silicon
  Ge
  GaAs
  CdTe
  CdZnTe
  Diamond
  Silicon Carbide, …

## Slide 4: Semiconductor Detectors
Semiconductor Diode detectors have been used, and highly evolved for decades.
Technology highly developed but high specialised.

## Slide 5: Sophisticated integration …

## Slide 6: Double-sided Silicon Detectors

## Slide 7
n-side (back-side)
  positive (fixed) charge at SiO2 - Si interface attracts electrons to n-side.
  Electron accumulation shorts n-side electrodes
  p+ “isolation” required
e- accumulation layer
Oxide layer

## Slide 8: Radiation Damage
Three main macroscopic effects are seen in high-resistivity diodes following energetic hadron irradiation:
Change of the doping concentration with severe consequences for the operating voltage needed for total depletion.
Fluence proportional increase in the leakage current, caused by creation of recombination/generation centres
Deterioration of charge collection efficiency due to charge carrier trapping leading eventually to a reduction in the signal height produced by mip’s.

## Slide 9
Defect Engineering
Thin detectors
High Bias Operation

## Slide 11: Effect of Temperature
Strong current reduction with reduced temperature.
(also Current Annealing)
Reverse Annealing of Effective Carrier concentration

## Slide 12: Hybrid Pixel Detectors
Electronics chip and sensor chip independently produced, bump bonded

## Slide 13: Integrated Pixel Detectors - MAPS
Electronics and detector element on a single substrate

## Slide 14: Silicon Drift Detectors
Positive Electrodes set up Drift Potential
Electrons drifted to readout anode pads.
Time/position -> 2D position.
F. Hartmann, Springer, 2009

## Slide 15: Integrated Pixel Detectors - DEPFET
Belle II Pixel detector

## Slide 16: Thinning of silicon detectors
eg. Belle II PXD
Rather complicated process.
Major benefits

## Slide 17: Integrated Pixel Detectors: HV-CMOS and HR-CMOS
With a High Resistivity Substrate, the deplection region can be increased over that of the MAPS detectors.
CMOS processing widely available, adaptable to HV and HR modification

## Slide 18: HR-CMOS Options
Drift structure
Triple Well Structure
Simple well structure

## Slide 19: Integration Possibilities, HV-CMOS/HV-CMOS Hybrid Pixel Development
Amplifier / Discriminator (~100 transistors) per Pixel, Bonded to Digital R/O Chip (>100M transistors)
Long-term aim: full integration on single, depleted substrate:
F.Hugging, Bonn - AIDA-2 15/4/2014

## Slide 21: ATLAS Diamond Beam Condition Monitor and Beam Loss Monitor

## Slide 22: Diamond Beam Monitor
Diamond offers advantages:
  radiation hardness
  fast signal response
  simple processing

## Slide 23: Diamond Detectors
Diamond Beam Monitor
IBL Pixel Layer

## Slide 24: Si/Diamond as Cryogenic BLM
Both seem capable of operation at LHe temperatures
Suggest operation of BLM within magnet cryostat
Kurfurst et al., NIM A782 (2015) 149

## Slide 25: LHC
Diamond detectors in beam monitoring.
3-D Detectors in ATLAS vertex detector

## Slide 26
From talk, J. Lange, ATLAS 3D Group
RD50 Workshop 22-24 June, 2015

## Slide 28: “Forward” Physics Detectors
Very small angle proton scattering:
  Good spatial resolution (~10um)
  Sensitivity close to edge.
  Good radiation intolerance.
  3D detectors very promising.

## Slide 29
J. Lange et al., JINST 10 (2015) C03031

## Slide 30: SuperKEKB - Diamond Beam Monitor
Belle II Pixel and Strip Vertex Detector (VXD) Abort monitors

## Slide 31: Belle II PXD Beam Abort

## Slide 32
– Based on experience from Belle, BaBar, CDF, LHC
– scCVD diamond sensors, measurement of currents:
          - typical pCVD sensor @ 500V:
                1nA = 7 mrad/s = 70 μGy/s
          - Noise a few pA, in current measurements

## Slide 33: Outlook
Silicon and Diamond detectors effective for both HEP detectors and Beam Monitoring / Beam Loss role.
Pixel devices essential for high rate / high luminosity environments (SuperKEKB, LHC, HL-LHC)
Si and Diamond capable of cryogenic operation
HR-CMOS, HV-CMOS offer future technology for significant integration options.