## Slide 1: Materials science research at Indus beamlines
Tapas Ganguli
Accelerator Physics and Synchrotrons Utilization Division
Raja Ramanna Centre for Advanced Technology
INDIA

## Slide 2
Plan of the presentation:
Introduction to Indus Synchrotrons
Brief details of the beamlines at Indus
Some examples of interesting research carried out by users
Brief review of materials research at APSUD, RRCAT (Intermetallic alloys, large bandgap oxides)

## Slide 3
Plan of the presentation:
Introduction to Indus Synchrotrons
Brief details of the beamlines at Indus
Some examples of interesting research carried out by users
Brief review of materials research at APSUD, RRCAT (Intermetallic alloys, large bandgap oxides)
ACKNOWLEDGEMENT
All the users who have used the beamlines for their research
The machine operation and maintenance team at Indus
All the beamline scientists
This presentation is on behalf of all them

## Slide 4
Indus Accelerator Complex: A schematic
Indus–1 and Indus-2 synchrotron radiation sources are in operation in round the clock mode, since Feb 2010
Indus-2
2.5 GeV
TL3
TL1
TL2
550 MeV, 10 mA
450 MeV, 125 mA
Booster
Indus-1
Microtron
20 MeV, 30 mA
200 mA
Operational beamlines in Indus-1: 7
Operational beamlines in Indus-2: 18
Indus-2 details
Lattice Double bend achromat
No. of periods: 8
Provision for 5 insertion devices, with 3 operational devices
Current operating emittance: 135 nm rad (plans underway to reduce it to < 50 nm rad)

## Slide 5
Indus at a glance:
A section of Indus-2 storage ring
Planar permanent magnet undulator
APPLE-II undulator
Frontends for beamlnes (Indus-2)
Indus-1 storage ring
Experimental area of Indus-2

## Slide 6
Operational beamlines in Indus-2: 18
Atomic molecular and optical Sciences
Extreme conditions XRD with a superconducting wavelength shifter
Protein crystallography with a superconducting wiggler
Spectroscopy and scattering in the tender x-ray range
Radiation safety studies
Photo emission electron microscopy
Some beamlines are under development
BL-1 Soft X-ray Absorption
BL-2 Engineering Applications
BL-3 Soft X-ray Reflectivity
BL-4 X-ray Imaging
BL-7 X-ray Lithography
BL-8 Dispersive EXAFS
BL-9 Scanning EXAFS
BL-10 Angle Resolved
Photoelectron Spectroscopy
BL-11 Extreme Conditions X-ray Diffraction
BL-12 Angle Dispersive X-ray
Diffraction
BL-13 Grazing Incidence X-ray
Scattering
BL-14 X-ray Photo Electron
Spectroscopy
BL-16 X-ray Fluorescence
Microprobe
BL-18 Small and Wide Angle X-ray
Scattering
BL-20 X-ray Magnetic Circular Dichroism
BL-21 Protein Crystallography
BL-23 Visible Diagnostics Beamline
BL-24 X-ray Diagnostic Beamline
More details at: http://www.rrcat.gov.in

## Slide 7
Number of user experiments
Number of publications
Scientists are researchers from nearly 150 institutes all over India have used the Indus beamlines
In the last few years, Indian industries (pharmaceutical industry) are also regularly using Indus beamlines
Facilities have contributed to several projects of national importance: Lunar missions of Indian Space Research Organisation (ISRO), Chandrayaan-I and Chandrayaan-II.
About 160+ structures deposited in the international protein data bank
Some typical user data:

## Slide 8: Facilities for X-ray diffraction and scattering
Angle dispersive XRD beamline, BL-12
High pressure cell
Low temp. ~5 K
Extreme conditions XRD Beamline BL-11
Engineering Appl. Beamline, BL-02
Energy range: 4 keV - 25 keV
Measurements for stress, phase analysis etc.
Designed for Engg. Components weighing upto 15 Kgs
Elastic constant measurements
Energy range: 4 keV to 25 keV
Both Goniometer and image plate options available
Low temperature upto ~ 5 K
High temperature upto 550oC
High pressure in Diamond cell
Crystal structure determination, phase identification etc.
Both energy dispersive and angle dispersive options available
Energy range: 4 keV to ~ 40 keV in the energy dispersive mode
High pressure and high temperature ~1200oC
Experimental station
Small and wide Angle X-ray scattering, BL-18
Experimental station
Energy range: 5 keV – 20 keV
2-Dimension online image plate (SAXS); q-range: 0.05 – 3.5 nm-1
Linear position sensitive gas detector (WAXS) q-range > 2.0 nm-1
Structural correlation in ~1-100 nm length scale

## Slide 9
Facilities for X-ray absorption
Energy range: 4 keV to 25 keV
Low temperature upto ~ 10 K
Measurement in transmission and fluorescence mode
Facilities to perform in-situ/in-operando studies
Near neighbor configuration, chemical state
EXAFS beamline,
BL-09
Polarized light Soft
X-ray beamline, BL-01
X-ray Magnetic Circular Dichroism beamline, BL-20
Energy range: 300 eV to 1000 eV (circular polarization)
Energy range: 300 eV to 2000 eV (linear polarization)
Low temperature upto ~ 20 K
Measurement in transmission and fluorescence mode
Magnetic field upto 1 Tesla
Element specific magnetic moment
Energy range: 100 eV to 1200 eV
Low temperature upto ~ 10 K
Facility for absorption in fluorescence and TEY mode
Near neighbor configuration, chemical state

## Slide 10
Some other beamlines
X-ray Fluorescence Microprobe BL-16
Energy range: 4 keV to 20 keV
Element detection down to Carbon
Microprobe 4.5 x 7.5 micron2
Total reflection XRF available for trace element detection, ppb level
Angle Resolved Photoelectron Spec. BL-10
Energy range: 30 eV – 1 keV
20 meV resolution at 30 eV
Sample temperature ~ 20 K
Determine the electronic density of states and band structure
Soft X-ray Reflectivity BL-03
Energy range: 100 eV - 1500 eV
Reflectivity measurements of thin films
To be upgraded with an wavelength dispersive emission spectrometer
Buried interface quality, intermixing
X-ray imaging BL-04
Energy range 8 to 35 keV
Absorption imaging
Phase contrast imaging
Micro tomography
Laminography

## Slide 11
Some examples of interesting research carried out by users at Indus beamlines

## Slide 12
Study 1: High Performance Lithium-Ion Batteries Using Layered 2H-MoTe2 as Anode
Study 2: Fast Anodes for Lithium-Ion Batteries Based on the 1T′-MoTe2 Phase Material
In-operando studies on Li ion batteries
Ref:
M.R.Panda et al. Small, Vol. 16, No. 2002669 (2020)
M.R.Panda et al. ACS Appl. Energy Mater., Vol. 5, pp 9625–9640 (2022)
The X-ray absorption studies on battery anode materials with different extent of lithiation gives a picture of the changes that take place with charging and discharging.
Unique lithium reaction pathway and storage mechanism, which is supported by density functional theory based calculations.
In-operando studies on the chemical and structural changes taking place in the anode, with charging and discharging have also been reported.
Schematic of the Synchrotron based XANES measurement setup

## Slide 13
In-situ X ray Abs. Spect. study of Co catalysts
In-situ studies on structure-activity correlation during catalytic reaction
Co based catalyst during Fischer-Tropsch reaction for the generation of CH4 from CO + H2 reaction was studied
Schematic of the setup
established
Ref.: C.Nayak et al. J. Synchrotron Rad.
Vol. 26, p 137, 2019
SBA-15 supported Co3O4 nanoparticle catalysts has been studied
It has been observed that with reaction temperature increasing from 280ºC-320ºC, activity of the catalyst increases significantly
Deactivation of the catalyst also observed with time.
XANES data rules out the formation of CoO as the cause of deactivation
Tentatively deactivation attributed to carbon deposition on the catalyst surface.

## Slide 14: Observation of RT ferroelectricity in spark-plasma sintered GdCrO3
GdCrO3 prepared by solid state synthesis is paramagnetic at room temperature
Spark plasma sintered GdCrO3 is ferromagnetic upto 450K
Structural refinement of high quality XRD data used to explain this observation
The previously known low temperature phase orthorhombic Pna21 was stabilized at room temperature by Spark plasma sintering method
High resolution, low noise XRD data helped in resolving the fine differences in the XRD pattern of the two phases.
Ref.: Suryakanta Mishra et al. Phys. Rev B 104, L 180101 (2021)
XRD patterns of the two samples,
comparison of the peak profiles in the inset

## Slide 15
Some other user results ….
Green Conversion of Hazardous Red Mud into X-ray Shielding Tiles
Ref.: Varsha Agrawal et al. J Hazardous Material, Vol. 424, p 127507 (2022)
Red mud is a solid hazardous alumina industrial waste, rich in iron, titanium, aluminum, silicon, calcium, etc.
The red mud contains 30–60% of hematite, thus suitable for shielding high energy X-rays and gamma rays.
Iron rich red mud was converted into diagnostic X-ray shielding tiles through ceramic route
Diffraction data of red mud indicating the several components present in the sample
Interfacial structure of epitaxial lattice-matched TiN/Al0.72Sc0.28N superlattices
Ref.: Bidesh Biswas et al. J. Vac. Sci. Technol. A Vol. 38, p 053201 (2020)
Metal-semiconductor TiN/(Al,Sc)N superlattices have attracted significant interest in recent years for thermoelectric applications
Interface plays a key role in determining its properties
TiN/(Al,Sc)N interfaces are abrupt, with an asymmetric interface roughness ranging from two-to-three unit cells.
Secondary structure or phase formation at the interfaces.
Understanding transport properties of metal-semiconductor structures for devices
Experimental and simulated scattering profile

## Slide 16: Study of interface reaction in a B4C/Cr mirror at elevated temperature using soft X-ray reflectivity
Boron carbide coated x-ray mirrors are used in high brilliance synchrotron beamlines.
In-situ annealing of B4C/Cr sample and soft x-ray characterizations are performed at Indus-1 reflectivity beamline.
At elevated temperature, reaction takes place at Cr/SiO2 interface
Soft x-ray reflectivity and SIMS analyses reveal that Cr diffuses towards Si substrate after 500oC temperature.
In this study the principal boron carbide layer was found intact upto 550oC temperature
Ref.: M.H. Modi et al. J. Synchrotron Rad. (2022). 29; /doi.org/10.1107/S1600577522004738
Schematic of the structure
Reflectivity with sample temperature

## Slide 17
Development of adaptable refractive correctors for X-ray optics
Advances in x-ray sources put greater demands on x-ray optics.
Fabrication errors in optical elements lead to deformation of the radiation wavefront, which prevents diffraction-limited imaging of the source.
Adaptable x-ray phase compensator using refracting elements has been fabricated at the X-ray lithography beamline BL-07 at Indus-2 and tested/used at Diamond light source UK.
Ref:
David Laundy et al. Optica , Vol. 6, p 1484 (2019)
T. E.J. Moxham et al. Optics Express, Vol. 30, p 19185 (2022)

## Slide 18
Brief review of materials research at APSUD, RRCAT
(Intermetallic alloys, large bandgap oxides)

## Slide 19
Ni:Ga0.9Cr1.1O3: A new p-type large bandgap semiconductor
Cr2O3 although is a p-type conductor, has poor conductivity
Our approach: Substitute Ga with unfilled p-levels, that increase the O 2p and Cr 3d level hybridization
Can be grown epitaxially on available substrates like Sapphire
Ni substitution further increases p-type conductivity
Single phase polycrystalline α-(NixGa0.9–x)Cr1.1O3 (0 ≤ x ≤ 0.02) synthesized by solid-state reaction method.
Ni doping improves delocalization of charge carriers, which results in reduction of resistance by around 104 times wrt. undoped material
p-type α-(Ni0.01Ga0.89)Cr1.1O3, with band gap of ~3.95 eV and work function of ~5.2±0.2 eV, is suitable as a hole transport layer in photovoltaic devices.
Ref.: R.Jangir et al. ACS Appl. Energy Mater. Vol. 5, p 8629 (2022); R. Jangir et al. J. of Alloys and Comp. Vol. 766, p 876 (2018)
Ni doped GaCrO3
Ni doped Cr2O3
Photoelectron spectra
Cr 3d
O 2p
Resistance vs T
Atomic configuration
Band alignment from PES data

## Slide 20: Revealing superstructure ordering in Co1+xMnSb Heusler alloys and its effect on physical properties
C1b structure
Superstructure
RT powder XRD patterns
Role of structure in enhancing the magnetic moment per formula unit of CoMnSb
Understand the progressive evolution of crystal structure and related physical properties in Co1+xMnSb (0 ≤ x ≤ 1) through a combined experimental and theoretical study
Detailed powder XRD and Rietveld refinement results: All samples show superstructure ordering; Max. Co concentration accommodated is ~ 0.45.
Superstructure is the key to the increased magnetic moment per formula unit, from 3 mb to 4 mb per formula unit
Ref.: Madhusmita Baral et al. Phys. Rev B 105, 184106 (2022)

## Slide 21
Thank you very much