## Slide 1
Progress of the High Field Magnet Technology
for the High-energy Particle Accelerators
Qingjin Xu
for the Superconducting Magnet Group at
the Accelerator Division, IHEP
Mar 30 2023
中国科学院高能物理研究所
Institute of High Energy Physics, CAS
李政道研究所-粒子与核物理研究所联合报告
AFAD2023, Melbourne, Apr. 12-14 2023

## Slide 2
2018
2019
2021
~90% SSL
R&D of the High Field Model Dipoles
2

## Slide 3
16 T Model Dipole: Nb3Sn 12~13 T + HTS 3~4 T
R&D of the High Field Model Dipoles
3

## Slide 4
R&D of the High Field Model Dipoles
Stress distribution in different loading steps
Assembly
4.2 K
13 T
4

## Slide 5
R&D of the High Field Model Dipoles
The calculation indicates that the temperature of hot spot is 237 K and the max voltage is 952 V. Safe.
5

## Slide 6
R&D of the High Field Model Dipoles
16-T Dipole with CCT configuration
Canted-Cosine-Theta (CCT) technology;
  Superior field quality;
  Stress management
  Developed industrial assembly line;
Graded Nb3Sn Rutherford cables;
Multiple replaceable coil modules;
The geometry of the 4 module CCT magnet
At 4.2 K, the magnet produces 16 T at 100% load-line with 8.8 kA operating current
CCT subscale
6

## Slide 7
R&D of the High Field Model Dipoles
Harmonics：10-4 | b2 | a2 | b3 | a3 | b4 | a4 | b5 | a5 | b6 | a6 | b7 | a7 | b8 | a8
Cross section-2D | 0.6259 | 0.0119 | 2.9824 | -0.0006 | 0.0537 | 0.0002 | 0.5189 | 0.0002 | 0.0183 | -0.0020 | -0.0845 | 0.0016 | -0.0036 | 0.0009
Integrated-3D | 1.5989 | 0.0101 | 3.8649 | -0.0320 | 0.3047 | 0.0802 | 1.4069 | -0.0175 | 0.0750 | -0.3695 | 0.1163 | 0.0734 | -0.0223 | -0.2090
High-order harmonics along axis - Bn
High-order harmonics along axis - An
7

## Slide 8
R&D of the High Field Model Dipoles
J. Wang et al, Superconductivity 3 (2022) 100019
8
Development of a Roebel-like Transposed Cable with the in-plane bending of HTS tapes

## Slide 9
Development of a Roebel-like Transposed Cable with the in-plane bending of HTS tapes
R&D of the High Field Model Dipoles
9

## Slide 10
R&D of the High Field Model Dipoles
Challenges: Stress control, quench protection, field quality control,……
Roadmap for Future
10

## Slide 11
Chart: Applied Magnetic Field (T)
| 0 | 5 | 15 | 20 | 25 | 30
REBCO: B ∥ Tape plane | 4144.6766 | 3507.9375 | 3148.3332 | 2909.0554 | 2090.4933 | 1888.9952
REBCO: B ⊥ Tape plane, 45 μm sub | 5478.1345 | 5053.3515 | 4372.0346 | 3812.2534 | 3348.8068 | 3146.724 | 2964.7726 | 2801.365 | 2663.2305 | 2530.35 | 2415.161 | 2307.3222 | 2215.5971 | 2121.427 | 2046.7953 | 1970.1838 | 1905.1216 | 1841.6283 | 1784.4676 | 1729.8653 | 1682.3664 | 1631.1403 | 1591.3007
REBCO: B ⊥ Tape plane | 4144.6766 | 1445.8386 | 975.0997 | 767.7508 | 655.6687 | 571.6114 | 526.7777 | 481.944 | 442.7183 | 428.1462 | 403.4904 | 386.6773 | 364.2626 | 341.8457 | 328.3952 | 319.4289 | 318.3073
Bi-2212: OST NHMFL 50 bar OP | 1243.4169 | 1159.7904 | 1097.571 | 1051.5861 | 1014.8275 | 981 | 955.0755 | 928.7776 | 905.6283 | 884.9933 | 865.478 | 846.7181 | 827.3047
Nb₃Sn: Internal Sn RRP® | 1754.8557 | 1454.9349 | 1190.9814 | 1072.6374 | 957.7741 | 855.0933 | 757.6336 | 268.0143 | 190.8587 | 118.9241 | 65.5533 | 28.3097
Nb₃Sn: High Sn Bronze | 166.6431 | 137.8146 | 111.0954 | 84.3762 | 60.8212 | 40.0788 | 19.3362 | 8.0861
Nb-Ti: LHC 4.2 K | 5106.8846 | 4054.1538 | 3180.5962 | 2710.2269 | 2217.4577 | 1724.6885 | 1411.1115 | 1187.1231 | 918.3423
Nb-Ti: Iseult/INUMAC MRI 4.22 K | 393.4783 | 291.3043 | 194.203 | 104.3478
Exponential Y-axis Labels | 10 | 100 | 1000 | 10000
Nb-Ti midrange maximal | 971.9231 | 687.3077 | 448.4615 | 393.4783
2212 Fitted Line for 50bar ASC'16 | 1381.5217 | 1248.5735 | 1162.079 | 1099.1369 | 1050.2486 | 1010.6145 | 977.4929 | 949.1799 | 924.5486 | 902.818 | 883.4258 | 865.9547 | 850.0872 | 835.5764 | 777.6921 | 691.6232
YBCO B perp linear extrap | 312.7055 | 264.5487 | 240.4379
IBS 2016
IBS 2019
IBS 2022
IBS 2025
IBS Technology: Status and Outlook
Stainless-steel stabilized IBS tape achieved the highest Je in 2022!
Significantly reduced the cost and raised the
mechanical properties.
11

## Slide 12
IBS Technology: Status and Outlook
Ic of Φ34mm-17 turns-DPC reached 60 A at 4.2 K and 32 T, world’s highest record up to now.
The First IBS Solenoid Coil at 32 T background field
12

## Slide 13
IBS Technology: Status and Outlook
13
Quench propagation study of the IBS coils
Experimental data shows significant quench propagation in the IBS coils! More testing will be carried out.

## Slide 14
IBS Technology: Status and Outlook
2008.02
2008.09
2016
2018
Discovery of IBS
2008.04
Discovery of
122 phase IBS
2020
100-m 7-core IBS tape fabricated
Je= 100 A/mm2
@ 10 T, 4.2 K
IBS solenoid at 24 T
Racetrack at 8 T
Je= 300 A/mm2
@ 10 T, 4.2 K
IBS solenoid at 32 T
Racetrack at 10 T
1.3 kA transposed cable
Je > 450 A/mm2
@ 10 T, 4.2 K
2022
H. Hosono
IBS (Tc 26K)
Z. Zhao
IBS (Tc 55K)
Je of IBS expected to be similar as ReBCO in 5 years with better mechanical properties and lower cost
14

## Slide 15
All the magnets delivered to CERN passed the performance double-check at 1.9 K.
Test results of the 1st full-length prototype from China:
“Each aperture, individually and combined, arrived to ultimate current without quench”
“Operation range test checked without quench”……
Development of CCT Magnets for HL-LHC
To be installed in the ATLAS & CMS interaction regions, help to raise the luminosity by 5 times
The 1st time CCT type magnets applied to an operating accelerator.
China provides 13 units CCT twin-aperture dipole magnets for HL-LHC
15

## Slide 16
Development of CCT Magnets for HL-LHC
Items | Values
CCT skew angle | 30°
No. of turns per layer | 365
Slot size in former (mm) | 2×5
Spacing per turn | 5.222
Inside/Outside diameter of the former (mm) | Inner former:105.35/119.35 Inner former:120.80/134.85
Inside diameter of the groove/slot(mm) | 1st layer: 109.15/119.15 2nd layer: 124.65/134.65
Reference radius (mm) | 35
Diameter of aperture (mm) | 105
Current (A) | 395
Ø 614 mm
Aperture
Cooling hole
Hole for tie rod
Yoke alignment
CCT Coils
Items | Values
Diameter of yoke (mm) | 614
Thickness of yoke lamination (mm) | 5.8
Diameter of aperture (mm) | 167
Position of aperture (mm) | 94.19
Yoke key slot(mm) | 8(3.01) ×6
Diameter of cooling hole (mm) | 110
Position of cooling hole (mm) | 205
16

## Slide 17: Training of MCBRD01
Aperture1 of the 1st series magnet
Aperture2 of the 1st series magnet
The 1st practice coil from Bama with new fabrication process wet wind plus 5-bar VPI.
The 2nd coil from Bama with direct wind process plus 5-bar VPI, similar to the process of the 1st prototype.
Development of CCT Magnets for HL-LHC
17

## Slide 18
HL-LHC Schedule for the Collaboration Board 2022
Development of CCT Magnets for HL-LHC
18
Successful design upgrade to solve the “long training problem”, significantly reduced the times of quench during training, ensured the project progress “on track”.

## Slide 19: Training of MCBRD02 & MCBRD03
Development of CCT Magnets for HL-LHC
AP1(CB12，25 quenches 526A) reached ±422A after 11 quenches.
AP2(CB09, 33 quenches 530A; after thermal cycle ＞500A) reached ±422A without any quenches.
19

## Slide 20
HL-LHC加速器升级中国贡献
Development of CCT Magnets for HL-LHC
20

## Slide 21
Summary
Long-term advanced superconducting magnet R&D for future high-energy accelerators is ongoing at IHEP-CAS.
Strong domestic collaboration for the advanced superconductor R&D (HTS & Nb3Sn): Stainless-steel stabilized IBS tape achieved the highest Je in 2022! Significantly reduced the cost and raised the mechanical properties.
10+ T model dipoles being developed at IHEP, reached 12.47 T at 4.2 K in mid 2021. 16 T (Nb3Sn+HTS) model dipole under development, and to be tested in 2023. 20+ T accelerator magnets expected to be realized in 2020s.
China & CERN Collaboration on accelerator technology: development of HL-LHC CCT magnets going well.
Thanks for your attention!
21