## Slide 1: Post-HIPing of Transparent Polycrystalline Alumina Ceramics Prepared by Pulsed Electric Current Sintering
Makoto Nanko1, Hien Huu Nguyen1 and Itaru Masuoka2
1. Department of Mechanical Engineering, Nagaoka University of Technology
2. Engineering Section, Heavy Machinery Department, Machinery Business, Kobe Steel, Ltd.
HIP2017
Sydney, Australia
Dec. 6, 2017

## Slide 2: INTRODUCTION
Optical transparency
Mechanical properties
Chemical inertness
Thermal conductivity
Optical lenses, windows, protectors
Host material for solid-state laser
Transparent Polycrystalline Alumina (TPA)
Properties
Applications
Pulsed Electric Current Sintering (PECS)
Fabrication methods
Notes: - windows for laser communications
- Insulators and heat radiation plates
- Metal matrix composites

## Slide 3
INTRODUCTION
TPA by Two-step PECS
(TS-PECS)
- 1st step: 1000°C in 60 min
- 2nd step: 1200°C in 20 min
- Heating rate: 100 oC/min
Sample size: Φ15 mm
As-sintered thickness: 3 mm
Good transparency
Homogeneous
10 mm
Density: 100%
Grain size: 0.33 μm

## Slide 4: INTRODUCTION
Transparent Al2O3 Prepared by PECS
  Transparent, but Darker: Carbon Contamination?
  Can Improve by HIPing?
    More Transparent
    More Clear

## Slide 5: Introduction
Macro-Defects Caused by Agglomeration
Optical Microscope
50 μm
OM Image Moving the Focus from the Surface
Can HIPing
Remove the Pores?

## Slide 6: Experimental Procedure
Slurry preparation
400oC, 60 min
Manual
milling
Al2O3
Cr(NO3)3.9H2O or Ti(OCH(CH3)2)4
Ball/powder: 5:1
Time: 24 h
Ball milling
30 min
Drying
Slurry mixture
TS-PECS
Size: 10 mm
1st step: 1000oC / 60 min
2nd step: 1200oC / 20 min
Heating rate: 100 oC/min
Applied press.: 100 MPa
High vacuum: <5×10-3 Pa

## Slide 7: Experimental Procedure
As-sintered samples  Grinding, Polishing
SolidSpec-3700DUV
: measured transmittance value of the sample
: transmittance of samples at thickness of 1 mm
: thickness of the sample (mm)
55 mm
Sensor
Sample
Mask with Φ5 mm hole
HIPing process
Heater: Mo
Atmosphere: Ar/ 100 MPa
1000 - 1400°C/ 1 h, 400°C/h
Transmittance

## Slide 8
SEM images
Edge
Center
Fracture surface
Radial axis
Density measurement
Dopants | HIPing temperature
Undoped Cr-doped Ti-doped | 0 1000 1200 1400
Sample notations
Experimental Procedure
Und.0  undoped Al2O3 without HIP
Cr.1400  Cr2O3 doped with HIP at 1400°C

## Slide 9
Results
Photos of all samples
NoHIP
HIP1000
HIP1200
HIP1400
Undoped
Ti-doped
Cr-doped

## Slide 10
Results: Density & Grain Size
Sample | Relative density (%) | Average grain size (μm) | 
 |  | Center | Edge
Undoped.0 | 99.9 | 0.36 | -
Cr.0 | 100 | 0.33 | -
Ti.0 | 99.9 | 0.27 | -
Undoped.1000 | 100 | 0.39 | 0.37
Cr.1000 | 99.9 | 0.38 | 0.36
Ti.1000 | 99.9 | 0.28 | 0.28
Undoped.1200 | 99.6 | 2.51 | 1.54
Cr.1200 | 99.5 | 2.23 | 1.42
Ti.1200 | 99.8 | 2.08 | 0.83
Undoped.1400 | 99.6 | 5.74 | 2.61
Cr.1400 | 99.5 | 4.43 | 2.54
Ti.1400 | 99.7 | 4.22 | 2.70

## Slide 11
Results
Grain size of undoped samples

## Slide 12
Results
Grain size of Cr2O3-doped samples

## Slide 13
Results
Grain size of TiO2-doped samples

## Slide 14
Results
Transmittance of undoped samples

## Slide 15
Results
Transmittance of Cr2O3-doped samples

## Slide 16
Results
Transmittance of TiO2-doped samples

## Slide 17
Discussion
Heterogeneous grain growth: faster at the center
Pore growth near the edge:
much slower than at the center
Influences of HIPing processes
Higher HIPing temperature
 Larger grain size + Slightly lower density
 Lower transmittance
4 μm
4 μm
Cr.1400 sample
Pores

## Slide 18
Discussion
Dopants
Cr: Slightly prohibit grain growth
basically higher transparency than undoped
Ti: Prohibit grain growth stronger than Cr-doped
A bit dark color
 lower transparency than undoped
Influences of dopants

## Slide 19
Discussion
At high HIPing temperature (1400°C)
Cr-doped: cloudy
 heterogeneous grain size
Ti-doped: many black dots
 formation of Al2TiO5???
Influences of dopants
Und.1400
Ti.1400
Cr.1400
Ti.1200

## Slide 20: Summary
Post-HIPing of Transparent Al2O3 Prepared by PECS
  HIPing CANNOT Improve Transparency
    HIPinng@1000°C: No Change
    HIPing@1200&1400°C: Grain Growth in the Inside Samples