## Slide 1: Efficient modeling of very large NNS parts (till 2.5 meter diameter) and key parameters to control dimensional Scattering in a +- 15 mm range.
AUTHORS
Gérard Raisson
Vassily Goloveshkin

## Slide 2
Introduction
Modeling analysis:
  Considerations on existing HIP models
  How to improve the model parameter identification?
  Effect of intial thermal conductivity
Determination of parameters to be mastered.
Conclusion

## Slide 3: Introduction (1)
Very large (Φ above 2.5 m up to to 3,5 m) HIP units are or will be available in short term.
Production of very large parts is possible and metallurgical studies have validated HIP process.
For such parts, cost of over thickness (material to be removed and machining) is a fundamental issue.
Optimum could be for a 2,5 m diameter part a dimensional scattering lower than +-15 mm, that is less 1%.

## Slide 4: Introduction (2)
Question: is it realistic? Yes, experience on net shape parts shows that with a very good control of powder, filling and HIP cycle, the main of the scatter comes from tooling.
However, gap between modeling and actual dimensions is still higher than the dimensional target. A calibration (iteration) part is necessary what is money and time consuming.

## Slide 5: Introduction (3)
Requirements for an efficient use of modeling are:
  Precision better than target (with a margin)
  Possibility to study effect of all involved process parameters.
In a first step, HIP modeling will be considered in sharing what is linked with mechanical model and what is linked with parameters identification
In a second step, sensitivity of some parameters will be estimated by modeling.

## Slide 6: Thermal conductivity
Thermal conductivity becomes a major phenomena for powder thickness above around 50 mm.
Relationship between heat conductivity and density is well established.
However initial conditions are key point:
  Filling density
  Low temperature pressure trajectory

## Slide 7
It will be seen later on that final dimensions are very sensitive to initial relative conductivity after low temperature pressurization
Estimation of initial relative conductivity can be done through:
  A specific identification trial
  A mechanical analysis (contact area).

## Slide 8: Estimation by micromechanical analysis of effect of initial density and pressurization on initial thermal conductivity
Chart: Powder pressure (bar)
| 0 | 25 | 50 | 100 | 150 | 200 | 250
0,62 | 0 | 0.062324 | 0.091726 | 0.13526 | 0.17003 | 0.20023 | 0.22751
0,66 | 0 | 0.091666 | 0.12954 | 0.18337 | 0.22504 | 0.2605 | 0.29205

## Slide 9
To calculate powder plasticity criteria, models mix (Green approach):
  Full dense material flow stress
  Coefficients translating effect of density on the discrepancy between full dense and partially densified powder.
For example LNT plasticity criteria is:
  σ0 is pressure inside the powder
  T is shear stress in the powder
  τS is full dense flow stress
Rheology of porous material

## Slide 10
The principle of full dense material is very questionable:
  Microstructure varies during densification and full dense material can be not representative
  Strain and strain rate are very inhomogeneous particularly in first steps of densification
  Only a set of (τS , f1, f2) has a physical meaning
Actually set (τS , f2) is identified during interrupted cycles or HIP dilatometer trial. Validity of this set is limited. It is necessary to use exactly the same temperature profile and a close to pressure profile.
Three HIP cycle with the same heating rate but three different dwell pressures show that with an unique τS=f(Temperature) law, f2 function of density is also very close for three dwell pressures.

## Slide 11
Chart: time (s)

## Slide 12
Chart: Temperature (°C)

## Slide 13
Chart: density

## Slide 14
It can be noticed that densification rates are very close particularly at high temperature. It could explain why it is not necessary to take in account viscous behavior.
Simple rigid plastic model is quite enough

## Slide 15
Chart: ρ

## Slide 16: Identification strategy
To improve precision of modeling, it is mandatory to have a consistent demarche (precision) and to have a better description of first step of densification (thermal conductivity).
Interrupted HIP trials don’t allow to describe precisely first steps for f2 below 70%.
HIP dilatometry could be the right process but methodology has to be very precisely defined:
  Difficulty of filling of small size capsules
  Pressure correction relatively high
  Sampling procedure.

## Slide 17: Estimation of thermal conductivity effect by modeling
Modeling of two parts were carried out:
  Massive flange: ID 366 mm OD 1100 mm H 100 mm, where initial conductivity after pressurization was varied.
  Massive ring: ID 250 mm OD 1250 mm H 500 mm, where filling density was varied. Two hypothesis to establish thermal conductivity in the beginning of cycle have been used.

## Slide 18: Shrinkage in function of initial conductivity for a massive flange ID 183mm, OD 1100mm, H 100 mm
Chart: Initial relative conductivity
| 0.1 | 8.0000000000000043E-2 | 6.0000000000000026E-2 | 4.0000000000000022E-2 | 2.0000000000000011E-2
 | 1.0651 | 1.0548 | 1.0366 | 1.0095 | 0.98195
Isothermal | 1.1209 | 1.1209

## Slide 19: Modeling of a IR=500mm, OR 1000 mm and H=500 Ring Effect of filling density
Chart: rho
| 0.66 | 0.65 | 0.64
Hypothesis 1 | 70 | 73 | 75
Hypothesis 2 | 80.9 | 83.9 | 85.1 | 87.5 | 89.3 | 104.2 | 114.8

## Slide 20: Modeling of a IR=500mm, OR 1000 mm and H=500 Ring Effect of filling density
Chart: 
| 0.66 | 0.65 | 0.64
Hypothesis 1 | 82 | 84 | 85
Hypothesis 2 | 69.7 | 72.6 | 75.3 | 77.8 | 81 | 80.6 | 83.5

## Slide 21: Results of modeling
Thermal conductivity is confirmed as a key factor in dimensioning
Effect of filling density is not trivial.
The way to treat initial density and related thermal conductivity has to be precisely established and validated.

## Slide 22: Strain-rate sensitivity of Capsule Steel
Densification rate varies a lot along cycle
It is necessary to take in count for capsule actual set (temperature -strain rate)
Parametric modeling of anisotropy of shrinkage shows that increases when:
  Temperature is growing
  Strain rate is lowering
  Capsule thickness- diameter is growing. .

## Slide 23
Chart: ez/eR f(γ) α=0,2
| 2 | 5 | 1 | 0.5 | 0.2
e/R=0,1 | 0.894 | 0.8588 | 0.92511 | 0.94597 | 0.97745
e/R=0,025 | 0.95103 | 0.91356 | 0.97145 | 0.98609 | 0.99251 | 0.88507

## Slide 24: Other discrepancy parameters
Powder:
  Process ?
  Filling density (1% generates 0,3% shrinkage change)
Capsule:
  Geometrical precision
  Plastic distortion during filling and handling
  Chocks during handling
Filling:
  Control of tapped density
  Homogeneity of filling density (heterogeneity can generate 3D distortion)
HIP cycle:
  Initial pressurization
  Heating rate
  Cooling rate particularly for ferritic steel (easy to be estimated)

## Slide 25: Powder
Powder issues are not only chemical analysis, and cost.
Others characteristics can be involved:
  Filling density
  Size distribution: weak but not negligible
  Process
  Minor elements

## Slide 26
Chart: Temperature (°C)
| 828.57142857142856 | 878.57142857142856 | 914.28571428571433 | 939.28571428571422 | 1030.3571428571422 | 1121.4285714285729 | 1182.1428571428571
AA | 0.76591 | 0.85 | 0.91955 | 0.95 | 1 | 1 | 1
PREP | 0.85909 | 0.95 | 1 | 1

## Slide 27: Conclusions
There is a great potential of improvement of modeling precision:
Target to get parts with a high precision does not need a sophisticated rheology but a consistent way to treat experimental data and a validity domain for identified parameters (f.e. Pressure and temperature).
New specific trials have to be developed in order to identify parameters involved to characterize first steps of densification (density and thermal conductivity)
We have presented 2 example s, numerous other parameters can have a noticeable effect on final precision. Modeling can give tolerance range to be respected.

## Slide 28: Conclusions
There is a great potential of improvement of modeling precision:
  consistency of identification methodology
  Specific identification for first steps of HIP cycle
Numerous parameters can have a noticeable effect on final precision. Modeling can give tolerance range to be respected.

## Slide 29: Conclusions
There is a great potential of improvement of modeling precision:
  consistency of identification methodology
  Specific identification for first steps of HIP cycle
Numerous parameters can have a noticeable effect on final precision. Modeling can give tolerance range to be respected.