## Slide 1: Taylor-Made Net-Shape Composite Components by Combining Additive Manufacturing and Hot Isostatic Pressing
Sebastian Riehm, Anke Kaletsch, Christoph Broeckmann (RWTH Aachen University, Aachen/Germany)
Vera Friederici, Sandra Wieland, Frank Petzold (Fraunhofer IFAM, Bremen/Germany)
HIP17 – 12th International Conference on Hot Isostatic Pressing, 2017-12-08, Sydney/Australia
Notes: - Ongoing research project together with Fraunhofer IFAM Bremen of Prof Frank Petzold

## Slide 2: Outline
Introduction
  Aim of Project
Experimental Work
  SLM of Capsules
  HIP of Capsules
  FEM Simulation
Results & Discussion
  Numerical Simulation of Shrinkage and Densification
  Metallographical Investigation
Conclusion

## Slide 3: Introduction

## Slide 4: Additive Manufacturing & Hot Isostatic Pressing
AM: Pros | & Cons
Building of complex geometries Overcome limits of conventional manufacturing Integrated into CAD/CAM process chain Material-saving New manufacturing method | Long building time needed Not very large parts possible Anisotropic properties Residual porosity Only one material at the same time
HIP: Pros | & Cons
Isotropic properties Very fine microstructure Full density achievable Applicable to a wide range of metallic materials | Simple geometries for powder HIP Complex process needed Closed porosity needed HIP parameters dependent on material selection

## Slide 5: Combination of Additive Manufacturing & Hot Isostatic Pressing
AM-build capsule for Powder HIP
  Virtually limitless freedom of geometry
  Design of capsule based on FEM simulation
Fill and close capsule with powder conventionally
  Either same material as capsule material
  Or second complemental material
HIP filled capsule
Project aim:
Complex-shaped composite component with functional outer layer and tough core exhibiting tailor-made properties and full density
AM Capsule
Powder
HIP
Composite Component

## Slide 6: Experimental Work

## Slide 7: Preliminary Choices
Capsule Design
Variable wall thickness
constant
varied: 1.0 mm 1.5 mm 2.0 mm
Materials Selection
Capsule | Bulk | 
Austenitic stainless steel AISI 316L (X2CrNiMo17-13-2; 1.4404) |  | Martensitic tool steel AISI L6 (56NiCrMoV7; 1.2714)
Carbide rich, wear resistant steel AISI A11 (X245VCrMo8-5-1; FeCrV10) |  | Martensitic tool steel AISI L6 (56NiCrMoV7; 1.2714)
Complex-shaped fully dense composite components with corrosion or wear resistant surface and tough core built in comparatively short time
Notes: 2nd enhanced design
  1st design plain cylinders
Short feed pipe at top with constant wall thickness to weld filling pipe
Session parallel, but look proceedings

## Slide 8: Determination of SLM Parameters
EOS M270 Dual Mode (at Fraunhofer IFAM, Bremen)
overhangs and different angles
Final parameter set
Capsules with different wall-thicknesses
(0.3 mm; 0.5 mm; 1.0 mm; 1.5 mm; 2.0 mm)
Fine tuning of parameters
overhangs and different angles
Parameter variation
Lines and squares,
cubes, blocks and thin walls
Job volume | 250 mm x 250 mm x 215 mm
Layer thickness | 40 µm
Line spacing | 100 µm
Laser type | Yb-color laser, 200 W
Focal spot size | 70–100 µm
Inert gas | Nitrogen
Substrate heating | max. 80°C
Recoater | ceramic

## Slide 9: SLM-building of HIP Capsules (316L)
1st Design
2nd Enhanced Design
Notes: Capsules with support structure on building plates
  Support structures to be removed
After some initital benchmark tests:
  Final SLM building parameters were set rather quickly
“good-natured“ material for SLM-building
1st design: short feed pipe not constant wall thickness -> under 1 mm not possible to TIG-weld

## Slide 10: SLM-building of HIP Capsules (A11)
Pure A11
Possible Solutions:
Test lines: best results with energy density of 75–100 J/mm³
Cubes with height > 1 mm: 80 oC substrate temperature not enough to avoid cracks and delamination
Higher substrate temperature → building above Martensite start temperature
Powder-mixing with low-carbon powder → decrease overall carbon content
Notes: Capsules with support structure on building plates
  Support structures to be removed
After some initital benchmark tests:
  Final SLM building parameters were set rather quickly
“good-natured“ material for SLM-building
1st design: short feed pipe not constant wall thickness -> under 1 mm not possible to TIG-weld

## Slide 11: SLM-building of HIP Capsules (A11)
1. Increase substrate temperature
2. Powder-mixing
Substrate temperature of 300 oC
Cubes of pure A11 can be built
Still cracks
A11 + 430L 300 oC substrate heating
only few cracks above 17.5 % 430L
  80 oC substrate temperature, 50% 430L:
500 µm
500 µm
A11 + 17.5 % 430L

## Slide 12: Mixture of A11 with 430L
Material | Hardness HV10
A11 | 836 ± 29
A11 + 17.5 % 430L | 784 ± 10
A11 + 50 % 430L | 475 ± 20
“Dilution” of wear-resistant properties?
Influence on Carbide Ratio
Measurement of Hardness
Chart: 430L [wt-%]
| 0 | 2.5 | 5 | 7.5 | 10 | 12.5 | 15 | 17.5 | 20 | 22.5 | 25
VC | 0.161 | 0.156 | 0.152 | 0.147 | 0.142 | 0.137 | 0.133 | 0.128 | 0.122 | 0.117 | 0.112
C in Austenite | 0.803 | 0.794 | 0.785 | 0.777 | 0.77 | 0.763 | 0.755 | 0.75 | 0.744 | 0.739 | 0.734
Chart: T [°C]
| 720.75388471177905 | 720.63208020050104 | 813.95538847117803
 | 2 | 0.1125 | 0.2385
 | 0.2385 | 0.2385 | 0.228 | 0.4394 | 0.8965 | 0.5836 | 0.5752
 | 0.5752 | 0.6851
T = 1200 oC
C in Austenite
VC

## Slide 13: HIP of SLMed Capsules
Cleaning
TIG-Welding of filling pipes
Powder-filling
Evacuating
Sealing
Powder size used for filling:
  316L: 0–500 µm
  L6: 63–300 µm
Achieved relative powder density after filling:
  316L: 65%
  L6: 61%
Chart: Time [h]
THIP = 1125 oC pHIP = 110 MPa tHold = 3 h Pressure above 750 oC
Argon atmosphere
Before HIP
After HIP
T [oC]
p [MPa]

## Slide 14: FEM-Simulation
Prediction of shrinkage and densification through HIP
Combined macroscopic model based on
  Kuhn-Downey for plasticity
  Abouaf-Chenot for viscoplasticity
Implemented as USER Subroutine for ABAQUS
Considers:
  Pressure load
  Temperature field
  Gravity
THIP
pHIP
tHold
Material properties
Initial
relative
density

## Slide 15: Results & Discussion

## Slide 16: Comparison of Real HIPed and Simulated Shrinkage
1 mm WT
Capsule 316L
Bulk 316L
1 mm WT
Capsule 316L
Bulk L6
Cone
Capsule 316L
Bulk L6
2 mm WT
Capsule 316L
Bulk L6
Next step:
Geometry design of net-shape capsule prior to HIP
Complex- and irregular-shaped capsules totally appropriate for SLM-manufacturing
— after HIP
— Simulation
Input parameters:
Material properties: 316L
Relative powder density from filling
Homogenous density distribution
Notes: Almost perfect for monolithic 316L
Slight deviations on L6 capsules:
  Not correct material properties
  Working on determining properties for L6

## Slide 17: 1 mm Wall Thickness, Capsule & Bulk 316L
Capsule | Bulk
50 µm
100 µm
500 µm

## Slide 18: 1 mm Wall Thickness, Capsule 316L, Bulk L6
Capsule | Bulk
500 µm
50 µm
100 µm
500 µm

## Slide 19: EDX of Intersection Between Capsule and Bulk
Capsule: 316L, Bulk: L6
Chart: [at-%]
| 6.57 | 10.88 | 11.13 | 8.83 | 12.61 | 14.65 | 13.55 | 18.79 | 16.86 | Schliff 17_0502 Stelle 1 | Schliff 17_0502 Stelle 2 | Schliff 17_0502 Stelle 3 | Schliff 17_0502 Stelle 4 | Schliff 17_0502 Stelle 5 | Schliff 17_0502 Stelle 6 | Schliff 17_0502 Stelle 7 | Schliff 17_0502 Stelle 8 | Schliff 17_0502 Stelle 9
Cr | 17.29 | 16.98 | 15.6 | 9.68 | 1.81 | 0.92 | 1.06 | 0.9 | 1.21
Ni | 11.37 | 10.36 | 9.76 | 8.59 | 1.88 | 1.33 | 1.77 | 1.35 | 1.63
2
3
4
5
6
7
1
Ni
Cr
Capsule Bulk

## Slide 20: SLM & HIP of Carbide-rich Steel A11
500 µm
500 µm
500 µm
SLMed cube of pure A11 | Pure A11 before HIP
SEM of pure A11 | Pure A11 after HIP

## Slide 21: EDX of A11 + 10% 430L after HIP (1/2)
Phase
Mapping
Element
Mapping
Back
Scatter

## Slide 22: EDX of A11 + 10% 430L after HIP (2/2)
Fe | C | Si | Mo
Cr | V | Mn | S

## Slide 23: EDX of A11 + 50% 430L before HIP

## Slide 24: Conclusion

## Slide 25: Composite Components Produced By SLM and HIP
Build complex- and irregular-shaped HIP-capsules by SLM
  SLM of 316L and L6 is possible without much effort
  Ongoing research on best parameter set for SLM of A11
Design net-shape capsules with help of numerical simulation
Fill, close and powder-HIP capsules conventionally
Result: composite components with functional outer layer and tough core
Ongoing: determination of best mixture for A11
Next: Demonstrator component with industrial partner

## Slide 26
We want to thank especially AiF e. V., FPM e. V. and all engaged companies for making this research possible.