## Slide 1
Heat treatment inside the HIP-Unit
12th International Conference on Hot Isostatic Pressing 2017
05.12. - 08.12.17 Sydney
N. Wulbieter, A. Rottstegge, W. Theisen

## Slide 2
Introduction
HIP cooling rates – measuring and benchmark
HIP-quenching of martensitic steels
Summary and outlook
Contents

## Slide 3
Advantages of fast cooling in a HIP-Unit
Shortens processing time
Densification and heat treatment in one process step
Benefits of gas-quenching:
  Clean surfaces
  Less distortion
Heat treatment under high pressure
Introduction

## Slide 4
HIP-Unit „Quintus QIH9“ with Uniform Rapid Quenching (URQTM)
Furnace: Ø 86 mm x 160 mm
Max. temperature: 1400 °C (molybdenum), 2000 °C (graphite)
Max. pressure: 207 MPa
Max. pressure for fast cooling:
  170 MPa
Process gas:
  Argon
  Nitrogen
Introduction

## Slide 5
Schematic of fast cooling in QIH9
Cold gas outside the heatshield is pressed into the hot zone
Hot gas is cooled when passing the heatshield which acts as a heatsink
Circulation of gas inside the pressure vessel
Fast cooling works since difference in temperature exists between gas in- and outside the heatshield
Introduction

## Slide 6
Introduction
HIP cooling rates – measuring and benchmark
HIP-quenching of martensitic steels
Summary and outlook
Contents

## Slide 7
Procedure
Test material: 1.4404 (AISI 316L)
Inserted thermocouples for determination of cooling rates
Start temperature: 1300 °C
Different sample diameters tested
Different gas inlet nozzles tested
Different pressures tested
HIP cooling rates

## Slide 8
Results for 1.4404 (Ø 30 x 90 mm) at 100 MPa
HIP cooling rates
Ø 1.9 mm
Gas nozzle

## Slide 9
Results for 1.4404 (Ø 30 x 90 mm) at 100 MPa
HIP cooling rates
Ø 3.2 mm
Gas nozzle

## Slide 10
Results for 1.4404 (Ø 30 x 90 mm) at 100 MPa
HIP cooling rates
Ø 6 mm
Gas nozzle

## Slide 11
Cooling rates as a function of gas pressure for the core of 1.4404 (Ø 30 x 90 mm)
HIP cooling rates
0.0
2.5
5.0
7.5
10.0
12.5
15.0

## Slide 12
HIP cooling rates
Ref.: R.B. Stewart (1989)
Literature: Density as a function of pressure (Argon)
22 °C
972 °C

## Slide 13
Chart: a in W/m²K
| unbew. Luft | Salzbad | Stickstoff, 6 bar | Helium, 6 bar | HIP N2, 1700 bar | unbew. Öl | bew. Öl
min | 40 | 400 | 350 | 450 | 487 | 1250 | 2000
Spalte1 | 10 | 50 | 50 | 50 | 87 | 250 | 200
Air
Salt bath
Nitrogen, 6 bar
Helium, 6 bar
HIP - 170 MPa
Oil
Oil with convection
Ref.: G.E. Totten (1997)
HIP cooling rates
Heat transfer coefficient for HIP (calculated) and conventional quenching media (literature)

## Slide 14
Zeit in s
Time in min
Zeit in h
Surface
Core
HIP cooling rates
56NiCrMoV7
Ref.: Dr. Sommer, Stahlwissen Navimat
Time in h
Time in s
Oil-quenching
Hardening temperature 850 °C
Ø 50 mm
Temperature in °C
N2 6 bar
HIP 170 MPa

## Slide 15
56NiCrMoV7
Zeit in s
Zeit in min
Zeit in h
HIP cooling rates
Hardening temperature 850 °C
Time in min
Time in h
Time in s
Ref.: Dr. Sommer, Stahlwissen Navimat
Temperature in °C

## Slide 16
Introduction
HIP cooling rates – measuring and benchmark
HIP-quenching of martensitic steels
Summary and outlook
Contents

## Slide 17
Hardening in HIP
Literature: Influence of pressure on thermodynamics and kinetics
Ref.: T.G. Nilan, 1967
Time in s
Temperature in °C
0 10 20
Pressure in GPa
Ref.: F.P. Bundy (1961)

## Slide 18
Oil vs. HIP
Hardening in HIP

## Slide 19
Oil vs. HIP
Hardening in HIP

## Slide 20
Oil vs. HIP
21MnCr5
Time in s
Time in min
Zeit in h
Hardening in HIP
Time in h
Oil
Hardening temperature 850 °C
HIP 170 MPa
Ref.: Dr. Sommer, Stahlwissen Navimat
Temperature in °C

## Slide 21
21MnCr5 Oil
21MnCr5 HIP (170 MPa)
330 ± 3 HV30
388 ± 5 HV30
Hardening in HIP
Oil vs. HIP

## Slide 22
Measurement of latent heat during isothermal holding as indicator for phase transformation
Hardening in HIP
X40CrMoV5-1 (AISI H13)

## Slide 23
Delay of isothermal transformation under HIP-pressure of 170 MPa
Hardening in HIP

## Slide 24
Influence of 170 MPa HIP-pressure on microstructure and mechanical properties
Hardening in HIP

## Slide 25
Influence of 170 MPa HIP-pressure on microstructure and mechanical properties
Hardening in HIP
Pearlite
Bainite

## Slide 26
Introduction
HIP cooling rates – measuring and benchmark
HIP-quenching of martensitic steels
Summary and Outlook
Contents

## Slide 27
Cooling speed in HIP-Unit with URQ is a function of gas pressure and gas inlet nozzle
Calculated thermal heat coefficient of HIP with 170 MPa ranks between oil and conventional gas quenching
Quenching under high pressure can effect the material properties
The delay of isothermal austenite to perlite transformation can be determined by measuring of latent heat
Summary

## Slide 28
Verification of calculated hardenability for different steels with increased geometry (Ø 80 mm)
Using electrical conductivity measurements to determine influence of pressure in more detail → TTT-diagrams under HIP-pressure
Research project with RWTH University Aachen:
  Densification and heat treatment in a single process step for near-net-shaped tool steels
  FEM Simulation of shrinkage and internal stresses during the process
Outlook

## Slide 29
Thank you for your attention!
Do you have questions?
Contact:
Nils Wulbieter
Ruhr-Universität Bochum
Bochum, Germany
wulbieter@wtech.rub.de