## Slide 1: Small Modular Reactor Vessel Manufacture/Fabrication Using PM-HIP and Electron Beam Welding Technologies David Gandy and Craig Stover (Electric Power Research Institute) Keith Bridger, Steve Lawler, and Matt Cusworth (Nuclear-AMRC) Victor Samarov and Charlie Barre (Synertech-PM)
Potential Nuclear Components

## Slide 3
Project Objectives
Three key objectives were identified for this project. These include:
Develop and demonstrate advanced manufacturing and fabrication technologies to rapidly accelerate the deployment of SMRs
Develop/demonstrate new methods for manufacture/fabrication of a Reactor Pressure Vessel (RPV) which could lead to production of a vessel in under 12 months.
Eliminate 40% of the costs of production of an SMR RPV, while reducing the overall schedule by up to 18 months.

## Slide 4
Manufacture of the key components for the reactor vessel includes both conventional forging and PM-HIP. The breakdown of the key A508 low alloy steel components are as follows:
PM-HIP (A508, Grade 3, Class 1)
Lower reactor head
Upper reactor head
Steam plenum
Steam plenum access ports/covers
Upper transition shell (in four sections)
Forgings (SA508, Grade 3, Class 1)
Lower transition shell
Upper flange
Lower flange
PZR (pressurizer) shell

## Slide 11
PM/HIP
Forged Bar (Longitudinal)
Uniform Microstructure (Duplex 2205)
ATLAS
Courtesy Carpenter

## Slide 12
Charpy Impact = >195 ft-lbs (hammer stopper)
ASTM Grain Size = 6-7
Photo’s from 3 different orientations.
ATLAS
Isotropic Mechanical Properties
Courtesy EPRI

## Slide 13
Manual and Automated UT Scans Performed
ATLAS
Superior Ultrasonic Inspectability
Courtesy EPRI

## Slide 14: ATLAS
Good tensile/yield properties
Good toughness: >122 ft-lbs (165 Joules)
No Porosity, homogenous microstructures
Good Fatigue properties
Inspection, near forging quality
ASME Code Case N-834
Sect III-Approved Sept 2013
Courtesy Rolls-Royce
Courtesy EPRI
PM/HIP 316L ASME Code Approval
Notes: 4 heats of materials (components) were manufactured and included in the large data package submitted to ASME along with the Code case.
The Code Case is presently out to Section III members as a letter ballot

## Slide 15: Gas Turbine Discs
Courtesy of Siemens

## Slide 16
before HIP
after HIP
Shrinkage during HIP

## Slide 19: Requirements to the HIP cycle and Equipment for the ATLAS PM HIPED parts

## Slide 20
Temperature Uniformity of in the HIP furnace at the ramp stage beginning with 100-200C
Temperature uniformity of +/- 25F measured on the external and internal surface of the parts at the dwell stage of HIP cycle
HIP cycle duration, assuming a 4 hour dwell, within 24 hours up to 1200C, 1000 bars
Design of the major components of the PCS incorporating damage tolerance (crack arrest, load shifting),
Inspectability, including UT of the major components of the PCS
Possibility of periodical disassembling and visual and NDT inspection of the major tension stressed parts to reveal cracks, if any, and enable to replace them

## Slide 21
HIP is becoming a cost efficient and winning alternative to machining of the forgings to the final complex shape and provides for large components for Nuclear Power Plants:
Material affordability;
Decrease of “buy- to fly” ratio 2-3 times for complex shapes;
Properties as wrought or better, shape- as cast or better;
Efficient Non-destructive inspection ;
Capability for re-design of critical components to their best performance;
CONCLUSIONS