## Slide 1: HIP Processing of Improved Tooling Materials for High-Productivity Hot Metal Forming Processes
Maxime Gauthier, Guillaume D’Amours, Fabrice Bernier
December 7th, 2017
HIP’17 - 12th International Conference on Hot Isostatic Pressing, Sydney, Australia, 5 – 8 December, 2017

## Slide 2: Outline
Introduction
Objectives
Development of HTC Tool steel composite by HIP
  Properties of HIPed Hot Work Tool Steel and HTC Tool Steel
  Conformal-Cooled, Hemispherical Toolings
Hot Stamping of Aluminum Sheets with HIPed Toolings
Conclusions

## Slide 3: Introduction
Hot stamping installations are expensive and process cycle time has to be minimized to increase productivity, especially for automotive applications;
Die cooling cycle can be long according to the conformal cooling design and the tool steel used;
Developing a High Thermal Conductivity (HTC) tool steel composite could help in decreasing die cooling time and improve hot stamping productivity;
HIP is a very efficient and versatile process to manufacture high-quality, hot-work tooling materials;

## Slide 4: Objectives
Develop and Characterize a HIPed, HTC tool steel composite
Process hemispherical, conformal-cooled toolings by HIP
Evaluate impact of tooling material on hot stamping of Al alloy sheets

## Slide 5: Development of HTC Tool steel composite by HIP
D2 steel powder was chosen as baseline;
The first candidate HTC tool steel composite was based on the addition of 30 vol.% of copper particles to D2 powder;
Two billets based on these compositions were HIPed:
  D2
  D2+30vol%Cu
The HIPed materials were then characterized and their thermal and mechanical properties were compared;

## Slide 6: Development of HTC Tool steel composite by HIP (cont.)
Initial Powders:
  D2 tool steel powder, spherical, -150+45 mm (Sandvik);
  Copper powder, grade 153A, spherical, 2%max+100mm/Bal+45mm/10%max-45mm (ACuPowder)

## Slide 7: Development of HTC Tool steel composite by HIP (cont.)
304L canisters were filled & tapped;
Vacuum Degassing
  14 h @ 150C, 4h @ 550C under mechanical vacuum (7x10-2 Torr)
Crimping and Sealing
  Crimping of vacuum tube using a 100-ton Hydraulic press;
  Sealing by TIG welding
Degassed and Sealed Canister, OD = 5,438’’ (138,1 mm)

## Slide 8: Development of HTC Tool steel composite by HIP (cont.)
Hot Isostatic Press:
  AIP10-30H from American Isostatic Presses, Inc.
HIP Cycles
  For D2:
    4h @ 1100C and 15000 PSI (103 MPa)
  For D2+30vol.%Cu:
    4h @ 1000C and 15000 PSI (103 MPa)
No additional heat treatment was applied to these materials;

## Slide 9: Properties of HIPed Hot Work Tool Steel and HTC Tool Steel
The HIPed D2 and D2+30vol.% Cu bulk materials were characterized:
  Metallography
  The following properties were evaluated:
    Heat Capacity (Cp);
    Thermal Diffusivity (a);
    Thermal Conductivity (k);
    Coefficient of Thermal Expansion (CTE);
    Hardness / Microhardness;
    Wear Resistance / Coefficient of Friction (CoF);

## Slide 10: Metallography  HIPed D2
50x
500x
98,9 % Dense

## Slide 11: Metallography  HIPed D2+30vol.%Cu
50x
500x
D2
Cu
98,2 % Dense

## Slide 12: Heat Capacity (Cp)
Bizarre behaviour of Cp vs Temperature for both materials
Will be investigated further to confirm or invalidate these results

## Slide 13: Thermal Diffusivity (a)
Thermal Diffusivity is significantly increased by adding 30Vol.% Cu to D2

## Slide 14: Thermal Conductivity (k)
Adding 30Vol.% Cu to D2 dramatically increases k at all temperatures:
17.6 to 33.5 @ 25C (x 1.9)
33.1 to 61.3 @ 200C (x 1.85)
22.8 to 55.5 @ 400C (x 2.44)

## Slide 15: Coefficient of Thermal Expansion (CTE)
It is clear from the graph that:
  CTED2+Cu >CTED2
  CTEradial >CTEaxial
The difference between materials is relatively small;
The radial-axial difference is encountered in both materials;
No major impact of difference in CTE is expected during sheet metal forming

## Slide 16: Hardness
53,3 ± 0,34
30,3 ± 2,32
As expected, the hardness of the Cu-containing material is much lower than the pure D2 counterpart

## Slide 17: Microhardness
594 ± 30
638 ± 21
77 ± 4
The microhardness of the D2 phase in D2+30Vol.%Cu is slightly higher than that in the D2 specimen  maybe some solid-solution strengthening;
The Cu phase is much softer, of course;

## Slide 18: Wear Resistance / Coefficient of Friction (CoF)
Wear Testing Parameters:
  Type: Ball on disk
  Charge: -50 N
  Slider from zero: 14 mm.
  Duration: 24000 sec.
  Linear Velocity: 15000mm/min (0.25m/sec.)
  Ball Size/Material: 10mm Sintered Alumina

## Slide 19: Wear Resistance / Coefficient of Friction (CoF) (cont.)
The wear resistance of the HTC composite is much lower than the HIPed D2 (higher volume and mass losses, deeper groove);
The D2+30Vol.%Cu material has a lower CoF, which is probably due to the presence of copper (soft metals like Cu are sometimes used as solid lubricants)

## Slide 20: Conformal-Cooled, Hemispherical Toolings
The processing of conformal-cooled, hemispherical toolings followed similar processing steps and HIP cycles as were used for HTC tool steel processing:
  Tooling made of D2 only was HIPed at 1100C;
  Toolings including copper were HIPed at 1000C.
The use of a copper core in two of the three designs enabled to HIP-clad a 2-mm-thick layer of either D2 or D2+30Vol.%Cu on the said core to improve cooling;

## Slide 21: Conformal-Cooled, Hemispherical Toolings (cont.)
Schematic cross-sections of canister with core and powder used to prepare HIP-clad toolings:
Solid Cu Core
304L Canister
Powder
Solid Cu Core
HIP & Machine
2 mm

## Slide 22: Conformal-Cooled, Hemispherical Toolings (cont.)
Schematic cross-sections of the dome part of toolings processed by HIP:
Water-Cooling Channels
D2
D2
Cu
Cu
D2+Cu

## Slide 23: Conformal-Cooled, Hemispherical Toolings (cont.)
Hemispherical toolings processed by HIP:
Cu Core
+ HIP-Clad [D2+30vol.%Cu)
Cu Core
+ HIP-Clad D2
D2

## Slide 24: Hot Stamping of Aluminum Sheets with HIPed Toolings
Hot Nakazima lab-scale test setup (490°C)
Hot stamping of high strength AA7xxx aluminium alloy sheets was carried out in the following way :
  Aluminium blanks are solutionized
  A blank is transferred to the press
  Tooling moves up and blanks are stamped
  Die closes and blanks are quenched
  Blanks are removed and the tooling cools

## Slide 25: Hot Stamping of Aluminum Sheets with HIPed Toolings (cont.)
The three different hemispherical toolings were tested;
Ten (10) hot stamping tests per tooling;
Punch cooling time of 7 min. between each test;
Three thermocouples were installed in each punch to measure temperature close to the contact surface.
All tested specimens are identical which shows a good repeatability from one stamping to another

## Slide 26: Hot Stamping of Aluminum Sheets with HIPed Toolings (cont.)
Hot Stamping Tests Results
  Three curves corresponding to three thermocouples per tooling;
  Heating-cooling curves are presented for the last stamping test of each batch;
  D2 temperature results are used as reference for the two other punches;
  Temperature derivatives which represent heat transfer and cooling rate are used for the analysis;

## Slide 27: Hot Stamping of Aluminum Sheets with HIPed Toolings (cont.)
D2
D2
D2 on Cu
HTC on Cu

## Slide 28: Hot Stamping of Aluminum Sheets with HIPed Toolings (cont.)
For the three toolings, the time required to reach punch temperature equilibrium after hot stamping was determined:
  *Gain in efficiency = [(cycle time D2/cycle time new material) -1] x 100

## Slide 29: Conclusions
A HTC composite hot work tooling material was successfully processed by HIP:
  Its thermal properties were improved over the D2 reference, while its mechanical properties were lower, except for an improvement in CoF;
  Work on an optimal HTC composite should continue;

## Slide 30: Conclusions (cont.)
Conformal-Cooled, Hemispherical Toolings were manufactured by HIP and used for hot stamping trials:
  Performance was as follows:
  HTC on Cu > D2 on Cu > D2
  Gains in efficiency were of 127% for HTC on Cu and 110% for D2 on Cu;
A thin, HIP-clad layer of HTC tool steel on a conformal-cooled copper core significantly contributes to productivity increase and should be considered for automotive sheet forming.

## Slide 31: Thank you
CONTACT
Maxime Gauthier
Senior Research Officer
Automotive and Surface Transportation Research Centre
National Research Council Canada
75 de Mortagne Blvd, Boucherville (Québec)
Canada, J4B 6Y4
Maxime.Gauthier@cnrc-nrc.gc.ca