## Slide 1
I. Iturriza
Additive Manufacturing and Laser Group. Materials and Manufacturing Division. Ceit-IK4
Sydney, 6th December 2017
PRECIPITATION OF Y-Ti-O NANOPARTICLES DURING THE HIP CONSOLIDATION OF GAS ATOMIZED FERRITIC POWDERS
Notes: ooo

## Slide 2
PRECIPITATION OF Y-TI-O NANOPARTICLES DURING THE HIP CONSOLIDATION OF GAS ATOMIZED FERRITIC POWDERS
D. Pazos1, N. Ordás1, E. Gil1, V. de Castro2, T. Leguey2, A. Anspoks3, J. Purans3 , P. Fernández4, I. Iturriza1*
1Ceit-IK4 and Tecnun (Universidad de Navarra), Manuel de Lardizábal 15, 20018, San Sebastián
2University Carlos III Madrid, Avda. de la Universidad 30, 28911 Leganés, Madrid
3Institute of Solid State Physics, University of Latvia, Kengaraga street 8, 1063 Riga, Latvia
4Ciemat. National Fusion Laboratory. Avda. Complutense 40, 28040 Madrid, Spain

## Slide 3
INTRODUCTION
ODS FS as structural materials in future fusion applications
EU Blanket designs
ODS FS
  Plates supporting the plasma facing material (W tiles)
  Intermediate material between W tiles and structural EUROFER (RAFM, reduced-activation ferritic-martensitic steel)
DEMO
HCLL (He Cooled Lithium-Lead) blanket
HCPB (He Cooled Pebble beads) blanket
WCLL (Water Cooled Lithium-Lead) blanket
DCLL (Dual Coolant Lithium-Lead) blanket
Fusion Engineering and Design 109–111 (2016) 1637–1643

## Slide 4
INTRODUCTION
ODS FS as structural materials in future fusion applications
Divertor
Basic requirements:
  High density dispersion of stable nanometric precipitates and dislocation structure to provide high creep strength, up to 750 C. Low DBTT temperature
  Benefits:
  Trapping of He into fine scale bubbles to prevent void swelling and GB embrittlement
  Operation temperature above displacement damage regime (> 0.3-0.4 Tm), no radiation hardening or embrittlement

## Slide 5
 cost of mechanically alloyed powders uniform alloying requires long process time
Local heterogeneities
Batch-to-batch ≠ composition
Contamination from milling media & air (C, N, O)
Prealloyed Fe-Cr-W-Ti powder
Y2O3
Ball mill
Issues associated with MA
HIP
Hot rolling
Recrystallization
Machining
Final product
Thermal treatment
Steel
can
+
+
Fe
Cr
W
Ti
Y2O3
Or
Mechanical alloying
Conventional route to produce ODS steels
INTRODUCTION
  Current challenges:
  High variability in properties
  Small, lab-scale batches available
  Low fracture toughness at RT
OBJECTIVE: To develop an alternative route able to face those challenges

## Slide 6
PROPOSAL
STARS route

## Slide 7
Atomized powder: Ti & Y in solid solution
Powder oxidation: ultra-thin Cr- & Fe-rich oxide layer
HIP at high temperature:
    Dissociation of metastable Cr- & Fe-rich oxides
    O diffusion from Prior Particle Boundaries
    Formation of Y, Ti-rich oxide dispersions
STARS route: Surface Treatment of gas Atomized powder followed by Reactive Synthesis

## Slide 8
Fe + Cr + W + Ti + Y
FeCrWTiY
powder
Oxygen adjustment
Higher processing rate of powder
Lower contamination levels
No local heterogeneities in composition
Control of Y in atomized powder  Industrializable process?
Control of oxygen uptake to allow complete dissociation of metastable oxides and Y and Ti reaction
Density and distribution of ODS phase
ADVANTAGES
CHALLENGES
Prealloyed Fe-Cr-W-Ti powder
Y2O3
STARS route vs Mechanical Alloying
STARS route: Surface Treatment of gas Atomized powder followed by Reactive Synthesis

## Slide 9
STARS: gas atomization of Fe-14Cr-2W-0,3Ti-0,23Y
Lab. Scale (<3 kg)
Industrial Scale
Composition (wt. %) |  |  |  | 
Fe | Cr | W | Ti | Y
Bal. | 13,9-14,1 | 1,9-2,0 | 0,27-0,3 | 0,20-0,23
  Spherical powder particles
  Fine control of composition, at laboratory and industry
  No metallic iron in the surface, Y segregation

## Slide 10
STARS: gas atomization of Fe-14Cr-2W-0,3Ti-0,23Y
XAS: X-ray Absorption Spectroscopy. Performed with synchrotron radiation (Soleil and Alba)
XANES: X-ray Absorption Near Edge Structure  metallic, oxide, carbide…
X-ray absorption near edge structure (XANES), also known as near edge X-ray absorption fine structure (NEXAFS), is a type of absorption spectroscopy that indicates the features in the X-ray absorption spectra (XAS) of condensed matter due to the photoabsorption cross section for electronic transitions from an atomic core level to final states in the energy region of 50–100 eV above the selected atomic core level ionization energy, where the wavelength of the photoelectron is larger than the interatomic distance between the absorbing atom and its first neighbour atoms
as-atomized
Composition (wt. %) |  |  |  | 
Fe | Cr | W | Ti | Y
Bal. | 13,9-14,1 | 1,9-2,0 | 0,27-0,3 | 0,20-0,23
  SEM & XAS: Y remains metallic inside particles (probably Fe-Y), available to form Y-Ti-O nanoparticles
How is the Y?

## Slide 11
Detailed XPS spectra of Cr & Fe of oxidized powder
  Fe Oxide layer thickness 7,5  18,5 nm
Fe2O3
Cr2O3 +Y2O3
STARS: surface oxidation of powder
  Y remains metallic inside particles, oxidized at the surface.
  Nanometric metastable Cr2O3 + Fe2O3 oxide layer provides oxygen to form Y-Ti-O nanoparticles during HIPping
  Oxidation at low temperature  Control of oxygen gain
  Oxygen uptake tailored to specific composition
L. Nyborg and E. Hryha, “Surface Oxides on Gas and Water Atomized Steel Powders,” Advances in Powder Metallurgy & Particulate Materials, vol. 2, pp. 153–161, 2014.

## Slide 12
STARS: HIP and reactive synthesis of nanoparticles
HIP at high temperature
Clean PPBs, free from metastable Cr-, Fe-rich oxides
Nanometric Y- and Ti-rich precipitation at GBs and inside grains
Y completely oxidized, but Ti remains in solid solution in matrix
Finer powder leads to finer and more homogeneous grain distribution and finer nanoparticles (NPs)
Effect of powder particle size
<20 µm, 1000 ppm Oxygen. HIP 1220 °C 2h
20-45 µm, 1000 ppm Oxygen. HIP 1220 ° C 2h
NPs
matrix
Elem. | Wt%
Fe | 52,2
Y | 14,8
Cr | 10,3
O | 8,3
Ti | 7,1
C | 4,9
W | 2,0
Al | 0,5
Y-Ti-O
Elem. | Wt%
Fe | 81,4
Cr | 13,4
C | 2,8
W | 1,9
O | 0,3
Ti | 0,2
Al | 0,0
Y | 0,0

## Slide 13
STARS: HIP and reactive synthesis of nanoparticles
HIP at high temperature
Grain growth takes place when oxygen content is lower, incomplete Y oxidation
Minimum Oxygen concentration function of powder particle size and HIP parameters: >1000 ppm
Higher oxidation degree of powders avoids also abnormal grain growth
Effect of oxygen concentration
<20 µm, 600 ppm Oxygen. HIP 1220 °C 2h

## Slide 14
STARS: HIP and reactive synthesis of nanoparticles
HIP at high temperature
An important fraction of Ti remains metallic, probably in solid solution in the ferritic matrix
Minor presence of Ti-rich carbides or oxides
High oxygen:
  Y-rich NPs are Y2O3
  Minor presence of Y-Ti-O (<10%)
Low oxygen:
  Y2O3 + partially oxidized Y
Oxide nanoparticles
YOx, x<3/2
W-,Ti-rich
Fe
Cr
W
Ti
Y
O
C
Notes: X-ray absorption spectroscopy measurements were performed at room temperature using the multipole wiggler beam line BL22 – CLÆSS at the ALBA synchrotron radiation facility . X-ray radiation was produced by the storage ring operated in the top-up mode at the energy E=3.0 GeV and the maximum stored current I=110 mA. The synchrotron radiation was monochromatized using a pair of Si(111) or Si(311) crystals, and focused onto the sample by toroidal mirror. Collimating and focusing mirrors were responsible for harmonic rejection. X-ray absorption near-edge structure (XANES) and extended x-ray absorption fine structure (EXAFS) at the Ti, Fe and Y K-edges were analysed using conventional methodology and two software packages – EDA and Athena . Theoretical calculations of X-ray absorption spectra were performed using the FEFF8.5L codes

## Slide 15
Linear combination analysis of the XANES spectra , using as-atomized powder and sample HIPped at 1220 °C + HT at 1320 ° C as standards
Monitoring of Y oxidation through XAS
STARS: HIP and reactive synthesis of nanoparticles
Notes: Meter el IN718

## Slide 16
STARS: HIP and reactive synthesis of nanoparticles
HIP at high temperature
Higher density in dislocation-rich areas
Ti remains partially in solid solution in ferrite
Oxide nanoparticles
Heterogeneous distribution: 1020-1022 m-3
Preferentially at or close to GBs
Round morphology and elongated
Large and small NPs (10-20 nm ~100 nm)
Most NPs <20 nm (80%).
 62% of NPs <10 nm.
20 nm
100 nm
500 nm
100 nm
TMTs to increase the density of dislocations, preferential sites for the nucleation of ODS phase

## Slide 17
STARS: Thermo-Mechanical Treatment
Experimental simulation of TMTs
Consolidation at low temperature to maintain metastable oxides at PPBs
Deformation at low temperature to maintain metastable oxides and introduce high density of dislocations (preferential nucleation sites of NPs)
Heat treatment at high temperature to dissociate metastable oxides and precipitate NPS
Example of deformation dilatometry schedule
HIP at low temperature

## Slide 18
STARS: Thermo-Mechanical Treatment
Experimental simulation of TMTs with dilatometry
True stress & strain calculated from experimental values and calculated instantaneous cross-sectional area.
800 C
750 C
700 C
900 C
850 C
800 C
Strain hardening during 3rd pass, especially with finer powder and deformation at lower temperature.
1500 ppm
Samples were sectioned along their longitudinal axis, selecting the region corresponding to a maximum area fraction of nominal strain and reduced strain gradient.

## Slide 19
<20 µm, 1500 ppm oxygen. HIP 900 °C 2h. + Dil. 800  1,1 + HT 1220 °C 2h
STARS: Thermo-Mechanical Treatment
Experimental simulation of TMTs with dilatometry
Abundant precipitation of extremely fine NPs.
Improved distribution of NPs
High density of dislocations
improved behaviour at high temperature

## Slide 20
Conclusions
Precursor powder containing Ti and Y at industrial scale, OBTAINED
FeCrWTiY
alloyed powder.
  Nanometric metastable Cr2O3 + Fe2O3 oxide layer provides oxygen to form Y-Ti-O nanoparticles when dissociates
Oxygen concentration and HIP parameters have a strong effect on the nature and distribution of NPs precipitated
HIP oxidized powders leads to a low concentration of NPs located close to grain boundaries
HIP low T +
Hot deformation +
HT high T
provide a remarkable increase of NP and their distribution
STARS route is potentially suitable to produce ODS FE

## Slide 21
Iñigo Iturriza; iiturriza@ceit.es
THANK YOU