## Slide 1: Influence of rapid cooling rates for HIP on mechanical and corrosion properties of UNS S32205
Arnulf Hörtnagl1, Paul Gümpel1, Michael Hamentgen², Beat Hofer³
Institute for Materials System Technology Thurgau at the University of Applied Sciences Konstanz (1)
Powder Metallurgy, Saar Pulvermetall GmbH, Saarwellingen (2)
Hofer Werkstoff Marketing Beratung (3)

## Slide 2: - Duplex stainless steel UNS S32205 - Effects of cooling rate - Influence of Process-Temperature - Experimental - Results - Conclusion and discussion
Outline

## Slide 3: Duplex stainless steel UNS S32205

## Slide 4: according ASTM S32205 Composition in wt. pct. Carbon 0.030 max Chromium 22.0-23.0 Nickel 4.5-6.5 Molybdenum 3.0-3.5 Nitrogen 0.14-0.20 Phosphorus 0.035 max Manganese 2.00 max Sulfur 0.020 max Silicon 1.00 max Iron Balance
temperature →
time →
Duplex stainless steel UNS S32205
Temperature-Precipitation diagram of duplex stainless steel UNS S32205 – influence of alloying constituents;
Source: J. Charles; Duplex Stainless Steels 1991

## Slide 5: Duplex stainless steel: - mixed microstructure - austenite / ferrite ratio usually 50/50 mix to 40/60 - twice the strength compared to austenitc stainless steels - improved resistance to localized corrosion - lean duplex: PREN > 25 - standard duplex: ≈ 22% Cr PREN > 32 - super duplex: PREN > 40 - hyper duplex: PREN > 48
Properties
Density 7.80 g/cm³
Specific heat 460 J/Kg K
Young´s modulus 19.5 x 104 MPa
Melting range 1420 – 1465 °C
0.2 % proof stress > 450 MPa
Tensile strength 650 – 880 MPa
Hardness < 293 HB
PREN 30.9 – 38.0
Duplex stainless steel UNS S32205

## Slide 6: Chromium equivalent Creq = % Cr + 1.4% Mo C + 0.5% Nb + 1.5% Si + 2% Ti Creq = 27.65 Nickel equivalent Nieq = % Ni + % Co + 0.5% Mn + 0.3% Cu + 30% N + 30% C Nieq = 9.76 Creq / Nieq = 2.83
Creq/Nieq
Temperature →
Alloy |  | Chemical Composition |  |  |  |  |  |  | 
UNS | DIN EN | C | Cr | Ni | Mo | Mn | N | Si | Cu
S32205 | 1.4462 | 0.03 | 22.40 | 5.21 | 3.4 | 1.23 | 0.10 | 0.30 | 0.11
Duplex stainless steel UNS S32205
2550
2550
2507
2205 high N
2205 low N
2304
2507
2205 high N
2205 low N
2304
Vertical section of an Fe-Cr-Ni phase diagram at 60% Fe
Source: J.C.Lippold, D.J. Kotecki; ISBN: 0-471-47379-0

## Slide 7: Aims - add value - reduce cost - lead time - increase safety - specify requirements
What is NORSOK?
Industry Initiative for the Competitive Standing of the Norwegian Offshore Sector
Norwegian Oil Industry Association
Federation of Norwegian Engineering Industries
Standards
M630 – Material Data Sheets for Piping
M650 – Qualification of Manufacturers of „Special Materials“
- Duplex Stainless Steels
- High Alloyed Austentic Stainless Steels
- Nickel Base Alloys (Castings)
- Titanium and Alloys (Castings)
Norsok M-630 Standard / Duplex stainless steel UNS S32205

## Slide 8
Requirements according Norsok M-630 Standard
Tensile Testing
Rp0.2 > 450 MPa
Rm > 620 MPa
A5 > 25 %
Hardness
maximum 28 HRC or 271 HB or 290 HV10
Impact Testing
according ASTM A 370 at -46°C
minimum 45 J / single 35 J
Micrographic Examation
according ASTM E 562
35-55 % ferrite content
Norsok M-630 Standard / Duplex stainless steel UNS S32205

## Slide 9: Effect of cooling rate

## Slide 10
σ – phase
carbides
475°C -embrittlement
Cr2N
χ-phase
temperature →
time →
Time-Temperature-Transformation diagram for various preciptitates appearing in duplex stainless steel UNS S32205; source: M. Sorg; NACE-2015-5611
Effect of cooling rate

## Slide 11: Approx. Cooling rate 1000°C-700°C: 1.7 K/min over all: 0.2 K/min χ-phase area 120-180 min 475°C – embrittlement more than 10 h
σ – phase
carbides
475°C -embrittlement
Cr2N
χ-phase
temperature →
time →
Approx. 46.0 % Austenite
32.5 % Ferrite
21.5 % intermetallic phases
Effect of cooling rate
TTT diagramm UNS S32205;
scoure: M. Sorg; NACE-2015-5611

## Slide 12: Approx. Cooling rate 1000°C-700°C: 5 K/min over all: 0.25 K/min χ-phase area 30-60 min 475°C – embrittlement more than 4 h
σ – phase
carbides
475°C -embrittlement
Cr2N
χ-phase
temperature →
time →
Approx. 47.5 % Austenite
41.0 % Ferrite
11.5 % intermetallic phases
Effect of cooling rate
TTT diagramm UNS S32205;
scoure: M. Sorg; NACE-2015-5611

## Slide 13: Approx. Cooling rate 1000°C-700°C: 10 K/min over all: 0.35 K/min χ-phase area 20-30 min 475°C – embrittlement more than 4 h
σ – phase
carbides
475°C -embrittlement
Cr2N
χ-phase
temperature →
time →
Approx. 49.0 % Austenite
43.5 % Ferrite
7.5 % intermetallic phases
Effect of cooling rate
TTT diagramm UNS S32205;
scoure: M. Sorg; NACE-2015-5611

## Slide 14: Approx. Cooling rate 1000°C-700°C: 20 K/min over all: 0.5 K/min χ-phase area 10-15 min 475°C – embrittlement approx. 1h
σ – phase
carbides
475°C -embrittlement
Cr2N
χ-phase
temperature →
time →
Approx. 50.5 % Austenite
46.5 % Ferrite
3.0 % intermetallic phases
Effect of cooling rate
TTT diagramm UNS S32205;
scoure: M. Sorg; NACE-2015-5611

## Slide 15: Apporx. Cooling rate 1000°C-700°C: 50 K/min over all: 3.5 K/min χ-phase area 5-10 min 475°C – embrittlement 10-20 min
σ – phase
carbides
475°C -embrittlement
Cr2N
χ-phase
temperature →
time →
Approx. 51.5 % Austenite
47.0 % Ferrite
1.5 % intermetallic phases
Effect of cooling rate
TTT diagramm UNS S32205;
scoure: M. Sorg; NACE-2015-5611

## Slide 16: Approx. Cooling rate 1000°C-700°C: 60 K/min over all: 15-20 K/min χ-phase area 2-5 min 475°C – embrittlement not reached
σ – phase
carbides
475°C -embrittlement
Cr2N
χ-phase
temperature →
time →
Approx. 52.1 % Austenite
47.7 % Ferrite
0.2 % intermetallic phases
Effect of cooling rate
TTT diagramm UNS S32205;
sources: M. Sorg; NACE-2015-5611

## Slide 17: - increase the cooling rate - reduce the process temperature
Effect of cooling rate
Temperature profile
TTT diagramm UNS S32205;
scoure: M. Sorg; NACE-2015-5611
σ – phase
carbides
475°C -embrittlement
Cr2N
χ-phase
temperature →
time →

## Slide 18: Influence of Process Temperature

## Slide 19: comparison of process temperatures → 1200°C → 1140°C → 1100°C → 1040°C without heat treatment approx. cooling rate critical temp.: 10 K/min over all: 1 – 2 K/min
1200°C : Ferrite 47% / Austenite 47.5 % / intermetallic phases 5.5 %
Influence of HIP-Temperature
1040°C : Ferrite 47.5% / Austenite 50 % / intermetallic phases 2.5 %
1140°C : Ferrite 47% / Austenite 51.5 % / intermetallic phases 1.5 %
1100°C : Ferrite 47.5% / Austenite 50.5 % / intermetallic phases 2 %
Notes: PPB – PriorParticalBoundary

## Slide 20: comparison of process temperatures → 1200°C → 1140°C → 1100°C → 1040°C without heat treatment part dimensions 200 x 200 x 400 mm³ approx. cooling rate critical temp.: 10 K/min over all: 1 – 2 K/min
Influence of HIP-Temperature
CPT UNS S32205;
sources: M. Sorg; NACE-2015-5611
Impact energy UNS S32205;
sources: M. Sorg; NACE-2015-5611

## Slide 21: Experimental

## Slide 22: Goal evaluate benefits of fast cooling in industrial HIP facilities Process parameters HIP-Temperature 1140°C for 4 h realized cooling rate approx. 15-20°C / min approx. 1. 000 kg
Experimental Setup
experimental component
HIP-Samples
one-half
conventional heat treatment
one-half
rapid cooling
(HIP facility)

## Slide 23: Investigated wall thickness / edge distance 10 mm / 5 mm 70 mm / 35 mm 120 mm / 60 mm 175 mm / 88 mm
Experimental Setup
sample conditions
  standard heat treatment with water quenching
  Jominy (ASTM A255-10 / DIN EN ISO 642) modified test setup
  no heat treatment after HIP
  HIP with rapid cooling (approx. 40-60 K/min)

## Slide 24: Goal develop and prove a new and cost efficient test method to illustrate the influence of cooling parameters and wall thickness for HIP products
Jominy End Quench Test ASTM A 255 is used to measure hardenability of steels
hardenability is a measure of the capacity of a steel to be hardened in depth when quenched form its austenitizing temperature (usually 800°C to 900°C)
specimen cylinder 100mm in length and 25mm in diameter
cooling rate decreases form the quenched end to the air cooled end: different cooling rates are generated
wall thickness cannot depict by the usual experimental setup
Jominy (ASTM A255-10 / DIN EN ISO 642) modified test setup
Image source:
http://www.wirebiters.com/george-jominy-end-quench-test/ Nov. 2017

## Slide 25: Modification increasing sample length form 100 mm to 200 mm add an isolation add several thermocouples drape in an aluminum casting
thermocouple
specimen
aluminum casting
isolation
ceramic tube
water jet
Jominy (ASTM A255-10 / DIN EN ISO 642) modified test setup

## Slide 26: Results

## Slide 27
Microstructure
edge distance
170 mm
65 mm
5 mm
modified Jominy
test setup
HIP-Process
with rapid cooling
standard heat treatment
water quenching

## Slide 28
Austenite/Ferrite ratio
Chart: standard heat treatment - water quenching
| 5 | 35 | 65 | 170
austenite | 54 | 53 | 51 | 48
ferrite | 46 | 47 | 49 | 52
precipitations | 0 | 0 | 0 | 0
Chart: modified Jominy test setup
| 5 | 35 | 65 | 170
austenite | 54 | 52 | 50 | 49
ferrite | 46 | 48 | 50 | 51
precipitations | 0 | 0 | 0 | 0

## Slide 29
Chart: HIP without heat treatment
| 5 | 35 | 65 | 170
austenite | 52 | 51 | 50 | 51
ferrite | 43 | 44 | 44 | 41
precipitations | 5 | 5 | 6 | 8
Chart: HIP with rapid cooling
| 5 | 35 | 65 | 170
austenite | 56 | 54 | 51 | 51
ferrite | 44 | 46 | 48 | 46
precipitations | 0 | 0 | 1 | 3
Austenite/Ferrite ratio

## Slide 30
Corrosion resistance
Chart: wall thickness in mm →
| 5 | 35 | 65 | 170
Standard heat treatment - water quenching | 65.2 | 65.6 | 64.7 | 63.2
modified Jominy test setup | 64.8 | 62.1 | 63 | 62
HIP-Process with rapid cooling | 63.2 | 63.1 | 62 | 59.8
HIP-Proces without heat treatment | 46 | 47 | 43.5 | 42

## Slide 31
Chart: wall thickness in mm →
| 5 | 35 | 65 | 170
Standard heat treatment - water quenching | 265 | 242 | 235 | 224.5
modified Jominy test setup | 255 | 238 | 215 | 205
HIP-Process with rapid cooling | 185 | 82 | 35 | 18
HIP-Proces without heat treatment | 26 | 21 | 18 | 16
Impact energy / toughness
brittle fracture
ductile fracture

## Slide 32
Chart: wall thickness in mm →
| 5 | 35 | 60 | 88
Schnellkühlung | 241 | 245 | 248 | 244
konventionelle Wärmebehandlung | 242 | 244 | 246 | 247
Chart: wall thickness mm
| 5 | 35 | 60 | 88
Schnellkühlung | 541 | 545 | 538 | 520
konventionelle Wärmebehandlung | 583 | 586 | 579 | 565
Yield strength
Mechanical properties
Hardness
max. 271 HB
according to NORSOK M-630 Standard
min. 450 MPa
according to NORSOK M-630 Standard

## Slide 33: Conclusion & Discussion

## Slide 34
The results of corrosion measurements do not illustrate a significant effect of heat treatment or wall thickness / edge distance
A small amount of intermetallic phases shows no significant reduction of corrosion resistance
Demands and requirements of the NORSOK Standard will be achieved by fast cooling after HIP-Process only for thin-walled components (up to approx. 70mm)
Notch impact energy is affected very strong by a small amount of intermetallic phases / precipitations
The fracture surface of non heat treatment specimens shows brittle characteristics due to precipitations
Conclusion of results

## Slide 35: UNS S2205
Example calculation
UNS S2205 1.000 kg
specific heat capacity approx. 0.5 KJ/kg K
temperature difference 350 K (1000°C to 650°C)
specific heat 175 MJ
to prevent intermetallic phases 120 seconds (175 K/min)
cooling power 1.45 MW
1.45 kW/kg
High cooling rate / Quenching
σ – phase
carbides
475°C -embrittlement
Cr2N
χ-phase
temperature →
time →
TTT diagram UNS S32205;
source: M. Sorg; NACE-2015-5611

## Slide 36: UNS N07718 INCONEL 718 ... usually smaller components ... lower critical temperature difference to cross ... approx. 6 minutes to avoid intermetallic phases
TTT diagram IN718
source: A. Mostafa et. al; metals 2017 – 7, 196; 7060196
High cooling rate / Quenching
temperature in °C →
time in h →

## Slide 37: UNS N07718 INCONEL 718
Example Calculation:
UNS N07718 1.000 kg
specific heat capacity approx. 0.435 KJ/kg K
temperature difference 300 K (1050°C to 750°C)
specific heat 130.5 MJ
to prevent intermetallic phases 360 seconds (50 K/min)
cooling power 0.36 MW / 360 KW
0.36 kW/kg
High cooling rate / Quenching
temperature in °C →
time in h →
TTT diagram IN718
source: A. Mostafa et. al; metals 2017 – 7, 196; 7060196

## Slide 38
Process temperature and wall thickness is influencing
      Ferrite/Austenite ratio
      Grain size
      corrosion resistance
      mechanical properties, in particular: toughness
Rapid cooling rates
      cannot replace conventional heat treatment to prevent intermetallic phases for thick-walled components made of UNS S32205
      Help to accelerate the HIP-Process in industrial scale
          Parts can be removed faster form your HIP-unite
          Increasing the economic efficiency of the HIP-process / HIP-facility
      help to control cooling rates
      can be used for “small parts” or less sensitive materials
Conclusion

## Slide 39: Thanks for your attention!
UNS S32205 - HIP-Temperature 1140°C / Beraha II etching