## Slide 1
Department of Materials Science and Engineering
The University of Sheffield
*n.c.hyatt@sheffield.ac.uk
Scientific Basis for Nuclear Waste Management Symposium
29th October – 3rd November 2017
Thermal Treatment of
High Dose Spent Absorbents
Neil C Hyatt*, Paul G. Heath, Laura J. Gardner, Claire L. Corkhill and Martin C. Stennett
The views expressed in this talk are the personal opinion of the speaker and do not necessarily reflect those of sponsors or funding agencies
@ISL_Sheffield

## Slide 2
March 11th 2011 Triple Disaster:
Earthquake, Tsunami and Nuclear Accident
Information credit:
http://www.bbc.co.uk/news/science-environment-12726628
A 9.0 magnitude earthquake resulted in 15m tsunami that inundated the Fukushima Daiichi NPP site (10m above sea level). Power outage and damaged back-up generators resulted in the loss of cooling to units 1-3, which lead to a level 7 major nuclear accident.
Information credit: TEPCO (http://www.tepco.co.jp/en/decommision
Generation of highly contaminated water
Notes: Reactors 1-3 lost active cooling of the core, water circulation functions (spent fuel)
Reactor cores 1-3 melted during the first three days
Plants 10 metres above sea level, sea pumps 4 m above sea level
Turbine halls were under 5 m of water at daiichi
After the earthquake units 1-3 were automatically shutdown, power via 6 external sources were lost due to earthquake damage so the emergency generators in turbine building basements took on the load of active cooling and heat exchange. The tsunami submerged the seawater pumps and dieseal generators. Residual heat from the fuels rods, led to the generation of steam, which was directed into the suppression chamber but the pressure still continued to rise.
As the water level decreased exposing the fuel, the temp rose to 2800oC. The pressure should normally vent through the stack however with the loss of power this backflowed into the top of the reactor building.
Until water treatment plants were built that could treat and recycle the water coolent, units 1-3 had to be stabilised with water additions, which began with clean water however that was replaced with sea water. In addition to cooling the reactors, the spent fuel ponds above the reactor cores needed active cooling.
14:46: A 9.0 magnitude earthquake: reactors 1-3 automatically shut down, reactors 4-6 in maintenance mode
Loss of power due to the earthquake
15:27: First tsunami hits the site
A 14-15 metre tsunami overcomes the se wall inundating the facility and disables the 12/13 backup diesel generators (all but one in the basements, fuel tanks washed away). And heat exchangers + sea pumps. Surviving generator for reactors 5+6
The emergency core cooling along with all electrical power supply faied
Reactors 1-3 lost active cooling of the core, water circulation functions (spent fuel)
Reactor cores 1-3 melted during the first three days
Plants 10 metres above sea level, sea pumps 4 m above sea level
Turbine halls were under 5 m of water at daiichi

## Slide 3
SARRY: IONSIV and crystalline silicotitanate
Kurion: “ion specific media” a.k.a. engineered chabazite
ALPS: CsTreat®, SrTreat® CoTreat® and SbTreat (Fortum Co.)
Image credit: TEPCO
Generation of High Dose Spent Absorbents
Photographs courtesy of TEPCO (1st April 2016)
Unit 2
Unit 3
Water Treatment Plan
Notes: Simplified active water and retrieval and recovery system (SARRY)
ALPS Multi-nuclide removal equipment
Designed to remove 62 radionuclides (excluding tritium and Cs)
- Waste materials (slurry, spend absorbent) are transferred into high integrity containers (HIC), stored at the temporary storage facility

## Slide 4
Challenges associated with High Dose Spent Adsorbents
Several ion-specific microporous materials
Key nuclides include: 90Sr, 137Cs, 60Co
Granular dispersible materials
Self heating (steam production)
Radiolysis (hydrogen production)
Stress corrosion cracking (sea salt aggravated)
HDSAs require waste conditioning process
Image: Yamagishi JNST 51 (2014) 1044.
Ref: TEPCO (http://www.tepco.co.jp/en/decommision/planaction/alps/index-e.html
3,232 HICs as of 21/06/2016
High Dose Spent Absorbents

## Slide 5
High Dose Spent Absorbents
Sellafield
SIXEP: Site Ion-exchange Effluent Plant (a.k.a. “the kidneys of Sellafield”)
Built to decontaminate pond water priotr to discharge to Irish Sea, operating since 1985
Process uses clinoptilolite ion exchange media and sand filtration bed
Waste arisings: 2,146.8 m3; activity a 2 x 10-2 TBq/m3 b,g 7 x 101 TBq/m3
Cement encapsulation potentially problematic: * Pozzolanic reaction with cement matrix * Volume increase by a factor of 5-10
Interest in alternative conditioning process for granular HDSA

## Slide 6
UoS HIP: Typical can diameter 30 – 300 mm
Image credit:
Stephanie Thornber
Hot Isostatic Pressing
Advantages of HIPing
No volatile off gas during process; min. secondary waste
One process for multiple waste streams
100 % waste loading possible
Conditioned waste volume minimised
Batch process: flexibility and accountability
Inherently scalable

## Slide 7
UoS HIP: Typical can diameter 30 – 300 mm
Hot Isostatic Pressing
B
A
Photographs of HIP canisters:
(A) Pre-HIP, (B) Post-HIP
Advantages of HIPing
No volatile off gas during process; min. secondary waste
One process for multiple waste streams
100 % waste loading possible
Conditioned waste volume minimised
Batch process: flexibility and accountability
Inherently scalable

## Slide 8
Case Study 1: Clinoptilolite
Notes: Optimization – reduce the risk of treatment of nuclear waste, if lower T and P is used the plant can have a higher throughput which improves productivity and the economics of HIPing a waste treatment method. To assess if successful, the performance will be measured. Evaluate and feed back in to fine tune the optimised HIP cycle conditions. Make the conditions as low as possible whilst maintaining a durable product.

## Slide 9
Clinoptilolite was supplied by the National Nuclear Laboratory
Oxide | wt. %
SiO2 | 76.5
Al2O3 | 13.6
TiO2 | 0.1
MgO | 0.8
Na2O | 3.8
CaO | 1.9
Fe2O3 | 1.1
K2O | 1.8
BaO | 0.1
SO3 | 0.1
SUM | 100.0
Composition: (Na,K,Ca)2‑3Al3(Al,Si)2Si13O36·12H2O
As-received Clinoptilolite
Clinoptilolite Structure
Cs/Sr exchanged – 10wt% Cs2O & 0.5wt% SrO
Mixed with sand and 5wt% Na2B4O7 or NaAlO2
HIP: 600oC bake out, 1200 oC / 2h, 100 MPa

## Slide 10
Clinoptilolite HIP wasteform

## Slide 11
Clinoptilolite HIP wasteform

## Slide 12
Clinoptilolite HIP wasteform

## Slide 13
Clinoptilolite HIP wasteform

## Slide 14
Clinoptilolite HIP wasteform
Clino-NaAlO2
Clino-Na2B4O7

## Slide 15
Clinoptilolite HIP wasteform
Cassingham et al., Min. Mag., 79, 1529-1542 (2015)

## Slide 16
Clinoptilolite HIP wasteform

## Slide 17
Clinoptilolite HIP wasteform

## Slide 18
Clinoptilolite HIP wasteform

## Slide 19
Clinoptilolite HIP wasteform

## Slide 20
Case Study 2: SrTreat®
Notes: Optimization – reduce the risk of treatment of nuclear waste, if lower T and P is used the plant can have a higher throughput which improves productivity and the economics of HIPing a waste treatment method. To assess if successful, the performance will be measured. Evaluate and feed back in to fine tune the optimised HIP cycle conditions. Make the conditions as low as possible whilst maintaining a durable product.

## Slide 21
SrTreat® was supplied by the Fortum Nuclear Services
OxideMnO2 | wt. %
TiO2 | 92.1
Na2O | 7.9
K2O | 0.0
SrO | 0.0
Cr2O3 | 0.0
MnO2 | 0.0
Fe2O3 | 0.0
NiO | 0.0
SUM | 100.0
Composition: “Na2Ti3O7·xH2O”
As-received Sr-Treat®
SrTreat® Structure
Sr exchanged – 14wt% SrO
HIP: 600oC bake out, 1200 oC / 2h, 100 MPa

## Slide 22
SrTreat® HIP Wasteform
Cs/Sr exchanged SrTreat® – HIPped without additives, i.e. 100 % waste loading
HIP: 600oC bake out, 1200 oC / 2h, 100 MPa
Sr Exchanged SrTreat®
1 mm
Waste form comprised of well defined sintered grains retaining evidence of the original Sr gradient as shown in the pre-treated powders
Hiped SrTreat®

## Slide 23
SrTreat® HIP Wasteform
Cs/Sr exchanged SrTreat® – HIPped without additives, i.e. 100 % waste loading
HIP: 600oC bake out, 1200 oC / 2h, 100 MPa

## Slide 24
SrTreat® HIP Wasteform
A = Na1.8Sr0.2Ti6O13 B = Na1.3Sr0.7Ti3O7 C = SrTiO3

## Slide 25
SrTreat® HIP Wasteform

## Slide 26
SrTreat® HIP Wasteform

## Slide 27
Thermal Treatment of
High Dose Spent Absorbents
The views expressed in this talk are the personal opinion of the speaker and do not necessarily reflect those of sponsors or funding agencies
@ISL_Sheffield
Conclusions
Hot isostatic pressing of HDSAs yields robust glass and ceramic wasteforms
Material dissolution rates are similar to or several orders of mag. below HLW glass
VSI is a powerful and necessary technique for resolving phase contributions
Net volume reduction of ca. 20% vs. untreated waste (vs. 5-10x dilution cement)
Capable of delivering >£100M savings in storage, transport and disposal

## Slide 28
Case Study 3: Chabazite
Notes: Optimization – reduce the risk of treatment of nuclear waste, if lower T and P is used the plant can have a higher throughput which improves productivity and the economics of HIPing a waste treatment method. To assess if successful, the performance will be measured. Evaluate and feed back in to fine tune the optimised HIP cycle conditions. Make the conditions as low as possible whilst maintaining a durable product.

## Slide 29
Chabazite was purchased from Verdi as product “Zeover”
Image credit: www.iza-online.org
Oxide | wt. %
SiO2 | 52.0
Al2O3 | 17.0
TiO2 | 0.5
P2O5 | 0.3
MnO | 0.2
MgO | 2.0
Na2O | 0.6
CaO | 5.7
Fe2O3 | 3.6
K2O | 6.1
H2O* | 12.0
*Structural water lost at 120 °C
70 % Chabazite – used in Kurion process
18 % Volcanic glass (i.e. obsidian glass)
5 % K-feldspar (K-aluminosilicates)
3 % Pyroxene (e.g. diopside)
2 % Biotite
2 % Phillipsite
Composition: (Na0.14K1.03Ca1.00Mg0.17)[Al3.46Si8.53O24]·9.7H2O
As-received Chabazite
Chabazite Structure

## Slide 30
Method: Chabazite (250g) was exchanged in a 0.1 M CsNO3 solution (using 1 L UHQ @ 18.2 MΩ) for 24 hours. The solution was then replaced and mixed for an additional 24 hours. After 48 hours, the ion exchanged (IX) chabazite was vacuum filtered and dried for 48 hours at 95 °C. IX chabazite: Cs2O 1.8 wt. %
Ideal bake-out temperature for Chabazite is >300 °C.
Therefore all HIP canisters were baked-out at 300 °C under vacuum
K-feldspar = orthoclase (KAlSi3O8)
Chabazite Ion Exchange

## Slide 31
Heterogeneous mix of chabazite, anorthite, K-feldspar and obsidian glass
Cs sorption only associated with the porous chabazite particles
Obsidian glass
Chabazite
Anorthite
K-feldspar
Obsidian glass
K-feldspar
Chabazite
Anorthite
Resin mounted and polished to a 1 µm finish
Chabazite Ion Exchange

## Slide 32
100 MPa
50 MPa
The chabazite structure has collapsed at all T and P studied, leading to the formation of multiphase glass-ceramics.
Phases formed include: albite, anorthite, diopside and K-feldspars, plus amorphous glass phase (diffuse scattering)
Increasing process temperature leads to formation of K-feldspar at expense of anorthite and diopside
A: CaAl2Si2O8 B: NaAlSi3O8 D: MgCaSi3O8 K: KAlSi2O6
K-feldspar
Anorthite+ Albite
HIPed Chabazite: XRD

## Slide 33
A: 1250 °C
B: 1150 °C
C: 1050 °C
A
Fe Oxide
Spinel vein
A
Formation of glass-ceramic microstructure with negligible porosity at all temperatures
Cs partitions primarily to K-feldspar crystallised from glass melt (bright phase)
1050°C: evidence of anorthite and K-feldspar relics, micro-cracks from differential thermal expansion vs. matrix
1150°C: relatively homogeneous microstructure with trace anorthite and feldspar relics
1250°C: Na-Ca-Al-Si glass with primary and secondary recrystallized Cs / K-feldspar, no relic material.
K
K
SEM/EDX: HIPed at 100 MPa
Cs-K
Cs-K
G(A)
Anorthite (A): CaAl2Si2O8 Albite (B): NaAlSi3O8 Diopside (D): MgCaSi3O8 K-feldspar (K): KAlSi2O6
A
Cs-K
G
G
Cs-K
Notes: Increasing the temperature leads to a complete incorporation of silicate minerals within the bulk matrix, no major microstructural difference can be assigned due to reduced pressure.

## Slide 34
Similar sequence of microstructure formation as at 100 Mpa
Cs primarily partitions to recrystallized K-feldspar phase
1250°C: Na-Ca-Al-Si glass with only primary Cs / K-feldspar, no relic material
1250oC / 50 MPa – simple two phase microstructure, lowest process pressure – dissolution experiments
A
Spinel vein
A
K
D
A: 1250 °C
B: 1150 °C
C: 1050 °C
SEM/EDX: HIPed at 50 MPa
Anorthite (A): CaAl2Si2O8 Albite (B): NaAlSi3O8 Diopside (D): MgCaSi3O8 K-feldspar (K): KAlSi2O6
Cs rich K
Cs-K
Cs-K
Fe Oxide
A
A
A
B
Notes: Increasing the temperature leads to a complete incorporation of silicate minerals within the bulk matrix, no major microstructural difference can be assigned due to reduced pressure.

## Slide 35
Case Study 2: CoTreat®
Removes radioactive Co, corrosion products (Mn, Fe, Ni, Zn)
Inorganic sodium titanium oxide (grain size 0.30-0.85 mm)
Decontamination factor: 500 to 2000
Max operating tem: 300 °C
Optimal pH range: 5 to 7
Ref: http://www.fortum.com
Part of the Fortum Nuclear Services Nuclide Removal System (NURES™)
Image adapted from Liu et al., (2010) J. Raman Spectroscopy

## Slide 36
The CoTreat® HDSA was ion exchanged with 200 ppm each of Ni, Fe, Mn, Zn, Ni, as:
Co(NO3)2·6H2O
Fe(NO3)3·9H2O
Mn(NO3)2·4H2O
Ni(NO3)2·6H2O
Zn(NO3)2·6H2O
Method: Two 24 hour exchanges at pH 7 in distilled and simulant ocean water. After 48 hours, the IX CoTreat was vacuum filtered and dried for 48 hours at 95 °C.
Prepared according to ASTM D1141-98 (2003)
Simulant ocean water
CoTreat® Ion Exchange

## Slide 37
High Temperature CoTreat®
The initial characterisation of CoTreat® indicated that the structure is based on a disordered sodium titanosilicate.
After ion exchange, subtle changes were observed in the diffraction patterns, this indicates that the exchange occurred within the titantate layers of the material.
After exposure of CoTreat to 1000 °C (1 hour) crystalline Na2Ti6O13 was observed, change in relative intensities at 1200 °C – volatilisation of Na2O
XRD
CoTreat® - 6 hr scan
Notes: HT – to see what is likely to form during HIP process

## Slide 38
The as-received CoTreat® consists of Ti and Na spherical particles of various sizes.
Uniform sorption of Co, Mn, Ni and Zn whilst the Fe appears localised within the between the larger CoTreat® particles.
CoTreat® - SEM/EDX

## Slide 39
The ideal bake-out temperature for CoTreat® is >200 °C.
Therefore all HIP canisters were baked-out at 300 °C under vacuum
CoTreat® (H2O exchanged)
Cs Exchanged CoTreat®
CoTreat® - Dehydration

## Slide 40
At 600 °C: crystallisation of anatase TiO2, plus residual non-crystalline component (diffuse scattering)
At 800-1200 °C: formation of rutile TiO2 and Na2Ti9O19 / Na2Ti6O13
At 1400 °C: only rutile observed – volatilisation of Na2O inventory
No distinctive separate phase incorporating Fe, Co, Ni, Zn
No difference in phase assemblage between ocean / distilled water exchange
Furnace programme: Ramp/Cool at 3 °C/min, dwell at T for 2 hours.
Distilled H2O
Ocean H2O
CoTreat® - XRD

## Slide 41
Effective sintering at 1200-1400oC, but substantial loss of Na2O inventory at 1200oC
600-1000oC: Ni, Co, Mn, Zn partition to Na2Ti9O19 / Na2Ti6O13 phase; Fe in separate Na-rich phase
1200-1400oC loss of Na2O inventory and formation of Na-rich phases; some phase separation of Mn and Ni phases
Residual porosity after sintering at all temperatures
CoTreat® - Distilled H2O
Notes: So prior to HIPing the IE materials, preliminary work looked at pressed pellets of the materials to get a rough understanding of what temperatures the materials start to react and where potential loss occurs. To see if HT processing works on these samples and if so, what phases are formed and when. Used to inform the HIP studies.

## Slide 42
Similar to materials sintered from distilled water exchange
Chloride retained up to 1000oC
CoTreat® - Ocean H2O

## Slide 43
100 MPa
37.68
38.15
38.98
29.24
25 MPa
39.74
38.10
31.49
28.94
Pre-dried at 300 °C for 12 hrs (general muffle furnace)
2
1
30.28
26.38
31.87
26.00
4
Distilled H2O
Ocean H2O
3
10 mm
10 mm
10 mm
10 mm
CoTreat® formed dense monoliths after the HIPed process
CoTreat® - HIPed at 1250 °C

## Slide 44
Similar phase assemblage irrespective of distilled / ocean water and pressure at 1250oC
The principal phases observed were rutile TiO2, Na2Ti9O19 and Na2Ti6O13
HIP containment enables retention of Na inventory
Lower pressure preferred for process scale application – reduced stored energy
HIPed CoTreat® - XRD
100 MPa
25 MPa

## Slide 45
Distilled H2O
Ocean H2O
Co, Fe, Ni, Mn, Zn partition mainly into Na2Ti9O19 / Na2Ti6O13 phases
Limited if any substitution into rutile TiO2 phase
Formation of traceNiCl2 and KCl in ocean water exchanged sample – encapsulated in Na-titanate matrix
Could consider isotopic dilution of Ni-63 by spiking with nat. NiO
HIPed CoTreat® - SEM/EDX

## Slide 46
Magnox Swarf2
Magnox fuel1
Magnesium potassium phosphate cement (MKPC) is a near neutral cementitious system with a high early compressive strength. Acid-base reaction:
Key characteristics
Rapid early strength
Set within 24 hours
Low water demand
Low permeability
Water is chemically bound within the crystal structure
Applications
MgO (s) + KH2PO4 (s) + 5H2O (l)  MgKPO4·6H2O (s)
Struvite-K
[1] www.sellafieldsites.com/solution/spent-fuel-management/magnox-reprocessing/ [Date accessed: Nov/2016]
[2] NDA (2010) ‘Geological Disposal: Package evolution status report.’ NDA Report No: NDA/RWMD/031
Magnesium Potassium Phosphate Cements
0.24 w/s: 1.7 MgO: 1 KH2PO4: 4.72 H2O with 50 wt. % FA (or GBFS) + 2 wt. % H3BO3
Notes: Emergency repair work (runways, roads, bridges)
Argonne National Laboratory (Ceramicrete) – stabilisation of various waste streams
Under investigation in the UK for reactive metal ILW encapsulation
To reduce the heat output from the exothermic acid-base reaction, MKPCs are blended with supplementary cementitious materials; in this case FA and GBFS.

## Slide 47
High field NMR (19.96 T) – University of Warwick
27Al
29Si
FA/MKPC GBFS/MKPC
Fly ash and slag have been demonstrated conclusively for the first time that FA and GBFS participate in the mechanical and microstructural development of blended MKPC binders through the formation of amorphous secondary reaction products. (Gardner et al., (2015) Cement and Concrete Research, vol. 74, pp. 78-87.)
Characterisation of MKPC binders
FA/MKPC
NMR: GBFS/MKPC shown only
Secondary reaction products
Notes: From the formulation experiments it was clear that the two SCMs result in differing mechanical and physical properties. To investigate this further detailed analysis on the chemical environments in both systems was carried out.
Start: To understand the MKPC binders, we had to analyse the chemical and microstructure environments of these blended MKPC binders after they have reacted, which involved the use of solid state NMR, SEM/EDX, XRD amongst other techniques especially as we expected there was an amorphous component to these systems
Different glasses fractions (FA/GBFS), resulting in a difference of compressive strength, which could likely be the result of partial dissolution of GBFS resulting in a postulated potassium aluminosilicate phase.
Even though my research has mainly focussed on cement, I feel that the techniques learnt and careful sample preparation will be applicable to glass research, especially alteration layers or precipitated phases.
To reduce the heat output from the exothermic acid-base reaction, MKPCs are blended with supplementary cementitious materials; in this case FA and GBFS. Through detailed SEM and solid state NMR, it was conclusively found that these SCMs take part in a secondary reaction, rather than being inert fillers, which was previously thought. The secondary reaction product is likely to be an amorphous potassium aluminosilicate phase. High field NMR conducted at the University of Warwick, revealed the presence of a second potassium environment that compared with the Al and Si NMR data from Durham University lead to the assumption of this type of phase. No evidence of alternative Mg or P phases was identified.
In the Al spectrum, the presence of the resonance at -9.5 ppm, clearly highlight that a reaction with the Al species occurred compared to the unreacted GBFS. In the Si spectrum,
There is a significant difference between the FA/MKPC and GBFS/MKPC binders at 0.24 w/s. FA/MKPC achieved a CS value of 24.7 MPa ± 3.0 MPa and GBFS/MKPC achieved a CS value of 34.7 MPa ± 0.5 MPa. The powder properties indicate that the density of GBFS was greater than FA, so it is expected to form a denser matrix in the reacted binders and thus, improve the mechanical properties. Also, the angular GBFS particles are expected to interlock much better with the matrix than the spherical FA particles, however this physical interlocking of the GBFS particles due to better particle packing cannot be solely attributed the significant 10 MPa difference observed in mechanical performance identified in the FA/MKPC and GBFS/MKPC systems as the 0.26 w/s GBFS/MKPC binder achieved comparable compressive strengths to the 0.26 w/s FA/MKPC binder.

## Slide 48
Data shown is for as-received CoTreat®
Phases: Struvite-K, MgO
MKPC Encapsulation - CoTreat® (25 wt. %)
or Ti(HPO4)2·2H2O
Formation of additional secondary reaction products
FA/MKPC + CoTreat®
GBFS/MKPC + CoTreat®
CoTreat®
FA
MKPC
MgO
CoTreat®
MgO
MKPC
GBFS

## Slide 49
Key findings
Chabazite can be completely converted into multiphase glass-ceramic product with stable minerals: K-feldspars, anorthite, albite and diopside formed.
The microstructural features vary as a result of T/P: at lower conditions, more angular features were observed (associated with K-feldspars and anorthite, CaAl2Si2O8).
Cs appears to be associated with K, Al and Si across all samples, although it is not incorporated into the anorthite regions.
Exposing CoTreat® to high temperature can predict the likely phases formed under HIP T/P conditions (up to 1200 °C).
HIPing ion exchanged CoTreat® can be successfully achieved at 100 and 25 MPa.
HDSAs can be encapsulated within MKPC (but with increased water additions!)
Evaluate the durability of the HIPed products using MCC-1 and PCT-B dissolution methods
Encapsulate the HDSA materials within cementitious systems (MKPC and PC) for comparison
Determine the radiation stability of the HIPed products
Ongoing Work
Conclusions

## Slide 50
This research was performed in part at the MIDAS Facility, at the University of Sheffield, which was established with support from the Department of Energy and Climate Change
Thank you!
We gratefully acknowledge funding support from:
Thank you to Dr Paul Heath and Stephanie Thornber
Acknowledgements