## Slide 1: Towards understanding the dissolution of vitrified nuclear waste in a cementitious geological disposal facility
Claire Corkhill, Colleen Mann, Daniel Backhouse, Adam Fisher, Russell Hand, Neil Hyatt
University of Sheffield
Scientific Basis for Nuclear Waste Management 2017, Sydney, November 2017
@clairecorkhill
@ISL_Sheffield

## Slide 2: High pH environments in geological disposal
Notes: We are interested in high pH glass dissolution for several reasons:
1. under slow groundwater flow conditions, the repository is likely to buffer to slightly alkaline pH – bentonite will buffer to values between 7 and 10.5, depending on the groundwater composition
2. there is potential for interaction of alkaline solutions from concrete vault structures on the long time scales of geological disposal
3. the potential co-location of vitrified UK HLW with cementitious UK ILW may lead to the interaction of vitrified products with a high pH, Ca-rich groundwater from the cement backfill

## Slide 3: Glass dissolution and high pH
Transition State Theory for glass: (Grambow, 1985)
When combined with Ca leached from cement, the formation of Si-gel is disrupted and a range of minerals are precipitated.
Under hyperalkaline conditions, the solubility of sparingly soluble species increases
Notes: Glass dissolution is a complex process, which is highly dependent on both the composition of the glass and the environment in which dissolution takes place. It can be described by a range of processes, which are here also split into several stages:
In the first, when glass comes into contact with water, interdiffusion between hydrogenated species and alkalis occurs, followed by hydrolysis of Si-O-M bonds. This part is known as the forward rate of reaction.
As the solution becomes saturated with dissolved species from the glass, particularly silica, thermodynamic quasi-equilibrium is approached, and a layer of si-containing gel recondenses on the glass surface. This forms a protective layer, and corresponds to a drop in the dissolution rate (the rate drop)
The residual rate refers to the period of glass dissolution where lots of different processes compete to keep the dissolution rate relatively low, for example further diffusion of water into the glass leads to the gradual build-up of gel and alteration layers containing various elements dissolved from the glass. It is also postulates that the slow transformation of amorphous alteration layer products into stable crystalline ones occurs. The mechanisms vary greatly depending on the glass and solution composition.
It has also been reported that glass dissolution can resume after long periods of time, again dependent on glass and solution compositions.

## Slide 4: Glass compositions
SiO2 | Al2O3 | B2O3 | MgO | BaO | SrO | Na2O | Li2O | Cs2O | ZrO2
47.67 | 2.55 | 18.65 | 6.82 | 0.15 | 0.17 | 9.57 | 9.24 | 0.24 | 0.77
Fe2O3 | CeO2 | Cr2O3 | La2O3 | Nd2O3 | Pr2O3 | Sm2O3 | Y2O3 | TiO2
1.31 | 0.45 | 0.29 | 0.13 | 0.39 | 0.12 | 0.08 | 0.06 | 0.03
P2O5 | NiO | MoO3 | Gd2O3 | Total
0.09 | 0.48 | 0.67 | 0.01 | 99.94
MW25 (mol%)
International Simple Glass (mol%)
SiO2 | Al2O3 | B2O3 | Na2O | CaO | SrO | ZrO2 | Total
56.2 | 6.1 | 17.3 | 12.2 | 5.0 | 0.17 | 3.3 | 100.1
Notes: Glass dissolution is a complex process, which is highly dependent on both the composition of the glass and the environment in which dissolution takes place. It can be described by a range of processes, which are here also split into several stages:
In the first, when glass comes into contact with water, interdiffusion between hydrogenated species and alkalis occurs, followed by hydrolysis of Si-O-M bonds. This part is known as the forward rate of reaction.
As the solution becomes saturated with dissolved species from the glass, particularly silica, thermodynamic quasi-equilibrium is approached, and a layer of si-containing gel recondenses on the glass surface. This forms a protective layer, and corresponds to a drop in the dissolution rate (the rate drop)
The residual rate refers to the period of glass dissolution where lots of different processes compete to keep the dissolution rate relatively low, for example further diffusion of water into the glass leads to the gradual build-up of gel and alteration layers containing various elements dissolved from the glass. It is also postulates that the slow transformation of amorphous alteration layer products into stable crystalline ones occurs. The mechanisms vary greatly depending on the glass and solution composition.
It has also been reported that glass dissolution can resume after long periods of time, again dependent on glass and solution compositions.

## Slide 5: What we’ve learnt (or now know what we don’t know)
Effect of high pH
Effect of Ca(OH)2 rich solutions
Effect of cementitious solutions

## Slide 6: Dissolution kinetics in the forward rate
Under conditions of the single pass flow through experiment, the saturation state of the system is zero:
Solution composition | pH |  | 
 | 23°C | 40°C | 70°C
THAM / HNO3 pH adjustment | 8.0 | 7.9 | 7.6
THAM / HNO3 pH adjustment | 10.0 | 9.8 | 9.3
LiOH / LiCl pH adjustment | 12.0 | 11.5 | 10.7

## Slide 7: Dissolution kinetics at high pH
23°C
40°C
70°C
90°C
 | η | Ea/ kJ mol-1 | log / g m-2 d-1 | / g m-2 d-1 | r2
B | 0.49 ± 0.05 | 76.6 ± 6.3 | 7.4 ± 0.9 |  | 0.96
Na | 0.52 ± 0.05 | 80.9 ± 6.4 | 8.1 ± 1.0 |  | 0.96
Si | 0.47 ± 0.06 | 88.9 ± 6.9 | 9.8 ± 1.0 |  | 0.96
 | η | Ea/ kJ mol-1 |  |  | r2
B | 0.49 ± 0.05 | 76.6 ± 6.3 | 7.4 ± 0.9 |  | 0.96
Na | 0.52 ± 0.05 | 80.9 ± 6.4 | 8.1 ± 1.0 |  | 0.96
Si | 0.47 ± 0.06 | 88.9 ± 6.9 | 9.8 ± 1.0 |  | 0.96
pH power law coefficent very similar to other borosilicate glasses (range 0.39 – 0.51)
Ea similar to other borosilicate glass compositions (70 – 90 kJ mol-1)
log values similar to SON68, AFCI, P0798 & ISG*
Cassingham et al. Mineralogical Magazine, 79, 1529 (2015) & (2017); *Fisher et al. in prep
MW25
Notes: The estimated error of log k is typically of the order of 10%. When standard propagation of error manipulation is undertaken, the error value is between two and three times the value of k, implying that k may become negative, which is physically impossible. The maximum negative error has been taken as being equal to k.

## Slide 8: What we’ve learnt (or now know what we don’t know)
What we’ve learnt
What we don’t know
How far do you need to push the compositional envelope to get different behaviour?
e.g. Ca, Zn variation of MW25?
MW25 behaves similarly to other borosilicate waste glasses with respect to pH, in the forward rate

## Slide 9
Chart: Time (days)
| 1 | 3 | 7 | 14 | 21 | 28 | 42 | 56 | 70 | 84 | 112 | 140 | 168
UDW | 0.00031941 | 0.00089586 | 0.001876 | 0.0027697 | 0.003319 | 0.0038139 | 0.0039493 | 0.0040442 | 0.004464 | 0.0048492 | 0.0055044 | 0.0059296 | 0.0064517
CSS | 7.0632e-05 | 0.00018252 | 0.00044779 | 0.00087833 | 0.0011845 | 0.0016685 | 0.0021874 | 0.0026058 | 0.0029339 | 0.0032975 | 0.0038165 | 0.0043491 | 0.0044493
MW25 glass dissolution in Ca(OH)2, 500C, CO2-exclusion
Corkhill et al. International Journal of Applied Glass Science, 4, 341 – 356 (2013)
Dissolution in the presence of Ca(OH)2 was an order of magnitude lower than in initially pure water.
Water
Ca(OH)2
NR(B) water = 1.29 x 10-4 g m-2 d-1
NR(B) Ca(OH)2 = 5.92 x 10-5 g m-2 d-1
SA/V = 10,000 m-1
Mg-Si phases were characterised on the surface of monoliths, and non-defined Ca-Si phases were observed.
SA/V = 10 m-1
Notes: Comparing boron release in deionised water and saturated calcium hydroxide solution we can see that the dissolution profiles are very different, thus the mechanisms of dissolution are expected to differ.
The dissolution rate was an order of magnitude lower in Ca(OH)2 than in initially pure water
When we look to the surface of monolith samples under the same conditions, we find that M-S-H phases (sepiolite) and uncharacterised C-S-H phases begin to form on the surface of the glass, which may be responsible for the observed “rate drop” in Ca(OH)2.
These were absent on the surfaces of glass leached in water.
In water, we observed an initial fast rate of Si release and solution saturation was achieved after ~28 days
In Ca(OH)2, the mechanism is clearly different - Ca was consumed during the first 28 days of dissolution and Si was not released until the Ca concentration reached a threshold. This implies that Ca was reacting with the evolving glass surface.
(We observe this behaviour irrespective of glass compositions studied).
Note that Ca depletion cannot be attributed to carbonation and precipitation of calcium carbonate, because the Ca concentration in the blank solution remains constant.
Consistent with the solution data (and XRD data on the previous page), a thick alteration layer comprising Ca, Si, Al and Mg was observed in a cross section of the glass reacted in Ca(OH)2, and in the region adjacent to the glass surface, we have found a thick calcium silicate layer.

## Slide 10
MW25 glass dissolution in Ca(OH)2
Chart: Time (days)
| 1 | 3 | 7 | 14 | 21 | 28 | 42 | 56 | 70 | 84 | 112 | 140 | 168
UDW | 0.00015633 | 0.00034167 | 0.00063508 | 0.00098567 | 0.0010291 | 0.0010528 | 0.00099417 | 0.00098801 | 0.0010134 | 0.00098671 | 0.0010084 | 0.00098701 | 0.00099385
CSS | 0 | 0 | 0 | 4.3109e-06 | 1.2993e-05 | 3.1388e-05 | 0.00011181 | 0.00021894 | 0.00033834 | 0.00044071 | 0.00060934 | 0.00076742 | 0.00081643
Chart: Time (days)
| 1 | 3 | 7 | 14 | 21 | 28 | 35 | 42 | 56 | 70 | 84 | 112 | 140 | 168
CSS | 709.8623 | 607.0318 | 439.3564 | 300.1155 | 226.4553 | 199.1749 | 137.7098 | 98.8032 | 83.4906 | 75.6277 | 62.7621 | 54.9614 | 45.5169
CSS Blank | 753.9758 | 807.7457 | 798.6157 | 864.2094 | 846.5136 | 857.7919 | 810.0248 | 850.2132 | 701.7303 | 691.9721 | 694.8424 | 717.2565 | 696.9341 | 710.065
Ca(OH)2
Blank
Water: Si solution saturation was rapid
Ca(OH)2: once Ca conc. dropped below 200 ppm and pH fell from ~12 to 10.5, Si was released to solution
A thick alteration layer comprising Ca, Si, Al and Mg was developed (C-S-H and M-S-H)
Corkhill et al. International Journal of Applied Glass Science, 4, 341 – 356 (2013)
Notes: In water, we observed an initial fast rate of Si release and solution saturation was achieved after ~28 days
In Ca(OH)2, the mechanism is clearly different - Ca was consumed during the first 28 days of dissolution and Si was not released until the Ca concentration reached a threshold. This implies that Ca was reacting with the evolving glass surface.
(We observe this behaviour irrespective of glass compositions studied).
Note that Ca depletion cannot be attributed to carbonation and precipitation of calcium carbonate, because the Ca concentration in the blank solution remains constant.
Consistent with the solution data (and XRD data on the previous page), a thick alteration layer comprising Ca, Si, Al and Mg was observed in a cross section of the glass reacted in Ca(OH)2, and in the region adjacent to the glass surface, we have found a thick calcium silicate layer.

## Slide 11
Dissolution occurs in 3 regimes:
1. Incubation regime (0 – 28 days):
Incorporation of Ca into the hydrated glass surface and precipitation of M-S-H phases
2. Intermediate regime (28 – 84 days):
Precipitation of C-S-H phases, including a range of compositions in the C-(N)-(A)-S-H and M-S-H systems; rapid Si dissolution
3. Residual regime (84 – 168 days):
Precipitation of lower Ca/Si ratio C-S-H phases; steady concentration of Ca; slower dissolution of Si
MW25 glass dissolution in Ca(OH)2
Notes: Together these data and thermodynamic modelling of the CaO-SiO-H2O system allow us to develop a mechanistic description of glass dissolution in saturated calcium hydroxide media.
A schematic of Ca and Si in solution is shown at the top as a reference to 3 identified regimes of dissolution:
In the incubation regime, Ca is incorporated into the hydrated glass surface. We also observe the precipitation of M-S-H phases (sepiolite) during this time.
The intermediate regime occurs when Si is rapidly released into solution. Si is able to react with Ca to form a range of C-S-H phases with a high Ca / Si ratio, and also with other dissolved elements (Al, Mg, Na) to form a range of phases in the C-(N)-(A)-S-H and M-(A)-S-H systems.
In the residual regime, the Ca concentration in solution becomes constant and Si release into solution is significantly slowed. During this time there is further precipitation of C-S-H, but with a lower Ca:Si ratio, and also continued precipitation of other phases in the C-(N)-(A)-S-H and M-(A)-S-H systems.
It is important to note that the continuous release of boron to solution implies that this alteration layer is not protective in nature.

## Slide 12: Alteration layer analysis
MW25 720d, Ca(OH)2 50˚C
MW25: SEM / EDX
(ISG) NL(B)720d = 20.13 ± 3.50 g m-2
(MW25) NL(B)720d = 41.2 ± 7.0 g m-2
MW25: TEM / SAED
Notes: Micro-focus XRD summed over a 10 µm2 area, combined with SAED confirmed the presence of the following phases corresponding to each of the regions: (A) amorphous Ca/Si gel; (B) acicular needles of mexinerite [Mg6Al2(OH)18)·4.5H2O]; (C) bright contrast Fe-rich phases (as yet unidentified). Also identified by µ-XRD were Portlandite [Ca(OH)2] and brucite [Mg(OH)2].

## Slide 13: Alteration layer analysis
MW25 720d, Ca(OH)2 50˚C
MW25: SEM / EDX
(ISG) NL(B)720d = 20.13 ± 3.50 g m-2
(MW25) NL(B)720d = 41.2 ± 7.0 g m-2
MW25: μ-XRD
Notes: Micro-focus XRD summed over a 10 µm2 area, combined with SAED confirmed the presence of the following phases corresponding to each of the regions: (A) amorphous Ca/Si gel; (B) acicular needles of mexinerite [Mg6Al2(OH)18)·4.5H2O]; (C) bright contrast Fe-rich phases (as yet unidentified). Also identified by µ-XRD were Portlandite [Ca(OH)2] and brucite [Mg(OH)2].

## Slide 14: Alteration layer analysis
ISG 720d, Ca(OH)2 50˚C
(ISG) NL(B)720d = 20.13 ± 3.50 g m-2
(MW25) NL(B)720d = 41.2 ± 7.0 g m-2
ISG: SEM / EDX
ISG: μ-XRD
Notes: Micro-focus XRD summed over a 10 µm2 area, combined with SAED confirmed the presence of the following phases corresponding to each of the regions: (A) amorphous Ca/Si gel; (B) acicular needles of mexinerite [Mg6Al2(OH)18)·4.5H2O]; (C) bright contrast Fe-rich phases (as yet unidentified). Also identified by µ-XRD were Portlandite [Ca(OH)2] and brucite [Mg(OH)2].

## Slide 15: What we’ve learnt (or now know what we don’t know)
What we’ve learnt
What we don’t know
How exactly is Mg influencing dissolution behaviour?
Quasi-equilibrium of Ca-Si phases controls dissolution of glass
Some alteration layer phases enhance dissolution, some reduce it.
Boron is not a good tracer for dissolution in Ca-rich solutions
29Si
11B
27Al
Na2O∙CaO∙(1–x)Al2O3∙xB2O3∙SiO2 (NCABxS) Na2O∙MgO∙(1–x)Al2O3∙xB2O3∙SiO2 (NMABxS)

## Slide 16: Dissolution in cement leachate
Synthetic Cement Water |  |  | 
 | YCWCa | ECW | OCW
Initial pH | 13.17 ± 0.02 | 12.58 ± 0.01 | 11.71 ± 0.04
Final pH | 13.12 ± 0.02 | 12.31 ± 0.11 | 11.61 ± 0.06
NaOH (1M) | P | P | P
KOH (1M) | P | - | -
KOH (0.1M) | - | P | -
Ca(OH)2 | P | P | P
Na2SO4 | P | - | P
CaCO3 | P | - | P
MW25
ISG
Up to 700 d at 70oC

## Slide 17: Dissolution of ISG in YCWCa
720 d
Zr
Al
B
Si
Element | Concentration (mg L-1)
Al | <0.2
Ca | 15.7
K | 12900
Mg | <0.01
Na | 3300
Si | 5.4
Cl- | <1
SO42- | 188

## Slide 18: Dissolution of ISG in YCWCa
Pore size: 7 – 15 nm

## Slide 19: Dissolution of ISG in YCWCa
Quartz (SiO2)
Phillipsite-K (Na4KAl5Si11O32.10H2O)
Rhodesite (Ca, Na2 K2)8Si16O40.11H2O)
Phillipsite-K
Notes: Rhodesite is not a zeolite, but the double layer silicates have a similar pore-filling structure
The ratio SiOz: Alz03 should be at least as high as for zeolite formation.

## Slide 20: Dissolution of ISG in YCWCa
70°C
30°C
70°C modelled successfully using an affinity based term
Same experiments at 30°C modelled:
< 160d = diffusion model
> 160d = affinity based model but with the saturation term removed

## Slide 21: MW25 dissolution YCWCa
Chart: Time (days)
| 1 | 3 | 7 | 14 | 21 | 28 | 50 | 56 | 70 | 84 | 112
Li4602 | -0.34537 | 0.27955 | 1.466 | 1.805 | 2.3474 | 2.9801 | 4.2019 | 4.6529 | 4.9754 | 4.4797 | 0
Na3302 | -4.7116 | 0.024551 | 0.72146 | 2.5324 | 2.4638 | 3.4345 | 4.7264 | 3.7151 | 4.6428 | 1.8825 | 0
Chart: Time (days)
| 1 | 3 | 7 | 14 | 21 | 28 | 50 | 56 | 70 | 84 | 112
Mg2798 | -0.065204 | 0.0086728 | 0.017954 | 0.030248 | 0.037419 | 0.052385 | 0.055973 | 0.067364 | 0.074517 | 0.074765 | 0
Chart: Time (days)
| 1 | 3 | 7 | 14 | 21 | 28 | 50 | 56 | 70 | 84 | 112
Al_2367 | 0.10452 | 0.58375 | 1.1191 | 1.2676 | 1.8438 | 1.4277 | 1.4971 | 1.2587 | 1.2504 | 1.1418 | 0
B_1818 | -0.0080697 | 0.36145 | 0.70111 | 1.1502 | 1.4345 | 1.6706 | 2.1897 | 2.129 | 2.424 | 2.5772 | 0
Si3905 | 0.088876 | 0.35991 | 0.71515 | 0.97174 | 1.2459 | 1.2055 | 1.3891 | 1.3013 | 1.392 | 1.3627 | 0
Rate (g m-2 d-1) based on Na, Li:

## Slide 22: MW25 dissolution YCWCa
Chart: Time (days)
| 1 | 3 | 7 | 14 | 21 | 28 | 50 | 56 | 70 | 84 | 112
Mg2798 | -0.065204 | 0.0086728 | 0.017954 | 0.030248 | 0.037419 | 0.052385 | 0.055973 | 0.067364 | 0.074517 | 0.074765 | 0
Rate (g m-2 d-1) based on Na, Li:

## Slide 23: What we’ve learnt (or now know what we don’t know)
What we’ve learnt
What we don’t know
Will dissolution in cement water lead to rate resumption?
How will glass dissolution evolve as a function of cement leaching?
What will happen if we use real cement leachates?
Why does Mg behave differently in cement leachate to Ca(OH)2?
Dissolution in cement water is complicated!

## Slide 24: Acknowledgements
PhD students:
Daniel Backhouse
Colleen Mann
Adam Fisher
Nate Cassingham
Dr. Eric Pierce (ORNL) Dr. Dan Crean (AWE)
Dr. Joe Ryan (PNNL) Prof. Neil Hyatt (UoS)
Dr. Jim Neeway (PNNL) Prof. Russell Hand (UoS)
Dr. Karine Ferrand (SCK.CEN)
Dr. Karel Lemmens (SCK.CEN)
Dr. Daniel Grolimund (PSI)
NucleUS Immobilisation Science Group

## Slide 25: Mg in MW25
Na2O∙CaO∙(1–x)Al2O3∙xB2O3∙SiO2 (NCABxS) Na2O∙MgO∙(1–x)Al2O3∙xB2O3∙SiO2 (NMABxS)
Replacement of Al2O3 by B2O3 leads to a decrease in the total number of Q4(X) units and an increase in symmetric Q4
Al was present in tetrahedral coordination, suggesting preferential charge compensation (over IVB)
~10 mol% of Na2O is charge compensated by ~10 mol% Al2O3, leaving CaO or MgO for IVB charge compensation
Fraction of IVB units is lower in Mg-glasses – Mg is IV-fold also, therefore it is not available for charge compensation of IVB units
Lower IVB units in Mg-glass results in lower number of Si-O-B bonds as seen in the 29Si
29Si
11B
27Al
Notes: Increasing the B/Al ratio of the alkali-alkaline-earth aluminoborosilicate glasses led to an overall decrease in the proportion of non-silicate tetrahedral species (IVAl + IVB) and a decrease in Si – O – X bonds (X = B, Al). This was found to correspond to an increase in dissolution rate for the Mg-bearing glass compositions compared to the Ca-bearing glass counterpart compositions
The relative frequency of the 29Si spectra peaks shifted to more negative values with increasing B/Al ratio for both the NCABxS and NMABxS
The replacement of Al2O3 by B2O3 leads to a decrease in the total number of Q4(X) units and an increase in symmetric Q4
The 27Al 3QMAS-NMR (Figure 2) spectra indicate that most of the Al present in the NCABxS and NMABxS glasses was in tetrahedral coordination . This implies that the Al tetrahedra are charge-compensated preferentially over the IVB tetrahedra, as suggested by Yamashita et al. [22], [23]. Thus, for the NCAB5S and NMAB5S glasses, ~10 mol.% of Na2O is likely charge-compensated by ~10 mol.% of Al2O3, leaving CaO or MgO for IVB charge-compensation. Albeit in three different configurations? That’s what the data shows (and what you have written in the results).
Systematic differences are observable between the 29Si and 11B spectra of the NCABxS and NMABxS series. The relative frequency of the peaks of the 29Si spectra is lower for each of the NMABxS glasses compared to their NCABxS counterparts (Figs. X and Y). In addition, the fraction of IVB units is lower for the NMABxS glasses than for the NCABxS glasses. This is attributed to the presence of Mg in the glass as tetrahedral IVMg units. Mg is known to exist in four-fold coordination in glasses, whereas this is not the case for Ca, which prefers XX coordination [26]. If Mg was in four-fold coordination, it would not be available for charge-compensation of IVB units, and would thus lead to a lower IVB fraction than for the equivalent CaO-containing glass. Units of IVMg would also require charge-compensation by Na+ cations [27], further reducing the number of cations available to charge-compensate the IVB units. The lower IVB fractions in the Mg-containing glasses would lead to lower numbers of Si – O – B bonds and hence fewer asymmetric Q4 silicate tetrahedra, resulting in more negative 29Si spectral shifts.
Ok, I get it, but there must be a better way to write this. Like, doesn’t this agree with the analysis of the B data? Point the reader to the figures for the claims you’re making, because it’s not easy to work out how you’re making these assertions (to my not-great-at-glass-structure brain, anyway).

## Slide 26
MW25 glass dissolution in Ca(OH)2
The following phases were predicted to form:
0 – 28 days: Sepiolite
28 – 84 days: tobermorite, sepiolite
84 – 168 days: analcime, phillipsite-Ca, tobermorite, sepiolite
Corkhill et al. International Journal of Applied Glass Science, 4, 341 – 356 (2013)
Secondary phase composition predictions
Chart: 
Ca:Si 0.5 | -0.22 | 3.87 | 5.29
Ca:Si 0.83 | -2.12 | 3.35 | 3.6
Ca:Si 1.0 | 5 | 15 | 10
Ca:Si 1.33 | 9.2 | 6.82 | 3.95
Ca:Si 1.5 | 1.38 | -6.75 | -14.52
0 – 28 days
28 – 84 days
84 – 168 days
Unsaturated
Saturated
Notes: Plotting the solution chemistry data on the CaO-SiO2-H2O phase diagram we can see that the solution chemistry evolves across the C-S-H stability fields, where C-S-H I is representative of high Ca:Si ratio calcium silicate hydrates and C-S-H II represents low Ca:Si precipitates.
This suggests that glass dissolution in Ca(OH)2 is governed by C-S-H solubility and hence, Ca and Si “quasi-equilibrium” in solution.
Geochemical modelling supports this behaviour, and predicts that at early stages of dissolution minerals with a high Ca:Si ratio are saturated in solution and are therefore likely to form, and with time the Ca:Si ratio of the saturated phases falls.
The predicted alteration layer phases from geochemical modelling are: