## Slide 1: THE CORROSION OF COPPER NUCLEAR WASTE CONTAINERS UNDER DEEP GEOLOGIC CONDITIONS
T.Standish, S.Ramamurthy, J.Turnbull, D.Zagidulin, J.J.Noel# and D.W.Shoesmith#
Department of Chemistry and #Surface Science Western,
Western University, London, Ontario, Canada
www.sun.chem.uwo.ca
www.surfacesciencewestern.com
dwshoesm@uwo.ca
This research is funded under a research agreement between the Canadian Natural Sciences and Engineering Research Council NSERC) and the Canadian Nuclear Waste Management Organisation (NWMO)

## Slide 2: The Proposed Canadian Container is a Steel Vessel Coated with a thin (~3mm thick) Corrosion Resistant Copper Layer
~2.5 m
~0.57 m
Notes: I can say that this is potentially the most dangerous failure mode (and that’s why NWMO is investing in researching this)
The motivation behind my research is ensuring the safe long-term management used nuclear fuel. Canada’s proposed long term management method involves placing used fuel bundles in a copper-coated carbon steel container (the Cu coating being either electrodeposited or cold spray), (sealing the containers), and placing them ~500 m below ground in a deep geological repository. In the repository, the containers will eventually come into contact with groundwater and can begin to corrode. This is where my research comes in.
These containers are the primary engineered barrier within the multi-barrier system proposed for the permanent disposal of spent nuclear fuel.

## Slide 3
Cold Spray Deposition
Electrodeposition
Cu powder (1 – 50 µm (diameter))
400oC
Pressurized carrier gas (He and/or N2)
Pulsed electrodeposition
Details proprietary
COATING PROCESSES

## Slide 4
Container Fabrication
Fuel Loading and Container Sealing
Notes: As we saw yesterday, two types of Cu coatings are used on the UFC – ED on body and CS on the region that’s welded shut.

## Slide 5
O2
OH-
Fe2+
Fe
H2O2
e-
OH-
Cu
CuClx(1-x)+
ϒ radiation
e-
Cu
CuClx(1-x)+
e-
O2
OH-
Radiolytic corrosion
Corrosion of the steel by galvanic coupling to the coating possibly at a defective weld (possible delamination)
Corrosion by residual groundwater oxidants
STEEL CONTAINER
Crevice corrosion due to residual water in the container at the weld region
Cu2S
SH-
Corrosion due to sulphide transport arising from remote microbial activity
Possible Container Corrosion Processes in Anticipated Repository Groundwaters (Expected to be Saline)
(Standish et al. Electrochim.Acta 211, 331 (2016)

## Slide 6: The importance of specific corrosion processes will change as the exposure environment evolves
Oxygen may not survive the partially re-saturated (moist) period
Dry
Moist
Wet
Corrosion in humid, aerated vapour
Corrosion in aerated aqueous environment
Galvanic corrosion of defected containers
Corrosion at a defective weld under anoxic conditions
Corrosion by remotely produced sulphide
Radiation dose rate at surface

## Slide 7
Radiolytic corrosion in humid aerated vapour

## Slide 8
H2O2
OH-
Cu
CuClx(1-x)+
ϒ radiation
e-
Radiolytic corrosion
STEEL CONTAINER
For short term processes, determine a corrosion allowance
Corrosion due to radiolytically-produced HNO3 in H2O condensed on the container surface.
Mechanism and rate determined in microcells.

## Slide 9
1.5 mL
Change in pH monitored in a small volume of aerated solution with various [HNO3]
Rate of H+ consumption independent of [HNO3] suggesting NO3- is not the main oxidant
HNO2 ↔ NO2- + H+
Observation of NO2- confirms NO3- is acting as an oxidant
Corrosion eventually inhibited
Attributed to the accumulation of corrosion products
O2 + 4H+ + 4e- → 2H2O
NO3- + 2H+ + 2e- → NO2- + H2O
2Cu → 2Cu+
Cu → Cu2+

## Slide 10
1
2
3
1
2
3
Evolution of the surface condition as corrosion progresses
Grain boundary etching in the early stages
Cu2O and CuO accumulate and eventually block corrosion
Precipitation of Raouite (Cu2NO3(OH)3) confirms all the NO3- is not consumed

## Slide 11
31d
119d
230d
363d
HNO3 unreactive in the absence of O2
Adsorbed NO3- and NO2- species appear to block the corrosion process
Small amount of O2 could catalyze reaction with HNO3 ??
4Cu + O2 + 2H2O → 4Cu+ + 4OH-
2Cu+ + NO3- + 2H+ → 2Cu2+ + NO2- + H2O

## Slide 12
Corrosion at a defective weld

## Slide 13
O2
OH-
Fe2+
Fe
e-
Cu
Cu
STEEL CONTAINER
Emplacement of the container in a repository with a defective weld would represent immediate coating failure
Corrosion damage to steel at the base of a drilled defect in a Cu coating measured by X-ray microtomography (µ-XRT)
Calculate the material loss as a function of oxidant consumption
Develop a finite element model to predict the extent of corrosion and validate with µ-XRT data
0.5 mm
2 mm
3 mm
Wire
Epoxy resin

## Slide 14: Electrochemical/analytical studies allows us to specify the key processes that must be Incorporated in to a corrosion model
Electrochemical results
Numerical database
Finite element model (using COMSOL Multiphysics modelling software)
Describe the evolution of damage to the steel under repository conditions
Notes: Long term aim: build the numerical database required to develop a finite element model (using COMSOL Multiphysics Modelling Software) to describe the evolution of damage to the steel under repository conditions
This introduces why we’re doing the tomography (direct model development and model validation);
Electrochem defines the chemistry and helps develop the model

## Slide 15
Non-destructive 3D imaging technique – visualizes internal features
  Directly investigate damage volume and geometry
Cu
Steel
Defect
0.5 mm
0.5 mm
Cu
Steel
Defect
Compare mass loss to O2 consumed: Volume  
X-Ray Microtomography

## Slide 16
Where are the corrosion issues ?

## Slide 17
A
B
Cu
steel
A – porosity in a cold-sprayed coating is an effective loss of coating thickness
B – Interfacial voids due to Cu particle impact on the steel
Uncorroded cold spray coated steel
Cold-spray/electrodeposited coating interface
Cold-sprayed
electrodeposited
Al/Si particles deposited at the coating interface by surface treatment prior to cold spray coating could act as crevice initiation sites

## Slide 18: Evolution of Corrosion Damage Volume
Annealed Cold Spray
Electrodeposited
O2-sparged
O2-sparged
Air-sparged
Air-sparged
Cu
Steel
0 h
0.25 mm
0.25 mm
0.25 mm
0.25 mm
Cu
Steel
Cu
Steel
Cu
Steel
Cu
Steel
0 h
0 h
Cu
Steel
0 h
21 h
38 h
21 h
21 h
17 h
38 h
38 h
38 h
Corrosion along Cu-steel interface
Less extensive
Corrosion
Corrosion
Notes: By monitoring the change in corroded volume over ~40 hours using synchrotron micro-CT, we can visually see how corrosion has propagated into steel and along the Cu-steel interface/that the extent of corrosion is greater with higher [O2] and that there has been some spread of corrosion along the interface, along with corrosion into the steel
Findings: interfacial corrosion; less extensive on ED.

## Slide 19
Volume  
Cold Spray
Annealed Cold Spray
Electrodeposited
● | Oxygenated
 | Aerated
Can calculate the amount of O2 consumed to cause this amount of corrosion and compare it to that available in the repository
Irrespective of the fabrication process the amount of corrosion damage is determined by the [O2]
Notes:   Effect of coating and [O2] on damage evolution; Despite the different geometry, the overall extent of damage is very similar.

## Slide 20
Joseph
Turnbull
Thalia
Standish
Dmitrij
Zagidulin
Jamie
Noel

## Slide 21
SUMMARY
Enough Already!
Thanks for your Attention
Questions?

## Slide 22
62-72 MPa
68-98 MPa
286-373 MPa
Cold Spray
Annealed Cold Spray
Electrodeposited
steel substrate
20 µm
steel substrate
20 µm
steel substrate
20 µm
Adhesion strength:
EBSD used to produce local misorientation maps (a measure of strain):
Cold Spray
Annealed Cold Spray
Electrodeposited
The Interfacial Corrosion Process Depends on the Coating Procedure
Notes: Damage at the Cu-steel interface due to the coating process decreases in the order cold spray > annealed cold spray >> electrodeposited
Interfacial strain decreases in the order cold spray > annealed cold spray >> electrodeposited. Ultimate tensile strength decreases in the order electrodeposited >> annealed cold spray ≈ cold spray.
A greater degree of misorientation between grains indicates greater strain.

## Slide 23: Distribution of Corrosion Products Formed Within the Defect in Oxygenated 3 mol/L NaCl
 | [Fe2+] | [Cl-]
Akaganeite (β-FeOOH) | High (≥ 0.5 M) | High (≥ 2 M)
Goethite (α-FeOOH) | High | Low
Goethite (α-FeOOH) | Low | High
Lepidocrocite (γ-FeOOH) | Low | Any (high [O2])
Formation of FeOOH in O2-containing solutions:
Base of the defect
Notes: To determine the composition of the corrosion products formed inside the coating defect, a specimen corroded for 24 hours in oxygenated 3 M NaCl was mounted in resin and cross-sectioned. Figure 16 shows an SEM micrograph of the base of the defect (which penetrated slightly into the steel when first drilled) and a series of Raman spectra recorded at the numbered locations on the image. The image shows a substantial oxide film on the exposed steel surface (location 1). The two broad Raman peaks at 350 and 500 cm-1 and the higher intensity peaks at 670 and 720 cm-1 suggest the presence of maghemite, γ-Fe2O3 [19,20], as indicated by the vertical lines. However, the dominant A1g mode of magnetite, Fe3O4 (670 cm-1) [21] and a peak attributable to akaganeite (β-FeOOH) (723 cm-1) [22] also occur in this region, making an unambiguous identification of the film impossible.
Raman analyses (location 2 in Figure 16) indicate the oxide formed (possibly maghemite) is identical to that formed on the steel surface at the base of the defect (location 1 in Figure 16). It seems likely, but is presently unproven, that the propagation of corrosion along the interface is due to the damaged nature of this location (as shown in Figures 6(c), 8(a), and 9(a) inflicted during the cold spray coating process. It also should be noted that the cold spray process used to form the coating cannot be considered to be optimized from a manufacturing standpoint.
Spectra recorded at locations 3 to 6 all exhibit the same peaks but with some variation in the intensities of individual bands. The vertical coloured lines indicate the characteristic Raman shifts for lepidocrocite (γ-FeOOH) [19,23], goethite (α-FeOOH) [19,23], and akaganeite [20,22]. These phases are expected to form in the presence of O2 and Cl- and which phase is dominant depends on their solution concentrations and that of Fe2+ [22]. Environments with high [Cl-] (≥ 2 M) and high [Fe2+] (≥ 0.5 M) favour the formation of akaganeite, while lower [Fe2+] favours lepidocrocite, and goethite forms when either [Cl-] of [Fe2+] is high while the other is low [22]. In solutions containing a high [O2], lepidocrocite forms preferentially to goethite [22,24] but can transform to goethite with time [25]. Inside the defect, the corrosion product is a mix of the above 3 phases with the peaks for akaganeite being relatively the most intense. This would be expected for the high [Fe2+] and [Cl-] conditions likely to prevail within the defect.