## Slide 1: Radiation stability study on melt processed and hot isostatically pressed multi-phase ceramics
Ming Tang,
Los Alamos National Laboratory, USA
Eric R. Vance,
Australian Nuclear Science and Technology Organisation, Australia
Jake W. Amoroso
Savannah River National Laboratory, USA
October 31, 2017, Sydney, AU
MRS2017-Scientific for Nuclear Waste Management Symposium 2017

## Slide 2: Multi-phase Ceramic Waste Forms
Objective: Develop a reference ceramic waste form for the combined HLW raffinate stream (containing undissolved solids and soluble technetium) and potentially the TRU waste stream from fuels fabrication processes
– Ceramic waste form
• Multi-phase ceramics based on SYNROC materials developed by researchers since the late 1970s
Demonstrated geologic stability
• Target phase assemblage based on waste stream
“Hollandite” – (BaxCsy)(A+3)2x+y(Ti+4)8-2x-yO16
“pyrochlore” – (A+3)2Ti2O7
“perovskite” – (A+2)TiO3
“Zirconolite” – CaZrTi2O7
– Process technology
• Melt-Processing
Proven technology to immobilize high-level waste
Relatively few complex steps
– Comparison of multi-phase ceramic waste forms produced via melt-processing and HIP methods

## Slide 3: Experimental

## Slide 4
HIP vs. Melt Process Microstructure

## Slide 5: Phase Analysis (XRD)

## Slide 6
Radiation in Nuclear Waste Forms
The principal sources of radiation in high-level wastes:
-decay of the fission products (e.g. 137Cs and 90Sr)
energetic electrons ( particles), low energy recoil nuclei, and  rays
-decay of the actinide elements (e.g., U, Np, Pu, Am and Cm)
energetic  particles (4.5 to 5.5 MeV), energetic recoil nuclei (70-100 keV), and some  rays
-decay produces photon
Several techniques to study radiation damage in nuclear wastes:
Actinides containing minerals
Short-lived actinides doping
Gamma irradiation utilizing 60Co or 137Cs sources
Neutron irradiation
charge particle (ion irradiation), which is a more cost-effective alternative to study radiation damage in materials in a rather short period of time

## Slide 7
In present study, we performs:
ion irradiations: ion implanter at Ion Beam Materials Lab, LANL
heavy ion Kr (400 keV) used to simulate alpha recoil, displacement damage
light ion α (He, 200 keV), for ionization process
Radiation in Nuclear Waste Forms
hundreds keV ions
Waste form samples
Damaged layer
~200-800 nm
Radiation effects (interaction of radiation with solids) include: (1)energy transfer to electron (ionization and electronic excitation from β/α particles, and γ rays), (2)energy transfer to nuclei (ballistic processes/atomic displacement from α recoil), (3)transmutations and gas production.

## Slide 8
Radiation damage study on ceramic waste forms
Structural/Microstructural evolution, microcracking, swelling/compaction
We will compare radiation response of multi-phase ceramic waste forms from different fabrication routes, HIPed and Melt processed

## Slide 9
Kr irradiation on multi-phase ceramics from SRNL (Melt) and ANSTO (HIPed)
GIXRD patterns obtained from CAF-11113 (SRNL) and SW-1732 (ANSTO) before and after 400 keV Kr ion irradiation to a fluence of 5 × 1014 Kr/cm2 (corresponding to peak displacement damage dose of ~ 1 dpa)
Three major crystalline phases including hollandite, zirconolite, and perovskite, are identified in both pristine multi-phase ceramic samples.
The onset of irradiation-induced amorphization was observed in both multi-phase ceramic samples.

## Slide 10
Cross-sectional TEM observation of Kr irradiated CAF-11113
Z: zirconolite
H: hollandite

## Slide 11
Cross-sectional TEM observation of Kr irradiated SW-1732
Z: zirconolite
H: hollandite

## Slide 12
He irradiation on multi-phase ceramics from SRNL (Melt) and ANSTO (HIPed)
GIXRD patterns obtained from CAF-44413 (SRNL) and SW-1727 (ANSTO) before and after 200 keV He ion irradiation to a fluence of 2 × 1017 He/cm2 (corresponding to peak displacement damage dose of ~ 5 dpa)
Three major crystalline phases including hollandite, zirconolite, and perovskite, are identified in both pristine multiphase ceramic samples.
The irradiation-induced amorphization was observed in both multiphase ceramic samples.

## Slide 13
Microcracking on He irradiated multi-phase ceramics by SEM
50 um
Pristine CAF-11113
hollandite
50 um
He irradiated CAF-11113
hollandite
melt
10 um
Pristine SW-1727
10 um
He irradiated SW-1727
hollandite
HIP

## Slide 14
10 um
Kr irradiated CAF-44413
2 um
Kr irradiated CAF-44413
Kr irradiated SW-1727
10 um
hollandite
Microcracking on Kr irradiated multi-phase ceramics by SEM
HIP
melt

## Slide 15
unirradiated
irradiated
Al foil
Swelling study experimental
Ion beam irradiation
AFM to get topography

## Slide 16
Swelling study on Kr irradiated multi-phase ceramic (HIPed) by AFM
2D
3D
+15%
-8%
unirradiated
irradiated
40x40 um

## Slide 17
Swelling study on Kr irradiated multi-phase ceramic (melt) by AFM
2D
3D
+2%
+1%
unirradiated
irradiated
40x40 um

## Slide 18
Conclusion
Similar radiation damage responses from HIPed and Melt processed multi-phase ceramic waste forms
For structural evolution, amorphization under light ion (He) irradiation occurs at higher dpa dose than heavy ion (Kr) irradiation, which suggests stronger radiation tolerance of ceramics under  and  decay environments
Extensive microcracks observed in hollandite phase of He irradiated ceramics (HIPed and Melt), but only a few isolated small cracks found in Kr irradiated samples
Different swelling & compaction in different crystalline phases of irradiated multi-phase ceramics

## Slide 19
Acknowledgements
This work is funded by
US DOE-NE Fuel Cycle Research and Development,
Material Recovery & Waste Forms Development Campaign

## Slide 20
SRIM simulations on hollandites

## Slide 21
2D
3D
Chart: 
Step height (nm)
unirradiated
irradiated
interface
Length (um)
-5%
Swelling study on He irradiated multi-phase ceramic (melt) by AFM
Chart: 
irradiated
interface
Step height (nm)
-3%
unirradiated
irradiated
40x40 um

## Slide 22
Swelling study on He irradiated multi-phase ceramic (HIPed) by AFM
2D
3D
Chart: 
unirradiated
irradiated
interface
-3%
Step height (nm)
Length (um)
Chart: 
unirradiated
irradiated
interface
Step height (nm)
Length (um)
-6%
unirradiated
irradiated
40x40 um