## Slide 1: Digital autoradiography on C-14 labelled PMMA impregnated rock samples using the BeaverTM
Mikko Voutilainen, Eveliina Muuri, Juuso Sammaljärvi, Marja Siitari-Kauppi
Department of Chemistry, University of Helsinki
Jérôme Donnard, Samuel Duval
AI4R, Nantes, France

## Slide 2: Background: In situ test sites
Grimsel, Switzerland
Grimsel test site (GTS) at an altitude of 1,730 m and at a depth of around 450 meters below the surface in central Switzerland
Olkiluoto, Finland
Underground rock characterization facility (ONKALO) on the coast of south-western Finland where the repository system is built in the depth of 400 meters below the surface
Äspö, Sweden
Äspö hard rock laboratory (HRL) on the coast of southern Sweden extends to depth of 500 meters and is located near Oskarshamn nuclear power plant
The underground rock characterization facilities in crystalline rock formations are used to collect data for safe disposal of spent nuclear fuel and to develop excavation and final disposal techniques in realistic conditions

## Slide 3: Background: In situ Diffusion and sorption experiments using radioactive tracers
Long Term Diffusion (LTD) experiments at GTS
Through- and In-diffusion experiments from source drillhole to observation drillhole
Long Term Sorption Diffusion Experiment (LTDE-SD) at Äspö HRL
In-diffusion experiment from natural fracture surface and from drillhole
Rock Matrix Retention Properties (REPRO) experiments at ONKALO
1. Through- and In-diffusion experiment in drillholes
2. Advection-matrix diffusion experiment in a drillhole

## Slide 4: Motivation
LTD experiment at Grimsel test site [1-2].
LTDE-SD at Äspö hard rock laboratory [3].
[1] Jokelainen et al.
J. Radioanal. Nucl. Chem.
295, 2153–2161, 2013
[2] Soler et al.
J. Contam. Hydrol.
179, 89–101, 2015
[3] Nilson et al.
SKB R-10-68, 2010.
[4] http://www.skb.se/taskforce/
Results affected by heterogeneous structure of the rock and can not be explained using homogenous models
→ Modelling Task 9 for SKB Task Force [4]
Cs-134
HTO
Na-22
Cs-137
Our part of the project:
Structure characterization
of rock samples using X-ray microtomography, SEM/EDS and C-14-PMMA autoradiogrphy

## Slide 5: Rock Samples Studied by C-14-PMMa autoradiography
Grimsel granodiorite
Äspö granodiorite
Olkiluoto veined gneiss and pegmatitic granite
The studied samples differ in terms of:
  Content of main minerals: Quartz, Plagioclase, K-feldspar and Biotite
  Alteration state: content of clay minerals, chloritization of biotite,…
  Mineral and pore structure

## Slide 6: C-14-PMMA Autoradiography
Technique is based on intruding C-14-labelled methyl methacrylate (MMA) into a centimeter scale sample. The distribution of this radioactive tracer is then characterized using autoradiography and porosity using image analysis.
Impregnation
Polymerization
Sawing & Polishing
Traditional Film
Autoradiography
Image Analysis
Filmless
Autoradiography
Counts/pixel
Porosity distribution

## Slide 7: Novel filmless autoradiography method: Le beaver
C-14
(β,156.5 keV)

## Slide 8: Traditional film autoradiography VS. Filmless autoradiography
Direct measurement without films:
  Improves sensitivity of the measurement especially with low activity areas
  Gives linear response as function of activity
  Calibration and effectivity calculation
Conversion of intensities to optical densities:
Calibration using several samples:
Conversion of optical densities to activities:
Determination of porosity:
Porosity for single calibration sample:
Porosity using efficiency and statistical simulations:

## Slide 9: Comparison of the results
Scanned
rock surface
Film
autoradiography
Olkiluoto
Pegmatitic granite
Grimsel
Granodiorite
Olkiluoto
Veined gneiss
Äspö
Granodiorite
Counts/pixel
Film
autoradiography

## Slide 10: Comparison of the ACTIVITY and POROSITY results
 | Film Autoradiography |  | Le Beaver Geant4 calibration |  | Le Beaver Standard calibration | 
 | Activity [Bq/ml] | Porosity [%] | Activity [Bq/ml] | Porosity [%] | Activity [Bq/ml] | Porosity [%]
Grimsel Granodiorite | 470 | 0.36 | 540 | 0.42 | 590 | 0.46
Olkiluoto Pegmatitic granite | 1200 | 0.31 | 2400 | 0.61 | 2600 | 0.67
Olkiluoto Veined gneiss | 610 | 0.15 | 1100 | 0.27 | 1200 | 0.30
Äspö Granodiorite | 2000 | 0.50 | 3100 | 0.79 | 3400 | 0.86
More sensitive filmless autoradiography gives slightly higher values than traditional film autoradiography
  Small artefacts interfere the comparison
Porosities and activities determined using standard calibration and standard calibration are in agreement

## Slide 11: Artefacts and current challenges of the method
Converting activity fluxes into specific activities
  Calibration standard
  Theoretical calculations (e.g. Geant 4) [1]
Artefacts caused by:
Areas with high activity
Sample preparation
[1] Delayre et al., Comparison of Storage phosphor autoradiography and Micro pattern gas detector based Electronic autoradiography for the porosity characterisation of hydrothermally altered samples from Petite-Anse, Martinique. Submitted to publication.

## Slide 12: conclusions
Films are not needed and the measurements are more sensitive especially when measuring low activities
Calibration can be done reliably using:
  Only one calibration standard
  Statistical calculations (e.g. Geant4)
Method offers reliable information about heterogeneity that can be used when analyzing the results of in situ experiments
Method can be used for wide variation of nuclides by changing electrical potentials and radioactive elements that are sorbed on mineral surfaces
Future prospects of the method:
  Performing α-spectroscopy is under development
  Separation of β-active elements with different β-energies, e.g. H-3 (18 keV) and C-14 (156 keV)

## Slide 13: Thank you!