## Slide 1: Solubility of the rhabdophane, LnPO4·0.667 H2O (Ln = La to Dy): implications for the long-term stability of monazite matrices.
a CEA, ICSM – UMR 5257 CEA-CNRS-UM-ENSCM, Bagnols-sur-Cèze, France
b Forschungszentrum Jülich, Institute for Energy and Climate, Jülich, Germany
S. Szenknecta; C. Gaussea; A. Mesbaha;
N. Claviera; S. Neumeierb; N. Dacheuxa.
01/11/2017, Sydney
stephanie.szenknect@cea.fr

## Slide 2: Why studying monazite ?
[1] Cuney M. et al Geology (2000) [2] Lumpkin G.R. The Canadian Mineralogist (1998) [3] Gramaccioli C. et al. American Mineralogist (1978)
[4] Ewing R.C. et al. Reviews in Mineralogy and Geochemistry (2002) [5] Clavier N. et al. Journal of European Ceramic Society (2011)
Most abundant lanthanides phosphate containing large amounts of Th and U [1] (up to 29 wt.% ThO2 [2] and up to 16 wt.% [3])
Unaltered chemical composition over 100 millions years (useful for geochronology)
Very high resistance to irradiation [4]
(self-annealing, low temperature of recrystallization)
Monazite
LnPO4
Monoclinic system P21/n
High capacity to incorporate various cations & polyoxoanions [5]
MIII/MIII : direct substitution
MIV/MIII : single substitution (limited to few %)
MII + MIV/MIII : coupled substitution
(MIII+PO4)/(MIV+SiO4): coupled mixed substitution
Identified as a promising radwaste matrix for the specific conditioning of trivalent or tetravalent actinides [4]

## Slide 3: What is known about chemical durability ?
Ma, J. et al. , J. Nucl. Mat. 2015, 465, 550-555. Oelkers, E. H.; Poitrasson, F., Chem. Geol. 2002, 191, 73-87. Teng, Y. et al., Ceram. Inter. 2015, 41, 10057-10062. Terra, O. et al., New J. Chem. 2003, 27, 957-967. Veilly, E. et al., Inorg. Chem. 2008, 47, 10971-10979. Zhao, X. et al., Ceram. Inter. 2015, 41, 11062-11068.
[1]
Far from equilibrium : RL,0
Lack of reliable kinetic data
Various protocols
Different solid compositions
Various temperatures
Numerous dissolution media
Very low dissolution rates
10-6 < RL,0 < 10-3 g.m-2.d-1
Need for a systematic study of the kinetics of dissolution


## Slide 4: What is known about chemical durability ?
[1] Lasaga, A. C., Fundamental approaches in describing mineral dissolution and precipitation rates. In Chemical Weathering Rates of Silicate Minerals, White, A. F.; Brantley, S. L., Eds. 1995; Vol. 31, pp 23-86. [2] Dacheux, N.; Clavier, N.; Podor, R., American Mineralogist 2013, 98 (5-6), 833-847.
Tlim = 90°C (La), 120°C (Ce), 150°C (Pr)
LnPO4 . ½ H2O
Rhabdophane
LnPO4
Monazite
LnPO4
Rhabdophane
Nd – Dy
T < Tlim
T > Tlim
H2O
H2O
180-250°C
700-900°C
H2O
Heating
Leaching
Leaching
La, Ce, Pr
Near equilibrium: impact of saturation
Need for a systematic study of the solubility of rhabdophane
Better constrain the relative stability domains of rhabdophane & monazite
Identification of neoformed phosphate-based phases
  LnPO4·0.5H2O
  Th2(PO4)2(HPO4)·H2O
  (UO2)3(PO4)2·5H2O…
T, saturation index and ionic radius dependency

[1]
[2]

## Slide 5: Outline
Monazite
LnPO4
Monoclinic system P21/n
Rhabdophane
LnPO4· 0.667H2O
Monoclinic system C2
Study of the solubility
Multiparametric study of the kinetics of dissolution
Microstructural evolution at the surface of pellet during dissolution
Leaching
Homogeneous thermal conversion

## Slide 6: Multiparametric study of the kinetics of dissolution of monazite, LnPO4 (Ln = La to Gd)

## Slide 7
[1] Jonasson, R.; Vance, E., Thermochimica acta 1986, 108, 65-72.
Dissolution kinetics of monazite : synthesis
T = 900°C [1]
t = 6 h
LnPO4 · 0.667H2O 
Rhabdophane
Characterization by XRD, SEM…
LnPO4
Monazite
CePO4
NdPO4
EuPO4
15.1 m2.g-1
8.3 m2.g-1
2.9 m2.g-1
Similar morphology but different size of needle like crystal
Pure Monazite obtained whatever the lanthanide element (La → Gd)
LnCl3 + H3PO4
Wet chemistry route
T = 90°C
t = 14 d

## Slide 8: Dissolution kinetics of monazite: methodology
0.1-0.5-1M HNO3
298 - 363 K
Dynamic conditions
ICP-AES
Analysis of the elementary concentrations
Reactive surface area (m2)
Concentration in solution (g.L-1)
Mass ratio of (Ei) in the solid
Far from equilibrium
Near equilibrium
Study of the effect of the temperature, pH and RG on the normalized dissolution rate, RL(i)
Static conditions
0.1 M HNO3 – 298 K
NdPO4 0.1 M -298 K
Dynamic conditions

## Slide 9: Dissolution kinetics of LnPO4: effect of T
LaPO4 0.1 M HNO3
Dynamic conditions
Increase of the dissolution rate with T
Change in the rate-limiting step?
Impact of f(ΔGr) ?
0.1 M
Determination of Eapp : Arrhenius plot
T  313 K

Similar behavior of all the lanthanides
(La → Gd)

Gausse et al. Dissolution Kinetics of Monazite: a multiparametric study (submitted to Applied Geochemistry)
(4 ± 2) ×10-5 g.m-2.d-1  RL,0 (Ln)  (4.0 ± 0.1)×10-3 g.m-2.d-1
(Ce, 298 K)
(Gd, 363 K)

## Slide 10: Dissolution kinetics of LnPO4: effect of (H3O+)
Similar behavior of all the lanthanides (La → Gd)
298 K: far from thermodynamic equilibrium
LaPO4 -298 K
Dynamic conditions
Determination of the partial order of the reaction relative to (H3O+)
Dissolution controlled by surface reactions


(4 ± 2) ×10-5 g.m-2.d-1  RL (Ln)  (4.8 ± 0.4)×10-3 g.m-2.d-1
(Ce, 0.1 M)
(Gd, 1 M)
Gausse et al. Dissolution Kinetics of Monazite: a multiparametric study (submitted to Applied Geochemistry)

## Slide 11: Dissolution kinetics of NdPO4: effect of f()
Dissolution of monazite in acidic media:
NdPO4 – 0.1 M – 298 K
Static conditions
t = 0
RL,0 (Nd) = (2.2 ± 0.4) ×10-4 g.m-2.d-1
RL (Nd) = (6 ± 1) ×10-6 g.m-2.d-1
Strong decrease of the dissolution rate with time:

Impact of the saturation of the solution relative to the rhabdophane: more stable than monazite at 298 K ?
+
Precipitation of rhabdophane in acidic media:
Need to determine the solubility products of rhabdophanes
Evidence the precipitation of a neoformed phase

Gausse et al. Dissolution Kinetics of Monazite: a multiparametric study (submitted to Applied Geochemistry)

## Slide 12
Determination of the solubility products of rhabdophane LnPO4·0.667H2O (Ln = La to Dy)

## Slide 13: Determination of the thermodynamic properties: methodology
Reversibility of the equilibrium
Stability of the phase of interest
  Polyphased samples
  Neoformed phases
Consistency of the database
Assessment of uncertainties
Solubility experiments
Speciation
Corrections of the activities
K°s,0
ΔRG°
ΔRH°, ΔRS°
C(i)
Time (days)
Ci,o
Equilibrium
RT ; 60°C ; 70°C ; 90°C
RT ; 70°C
Over-saturation experiments
Under-saturation experiments
Composition of the solution
Non-ideality of the solution
Choosing the thermodynamic database (LLNL)

## Slide 14: Solubility experiments
ICP-AES
Analysis of the elementary concentrations
Over-saturation Conditions
0.1M HCl
295–333 -343-363 K
Steady state
Solubility Controlled
by rhabdophane
pH = 0.70 0.05
Under-saturation Conditions
0.1M HCl
295 - 343 K
Use of synthesized pure rhabdophane
for La to Dy (except Tb)
Gausse, C.; Szenknect, S.; Qin, D. W.; Mesbah, A.; Clavier, N.; Neumeier, S.; Bosbach, D.; Dacheux, N., European Journal of Inorganic Chemistry, 2016 (28), 4615-4630.
Steady state
pH = 1.05 0.05
343 K
Solubility Controlled
by rhabdophane
295 K
363 K
333 K
343 K

## Slide 15: Thermodynamic constants of Nd-Rhabdophane
Under-saturation
Over-saturation
(low impact)
–ΔRH˚/R

Demonstration of the thermodynamic equilibrium
Retrograde solubility
Dissolution reaction: exothermic
Gausse, C.; Szenknect, S.; Qin, D. W.; Mesbah, A.; Clavier, N.; Neumeier, S.; Bosbach, D.; Dacheux, N., European Journal of Inorganic Chemistry, 2016 (28), 4615-4630.

## Slide 16: Comparison with literature data for Nd-monazite
  Values previously assigned to monazite on the entire range of temperatures
  Demonstration of the control of the concentrations in solution by Nd-rhabdophane for T  363 K (thanks to over- and under-saturation experiments)
Due to similarities between the phases.
Due to the very low amount of dissolved monazite.
Monazite
Rhabdophane
Values reported in the litterature determined by dissolution of Nd-monazite

Gausse, C.; Szenknect, S.; Qin, D. W.; Mesbah, A.; Clavier, N.; Neumeier, S.; Bosbach, D.; Dacheux, N., European Journal of Inorganic Chemistry, 2016 (28), 4615-4630.

## Slide 17: Thermodynamic constants of LnPO4·0.667H2O (La to Dy)
/ 295 K
333 K
/ 343 K
 363 K
Minimum of solubility observed at the middle of the lanthanides series (Nd-Sm)
-30 ± 8 kJ.mol-1 (Pr)  RH°(LnPO4· 0.667 H2O)  -17 ± 7 kJ.mol-1 (Eu)
-594 ± 23 J.mol-1.K-1(Pr)  RS°(LnPO4· 0.667 H2O)  -546 ± 19 J.mol-1.K-1(Eu)
Gausse, C.; Szenknect, S.; Qin, D. W.; Mesbah, A.; Clavier, N.; Neumeier, S.; Bosbach, D.; Dacheux, N., European Journal of Inorganic Chemistry, 2016 (28), 4615-4630.

## Slide 18: Enthalpy of dehydration reaction
[1] Ushakov, S. V.; Helean, K. B.; Navrotsky, A.; Boatner, L. A., Journal of Materials Research 2001, 16 (9), 2623-2633.
[2] Mesbah, A.; Clavier, N.; Elkaim, E.; Szenknect, S.; Dacheux, N., J Solid State Chem 2017, 249, 221-227.
RH° (Rh  M + 0.667 H2O)= fH°(LnPO4) + 0.667 fH°(H2O) - fH°(LnPO4· 0.667 H2O)
RH° ( 298 K)
Dehydration process studied over the combination of in situ high resolution synchrotron powder diffraction and TGA experiments [2]


## Slide 19: Implication for the long-term behavior of Nd-monazite
[1] Johnson, J. W. et al., Computers & Geosci., 1992, 18, 899-947.
Far from equilibrium
Near equilibrium
ΔRG (kJ.mol-1)
NdPO4 – 0.1 M – 298 K
Static conditions
For the calculation of IAP*:
speciation with LLNL TDB [1]
Strong influence of the solution saturation state
Kinetic regime
Strong decrease of the monazite dissolution rate approaching equilibrium with rhabdophane
Favorable to the use of monazite as a radwaste matrix


## Slide 20
Monitoring the microstructural evolution at monazite surface during dissolution
Powder
Pellet

## Slide 21: Methodology
Szenknect, S.; Finkeldei, S.; Brandt, F.; Ravaux, J.; Odorico, M.; Podor, R.; Dacheux, N.; Bosbach, D., J. Nucl. Mater. 2017, 496, 97-108.
Szenknect, S.; Mesbah, A.; Horlait, D.; Clavier, N.; Dourdain, S.; Ravaux, J.; Dacheux, N., J. Phys. Chem. C 2012, 116 (22), 12027-12037.
Monitoring microstructural evolution at the surface of Nd-monazite sintered pellet:
use of complementary techniques
ESEM
AFM
Grazing Incidence X-rays
AFM : track potential topographic changes of the surface of the solid at a nanometric scale
ESEM : Monitoring of the evolution of the microstructure of the pellet at a submicron scale
GI-XRR : access to physical properties of the solid surface (electron density, roughness)
0.25 M HNO3 90°C

## Slide 22: Microstructural evolution at the surface of Nd-monazite: ESEM
t = 0 d
t = 284 d
t = 11 d
t = 162 d
ESEM images of a selected area
NdPO4
0.25 M HNO3 90°C
m/m0 = 0.32 %
SI(rhabdophane) = –0.07
RG = -0.4 kJ.mol-1
Detachment of grains
Preferential dissolution at grain boundaries and pre-existing defects
Chemo-mechanical corrosion  Detachment of grains

## Slide 23: Microstructural evolution at the surface of Nd-monazite: AFM
Preferential dissolution at grain boundaries and pre-existing defects
Chemo-mechanical corrosion  Detachment of grains
20 to 162 days: holes created by grain detachment became wider
162 to 284 days: evolution stopped
NdPO4
0.25 M HNO3 90°C

## Slide 24: Microstructural evolution at the surface of Nd-monazite: GI-XRR
RG = -0.4 kJ.mol-1
Strong influence of the solution saturation state
No oscillation observed: absence of surface layer or secondary phase precipitated at the surface pellet
Increase then stabilization of microstructural properties (roughness and porosity):
Slow down linked to saturation state of the solution

?
NdPO4
0.25 M HNO3 90°C

## Slide 25: Conclusions / prospects
[1] Qin, D.; Gausse, C.; Szenknect, S.; Mesbah, A.; Clavier, N.; Dacheux, N., The Journal of Chemical Thermodynamics 2017, 114, 151-164.
[2] Qin, D. W.; Mesbah, A.; Gausse, C.; Szenknect, S.; Dacheux, N.; Clavier, N., Journal of Nuclear Materials 2017, 492, 88-96.
Very high chemical durability of LnPO4 (Ln = La to Dy) monazite confirmed even in acidic media and far from thermodynamic equilibrium
Relative stability domains of monazite and rhabdophane better constrained:
   control of the saturation state of the leaching solution by rhabdophane for T < 363 K
Quantification of the impact of the saturation state of the solution relative to the rhabdophane on the normalized dissolution rate of monazite
   decrease of the dissolution rate: positive impact in the context of nuclear waste disposal
Impact of microstructural parameters on the chemical durability :
  Synthesis  Sintering  Dissolution
  Transposition of the methodology for the study of the durability of Ln1-xCaxThxPO4 cheralites (Ph. D. of Danwei Qin at ICSM 2016-2020) [1], [2].

## Slide 26: Thank you !
Interfaces of Material in Evolution (LIME)
Dr. Clémence Gausse !
clem.gausse@orange.fr
Study of Matter in Environmental conditions (L2ME)

## Slide 28: Preparation of the monazite pellet
NdPO4
Monazite powder
Mechanical grinding:
45 min – 30 Hz
Uniaxial pressing:
500 MPa
Sintering:
1400°C – 8h – air
Homogeneous pellet
87% of total density with 6% of open porosity and 7% of closed porosity