## Slide 1: Aqueous leaching of high burnup UO2 fuel under hydrogen conditions
Anders Puranen1, Olivia Roth1,
Lena Evins2, Kastriot Spahiu2
1Studsvik Nuclear AB
2SKB Sweden
Scientific Basis for Nuclear Waste Management
Sydney 2017

## Slide 2: Introduction
The majority of irradiated fuel leaching studies have been performed under oxidising (aerated) conditions
H2 is anticipated to form in a breached deep repository container
  In the Swedish KBS-3 repository design H2 pressures of ~50 bar may occur
    One H2 source corrosion of iron components at deposition depth of ~500 m
  Uranium concentration expected to be controlled by U(IV) solubility (am), ~3E-9 M
    Inhibition of UO2 matrix dissolution
Limited data on fuel behaviour under strong hydrogen pressures
This experiment
Leaching of freshly crushed high burnup UO2 fuel to assess radionuclide release and dissolution rates under hydrogen conditions
The employed fuel was irradiated in a commercial power reactor under standard operating conditions (FGR ~2.6%, peak cycle LHR ~24 kW/m)

## Slide 3: Experimental overview
Fuel: PWR, local pellet BU ~65 MWd/kgU, irradiated in Ringhals 3 (rod 3V5Q13)
  Additional rod data in SKB Technical Report TR-11-03
2 g worth of freshly crushed fuel fragments ~1-2 mm size, placed in a gold fine mesh basket and pre-leached (2 mM NaHCO3 solution)
  Cumulative pre-leaching under argon bubbling (4 contacts, 6 days total)
Autoclave leaching (430 days)
  Argon purging followed by pressurisation with 100% hydrogen to 50 bar, no gas replenishment. Total pressure evolution ~50 -> 29 bar. Room temperature.
  Simplified granitic groundwater, 10 mM NaCl, 2 mM NaHCO3
  No replenishment of leaching solution, 950 -> 650 ml
  Liquid sampling system fitted with an in autoclave quartz filter (P4 frit, 10-16 µm)
  Solution samples centrifuged and analysed by ICP-MS
  Gas-MS sampling

## Slide 4: Fuel crushing and autoclave overview
Autoclave with quartz inner vessel and PEEK internals, without lower portion of the pressure vessel
~1-2 mm-sized fragments was obtained by compression of the cladding and fracturing of the fuel (no milling)

## Slide 5: Pre-leaching, under argon bubbling
Cumulative pre-leaching, the sample is transferred to a new flask and leaching solution at each sampling
Note near constant U & Sr concentration in each sampling
Decreasing Cs-133, 135, Tc-99 & Mo-100 concentrations for each new leaching exposure

## Slide 6: Pre-leaching, under argon bubbling
Pre-leaching of freshy crushed fragments to remove part of the instant release inventory
Same data as in previous slide but plotted as cumulative fraction of inventory released
~0.45% of Cs, ~0.1-0.04% of Tc, Mo, Sr and U inventory released in the 6 day pre-leach
Note coherent fractional releases for Cs-133 & 135, Tc-99 & Mo-100 and Sr-90 & U-238

## Slide 7: Results from the autoclave exposure, fill gas 50 bar H2
Redox sensitive U decreasing to solubility levels of UO2(am) ~2-4E-9 M
Gradually decreasing release rates of Cs and Sr
Redox sensitive Tc at very low concentrations ~2-7E-10 M
Mo concentration fairly constant, complex redox chemistry
No exchange or refilling of solution between samplings

## Slide 8: Results of autoclave exposure, fill pressure 50 bar H2 Fraction of Inventory in Aqueous Phase
Release of redox insensitive & weakly adsorbing Cs and Sr mainly in the first days
  Cs release during 6 day pre-washing ~0.45%, in autoclave 363 day release ~0.8%
  Sr release during 6 day pre-washing ~0.05%, in autoclave 363 day release ~0.02%
  ”Low” per day fraction of inventory release rates beyond 70 days, ~1-2 orders of magnitude less than leaching in areated conditions

## Slide 9: Autoclave gas-MS analysis at 363 days
Trace gases: ~345 ppm He, 169 ppm N2, 39 ppm O2, trace H2O and CO2 not quantified
Trace Xe signal, below quantification limit (~10 ppm)
Xe-signal appears fissiogenic, Xe-136, 134, 132 ratios in fair agreement with pin puncture (far from natural Xe isotopic composition)
Hydrogen ~98.5%
Argon ~1.4%
Trace Xe

## Slide 10: Conclusions
The uranium concentration decreased to UO2 solubility limits (<4E-9 M) within 70 days
  Indicates hydrogen inhibition of UO2 matrix dissolution
Strongly decreasing Cs and Sr releases rates under hydrogen conditions
  Total Cs relases ~0.45% (pre-wash) + 0.8% in autoclave (in pile FGR was 2.6%)
  Sr fraction of inventory release ~1-2 orders of magnitude lower than Cs
  ”Low” per day release rates beyond 70 days compared to areated fuel leaching
    Work underway to quantify and compare release rates under hydrogen conditions with previous studies in areated conditions
Trace in autoclave Xe fission gas release detected
    Gas-MS analytical method under improvement to facilitate fission gas detection and quantification in autoclave experments