## Slide 1: Alkali technetium oxides and their relation to Tc loading in nuclear waste glasses
John McCloy, Jamie Weaver, Chuck Soderquist, & others
Sydney, Australia
November 2, 2017
Notes: Alkali technetium oxides and their relation to Tc loading in nuclear waste glasses
John McCloy, Jamie Weaver, Chuck Soderquist (+others in acknowledgements)
Because of their radioactive nature, solid technetium-99 oxides have been rarely studied, and there is a dearth of modern spectra and diffraction patterns in the literature. This publication aims to address this by detailing a low-temperature synthesis method for pure, crystalline alkali pertechnetates, along with complete analysis by static and magic-angle-spinning nuclear magnetic resonance, Raman, neutron diffraction (ND), and X-ray absorption spectroscopy (XAS). Insight gained from these studies brings a deeper understanding of the periodic chemistry of alkali (Na,K,Rb,Cs) pertechnetates. Additionally, we report attempts to make 5- and 6-coordinate pertechnetate compounds of K, Na, and Li, i.e. TcO5 - and TcO6 -. It was found that higher coordinated species are very sensitive to water, and easily decompose into their respective pertechnetates. It was difficult to obtain pure compounds, but mixtures of the pertechnetate and other phases were frequently found, as evidenced by XAS, ND, and Raman spectroscopy. Additionally, we summarize other work on Tc loading in glasses, effect on glass structure, and salt formation in overloaded samples. For glasses, XAS chemometrics based on principal component analysis and linear combination fitting suggests that Tc is speciated first as isolated Tc4+, as Tc content is increased, there is more Tc7+ which partitions first to K neighbors then to isolated sites. Preliminary work is reported assessing HTcO4 and related compounds and their relationships to mechanisms of Tc volatility.

## Slide 2: Acknowledgements
Chuck Soderquist
Paul Gassman
Eric Walter
Nancy Washton
Andy Lipton
UP# 48294
Wayne Lukens
Jamie Weaver
Jason Lonergan
Albert Kruger

## Slide 3: Outline
Motivation
Tc in glass
TcO4 compounds
TcO5, TcO6 compounds
Simulations & ongoing work

## Slide 4: Technetium – why do we care?
Tc-99 is problematic radionuclide
  Half life 213,000 years
  TcO4- highly mobile in ground water
  Redox quite different than surrogate Re
For Hanford mission, Tc-99 is concern
  Hanford site: ~1500 kg (~25,000 Ci) of 99Tc, 50-90+% to be immobilized in LAW glass
  Low retention of Tc: Solubility? Volatility?
Notes: Characteristics of Tc-99
Specific disposal situation at Hanford
Where is the Tc at Hanford
----------
http://periodictable.com/Samples/043.1/s9s.JPG

## Slide 5: Tc in glass
A lot of Tc can go into glass
In glass, structure may be more complicated than traditional view
Not clear if Tc is clustering or crystallizing in glass
Salt phase formation
4000 ppm Tc (WC)
Tc7+/Tc4+ 0 – 0.15
Tc7+/Tc4+ 0.2 – 0.8
Soderquist et al, J. Nuclear Materials, 449, 173 (2014).
Gassman et al, J. Raman Spectroscopy, 45, 139 (2014).
Soderquist et al, J. Nuclear Materials, 99, 3924 (2016).
Notes: Commonly accepted structural view
A lot can go in!
Not clear if it is clustering or crystallizing
  Raman, XAS, SEM
Soderquist, C.Z., E.C. Buck, J.S. McCloy, M.J. Schweiger, and A.A. Kruger, "Formation of Technetium Salts in Hanford Low-Activity Waste Glass," Journal of the American Ceramic Society, 99(12), 3924–3931 (2016).
Soderquist, C.Z., M.J. Schweiger, D.-S. Kim, W.W. Lukens, and J.S. McCloy, "Redox-Dependent Solubility of Technetium in Low Activity Waste Glass," Journal of Nuclear Materials, 449(1-3), 173-180 (2014).
Gassman, P.L., J.S. McCloy, C.Z. Soderquist, and M.J. Schweiger, "Raman analysis of perrhenate and pertechnetate in alkali salts and borosilicate glasses," Journal of Raman Spectroscopy, 45(1), 139-147 (2014).

## Slide 6: Pertechnetate Synthesis
1. NH4TcO4
2. Cation Exchange Column
3. Distillation & Crystallization
HTcO4
LiTcO4
NaTcO4
KTcO4
RbTcO4
CsTcO4
Na3TcO5
K3TcO5
Na5TcO6
K5TcO6
Li5TcO6
Synthesis completed in a specialized hood in the Radiochemical Processing Laboratory (RPL) at Pacific Northwest National Laboratory
Batch sizes 0.5 – 20.0 grams of solid Tc oxides
From M+TcO4 and M+OH or M+2CO3

## Slide 7: Analysis
Special tools and techniques had to be developed for loading & analyzing Tc-99 compounds
Issues included performing sample loading in radiological hood and sometimes inside glove bag, all to prevent dispersibility & interaction with water
MAS NMR
Raman
XAS
Neutron diffraction
ND ~1200 μCi (44.4 MBq)
NMR ~100 (3.70)
Raman ~50 (1.85)
XAS ~43 (1.59)
Notes: In radiological hoods
In glove bags (to keep water out)
  NMR
  ND
  XRD
  EXAFS, XANES
  Raman
XAS – 5 mg pertechnetate in 50 mg BN (per Wayne)
Per Chuck: Eight samples for XANES analysis are scheduled to ship tomorrow. Each sample has two or three milligrams of a
technetium compound, total activity conservatively estimated at 340 μCi.
So: 340/8=

## Slide 8: TcO4 Pertechnetates: Neutron Diffraction
Gray = 99Tc
Red = O
*
*Hump is SiO2 glass background from sealed tube holder due to having less Tc powder for these
*
Initial difficulties with capillary XRD led to the use of ND
Compound | Tc -O bond length (Å) | O-Tc-O Angle (degrees) | Alkali-O bond length (Å) | χ2
NaTcO4 | 1.71(2) | 107.29(1); 113.92(6) | 2.56(1), 2.61(1) | 20.160
KTcO4 | 1.74(8) | 109.02(4); 110.0(5) | 2.83(5); 2.86(8) | 21.530
RbTcO4 | 1.72(3) | 109.18(4); 110.04(74) | 3.02(1) | 1.210
CsTcO4 | 1.66(1); 1.70(3) | 109.33(12); 113.6(4); 107.29(18); 109.9(4) | 3.05(9), 3.31(9), 3.24(6), 3.64(5) 3.13(9), 3.67(7), 3.08(9), 3.17(4), 3.77(4), 3.07(7), 3.46(6), 3.26(5) | 4.840
Scheelite (I41/a)
Ps-scheelite (Pnma)

## Slide 9: TcO4 Pertechnetates: Tc K-edge XAS
NaTcO4
XANES
NaTcO4
EXAFS
XANES transitions quite different, especially in sp and f transitions
For EXAFS, Tc-O bond distances very similar, but Na seems undercoordinated
Compound | # Neighboring O Atoms | s2 (Å2) | Tc-O Distance (Å)
NaTcO4 | 3.6(2) | 0.0007(3) | 1.731(3)
KTcO4 | 4.1(2) | 0.0010(3) | 1.736(3)
RbTcO4 | 4.3(3) | 0.0011(5) | 1.713(5)
CsTcO4 | 4.1(2) | 0.0011(3) | 1.723(5)
Notes: Density of states calculations preformed in FEFF, allows us to now use XANES data to help identify the presence of different pertechnetate salts in glass

## Slide 10: TcO4 Pertechnetates: Raman
High resolution confocal Raman
532 nm excitation
1800 grooves/mm
Some trends evident, particularly in spacing between stretching modes
CsTcO4 (pseudo-scheelite) closely resembles RbTcO4 (scheelite)
Large cation: vibrations similar to isolated TcO4
ν3(Bg)
ν1(Ag)
ν3(Eg)
Notes: Alkali pertechnetates were analyzed using a Horiba high-resolution confocal inverted-stage microscopic Raman spectrometer (LabRam HR8000) with 600 or 1800 grooves/mm diffraction gratings, using a Nikon Eclipse Ti microscope. Laser excitation at 532 nm was provided by a Quantum Laser MPC-3000, which delivered ~20 mW of power to samples with an approximate spot diameter of 1 μm on the samples. Spectra were recorded using a Peltier-cooled Horiba Synapse charge-coupled device (CCD) detector with a 1024 × 256 pixel array. The spectrometer was calibrated using the line positions of a Hg pen lamp, and the band position of an amorphous Si wafer was used for frequency verification. Spectral resolution of the system, as described, was 1.8 cm-1 /pixel with a laser spot size of 1.1 μm. The spectrometer was preliminarily centered at 1000 cm-1 Raman shift from the 532 nm laser excitation, precluding measurement of some small shift external (skeletal) modes. The spectrometer position was changed to 950 cm-1 to capture these low wavenumber peaks, allowing data collection from 1750 to ~50 cm-1. The number of spectral acquisitions, count times, and the diameter of the confocal iris were varied to maximize the signal-to-noise ratio of spectra. Crystalline alkali pertechnetates only required 2–10 s of acquisition time to achieve very strong signal-to-noise ratios. Spectra from the crystalline solids did not require any spectral manipulation to provide very strong and well resolved Raman bands. On some occasions it was observed that mode intensities varied as a function of where on the sample the laser was probed. It is assumed that this is due to the various crystallographic orientations and geometry of the experiment.
-------
Is there an equivalent “shielding/deshielding” effect on nu_1 relative to TcO4-? – doesn’t seem like it.. Unless the shielding due to H in HTcO4 (has a larger WN nu_1) is relative to TcO4-(aq) where the water molecules are the “counter ion” or ligand. The WN shift for Na is lower than all the other measured alkali, and is lower WN that free TcO4-.. Is this a way of saying it’s “stiffer” and doesn’t transfer the energy to the vibration as well? Would this be something like a more covalent bond then?

## Slide 11: TcO4 Pertechnetates: Tc-99 NMR
“Static” NMR
MAS NMR
Tc-99 referenced to TcO4-(aq)
Red (simulation); Black (experiment)
Tc-99 is a spin 9/2 nucleus:
1: -1/2 ↔ +1/2 (“central transition”, left after MAS)
3: -3/2 ↔ -1/2
5: -5/2 ↔ -3/2
7: -7/2 ↔ -5/2
9: -9/2 ↔ -7/2
1
Smaller Cq (MHz), tighter distribution of transitions in frequency space
3
5
7
Cq(MHz)= 1.36,
δiso (ppm) = -16.8, ηq=0.228
Cq= 3.88, δiso = -13.4, ηq=0
Cq= 5.33, δiso = 1.5, ηq=0
Cq= 9.38, δiso = 43.5, ηq=0
750 MHz (17.6 T)
central transition
Spinning sidebands
750 MHz (17.6 T)
18 kHz (MAS)
Notes: ?Spinning not fast enough to remove all quadrupolar effects on NaTcO4
?self irradiation causing reduction or defects
?impurity (nitrates),
---
Solid-state 99Tc NMR spectra were acquired at ambient temperature in a wide-bore (89 mm) Bruker Biospin Ultrashield™ magnet operating at 16.6 T (750 MHz for 1H) utilizing an AVANCE III spectrometer with a homebuilt 3.2 mm HX MAS probe (double tuned at 1H and 99Tc). Chemical shifts were referenced to external aqueous TcO4- (0.0 ppm). Solid samples of approximately 75µg of powdered alkali pertechnetate were packed into specially designed Torlon® inserts that were sealed and placed inside commercial 3.2 mm PENCIL style (Agilent or Revolution NMR) zirconia NMR rotors. Magic angle spinning (MAS) spectra were collected with selective RF pulses of 37 kHz (1.35 µs selective π/2), spin rate of 18 kHz, recycle times of 1.5 s. Static spectra were obtain utilizing a spin echo sequence (π/2 – τ – π/2 – τ) with τ values of 50 µs and 1µs selective π/2 pulses (50 kHz RF). The 99Tc spectra were analyzed using finite pulse simulations with the SIMPSON program.(Bak et al., 2000)

## Slide 12: TcO4 Pertechnetates: “Size matters”
From Tc-99 NMR, alkali size (# electrons) influences O in Tc-O bond, thus influencing Tc-99; for NaTcO4:
  Na higher EN than other alkali thus attracts e-
  charge density relatively higher on alkali side of O
  Tc deshielded relative to TcO4-
  Larger difference in O-Tc-O bond angles (more asymmetric) -> larger quadrupolar coupling
Bigger counter cation -> bigger unit cell
despite crystal structure change at Cs
Isotropic chemical shift
Quadrupolar coupling
Unit cell volume
ηq>0
ηq=0
TcO4- (aq)
De-shield
Shield
Weaver, J., C.Z. Soderquist, N.M. Washton, A.S. Lipton, P.L. Gassman, W.W. Lukens, A.A. Kruger, N.A. Wall, and J.S. McCloy, "Chemical Trends in Solid Alkali Pertechnetates," Inorganic Chemistry, 56(5), 2533-2544 (2017).
Notes: Tc is not bound
Is the influence on the Tc-O bond
Related to Tc-O distances
Eta – asymmetry of quadrupolar coupling; was equal to zero for the scheelite
structures because of their axial symmetry but not for CsTcO4
Cations is interacting with oxygen which is influencing Tc-O bonds which effects delta and Cq
Tugging between cation & Tc
Deshielding: splitting between energy levels becomes larger
Shielding: splitting between energy levels becomes smaller
Jamie:
NaTcO4
ppm shift is high and positive (NMR)
  Low shielding, reduced electron density around Tc atom
  Oxygen is pulling electrons away more efficiently than with other counter cations
Cq is large (NMR)
  Transitions of spin states is more spread out (i.e. more energy is needed to go from one spin state to the next) <- need to double check this
  Still not sure why the transitions are showing up so strongly… might be due to good, consistent symmetry at the nucleus
  The nucleus is interacting more strongly with non-uniform electric field gradients
  The nucleus is strongly interacting with the electron density
6s->5p orbital interaction peak is stronger than other alkali (XANES)
  Also 4f transition is less strong than other alkali
  Need to look into this more…

## Slide 13: 5- and 6-coordinated Tc(VII) Pertechnetates?
2Li2O + LiTcO4 → Li5TcO6 (250-450°C)
2Li2CO3 + LiTcO4 → Li5TcO6 + 2CO2 (600-650°C)
Li2O + LiTcO4 → Li3TcO5 (reaction T unknown)
4Li5TcO6 → 2Li6TcO6 + Tc2O7(gas) + 4Li2O + ½O2(gas) (>650°C)
Li6TcO6 → Li4TcO5 + Li2O (750°C)
2Na2O + NaTcO4 → Na5TcO6 (250-450°C)
Na2O + NaTcO4 → Na3TcO5 (250-450°C)
K2O + KTcO4 → K3TcO5 (250-450°C)
750°C)
Tc(VII)
Tc(VI)
Tc(V)
TcO4-
TcO53-
TcO65-
Tc(VII)
B. Kanellakopulos, The ternary oxide of 3-to 7-valent technetium with alkalis, Kernforschungszentrum. Inst. Radiochem., Karlsruhe, Germany, IssueAEC Accession No. 31424, Rept. No. KFK-197 (1964).
Keller, C. and B. Kanellakopulos, "Ternary oxides of tri- to septivalent technetium and alkali metals," Journal of Inorganic and Nuclear Chemistry, 27(4), 787-95 (1965).
Notes: 6 LiTcO4 + Tc+ 18 Li2O -> 7 Li6TcO6 – not correct
8 Li5TcO6 -> 6LiTcO6 + Tc2o7 + 1.5 O2 + 2 Li2O – not correct
Tc6+
Li4TcO5 is stable to at least 900°C. Like the Tc(VII) oxyanions, these Tc species are hypothesized to be sensitive to atmospheric moisture, and could quickly revert to pertechnetate salts if present at the surface of a sample when it is exposed to a humid atmosphere. Keller and Kanellakopulos [10] report that the Tc(VI) compounds dissolve in water to give a pink solution, which disproportionates to TcO4- and TcO2·nH2O (the same behavior as TcO42-). These Tc(VI) oxyanions are probably quite sensitive to atmospheric moisture and may quickly disappear from the surface of the sample when it is dissected and crushed. The simple Tc(VI) anion TcO42- is known to be extremely sensitive to moisture [12].
Figure 1. Potential Tc(VII) structures for Tc in oxide glass (left: TcO4-, middle: TcO53-, right: TcO65-).

## Slide 14: TcO5 and TcO6
Several synthesis approaches: Very hygroscopic, difficult to characterize
Probably impure: Na3, K3, Li5, Na5, K5
XAS: appear to be different than TcO4
EPR: some even Tc states due to impurity? radiolysis?
Raman: Li5ReO6 successful & matched literature
NMR: Li5TcO6 has strange Tc-99 pattern
Weaver, J., C. Soderquist, P. Gassman, E. Walter, W. Lukens, and J.S. McCloy, "Synthesis and Characterization of 5- and 6- Coordinated Alkali Pertechnetates," MRS Advances, 2(10), 525-542 (2017).
Compounds are difficult to make in pure state; not very stable so hard to characterize; crystal structures not generally known
Neighbor | # of Neighbors | Distance (Å) | s2 (Å2)
O | 4 | 1.72(1) | 0.0031(4)a
O | 1 | 2.03(3) | 0.0031(4)a
K3TcO5

## Slide 15: Current and future work
Establish DFT methods on TcO2, Tc2O7 and compare to literature & spectroscopy
Calculate KTcO4, NaTcO4 and compare cal/exp Raman, NMR
Calculate “unknowns” LiTcO4 and “HTcO4”
In parallel, synthesize & characterize ReO5 and ReO6 compounds to refine methods
Electronic DOS
Phonon DOS
TcO2

## Slide 16
Thanks for staying to (almost) the bitter end of MRS 2017!