## Slide 1
Progress on Ongoing Waste form HIP projects
E. R. Vance, D. J. Gregg and D. T. Chavara
ANSTOsynroc, Locked Bag 2001, Kirrawee DC, NSW 2232, Australia
MRS2017, November 01, Sydney

## Slide 2: Projects
FLiNaK waste
Spent UO2 fuel
ANM ILW
Acidic 99Mo ILW
99Mo LLLW
CuI

## Slide 3: HIP process summary

## Slide 4: Idaho HLW calcines (USA)
Waste loading: 80%
Scale: 30 Kg
Durability: 100 x EA Glass
Final Volume: 35% reduction
(relative to untreated calcine)
glass
90mm

## Slide 5: LiCl-KCl pyroprocessing waste
A lot of work on sodalite, Na4Al3Si3O12Cl, for 0.59LiCl-0.41KCl eutectic (waste loading ~13 wt.%).
Sintering with glass precursors-glass necessary to incorporate many FPs.
HIPing with glass precursor
Some work on removing Cl then using borosilicate glass for what’s left, but some 36Cl to consider

## Slide 6: FLiNaK pyroprocessing waste
Little work on FLiNaK eutectic (0.29LiF-0.12NaF-0.59KF): candidates include Ca10(PO4)6F2 apatite with non-Li alkalis in Ca site- need some glass for Li- but waste loading <10 wt%
Our approach is to add Ca to allow F to inhabit CaF2 and Al,B, Si oxides for alkalis to inhabit glass.

## Slide 7: FLiNaK
Starting chemicals were LiF,NaF and KF, plus Ca(OH)2, Al(NO3)3.9H2O,H3BO3, Ludox 50, stir-dried in water and calcined in air at 600oC.
XRF agreed well with starting composition
XRD: CaF2 with amorphous and minor phases.
LOI at 800oC: <~3%
Plan is to HIP at 700 and 800oC

## Slide 8: Calcined FLiNaK waste forms
Shows major CaF2 + minors
*
*
*
*
*
*

## Slide 9: Sintered FLiNaK waste forms
Shows major CaF2 + minors
*
*
*
*
*
*

## Slide 10: Spent UO2 Fuel
Original was sintered Synroc-F. Major phase is CaUTi2O7 plus minor hollandite and rutile. Waste loading ~45 wt%.
We have added glass for reactivity (using sol-gel methods) and second string of FP immobilisation and HIPed at 1250oC/100MPa to get near 100% T.D.
Optimising redox conditions between allowing U5+ in over-oxidised conditions and Ti3+ in over-reduced conditions
Scale-up to L+ size to be carried out

## Slide 11: ANM ILW waste
~5000L/yr, mainly 6M NaOH
Achieved waste loading of ~26 wt% on HIPing ~25L container of calcine at 1100oC/100MPa
Composition can tolerate chemical variations of +/- 10% and insensitive to minor impurities.
©

## Slide 12: Acidic 99Mo ILW
Waste is UO2(NO3)2 solution plus minor FPs.
Waste form is close to synroc-F (Carter et al., JNM, 384, 322-6 (2009), HIPed at 1250oC/100MPa.
Project is scale-up to ~1L size with ~20 wt% glass addition
Waste loading ~ 35 wt%.

## Slide 13: ANM LLLW
Waste is basically Li2SO4 with minor components
Both alkalis and sulphate are problematic for cement so have looked at HIPed waste form (850oC/100 MPa) in which SO42- precipitated as BaSO4 and Li incorporated in glass.
Waste loading close to 20 wt% and passes PCT for all elements.

## Slide 14: CuI
CuCl powder will exchange Cl for I (near 100%)
CuI stable in Ar up to melting point of 605oC
Low Ksp
HIPed CuI powder at 550oC/100MPa) gave ~85% T.D.
I release in PCT <1%, but while OK with Ni or Cu powder, complete dissolution with Fe powder.
Can be made from Cu2+ salts

## Slide 15: CuI
However for extra protection sintered a pellet at 550oC in Ar (wt loss ~2% due to oxidation) and surrounded it with Sn metal powder and HIPed at 200oC (M.P. of Sn is 231oC)

## Slide 16: Conclusion
Substantial progress is being made in several projects.
  Molten salt waste (Cl and F)
  ANM Wastes: ILW, LLW, legacy ILW acidic and filter cups
  Engineered wasteform for spent fuel
  Iodine wastes
  HIPed glass