## Slide 1: Current advances on titanate-based glass-ceramics for actinide immobilization Y. Zhang, L. Kong, I. Karatchevtseva, R.D. Aughterson, T. Wei, D.J. Gregg, Z. Zhang, G.R. Lumpkin, E.R. Vance, G. Triani Scientific Basis for Nuclear Waste Management Symposium 2017, Sydney , Australia, 29 October ‒ 3 November 2017

## Slide 2: Glass-ceramics for actinide immobilization
Actinide wastes generated from the entire nuclear fuel cycle:
  Conditioned for safe storage and future disposal
  Matrix: glasses and ceramics; glass-ceramics—emerging
Advantages of glass-ceramics for actinide immobilization:
  Durable ceramic phases to host actinides
  Chemical and processing flexibility of glass to accommodate processing chemicals
Titanate ceramic phases to be considered:
  Zirconolite (CaZrTi2O7)—France, ANSTO, NNL, Sheffield Uni
  Pyrochlore (Ln2Ti2O7/Ln2TiO5)
  Brannerite (AnTi2O6)

## Slide 3: ANSTO’s research effort
Zirconolite glass-ceramics: before year 2000
  Ln surrogate work for processing conditions
  ANSTO—NNL agreement on Pu residues wastes
  U validations
  Pu validations
Pyrochlore glass-ceramics: from year 2008
  Ln surrogate work for processing conditions
  U and Pu validations
Brannerite glass-ceramics: from year 2008
  U and Pu validations
Highlights on U and Pu validations

## Slide 4: Case1: Zirconolite glass-ceramics
Zhang et al., J. Nucl. Mater., 490 (2017) 238-241.
Sample | SiO2 | B2O3 | Al2O3 | Na2O | CaO | CaF2 | ZrO2 | TiO2 | PuO2 | Gd2O3
Pu1 | 17.9 | 0.9 | 12.4 | 2.2 | 17.8 | 9.2 | 15.6 | 18.3 | 3.4 | 2.3
Pu2 | 14.6 | 0.8 | 10.8 | 1.8 | 8.4 | 14.8 | 17.9 | 21.0 | 5.2 | 4.7
Pu3 | 18.0 | 0.9 | 12.5 | 2.2 | 17.3 | 9.2 | 15.7 | 18.4 | 3.5 | 2.3
Pu4 | 14.5 | 0.8 | 10.7 | 1.8 | 8.3 | 14.8 | 17.4 | 20.9 | 5.7 | 5.1
Sample processing conditions |  |  |  |  | Characterization results |  |  |  |  | 
Sample | Redox buffer | Processing |  | Targeting Pu f. u. | Zirconolite phase composition* |  |  |  | Pu valence (EDS/DRS) | 
Pu1 | Ni | 1270 oC, 2h |  | 0.1 | Ca0.8Gd0.1Pu0.1ZrTi1.7Al0.3O7 |  |  |  | 4+/4+ | 
Pu2 | Ni | 1270 oC, 2h |  | 0.15 | Ca0.55Gd0.18Pu0.13□0.14ZrTi1.7Al0.3O7 |  |  |  | 4+/4+ | 
Pu3 | Fe | 1270 oC, 2h |  | 0.1 | Ca0.68Gd0.1Pu0.1□0.12ZrTi1.68Al0.32O7 |  |  |  | 3+/‒ | 
Pu4 | Fe | 1270 oC, 2h |  | 0.15 | Ca0.55Gd0.2Pu0.15□0.1ZrTi1.75Al0.25O7 |  |  |  | 3+/‒ | 

## Slide 5: Case 2: Pyrochlore glass-ceramics with higher An loadings
Zhang et al., J. Nucl. Mater., 432 (2013) 545-547.

## Slide 6: Case 3: Brannerite glass-ceramics
Zhang et al., J. Am. Ceram. Soc., 100 [9] (2017) 4341-4351.
Oxide compositions (wt %) |  |  |  |  |  |  | 
Samples | SiO2 | Na2O/CaO | B2O3 | Al2O3 | TiO2 | Y2O3/Gd2O3/HfO2 | UO2/PuO2
U1 | 35.5 | 6.1/0 | 3.4 | 5.0 | 23.2 | 7.9/0/0 | 19.0/0
U2 | 35.5 | 6.1/0 | 3.4 | 5.0 | 21.0 | 3.6/0/0 | 25.8/0
Pu1 | 42.6 | 7.3/5.1 | 4.1 | 6.0 | 14.9 | 0/3.3/1.9 | 9.8/4.9
Pu2 | 35.5 | 6.1/6.3 | 3.4 | 5.0 | 18.6 | 0/4.1/2.3 | 12.2/6.1
Sample design and processing conditions |  |  |  |  | Results |  | 
Samples | Targeting phase |  | Conditions |  | Phase identified |  | U valence Design/Observed
U1 | Y0.5U0.5Ti2O6 |  | 1200 oC in air |  | Y0.5U0.5Ti2O6 |  | 5+/5+
U2 | Y0.25U0.75Ti2O6 |  | 1200 oC in air |  | Y0.5U0.5Ti2O6 UO2 (<1%) |  | 5+; 4+/5+
Pu1 | Gd0.2Hf0.2U0.4Pu0.2Ti2O6 |  | 1200 oC in argon |  | Gd0.2Pu0.3U0.5Ti2O6 (U/Pu)O2 (<5%) |  | 5+; 4+/5+
Pu2 | Gd0.2Hf0.2U0.4Pu0.2Ti2O6 |  | 1200 oC in argon |  | Gd0.1Hf0.1Pu0.2U0.6Ti2O6 CaTiSiO5 (20%) TiO2 & (U/Pu)O2 (<3%) |  | –

## Slide 7: Micro-structure and spectroscopies
Zhang et al., J. Am. Ceram. Soc., 100 [9] (2017) 4341-4351.

## Slide 8: Case 4: Formation of uranium brannerite with Y/Ce/Eu in glass
Zhang et al, J. Alloys Compds., under review.

## Slide 9: Micro-structures and spectroscopies
Zhang et al., J. Alloys Compds., under review.

## Slide 10: Case 5: Phase evolution from pyrochlore to brannerite in glass
Oxide compositions (wt%) |  |  |  |  |  |  |  | 
Samples | SiO2 | Na2O | B2O3 | Al2O3 | TiO2 | Y2O3/Gd2O3 | CaO | UO2
Y1 | 35.32 | 6.07 | 3.41 | 4.99 | 21.04 | 29.16/0 | ‒ | ‒
Gd1 | 34.02 | 5.85 | 3.28 | 4.81 | 16.14 | 0/35.90 | ‒ | ‒
U1 | 34.99 | 6.02 | 3.38 | 4.95 | 16.56 | 22.96/0 | 4.27 | 6.86
U2 | 34.49 | 5.93 | 3.33 | 4.88 | 15.17 | 21.02/0 | 2.61 | 12.57
U3 | 31.65 | 5.44 | 3.05 | 4.47 | 16.35 | 22.66/0 | 2.81 | 13.55
U4 | 29.50 | 5.07 | 2.85 | 4.17 | 15.24 | 0/33.91 | 4.20 | 5.05
U5 | 29.54 | 5.08 | 2.85 | 4.18 | 14.01 | 0/31.18 | 3.86 | 9.29
Sample design and processing conditions |  |  |  |  | Results |  |  | 
Samples | Design phase |  | Conditions |  | Phase identified |  | U valence (DRS) | 
Y1 | Y2Ti2O7 |  | 1200 oC in air |  | Y2Ti2O7 |  | – | 
Gd1 | Gd2Ti2O7 |  | 1200 oC in air |  | Gd2Ti2O7 |  | – | 
U1 | YCa0.75U0.25Ti2O7 |  | 1200 oC in air |  | Y1.40Ca0.35U0.20Ti1.95O7 |  | 5+ | 
U2 | YCa0.5U0.5Ti2O7 |  | 1200 oC in air |  | Y0.5U0.5Ti2O6 Y1.50Ca0.28U0.22Ti2O7 (40%) TiO2 & UO2 (<2%) |  | 5+ 5+ | 
U3 | YCa0.25U0.75Ti2O7 |  | 1200 oC in air |  | Y0.5U0.5Ti2O6 ; Y1.70Ca0.15U0.15Ti2O7 (<10%) TiO2 & UO2 (<5%) |  | 5+ 5+ | 
U4 | GdCa0.8U0.2Ti2O7 |  | 1200 oC in air |  | Gd1.50Ca0.30U0.15Ti1.95O7 |  | 5+ | 
U5 | GdCa0.6U0.4Ti2O7 |  | 1200 oC in air |  | Gd1.38Ca0.31U0.26Ti1.95O7 Gd0.53U0.51Ti1.91O6 (45%) TiO2 & UO2 (<3%) |  | 5+ 5+ | 
Zhang et al., J. Am. Ceram. Soc., 100 [11] (2017) 5335-5346.

## Slide 11: Structures and phase evolution
Zhang et al., J. Am. Ceram. Soc., 100 [11] (2017) 5335-5346.
Y2Ti2O7
Gd2Ti2O7
Gd
Y
Py
Br

## Slide 12: U substitution on Y site of Y2Ti2O7—SEM/EDS
Zhang et al., J. Am. Ceram. Soc., 100 [11] (2017) 5335-5346.

## Slide 13: TEM-SAED U in residue glasses
Zhang et al., J. Am. Ceram. Soc., 100 [11] (2017) 5335-5346.

## Slide 14: Summary and future work
Summary:
  Titanate (zirconolite/pyrochlore/brannerite) based glass-ceramics have been developed as potential waste forms
  Actinide validations on these glass-ceramic systems have been primarily addressed
  Pu(III)/Pu(IV) and U(IV)/U(V) can be incorporated in the designed ceramic phases
  End products showing good chemical durability
  Future work:
  Further plutonium validations with HIPPed glass-ceramics
  Ion irradiation studies currently in progress
  Accelerated alpha-radiation damage studies with Pu-238 doping
  Processing windows and waste form consolidation conditions
  Formulations for various actinide waste streams

## Slide 15: Acknowledgement
Collaborators and ANSTO colleagues:
  Gordon Thorogood; Jessica Veliscek Carolan; Mihail Ionescu
Nuclear Materials Development and Characterization (NMDC) and Australian Synchrotron platforms at ANSTO for facility access
Thank you for your attention!
Questions?