## Slide 1
Zhaoming Zhang1, Kathryn Spiers2, Lou Vance1,
Joel Davis1, Greg Lumpkin1, Mark Blackford1
1Australian Nuclear Science & Technology Organisation (ANSTO), Lucas Heights, NSW, Australia
2Australian Synchrotron, Clayton, VIC, Australia
Partitioning of Ce, as a Simulant for Pu, in a Multi-phase Ceramic Nuclear Waste Form

## Slide 2: Outline
Pyrochlore and zirconolite ceramic waste forms are leading candidates for the immobilisation of Pu-rich nuclear wastes.
Ca0.71Ce0.52Y0.088Hf0.22Ti2O~x (x = 6.06 – 6.32) with Ce as substitute for Pu. Sintered in (1) air at 1400oC for 10 hrs, (2) Ar at 1350oC for 16 hrs.
XRD & SEM for phase assemblage and microstructure.
Determine Ce valence in individual mineral phases: (1) XANES imaging, and (2) EELS/TEM.

## Slide 3: XRD pattern: Ar sintered sample
Perovskite (Pm-3m): a =3.8533 Å
Zirconolite 4M (C2/c): a=12.5051 Å, b=7.2294 Å, c=22.9608 Å, b=84.9335º
Rutile (P42/mnm): a =4.6289 Å, c =2.9859 Å
Z
Z
R
Z
Z
P
Z
R
P
P
P
P
R
Z
Z

## Slide 4: SEM image and EDX: Ar sintered sample
Perovskite (ABO3):
(Ca0.44Ce0.37Hf0.01□0.18)Ti0.99O3
No Y, very little Hf
Rutile (TiO2):
(Ti0.91Hf0.09)O2
Z
P
R
pore
Zirconolite 4M: (Ca0.64Ce0.38)(Hf0.57Y0.39)Ti2.02O6.97

## Slide 5: XANES at the Ce L3-edge: Ar sample

## Slide 6: XRD pattern: air sintered sample

## Slide 7: SEM image and EDX: air sintered sample
Perovskite (ABO3):
(Ca0.58Ce0.27Hf0.01□0.14)Ti1.00O3
No Y, very little Hf
Rutile (TiO2):
(Ti0.91Hf0.09)O2
Py
P
R
pore
Pyrochlore (A2B2O7): (Ca0.79Ce0.72Hf0.32Y0.17)Ti1.94O7

## Slide 8: XANES at the Ce L3-edge: air sample
Question:
Ce4+ in pyrochlore
& Ce3+ in perovskite?

## Slide 9: Cerium oxidation state: XANES imaging
500μm
100μm
Notes: Still

## Slide 10: XANES imaging of air sintered sample
500μm
100μm
Notes: Animation

## Slide 11: XANES Imaging of air sintered sample
25mm


 | Ca (at%) | Ce (at%) | Y (at%) | Hf (at%) | Ti (at%)
X-ray | 6.41 | 4.78 | 1.05 | 2.38 | 17.75
EDX | 7.22 | 6.58 | 1.55 | 2.90 | 17.75
pyrochlore ↔ Ce4+

## Slide 12: XANES Imaging of air sintered sample
25mm


 | Ca (at%) | Ce (at%) | Y (at%) | Hf (at%) | Ti (at%)
X-ray | 12.94 | 4.58 | 0.51 | 0.99 | 20.54
EDX | 11.94 | 5.47 | 0 | 0.27 | 20.54
perovskite ↔ Ce3+

## Slide 13: RT EELS(TEM) measurements at Ce M5,4-edges
Ce3+ ↔ perovskite, and Ce4+ ↔ pyrochlore (reduction?)

## Slide 14: Conclusions
Sintering in air → pyrochlore-rich ceramics incorporating Ce4+ with minor perovskite incorporating Ce3+
Sintering in Ar → perovskite + zirconolite 4M, both incorporating Ce3+
XANES imaging can provide us with information on the chemical speciation in individual mineral phases of multi-phase ceramics. However, it is difficult to probe individual grains.
EELS/TEM is a complementary technique.

## Slide 15: Thank you