## Slide 1: Quantification of irradiation induced structural disorder in nuclear waste-form ceramics with µ-luminescence spectroscopy of lanthanides
Lenz, C.1,2, Lumpkin, G.R.1, Thorogood, G.J.1, Ionescu, M.1, Nasdala, L.2
1 Australian Nuclear Science and Technology Organisation, Lucas Heights, Sydney, Australia
2 Institut für Mineralogie und Kristallographie, Universität Wien, Austria

## Slide 2
Challenges & Motivation
How to quantitatively characterise the structural state (crystallinity) of individual grains/crystallites in multi-phase ceramics proposed as nuclear waste-forms (e.g., SYNROC, glass-ceramics)?
Zirconolite glass-ceramics
Image width: 70 µm (each)
after Day et al. (2015)

## Slide 3
Challenges & Motivation
Zircon crystals from Andirondak Mts. after Nasdala et al. (2005)
Estimate radiation-damage accumulation in accessory minerals on µm-scale (e.g., zircon and other accessories!)
How to quantitatively characterise the structural state (crystallinity) of individual grains/crystallites in multi-phase ceramics proposed as nuclear waste-forms (e.g., SYNROC, glass-ceramics)?

## Slide 4
Ln3+ luminescence spectroscopy
Lanthanides are common (trace) elements in natural accessory minerals, e.g., zircon (ZrSiO4), monazite & xenotime (LnPO4), titanite (CaTiSiO5)
Lanthanides may easily substitute in the crystal structure of many waste-form phases; and are commonly used as non-hazardous surrogates for some actinides (e.g., Pu, U, and Th)
Fig. Laser-induced photoluminescence spectra of synthetic xenotime−(Y) and monazite−(Ce) doped with Sm3+ (λexc= 488 nm; 77 K)
Xenotime−(Y), YPO4:Sm3+
D2d
C1
Monazite−(Ce), CePO4:Sm3+
selected Ln have unique luminescence characteristics:

## Slide 5
Dy3+ in CaTiSiO5 quenched glass
Dy3+ in titanite (CaTiSiO5) crystal
Application as structural probe!
Lanthanides are common (trace) elements in natural accessory minerals, e.g., zircon (ZrSiO4), monazite & xenotime (LnPO4), titanite (CaTiSiO5)
Lanthanides may easily substitute in the crystal structure of many waste-form phases; and are commonly used as non-hazardous surrogates for some actinides (e.g., Pu, U, and Th)
selected Ln have unique luminescence characteristics:
Ln3+ luminescence spectroscopy

## Slide 6
Fig. Graphical representation of a MD simulation of a single 30keV recoil from a decay-event in zircon (after Trachenko et al. 2003)
= Dy3+
4F9/2 → 6H15/2
Ln3+ luminescence spectroscopy

## Slide 7
Fig. Graphical representation of a MD simulation of a single 30keV recoil from a decay-event in zircon (after Trachenko et al. 2003)
= Dy3+
4F9/2 → 6H15/2
Amorphous fraction = 40%
Amorphous fraction = 75%
Ln3+ luminescence spectroscopy

## Slide 8
Fig. The amorphous fraction of Sri Lankan zircon samples estimated by the bulk techniques XRD and NMR (summarised by Zhang and Salje 2001)
Test with well-characterised, homogeneous, gem-quality samples from Sri Lankan gravels
Direct impact model:
A test example:
Sri Lankan zircon single-crystals
Fig. The amorphous fraction of Sri Lankan zircon samples as obtained by laser-induced photoluminecence of Dy3+
PL data

## Slide 9
x
y
hyperspectral mapping
planar
sample
Confocal laser spectroscopy
Horiba Lab-Ram HR Evolution with x-y-table
Laser spectroscopy may be performed with confocal spectrometer set-up with spatial resolution down to 1 µm

## Slide 10
cold-pressed, sintered, mono-phase, polycrystalline zircon (ZrSiO4) ceramic pellet
Heavy ion irradiation with a 10MV Tandem-Accelerator
Application example:
Heavy-ion irradiated ceramics − Zircon
Au ions, with 35, 22, 14 and 7 MeV at RT
max. total fluence 6.5x1013 ions/cm²
Chart: SRIM simulation for Zircon, ZrSiO4 (DE after Moreira et al. 2009)
50%
21%
16%
13%

## Slide 11
10 µm
Chart: 
| 0.50340099999999999 | 1.0067999999999999 | 1.5102100000000001 | 2.0136099999999999 | 2.51701 | 3.0204200000000001 | 3.5238200000000002 | 4.0272199999999998 | 4.5306199999999999 | 5.0340299999999996 | 5.5374299999999996 | 6.0408299999999997 | 6.5442400000000003 | 7.0476400000000003 | 7.5510400000000004 | 8.0544499999999992 | 8.5578500000000002 | 9.0612499999999994 | 9.5646500000000003 | 10.068099999999999 | 10.5715 | 11.0749 | 11.5783 | 12.0817 | 12.585100000000001 | 13.0885 | 13.591900000000001 | 14.0953 | 14.598699999999999 | 15.1021 | 15.605499999999999 | 16.108899999999998 | 16.612300000000001 | 17.1157 | 17.6191
 | 69.6618 | 68.9249 | 60.9027 | 54.9688 | 51.4687 | 45.6266 | 37.9664 | 31.3765 | 25.6162 | 21.3725 | 16.3346 | 10.4507 | 3.571 | 1.1494 | 1.0324 | 0.61674 | 0.037391 | 0.006801 | 0 | 0.016471 | 0.061441 | 0.015391 | 0.048209 | 0.021791 | 0.0033435 | 0.13076 | 0.099257 | 0.06673 | 0.064563 | 0.092643 | 0.037068 | 0.071907 | 0.15727 | 0.42472 | 0.21923
Amorphous fraction obtained from PL of Dy3+
Direction of heavy-ion irradiation onto the sample
cold-pressed, sintered, mono-phase zircon (ZrSiO4) ceramic pellet
Heavy ion irradiation with a 10MV Tandem-Accelerator
cut, mount and polished
Au ions, with 35, 22, 14 and 7 MeV at RT
max. total fluence 6.5x1013 ions/cm²
FIB foil preparation for TEM
Application example:
Heavy-ion irradiated ceramics − Zircon

## Slide 12
Heavy-ion irradiation
Fig. TEM image and SAED patterns of irradiated zircon ceramic
Application example:
Heavy-ion irradiated ceramics − Zircon

## Slide 13
Zircon
Gabbro, Mulcahy lake intrusion,
Ontario, Canada
(2733 ± 1 Ma)
Test on natural analogue: Zircon
Zircon
Potassic granulite,
Plešovice quarry, Czech Republic
(337.13 ± 0.37 Ma)
50 µm
1 mm
Overgrowth rim
U < 10 ppm
Zoned core
80 – 200 ppm U

## Slide 14
Summary & Outlook
Laser-induced photoluminescence spectroscopy of Ln3+ is a promising tool for the quantification of irradiation-induced damage in crystalline waste-form materials and accessory minerals.
The amorphous fraction can be directly derived from PL emission spectra
  Similar experiments with xenotime (YPO4) and zirconolite (CaZrTi2O7) ceramics using the prominent Nd3+ emission have been conducted succesfully!
PL mapping with confocal spectrometer set-ups provides a detailed characterisation and visualisation of complex radiation-damage accumulation on µm scale.
Compare amorphous fraction obtained with PL with bulk, but surface sensitive Grazing-incidence XRD data
Ion-irradiation experiments with some more potential waste-form/nuclear-fuel materials

## Slide 15
Thank you for your attention!
Special thanks:
Technical assistance
Chutimun Chanmuang (Uni Vienna)
Rob Aughterson (ANSTO)
Joel Davies (ANSTO)
Sample synthesis
Daniel Gregg & Lou Vance (ANSTO)
Dominik Talla (Uni Vienna)
Sample preparation
Andreas Wagner (Uni Vienna)
Kim Lou (ANSTO)

## Slide 16
Chart: Depth below surface [µm]
Additional information

## Slide 17
Fig. Diagram of energy levels of Ln3+ in LnCl3 (“Dieke diagram”; after Dieke and Crosswhite 1968)
Dieke diagram:
Principal f-f transitions

## Slide 18
Spatial resolution: Confocal optics vs. Electron-beam interaction
Fig. Simplified sketch (not to scale) of the beam path of a confocal Raman spectrometer near the focused surface of the sample. The analyzed volume-area is shown in gray. Its extension below the sample surface exceeds appreciably the depth of the irradiation-damaged zone (hatched). Note also that the real lateral resolution exceeds the focal-spot size (after Nasdala et al. 2010).

## Slide 19
REE3+ intensities – Orientation dependence

## Slide 20
Fig. Effect of temperature on the PL spectra of various gem-quality zircon samples ranging from well crystallised to severely radiation damaged. (A) Pairs of spectra showing the Dy3+ emission (4F9/2  6H13/2) at ambient and low temperature. (B) Plot of the FWHM of Dy3+ sublevel I (see arrow in A) against temperature. Note that FWHMs of Dy3+ Stark’s levels depend strongly on the sample’s degree of radiation damage (cf. Fig 5) whereas temperature has rather moderate effects.
Band widths and the effect of temperature

## Slide 21
Band widths and compositionally-induced disorder

## Slide 22
Fig. Series of BSE and CL image (modified after Nasdala et al. 2006) and PL map (λexc = 473 nm) of a cut zircon from a rhyolite tuff from the Gyulakeszi formation near Pécs, Hungary (sample M2). The non-uniformity of the BSE intensity within the annealed crystal half indicates that slight FWHM variations of the PL might be due to moderate chemically-induced band broadening (after Lenz et al. 2015).
Band widths and structural disorder