## Slide 1: Development of Ion Beam Irradiation of Glass-Ceramic Waste Form at ANSTO
Australian Nuclear Science and Technology Organisation, Australia
MRS2017-Scientific Basis for Nuclear Waste Management Symposium 2017, Sydney Australia, 29 October - 3 November 2017
Tao Wei, Mihail Ionescu, Yingjie Zhang, Linggen Kong, Daniel Gregg, Alan Xu, Inna Karatchevtseva, Greg Lumpkin, Lou Vance, Ken Short

## Slide 2
A series of zirconolite and pyrochlore glass-ceramics have been developed at ANSTO.
Zirconolite and pyrochlore ceramics have the excellent chemical durability for the actinide immobilization;
Glasses have process and chemical flexibility.
Glass-Ceramic Waste Form
Gd2Ti2O7 pyrochlore-glass
CaZrTi2O7 zirconolite-glass

## Slide 3
α–decay of actinides – a most serious damage:
Helium accumulation and helium bubbles;
Displaces around atoms in the trajectory;
Defects in the crystalline lattice;
Order-disorder transformation and irradiation-induced amorphisation.
Ion beam irradiation to simulate radiation damage.
Higher damage rate ( up to 10-3 dpa/s);
Controlled irradiation temperatures;
Minimal radio-activity on the samples.
Radiation Damage of Waste Form

## Slide 4: Ion Beam Irradiation Facilities at ANSTO
Four tandem ion accelerators;
ANTARES 10MV Van de Graaff
STAR 2MV Tandetron
SIRIUS 6MV Pelletron
VEGA 1MV Pelletron
Three ion irradiation beamlines at cryogenic and elevated temperatures.
10MV ANTARES and 6 MV SIRIUS accelerator: Au, Ni, Si, Fe, Ta, and Te ion beams, energy up to 35 MeV for Au ion beam;
2 MV STAR accelerator He ion beam, flux: 1.4 E12 ion/cm2/s;
Two low-energy He ion implanters (80 KeV).

## Slide 5: Ion Beam Irradiation
Displacement damage (dpa) produce by 21 MeV Au ion irradiation up to 1 x 1015 ion/cm2
Gd2Ti2O7
CaZrTi2O7
~ 1 dpa near the surface
~ 2.7 - 3.3 dpa at the depth of 3 μm

## Slide 6
Post-irradiation Examination
Microstructural characterization
Glazing-incidence X-ray diffraction (GIXRD)
Raman spectroscopy
Carl Zeiss Auriga 60 crossbeam FIB-SEM system
Jeol F2200 FS™ transmission electron microscopy (TEM)
TEM specimen made by FIB
Cut and lift the TEM specimen in SEM
MTS™ Agilent® nano-indentation hardness testing
In situ micro-mechanical testing

## Slide 7
Zirconolite-glass
Au ion beam irradiation effects
Surface SEM images
50 μm
50 μm
Irradiated (4E+14 Au ion/cm2)
Irradiated (1E+15 Au ion/cm2)
Unirradiated

## Slide 8
GIXRD Results of Zirconolite-glass
Crystallinity is reduced due to 21 MeV Au ion beam irradiation

## Slide 9: GIXRD Results from Different Grazing Angles

## Slide 10
1x1014 Au ion/cm-2
Raman spectra results
of irradiated zirconolite-glass
1x1015 Au ion/cm-2
Cross-section

## Slide 11
Raman spectra of Zirconolite-glass
Compared with different irradiation fluences
Measured at 3 µm from irradiation surface
Measured at 4 µm from irradiation surface

## Slide 12
Surface swelling/melting of glass-Gd2Ti2O7
Pyrochlore-glass irradiated by Au ion beam 1X1015 ion/cm2 at 21 MeV

## Slide 13
Bubbles in the interface of glass-Gd2Ti2O7
irradiated by He ion beam 3x10 17 ion/cm2
Pyrochlore-glass irradiated by He ion beam 3x10 17 ion/cm2 to simulate the alpha decay

## Slide 14
Nano-indentation Results
Au ion beam irradiated
at a fluence of 1 x 1015 ion/cm2
Unirradiated Zirconolite

## Slide 15: In situ Micro-compression Test
T. Wei, et al. Nuclear Instruments and Methods in Physics Research B: (2017) 409: 288-292
Helium beam irradiated intermetallic TiAl specimens compared to unirradiated ones.

## Slide 16: Summary
ANSTO has the capability to conduct ion beam irradiation on nuclear waste form using accelerators on site. Facilities for post-irradiation examination has been developed at ANSTO.
Zirconolite-glass and pyrochlore-glass was irradiated by
Au ion beam up to 1x1015 ion cm-2 to produce displacement damage;
He ion beam up to 3 x1017 ion cm-2 to simulate the α-decay .
GIXRD results show crystallinity of zirconolite is reduced as Au ion irradiation fluence increases;
Raman spectra results show most damaged region by the 21 MeV Au ion beam irradiation is about 3 µm under the irradiation surface;
The hardness of the zirconolite-glass is reduced due to the displacement damage by Au irradiation;
Helium bubbles are observed on the boundary of Gd2Ti2O7-glass in the surface of He irradiated samples (3x1017 ion/cm2) under SEM.

## Slide 17: Thank for your attention