## Slide 1: A study to develop a new glass formulation for the immobilisation of HLW containing molybdenum and large amounts of sodium
Russell J Hand, Clive Brigden & Lisa Hollands
ISL, University of Sheffield
Mike T Harrison; Cath Stephen, Michelle Eccles
NNL
Katy Spencer, Rebecca Sparkes, Michael Ingrams, Hannah Paterson
Sellafield Ltd
John Longmore, Rowan Patel
Cera Dynamics Ltd

## Slide 2: 1. Introduction
Background
Post-operational clean out (POCO) marks a transition from normal operations to decommissioning of the 8 "oldside" highly active storage tanks (HASTs) at Sellafield.
Last transfer of highly active liquor to these tanks was in 1971. There is no agitation facility. Large amount of precipitated solids (~ 2000 kg) have accumulated.
One of the main constituents is zirconium molybdate hydrate (ZMH) (ZrMo2O7(OH)2.2H2O).
An excess of washout reagent, possibly sodium carbonate (Na2CO3) is required to dissolve the solids for removal.

## Slide 3
Requirements
A vitreous wasteform particularly capable of:
Accommodating large amounts of sodium and some molybdenum.
Fabricated from a base glass + waste combination procedure.
Melt at the operational temperature of ~ 1050°C.
Titanium in glasses
Titania (TiO2) can form glasses when combined with a primary glass former.
Large amounts of sodium can be accommodated (up to ~ 40 mol% Na2O) [1-3].
TiO2 can help to lower the fusion temperature and viscosity of the system.
TiO2 rarely features in nuclear waste glasses. The Indian AVS glass is an example, with a sodium content of 20.8 wt% Na2O reported [4] and with a base glass TiO2 content of 9.5 wt% (7.9 mol%) [5].

## Slide 4: 2. Experimental Strategy
Baseline series: The composition of the glass at full sodium content and prior to any waste substitution.
Base glass:
Composition derived from the relevant baseline series composition with the sodium content lowered to allow for the sodium content of waste.
Full product glass: Composition derived from baseline series plus waste components.

## Slide 5: 3. Liquid-liquid Na2MoO4 Phase Separation Effect of Al2O3 vs B2O3
 | Na2MoO4 phase separation/% |  |  | 
 | Al2O3 (mol%) |  | B2O3 (mol%) | 
Target MoO3 /wt% | 2.5 | 10.0 | 10.0 | 15.0
3.4 | 19 | 6 | Nil | Nil
6.4 | 62 | - | Nil | Nil
7.4 | - | - | 5 | Nil
9.0 | 85 | 100 | 31 | 3
Extent of liquid-liquid phase separation
Extent of liquid-liquid phase separation
Significant Na2MoO4 phase separation occurs for relatively small amounts of Al2O3 and melt temperature and pour viscosity increase.
B2O3 significantly lowers phase separation and helps to lower melt temperature and pour viscosity (supported by [6-7]).
However, large amounts of B2O3 also lower aqueous durability of the glass. Al2O3 has been known to improve durability in glass.

## Slide 6: 4. X-ray Diffraction Patterns
Intensity/I
ICCD pdf:
12-0773: Na2MoO4 - Cubic (Fd-3m); 26-0968: Na2MoO4 - Orthorhombic (Fddd); 70-1710: Na2MoO4.2H2O - Orthorhombic (Pbca)
Target 0.0 Al2O3 15.0 B2O3 (mol%) 9.2 MoO3 (wt%)
Target 2.5 Al2O3 5.0 B2O3 (mol%) 3.4 MoO3 (wt%)

## Slide 7: 5. Sample photos
2.5 mol% B2O3
5.0 mol% B2O3
7.5 mol% B2O3
10.0 mol% B2O3
No Al2O3
2.5 mol% Al2O3
All 3.4 wt% MoO3
Note:
Increase in translucency/transparency with increasing B2O3 content.
Increase in opacity in presence of Al2O3
What causes the opacity?

## Slide 8: 6. SEM Micrographs
Samples contain sub-micron scale small white crystals (< ~ 0.5 µm).
Enriched in Mo. Thought to be finely dispersed small crystallites of Na2MoO4.
A small amount will turn the sample opaque, due to light scattering.
Target sample content : 2.5 mol% Al2O3, 5.0 mol% B2O3 – 3.4 wt% MoO3

## Slide 9: 7. Durability studies
PCT-B based tests. 150-75 µm, deionised H2O, 90°C, SA/V 2000 m-1. Target MoO3 = 3.4. wt%.
A relatively small amount of Al2O3 very significantly decreases element leach rate.
General increase in boron element leach rate with increasing B2O3 content (sodium appears more independent). More significant at higher B2O3 content.
Chart: Sodium (Na)
| 7 | 14 | 28 | 7 | 14 | 28 | 7 | 14 | 28 | 7 | 14 | 28
Na NLi/ g m-2 | 2.7951 | 2.7178 | 3.5078 | 4.2526 | 2.6286 | 1.9376 | 3.2001 | 2.29 | 4.1043 | 2.7186 | 2.9961 | 1.7167 | 3.4188 | 1.9625 | 4.2482 | 2.6457 | 4.952 | 3.01 | 5.8016 | 3.0972 | 6.4664 | 4.044
Chart: Boron (B)
| 7 | 14 | 28 | 7 | 14 | 28 | 7 | 14 | 28 | 7 | 14 | 28
B NLi/ g m-2 | 2.7896 | 1.2482 | 3.545 | 4.5043 | 2.9481 | 1.018 | 3.6317 | 1.35 | 4.9079 | 1.6101 | 4.3298 | 1.872 | 5.038 | 1.8938 | 6.4358 | 2.7468 | 9.6528 | 5.701 | 10.3414 | 5.2774 | 12.3182 | 7.4857

## Slide 10
Chart: Molybdenum (Mo)
| 7 | 14 | 28 | 7 | 14 | 28 | 7 | 14 | 28 | 7 | 14 | 28
Mo NLi/ g m-2 | 2.6364 | 1.1647 | 3.4143 | 4.4224 | 2.8572 | 1.0113 | 3.5871 | 1.2917 | 4.9604 | 1.4667 | 3.7608 | 1.0792 | 4.3867 | 1.0098 | 5.6109 | 1.4114 | 7.3713 | 1.9593 | 7.5018 | 1.8092 | 8.7697 | 2.7645
Chart: Silicon (Si)
| 7 | 14 | 28 | 7 | 14 | 28 | 7 | 14 | 28 | 7 | 14 | 28
Si NLi/ g m-2 | 2.278 | 1.0517 | 2.86 | 3.7042 | 2.114 | 0.93559 | 2.57 | 1.1357 | 3.5545 | 1.3306 | 2.0844 | 0.88781 | 2.4088 | 0.86014 | 3.1603 | 1.1461 | 2.8289 | 0.98306 | 3.1802 | 0.93497 | 3.986 | 1.3066
A relatively small amount of Al2O3 very significantly decreases element leach rate.
Molybdenum release rate shows a general increase with increasing B2O3 content without Al2O3.
Silicon release rate appears to be independent of B2O3 content.

## Slide 11: Normalised Element Release Up To 56 days
Low release rates for all elements.
Comparable with other high sodium and molybdenum containing waste glasses from literature [8-9].
Al release congruent with Si.
Ti below limit of detection and Zr ~ 2 orders of magnitude lower than the Mo release rate (50 ppb level in solution).
Silicon concentration 3-4 orders of magnitude below that which might be expected in pH range generated (12.6 to 12.8 [10]).
 | Sample Target Composition |  |  |  |  |  | 
Oxide | Na2O | TiO2 | Al2O3 | B2O3 | SiO2 | MoO3 | ZrO2
mol% | 32.5 | 25.2 | 2.4 | 4.9 | 32.5 | 1.6 | 0.81
wt% | 29.2 | 29.2 | 3.6 | 4.9 | 28.3 | 3.4 | 1.5

## Slide 12: 8. Conclusions and Further Work
Homogeneous full product waste glasses containing large amounts of Na2O and TiO2 (each at around 29 wt%) and MoO3 at 3.4 wt% can be made.
Show low normalised release rates for all elements. Comparable to other high sodium and molybdenum-containing glasses from literature.
A base glass can be successfully combined with a simulated waste feed to produce a full product glass with 50% of sodium (i.e. around 14.5 wt% Na2O) coming from the waste.
Further work to include:
Determination of the boundary limits for waste incorporation.
Characterisation of the barrier layer.

## Slide 13: References
Turnbull, R. C. and W. G. Lawrence (1952). "The role of titania in silica glasses” J. Amer. Ceram. Soc. 35 (2) 48-53.
Hamilton, E. H. and G. W. Cleek (1958). "Properties of sodium titanium silicate glasses” J. Res. Nat. Bur. Standards. 61 (2) 89-94.
Strimple, J. H. and E. A. Giess (1958). "Glass formation and properties of glasses in the system Na2O-B2O3-SiO2-TiO2" J. Amer. Ceram. Soc. 41 (7) 231-237.
Rani, N., J. P. Shrivastava, and R. K. Bajpai (2010). "Corrosion Mechanism in the Obsidian and its Comparison with the Nuclear Waste Glass for Long-Term Performance Assessment in the Geological Repository." Open Corr. J. 3 16-27.
Mishra, P. K., V. De, et al. (2013). "Preparation and characterisation of glass product with modified composition for vitrification of high level radioactive waste." J. Thermal Anal. Calorim. 112 (1) 103-108.
Caurant, D., O. Majerus, et al. (2007). "Effect of molybdenum on the structure and on the crystallization of SiO2-Na2O-CaO-B2O3 glasses." J. Amer. Ceram. Soc. 90 (3) 774-783.
Caurant, D., O. Majerus, et al. (2010). "Structural investigations of borosilicate glasses containing MoO3 by MAS NMR and Raman spectroscopies." J. Nucl. Mater. 396 (1) 94101. 56.
Muller, I. S., K. S. Matlack, et al. (2010). "Waste Loading Enhancements for Hanford LAW Glasses." Office of River Protection VSL-10R1790-1, Final Report.
Nicoleau, G., S. Schuller, et al, (2015). “Phase separation and crystallization effects on the structure and durability of molybdenum borosilicate glass.” J. Non-crystalline sollids. 427, 120-133.
Okamoto G., T. Okura, and K. Goto (1957). “Properties of silica in water.” Geochimica et Cosmochimica Acta, 12 123-132.