## Slide 1
Ian Farnan & Katie Gunderson
Lou Vance
ANSTO
Laura Martel & Joseph Somers
JRC-ITU Karlsruhe
Department of Earth Sciences & Cambridge Nuclear Energy Centre
31P nuclear magnetic resonance as a probe of plutonium incorporation and radiation damage in phosphates
MRS SBNWM Sydney, Australia, 29 October - 3 November 2017

## Slide 2: Radiation resistance of zircon and xenotime
Meldrum et al. [2000]
Monoclinic and tetragonal
phosphates are significantly more radiation tolerant than the corresponding silicate as measured by the critical amorphisation temperature
MRS SBNWM Sydney, Australia, 29 October - 3 November 2017

## Slide 3: Radiation resistance of zircon and xenotime
Weber et al. [1997]
Monoclinic and tetragonal
phosphates are significantly more radiation tolerant than the corresponding silicate as measured by the critical amorphisation temperature
MRS SBNWM Sydney, Australia, 29 October - 3 November 2017

## Slide 4: Comparison of zircon and xenotime
Zircon (ZrSiO4)
Orthosilicate (no bridging oxygens)
Q0 silicon forming chains with ZrO8 dodecahedra
actinides can substitute onto Zr site
MRS SBNWM Sydney, Australia, 29 October - 3 November 2017
phosphorus
Xenotime (YPO4)
YO8
Y
Orthophosphate

## Slide 5
Lattice parameter variation in orthophosphates
MRS SBNWM Sydney, Australia, 29 October - 3 November 2017

## Slide 6
Plutonium in xenotime
Can it substitute Pu into its structure?
MRS SBNWM Sydney, Australia, 29 October - 3 November 2017
Shift to lower 2 theta

## Slide 7
RE phosphates with xenotime structure
Pu solubility limit 5.4%
Plutonium in xenotime
MRS SBNWM Sydney, Australia, 29 October - 3 November 2017

## Slide 8
Pu glovebox (GB) constructed on rails to slide under elevated 9.4 T WB magnet
Transuranic MASNMR, European Commission Joint Research Centre
Magnet legs 1.8 m, standard MAS stators supplied in NB probe bodies with length for 600 MHz system to allow mounting in GB.
1.3 mm rotor diameters allow samples to be spun to 55 kHz (3.3 x 106 rpm)
This removes paramagnetic susceptibility broadening of 5f electrons and yields high resolution spectra.
MASNMR of actinide materials - glovebox approach
MRS SBNWM Sydney, Australia, 29 October - 3 November 2017

## Slide 9
Pu incorporation in xenotime 31P NMR
4 % Pu in YPO4 (xenotime)
31P MASNMR @ 55 kHz
500 s pulse delay
MRS SBNWM Sydney, Australia, 29 October - 3 November 2017

## Slide 10
Pu incorporation in xenotime
4% Pu in YPO4 (xenotime)
31P MASNMR @ 55 kHz
50ms pulse delay
main peak
MRS SBNWM Sydney, Australia, 29 October - 3 November 2017

## Slide 11
structural radiation damage in xenotime
4% 238Pu in YPO4, 2.1 x 1018 alpha/g
31P MASNMR @ 55 kHz
MRS SBNWM Sydney, Australia, 29 October - 3 November 2017

## Slide 12
Pu radiation damage in xenotime
500 s pulse delay
31P MASNMR @ 55 kHz
4% 238Pu in YPO4, 2.1 x 1018 alpha/g
29Si MASNMR @ 5 kHz
Natural zircon 238U /570 million years
MRS SBNWM Sydney, Australia, 29 October - 3 November 2017

## Slide 13
structural radiation damage in xenotime & zircon
31P MASNMR shifts in phosphate glasses
31P MASNMR @ 55 kHz
4% 238Pu in YPO4, 2.1 x 1018 alpha/g
29Si MASNMR @ 5 kHz
MRS SBNWM Sydney, Australia, 29 October - 3 November 2017

## Slide 14
Swift heavy ion radiation damage in xenotime
2 GeV Pb
31P MASNMR @ 20 kHz
MRS SBNWM Sydney, Australia, 29 October - 3 November 2017

## Slide 15
238Pu damage in YPO4 (xenotime) and ZrSiO4 (zircon) from XRD
Pu radiation damage in xenotime
MRS SBNWM Sydney, Australia, 29 October - 3 November 2017

## Slide 16: Acknowledgements
Bill & Melinda Gates Foundation, Engineering & Physical Sciences Research Council (UK)
European Commission Framework 7 - Euract-NMR project: www.euract-nmr.eu
MRS SBNWM Sydney, Australia, 29 October - 3 November 2017
Summary
Can observe substitution of Pu into the xenotime structure by NMR
(transferred hyperfine shift from 5f electrons to phosphorus) - quantitative effect.
The structure of xenotime recovers from heavy recoil more readily than zircon
(phosphate vs silicate)
This is true for measured amorphised fraction and unit cell swelling.
The amount of radiation damage is lower and has a different structure
Amorphous structure is chemically controlled (lower tendency to polymerise)
Amorphous structure is similar for heavy recoil damage and SHI damage

## Slide 17
Alpha decay event
alpha particle travels about 13 µm and causes ionisations and a few atomic displacements along track then 100-200 atomic displacements at end of track.
recoil of heavy daughter causes ~5000-6000 atomic displacements within 25 nm of event.
~ 5 MeV
86 keV

## Slide 18
Ce incorporation in xenotime
pd=500s
pd=250ms
3% Ce in YPO4 (xenotime)
31P MASNMR @ 20 kHz
MRS SBNWM Sydney, Australia, 29 October - 3 November 2017

## Slide 19: Alpha radiation damage
Alpha recoil in zircon (ZrSiO4)
30 keV heavy daughter recoil
ATAS 2016, Richland, WA, 7-10 November 2016

## Slide 20: NMR as a measure of radiation damage
ATAS 2016, Richland ,WA, 7-10 November 2016
Single pulse 29Si MASNMR (π/12 pulse every 300 s)

## Slide 21: Strategies for MASNMR of actinide materials
ATAS 2016, Richland, WA, 7-10 November 2016
PTFE secondary containment
Sample core
Pencil rotor
AlN inner rotor
Internal triple containment
Fast spinning requires small rotors
small rotors not compatible with internal containment

## Slide 22: MASNMR of actinide materials - glovebox approach
Challenges for MASNMR in alpha GB
can only use approved connectors in and out:
electrical/RF
and gas
MAS probes introduce 100-200 l min-1 N2 into GB
rad GBs operate at 0.95 atm, over pressure triggers alarm for lab.
ATAS 2016, Richland, WA, 7-10 November 2016

## Slide 23: MASNMR of actinide materials
Actinide dioxides 17O MASNMR at 55kHz (1.3 mm rotor)
U0.4Th0.6O2
OTh4
ATAS 2016, Richland, WA, 7-10 November 2016

## Slide 24: Comparison of zircon and xenotime
Xenotime (YPO4)
Orthophospate (no bridging oxygens)
Q0 phosphorus forming chains with YO8 dodecahedra
actinides can substitute onto Y site ?
ATAS 2016, Richland ,WA, 7-10 November 2016

## Slide 25: NMR measurement of radiation damage
Partitioning between daughter recoil and alpha particle
α - particle damage without recoil
10B (n, α) reaction
10B
n0
7Li
4He2+
2
ATAS 2016, Richland, WA, 7-10 November 2016

## Slide 26: NMR measurement of radiation damage
10B (n, α) reaction
0
7Li MASNMR 28 day xenotime sample - direct detection of the 10B(n,α) nuclear reaction
7Li signal intensity
3
2
1
7Li atoms x1018
7Li calibration with spodumene (LiAlSi2O6)
0.6
2.6
4.6
6.6
8.6

## Slide 27: NMR measurement of radiation damage
10B (n, α) reaction
Xenotime
Pore
α-particle range
7Li signal intensity
3
2
1
7Li atoms x1018
7Li calibration with spodumene (LiAlSi2O6)
0.6
2.6
4.6
6.6
8.6

## Slide 28: NMR measurement of radiation damage
10B (n, α) reaction
31P MASNMR @ 20 kHz

## Slide 29: Swelling vs particle energy
alpha + recoil
alpha only (+ 7Li)