## Slide 1: Radionuclide Sorption Behaviour on Fresh and Aged Cementitious Materials: A Comprehensive Database With 25 Elements
Land AND Water
MRS 2017 Sydney
Dirk Mallants, Michael Ochs, Lian Wang
30 October-2 November 2017

## Slide 2
Challenge:
  Safety assessments require
    sorption parameters (RD) for large set of radionuclides for cementitious engineered barriers
    sorption parameters account for cement evolution (degradation)
Solution:
  Develop comprehensive RD database for cementitious materials (benchmark cement)
  Establish relationship between RD and main phases of cement evolution
Objective
  Compile RD values from literature following strict selection and analysis procedures (QA/QC, international expert panel, process description)
  Select best estimate (uncertainty) RD values for 25 elements for 4 cement evolution phases
Challenge & Solution

## Slide 3: Cementitious Materials as Engineered Barrier
Multiple Engineered Barriers for LLW
Repository
Surface repository
  Faster cement degradation
  Oxidising conditions
Conditioning Matrix
Concrete Disposal
Container &
Backfill Material
Structural Material
For Concrete Vault

## Slide 4: Evolution of cementitious materials
Simplified model
Four States:
  I: pH > 12.5 due to the presence of high concentrations of alkalis (Na and K)
  II: pH12.5 controlled by the solubility of portlandite (Ca(OH)2)
  III: 10.5<pH<12.5 regulated by the equilibrium of amorphous C-S-H with the infiltrated water from the surrounding non-cementitious materials
  IV: pH < 10.5 controlled by aggregates (calcite - CaCO3 <> AAR)
II
III
IIV
Ca(OH)2
CSH
Calcite
Ca↓ => Ca/Si↓
150 m2/g
1 m2/g
6 m2/g
75wt%
60wt% HCP
25wt% HCP
Notes: ONDRAF/NIRAS decided to apply the same
formulation to the cementitious backfill (premix mortar) but replacing siliceous sand by a
calcareous sand (limestone). Alkali-aggregate reaction (AAR) is a well known cause of
concrete deterioration. It arises from use of reactive (with cement) siliceous aggregates and
results in expansion and cracking. AAR is eliminated by using sand-grade high-purity
limestone aggregate (for coarse as well as for fine aggregate).

## Slide 5
CSH
AFt
AFm
Afm, Aft: calcium aluminiumsulphate hydrates
Notes: Ettringite and Tca (tricarboaluminate) is AFt: calcium aluminumsulphate hydrate
Afm: monocarboaluminate and strätlingite (containing silicium)

## Slide 6: 25 Elements: Radionuclides & Metals
Ag: 108mAg, 110mAg
Am: 241Am
Be: 10Be
C: 14C
Ca: 41Ca, 45Ca
Cl: 36Cl
Cs: 137Cs
H: 3H
I: 125I, 131I, 129I
Mo: 93Mo
Nb: 94Nb
Ni: 59Ni, 63Ni
Np: 227Np
Pa: 231Pa
Pb: 210Pb
Pd: 107Pd
Pu: 238Pu, 239Pu, 240Pu, 241Pu
Ra: 226Ra
Se: 79Se
Sn: 126Sn
Sr: 90Sr
Tc: 99Tc
Th: 230Th, 232Th
U: 234U, 235U, 238U
Zr: 93Zr

## Slide 7: Cesium Sorption
Best Estimate [LL-UL] RD (L/kg)
State 1: i.d. [0.1 - 10]
State 2: 2 [0.1 - 50]
State 3: 20 [1 - 300]
State 4: i.d.
Evolving cement

## Slide 8: Cs: Sorption Mechanisms
Sorption mechanism:
  Simple speciation: Cs+
  Cs sorption mainly via ion exchange on the CSH phases
  Sorption on impurities in aggregates (clays, silica gel, …)
State I: i.d. [0.1 – 10 L/kg]
  Competition from other alkali metal ions (K, Na), ionic strength

## Slide 9: Cs: Sorption Mechanisms
State II: 2 L/kg [0.1 – 50]
  Ionic strength and alkali decrease, sorption increases
  Competition with Ca for negatively charged CSH surfaces

## Slide 10: Cs: Sorption Mechanisms
State III: 20 L/kg [1 – 300]
  Cs sorption increases with decreasing C/S ratio due to the condition of the interlayer CSH surface which changes sign as a function of C/S ratio
  Lower Ca2+ => increase in surface sites with high affinity for Cs

## Slide 11: Cs: Sorption Mechanisms
State IV: i.d.
  calcareous aggregates contribute only slightly to Cs sorption
  higher silica and clays will give higher Rd values for caesium.

## Slide 12: Uranium Sorption
Evolving cement
Best Estimate RD U(VI) (L/kg)
State 1: 2,000 [400 – 10,000]
State 2: 30,000 [3,000 – 300,000]
State 3: 30,000 [10,000 – 300,000]
State 4: 50 [5 – 500]

## Slide 13: U: Sorption Mechanisms
U (VI)-speciation
Solubility-controlling phase: CaUO4(c) 10-7 – 10-5 M
Sorption mechanisms:
  Linear sorption onto HCP and CSH, with U(VI) uptake increasing with decreasing Ca [Pointeau et al. 2008]
  Non-linear sorption onto CSH: co-precipitation of Ca and U(VI) on the sorbent [Tits et al. 2008]
  Ca influences U sorption
Notes: U(VI) speciation in an oxidising cementitious environment is dominated by the hydrolysis species UO2(OH)3- and UO2(OH)3-2

## Slide 14: U (VI) Sorption
State I : 2000 L/kg [400-10,000]
  Weaker sorption than in State II, III
State II: 30,000 L/kg [3,000 – 300,000]
  Higher Ca than State III => more competition for sorption sites
State III: 30,000 L/kg [10,000 – 300,000]
  Increased sorption due to loss of Ca resulting in increased availability of silanol sites for U sorption
  High sorption due to high surface area of CSH (150 m2/g)
State IV: 50 L/kg [5 – 500]
  Low sorption on calcite (small reactive surface: 0.2 – 1 m2/g)

## Slide 15
Summary of RD values for evolving cement
Chemical degradation (evolution) of cement does generally not result in decreased sorption
CSH provide high density of non-specific sorption sites across both States II-III
Decrease of CSH mass during State III compensated by higher affinity due to decreased Ca in solution
, U (+VI)

## Slide 16: Conclusions
Critically reviewed radionuclide sorption data on cementitious materials for 25 elements
For each element sorption data were grouped according to one of four cement degradation states
Sorption behaviour was explained on the basis of cement pore water composition and available solid phases for sorption
Derived best estimate, LL, UL sorption values following expert panel elicitation
Cement degradation across State II-III does generally not result in decreased sorption values

## Slide 17: Acknowledgements
John Berry
Virginie Blin
Pierre de Cannière
Christoph Gallé
Fred Glasser
Eric Giffaut
Alan Hooper
Diederik Jacques
David Lever
Evelien Martens
Bernhard Schwyn
Ludovic Vielle-Petit
Erich Wieland
Steve Williams

## Slide 18: Thank you
CSIRO Land and Water
  Dirk Mallants Senior Principal Research Scientist
    t +61 8 8303 8595
    e dirk.mallants@csiro.au
    W http://www.csiro.au/en/Organisation-Structure/Divisions/Land-and-Water/DirkMallants.aspx
Land and water Flagship

## Slide 19
Backup Slides

## Slide 20: Benchmark Cement-1 Composition for LLW Disposal
Notes: Alkali-aggregate reaction (AAR) is a well known cause of
concrete deterioration. It arises from use of reactive (with cement) siliceous aggregates and
results in expansion and cracking. AAR is eliminated by using sand-grade high-purity
limestone aggregate (for coarse as well as for fine aggregate).
The alkali-dolomite reaction, another reported cause of deterioration induced by aggregates, will be entirely avoided by
using limestones low in magnesia (no more than 2% each of magnesium, silicon and aluminum
as oxide) [68].

## Slide 21: Benchmark Cement-2 Composition for LLW Disposal

## Slide 22: Procedure for data selection and analysis
Kd (linear & reversible) or Rd (uptake)?
Experimental or calculated (thermodynamic models) values?
Batch tests or dynamic leaching experiments (model uncertainty)?
Keeping control of the oxidation state (redox sensitive elements)?
Dominant aqueous speciation for given experimental conditions?
Liquid-to-solid separation technique (removal of colloids)?
Liquid-to-solid (L/S) ratio (low reliability if high sorption & low L/S)
Single measurement point versus sorption isotherm
Initial tracer concentration (sorption, not solubility limitation)
Contact time for batch tests (equilibration time)
Pore water characteristics (cement state)
Solid type (crushed concrete, hardened cement paste, pure mineral phases eg CSH)
Focus on State II and III (State I is very short, IV has little sorption capacity)
Notes: The sorption process can be quantified through use of the Kd constant if it is experimentally
demonstrated that sorption is linear and reversible. In the majority of the reported experimental
studies, however, neither the linearity nor the reversibility were tested. As a result, the reported
sorption values should be considered as a distribution ratio Rd (ℓ/kg):

## Slide 23: U(IV) Sorption
Based on Th(IV) data (chemical analogy); single species Th(OH)4 (aq)
State I, II, III, IV:
  30,000 L/kg
Thorium