## Slide 1: Highly porous and stable metal–organic frameworks for actinide extraction and storage
CARBONI Michaël
Research Scientist at the French Atomic Energy Commission

## Slide 2: Metal-Organic Frameworks (MOFs)
Crystalline solids
Composed of organic ligands connected by metal ions or metal-clusters
Pores are interconnected to form network of channels
Very high surface areas
Versatile, tunable materials
MOF ?
Various applications
Carboni, M. ; Lin, Z., Abney, C.W. ; Zhang, T. ; Lin, W., Chemistry, A European J, 2014, 20, 14965.

## Slide 3: Hybrid materials for Actinides Extraction
Metal extraction (Functionalization)
Metal precipitation (In-Situ)
Conversion (Chemical or heat treatment)
Storage
Step 1
Step 2
Extraction + Storage

## Slide 4: Metal extraction
Oak Ridge National Lab + NEUP :

## Slide 5: Metal extraction
We have developed a library of 9 different materials based on amidoxime, phosphoric acid, and carboxylic acid functional groups
Vivero-Escoto, J.L. ; Carboni, M. ; Abney, C.W. ; deKrafft, K.E. ; Lin, W. Microporous and Mesoporous Materials, 2013, 180, 22.

## Slide 6: Metal extraction
Vivero-Escoto, J.L. ; Carboni, M. ; Abney, C.W. ; deKrafft, K.E. ; Lin, W. Microporous and Mesoporous Materials, 2013, 180, 22.
Pros
- Easy to functionalize
- Hydrophilic
Cons
- Non-specific adsorption of U by MSN
- Stability
Artificial Seawater
Basic Water
Best material
In basic water
qe = 185.2 mg/g
In artificial Seawater
qe = 66.7 mg/g

## Slide 7: Metal extraction
Carboni, M. ; Abney, C.W. ; Taylor-Pashow, K. M. L. ; Vivero-Escoto, J.L. ; Lin, W. Industrial & Engineering Chemistry Research, 2013, 52, 43, 15187.

## Slide 8: Metal extraction
Carboni, M. ; Abney, C.W. ; Taylor-Pashow, K. M. L. ; Vivero-Escoto, J.L. ; Lin, W. Industrial & Engineering Chemistry Research, 2013, 52, 43, 15187.
Pros
- No U sorption of by MCNs
- Stability
Cons
- Hard to functionalize
- Hydrophobicity
60 mg/g

## Slide 9: Lab Activities on MOFs
MOFs for metal extraction ?

## Slide 10: Metal extraction
1 - Navarro Amador, R., Carboni, M., Meyer, D. , Mater. Lett. 2016, 166, 327.
2 - Manna, K; Zhang, T., Carboni, M.; Abney, C.W.; Lin, W., JACS, 2014, 136, 13182
Zr MOFs UiO Family
High Stability
Easy tunability
Easy to synthesize
(1)
(2)

## Slide 11: Metal extraction
Carboni, M. ; Lin, Z., Abney, C.W. ; Zhang, T. ; Lin, W., Chemistry, A European J, 2014, 20, 14965.
First example
Zr6L4
Zr6L6
X-ray Structure

## Slide 12: Metal extraction
Carboni, M. ; Abney, C.W. ; Liu, S. ; Lin, W., Chemical Science, 2013, 4, 2396.
Second example

## Slide 13: Metal extraction
Carboni, M. ; Abney, C.W. ; Liu, S. ; Lin, W., Chemical Science, 2013, 4, 2396.
Intra-sorbent distances of 4.5 – 4.8 Å
Cooperative binding interactions help explain high U affinity

## Slide 14: Metal extraction
5
10
15
20
25
30
35
40
45
50
55
60
0,1M H
2
SO
4
1M H
2
SO
4
0,1M H
2
SO
4
+ 1,4M SO
4
2-
2 Theta (°)
Stability of Zr-MOF in sulfuric conditions
OK

## Slide 15: Metal extraction
5
10
15
20
25
30
35
40
45
50
55
60
avant contact
0,01M H
3
PO
4
0,1M H
3
PO
4
2 theta (°)
Stability of Zr-MOF in phosphoric conditions

## Slide 16: Metal extraction
5
10
15
20
25
30
35
40
45
50
55
60
0,1 M H
3
PO
4
1 M H
3
PO
4
2 Theta (°)
Lanthanide MOFs in phosphoric media ?
How to o increase the stability ?
Phosphonate linker instead of carboxy?

## Slide 17
Metal precipitation
- Perez, E., Navarro-Amador, R., Carboni, M., Meyer, D., Materials Letters, 2016, 167, 188.
- E. Perez, M.L. Andre, R. Navarro Amador, F. Hyvrard, J. Borrini, M. Carboni, D. Meyer Journal of Hazardous Material, 2016, 317, 617.
Selective precipitation as MOF
Thermal conversion
Storage

## Slide 18: Metal precipitation
Phosphonates vs. Carboxylates: stronger bonds to metals
Bonds with Mn+ (n = 1-4): metal valence increases, solubility decreases
Unconvertional MOFs: lack highly order structure, insolubility, great thermal stability
Monazites
Light rare-earth elements (ThO2: 29 wt%; UO2: 16 wt%)
Can be converted from phosphonate-based MOFs
(Ref: Perez et al.)

## Slide 19: Metal precipitation
Lanthanide organophosphonates
Ln3+
Ligand
Spacer
1 : 1 : 2
[Ln_ligand_spacer]
+
+

## Slide 20: Metal precipitation
Monazite lanthanide phosphates
LnPO4
Thermal conversion
BDP-based Ln organophosphonates
[Ln_BDP]
[Ln_BDP_spacer]

## Slide 21
Thank you for your attention
Past Lab
New Lab