## Slide 1: Alkali tin silicate glass as a wasteform for the immobilisation of plutonium
Amber R. Mason, Neil C. Hyatt and Martin C. Stennett
The Scientific Basis for Nuclear Waste Management Symposium 2017
Sydney, Australia
@AmberRose1605 @ISL_Sheffield

## Slide 2: Introduction
Upon completion of fuel reprocessing in the UK, 140t of PuO2 stockpile will be stored as zero value asset at Sellafield
UK government policy – either reuse in MOx or immoblilisation and disposal in geological disposal facility (GDF).
Dual track strategy also suggested1 since some material unsuitable for recycle
Develop wasteforms to immobilise this waste stream for over 100000 yrs
1. Hyatt, N. C. (2017). Plutonium management policy in the United Kingdom: The need for a dual track strategy. Energy Policy, 101, 303–309

## Slide 3
Alkali tin silicate glass
Alkali Tin Silicate (ATS) glass – type of borosilicate glass developed in the US for immobilization of wPu2
Increased alkali elements to increase Pu waste loading
Sn added to improve chemical durability
Objectives
Determine solubility of CeO2 as function of melt temperature
Determine solubility of CeO2 in presence of Fe(0) reduction
Determine feasibility of batchwise HIP (Hot Isostatic Pressing) processing
Note: melt temperature <1300oC to limit melter corrosion
Reagent | Al2O3 | B2O3 | CeO2 | K2O | Li2O | Na2O | SiO2 | SnO | TiO2 | ZrO2
wt% | 1.73 | 10.05 | 6.37 | 7.50 | 10.15 | 15.34 | 39.31 | 2.51 | 1.84 | 5.20
mol% | 1.06 | 9.00 | 2.31 | 4.97 | 21.20 | 15.43 | 40.80 | 1.16 | 1.44 | 2.63
2. Bates, J. K. et al. (1996). Glass as a waste form for the immobilisation of plutonium. Mat. Res. Soc. Symp. Proc., 412, 57–64.

## Slide 4
Wasteform Optimisation
Fabrication
Reagent type
Oxide, carbonate, chloride etc.
Hydrated?
Synthesis route
Cold uniaxial press
Hot isostatic press
Glass melting
(stirring?)
Techniques
- XRD
- SEM with EDX
- XAS
Characterisation
Final Characterisation
Dissolution tests
Radiation stability tests
Synthesis Parameters
Temperature
Time
Sintering atmosphere
Excess reagents
Optimisation
Notes: Add according to percentage batch mass – Dark amber colour associated with Ce 3+

## Slide 5
ATS Glass Matrix
Synthesis Temp. (oC) | mol% CeO2 |  |  | 
 | 2.5 mol% | 5 mol% |  | 10 mol%
 |  | No Fe | Fe | 
1100 |  |  |  | 
1200 |  |  |  | 
1300 |  |  |  | 







Notes: Add according to percentage batch mass – Dark amber colour associated with Ce 3+

## Slide 6
u-CeO2
Xray Diffraction Results I

## Slide 7
u-CeO2
Xray Diffraction Results II

## Slide 8
1100oC 5 mol% CeO2 & Fe(0)
ATS Glass - SEM
10µm
100µm
Ce
Si
Al
Na

## Slide 9
ATS Glass - XANES
Measured Ce L3 edge (5723eV) at BM26 ESRF, Grenoble
Ce3+=62(±2)%
Ce3+=21(±1)%
Ce3+=70(±1)%
Ce3+=100 (±1)%
Ce3+=100 (±1)%
Ce3+=100 (±1)%
Linear combination fitting4 used to determine the percentage of Ce3+ in each sample.

## Slide 10: Hot Isostatic Pressing (HIP)
HIP production of glass wasteforms not well established
Potential advantages
  Batchwise process – accountancy, safeguards, criticality, and security
  Processing in sealed container so no-off gas requirements
  Scalable and adaptable to different an variable waste feed
Initial study: ATS glass frit mixed with waste surrogate (CeO2)
Scale: 30ml stainless steel can
BEFORE
AFTER
Notes: Describe HIPing

## Slide 11
HIP Run | 5 mol% CeO2 | 
 | No Fe | Fe
1100oC 20MPa 4hr dwell |  | 
1250oC 20MPa 6hr dwell |  | 
ATS Glass HIP Matrix
u-CeO2 l- Fe3O4 n- Fe
Two HIP runs completed so far
Must consider effects of SS can on redox potential of melt
Notes: Most successful as this is free from Ce

## Slide 12
1100oC 20MPa 5 mol% CeO2
ATS Glass HIP 1 and 2 - SEM
100µm
10 µm
Ce
Zr
Al
Ce
Na

## Slide 13
1250oC 20MPa 5 mol% CeO2 & Fe(0)
ATS Glass HIP 3 and 4 - SEM
20µm
Si
Al
Na
Fe
3µm
Notes: Both cans displayed similar quantities of Fe present.

## Slide 14
1100oC 20MPa 4hr
1250oC 20MPa 6hr
ATS Glass HIP - XANES
Measured Ce L3 edge (5723eV) at BM26 ESRF, Grenoble
Ce3+=100(±1)%
Ce3+=71(±4)%
Ce3+=100(±1)%
Ce3+=100(±1)%
Linear combination fitting4 used to determine the percentage of Ce3+ in each sample.

## Slide 15
Conclusions
Ce solubility is associated with reduction of Ce4+ to Ce3+
CeO2 solubility up to 5 mol% at 1300oC
Equimolar addition of Fe(0), CeO2 solubility at 5 mol% at 1100oC
HIP processing of ATS glasses demonstrated to be feasible
Results promising for application:
  Reduction in melt temperature advantageous
  Increase in CeO2 solubility implies higher waste loading possible
  HIP offers batch processing technology
5. C. Lopez et al., Solubility of actinide surrogates in nuclear glasses. Journal of Nuclear Materials. 312, 76–80 (2003).

## Slide 16
Future Work
Refine addition of Fe and Ce to optimise waste loading in ATS HIP cans.
Fit EXAFS data to give information about the coordination environment of Ce and Fe.
Dissolution testing using PCT B method to investigate the durability of ATS glass.
Ion irradiation of samples at Inter University Accelerator Centre, New Delhi – further characterisation of samples.
Use U as Pu surrogate to investigate solubility in ATS glass
Continue work with zirconolite ceramics for PhD project
Notes: Image: http://www.antenchem.com/UpFiles/EN2014/7/24/2014072456846485.gif

## Slide 17: Thank you for listening
Any questions?
Thank you to my supervisors for their patience and guidance and everyone at the ISL for training and assistance, particularly Dr. Laura Gardner, Steph Thornber, Dan Bailey, Dr. Florent Tocino and Jack Clarke.
This research was performed at the MIDAS Facility, at the University of Sheffield, which was established with support from the Department of Energy and Climate Change.
Acknowledgements