## Slide 1
Effect of Platinum-Group Metals (PGM) on the dissolution of uranium dioxide
INSTITUT DE CHIMIE SEPARATIVE DE MARCOULE
T. Cordara 1, S. Szenknect 1, L. Claparede 1,
Mesbah 1, C. Lavalette 3 , R. Podor 2
N. Dacheux 1
1 ICSM/LIME, UMR 5257, CEA, CNRS, Univ. Montpellier, ENSCM
2 ICSM/L2ME, UMR 5257, CEA, CNRS, Univ. Montpellier, ENSCM
3 AREVA NC / BG aval / DO recyclage / RDP, Paris

## Slide 2
Transverse approach of the material elaboration
Model compounds :
New ways of synthesis
New precursors
Properties in use :
Chemical durability
Long-term behavior
Sintering :
densification
microstructure
Optimized Syntheses
Dissolution of AnO2, (An,Ln)O2-x / Fluorite-type prepared from oxalate precipitation
  Conventional parameters ( chemical composition, temperature, acidity, … )
  Structural parameters ( oxygen vacancies, superstructure, secondary phases … )
  Microstructural parameters ( crystal defects, crystallite size, densification rate, … )
Dissolution
Leaching
How can sample preparation impact dissolution ?
1
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017

## Slide 3
Distribution of FP in SNF
2
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
Spent Nuclear Fuel
  U (95 wt.%) – Pu (1 wt.%)
  MA (0.1 wt.%) – FP (4 wt.%)
More than 40 FP
4 main types
PGM
(Ru, Rh, Pd)
 0.6 mol.%
Lanthanides
(La, Ce, Pr, Nd)
 1 mol.%
Which impact of PGM on UO2 dissolution ?
P. Burns, R.C. Ewing, A. Navrotsky, Science 2012, 335, 1184-1187
PRECCI Report, CEA, 2001, CEA-R-5958E

## Slide 4
Model compounds
Synthesis / Densification
Dissolution experiments
Macroscopic dissolution rates
Monitoring of solid/liquid interface
Evolving structural and microstructural parameters
Macroscopic description of the dissolution
Impact of dissolving solution :
pH, T, redox, composition…
Microscopic description of the evolving interface
Structural and microstructural control of starting materials
Operando analysis (ESEM, X-EDS, G-XRD, XRR, AFM)
 Topography, porosity, chemical composition of interface
RL = k0  e-EA/RT  a(H3O+)n  g(I)   a(i)ni  f (RG (,T) )
Methodology
3
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017

## Slide 5
Samples elaboration
----
Evaluation of the reactive surface area during dissolution: SESAM method
Notes: 5
5

## Slide 6
a = 5.466 Å
Literature :
a = 5.469 Å
Preparation of UO2 (reference)
Conversion
Oxalate precipitation
500oC / 4 h
Air
then
Ar / H2
4
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
R. T.
H2C2O4 : + 50%
Recovery yield (U) = 99.9 %
Washing
(H2O – EtOH)
Drying
(90oC)
U(C2O4)2 . 2 H2O
10 µm
UO2
5 µm
J. Tsuji, J. Alloys Compds, 1998, 271, 391
Platelet grains
3 µm in size
Application to PGM
U : 98.8 %
Ru : 6.5 %
Pd : 0 %
Rh : 17.8 %

## Slide 7
Preparation of PGM doped UO2
Conversion
Hydroxide precipitation
5
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
10 µm
U(IV) + PGM
HCl
msynthesised ≤ 1 g
Room temperature
Excess of NH4OH
Washing
(water + ethanol)
Precipitate
+
EtOH
Drying under vacuum
T = 40oC
800oC / 4 h
Ar / H2
Recovery yield
U : 99.9 %
Ru : 90 %
Pd : 100 %
Rh : 85 %
UO2 doped with 3% PGM
Rh (10%) – Ru (55%) – Pd (35%)
J. Martinez, Patent FR3016360 – WO2015/107086, 2015
N. Clavier et al., Chem. Phys. Chem., 2017, 18, 2666-2674
Highly reactive
120 – 150 m2.g-1
Crystallite size: 2-5 nm
a = 5.470 Å
a = 5.466 Å (UO2)
Crystallite size: 130 nm
No PGM in
UO2 structure

## Slide 8
Densification rate : 89%
PGM-aggregates < 0.5 µm
UO2 grains size ≈ 1 µm
Preparation of sintered samples
Uniaxial pressing
RT – 500 MPa
Heating treatment
1550oC / 8h
Ar – 5% H2
Characterization
PXRD, BET, ESEM, Pycnometry
6
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
Grinding step
30 Hz / 30 min
UO2 + PGM
2 µm
Densification rate : 93%
Ru, Rh, Pd bearing aggregates located at GB
(surface + inner)
5 µm
SNF
J. Noirot, Monographie CEA, 2009, 25-28
4 µm
UO2

## Slide 9
Image
Sample
Integration on sample surface

Integration on sample volume

Disc surface

Integration on image surface

Grayscale threshold then binarization:
Surface area of the pores
Correction by the
open porosity ratio

A = π  2 / 4


A = π  2
Sample height
Estimated specific
surface area
Evaluation of Specific Surface Area (SSA) :
SESAM method
7
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017

## Slide 10
SESAM
Sintered pellets
BET
Single crystals
Powders
Porous materials
Geometrical
≈ 1×10-3
≈ 5×10-1
* T. Cordara, PhD, ICSM/CEA, Univ. Montpellier, Nov. 2017
Compound | Specific Surface Area (m2.g-1) |  | 
 | BET method (Kr) | SESAM method | Geometrical
CeO2 | 0.180 (20 pellets ,  5 g) | 0.241 | 3.3  10-4
UO2 (reference) | < LoD | 5.0  10-2 | 2.6  10-4
UO2 + PGM | < LoD | 2.0  10-2 | 2.6  10-4
U0.9Ln0.1O1.95 | 1.5  10-2 (5 pellets ,  1 g) | 5.0  10-2 | 2.9  10-4
 76 - 730
 1.3 - 3
Evaluation of SSA: SESAM method
8
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017

## Slide 11
Macroscopic study
---
Multiparametric expression of the dissolution kinetics
A.C. Lasaga, Kinetic Theory in the Earth Sciences, Princeton Univ. Press, 1998
Notes: 11
11

## Slide 12
ICP–AES
ICP-MS
a liquid scintillation
Static conditions
Sintered Pellet
Dissolution test: experimental device
RL(i) ≈ RL(j): congruent dissolution
RL(i) ≠ RL(j): incongruent dissolution
9
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
Leachate
Dissolution reactor
Pellet
Magnetic stirrer
Support
Reactive surface area (m2)
Amount of (i) in solution (g)
Mass ratio of (i) in the solid

## Slide 13
General trend of UO2 dissolution in nitric acid
T. Cordara et al., J. Nucl. Mater. 2017, 496, 251-264
10
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
Kinetics
3 domains
RL.pulse (U)
RL.0 (U)
RL.t (U)
≈ 0.05
≈ 0.5
Dissolved mass, m/m0 (%)
Leaching time (days)
RL,pulse
RL,0
Increase of S
Increase of autocatalytic species
↗↗ of RL(t)
Steady state:
Constant rate
≈ 90



Normalized dissolution rate
RL.0 (U) expressed in g.m-2.d-1
Induction period
Notes: The influence of the uranium mole loading on the normalized dissolution rates was studied for several Th1-xUxO2 solid solutions samples with various chemical compositions in 2 mol.L-1 HNO3 and at 60°C
You can see that after 170 days of leaching test , only 20 percent of the mixed oxide with a uranium mole loading of 0,16 are dissolved….
Conversely to that was observed for Th1-xCexO2 solid solutions, the substitution of thorium by uranium (IV) led to a significant modification of the chemical durability of Th1-xUxO2 solid solutions. Indeed, an increase of the normalized dissolution rates RL,0(U) and RL,0(Th) by three orders of magnitude is observed between Th0.84U0.16O2 and Th0.29U0.71O2. This strong effect is probably due to oxidation of tetravalent uranium into uranyl at the solid/liquid interface, as already described by De Pablo, as you have seen during Nicolas Dacheux talks.
the dissolution could occur in three steps: initial oxidation of uranium at the solid/liquid interface, protonation on the U(IV), Th(IV), U(VI) sites then detachment of the complexes formed at the interface.

## Slide 14
n = 4.1 – 5.0
Impact of acid concentration on UO2 dissolution
0.1 – 0.5 – 1 – 2M – 4M HNO3
T : 22oC – 40oC – 60oC
Static conditions
Reference Sintered UO2
RL = kT’  (H3O+) n
11
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
Log (NO3-) or Log (H3O+)
Log RL,0 (U) in g.m-2.d-1
Modification of the preponderant dissolution mechanism with acid concentration
CHNO3 < 0.5 M  Surface controlling reactions
CHNO3 > 0.5 M  Redox controlling reactions
0.3M HNO3
0.5M HNO3
Notes: The influence of the uranium mole loading on the normalized dissolution rates was studied for several Th1-xUxO2 solid solutions samples with various chemical compositions in 2 mol.L-1 HNO3 and at 60°C
You can see that after 170 days of leaching test , only 20 percent of the mixed oxide with a uranium mole loading of 0,16 are dissolved….
Conversely to that was observed for Th1-xCexO2 solid solutions, the substitution of thorium by uranium (IV) led to a significant modification of the chemical durability of Th1-xUxO2 solid solutions. Indeed, an increase of the normalized dissolution rates RL,0(U) and RL,0(Th) by three orders of magnitude is observed between Th0.84U0.16O2 and Th0.29U0.71O2. This strong effect is probably due to oxidation of tetravalent uranium into uranyl at the solid/liquid interface, as already described by De Pablo, as you have seen during Nicolas Dacheux talks.
the dissolution could occur in three steps: initial oxidation of uranium at the solid/liquid interface, protonation on the U(IV), Th(IV), U(VI) sites then detachment of the complexes formed at the interface.

## Slide 15
0.1 – 0.5 – 1 – 2M HNO3
T : 22oC – 40oC – 60oC
Static conditions
Reference Sintered UO2
Impact of the acid concentration on the activation energy due to change in predominant mechanism:
Surface controlling  Redox controlling reactions
12
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
Impact of temperature on UO2 dissolution
Ln RL,0(U) (g.m-2.d-1)
Opposite T (K-1)
Eapp = 87  8 kJ.mol-1
Eapp = 127  8 kJ.mol-1
Notes: The influence of the uranium mole loading on the normalized dissolution rates was studied for several Th1-xUxO2 solid solutions samples with various chemical compositions in 2 mol.L-1 HNO3 and at 60°C
You can see that after 170 days of leaching test , only 20 percent of the mixed oxide with a uranium mole loading of 0,16 are dissolved….
Conversely to that was observed for Th1-xCexO2 solid solutions, the substitution of thorium by uranium (IV) led to a significant modification of the chemical durability of Th1-xUxO2 solid solutions. Indeed, an increase of the normalized dissolution rates RL,0(U) and RL,0(Th) by three orders of magnitude is observed between Th0.84U0.16O2 and Th0.29U0.71O2. This strong effect is probably due to oxidation of tetravalent uranium into uranyl at the solid/liquid interface, as already described by De Pablo, as you have seen during Nicolas Dacheux talks.
the dissolution could occur in three steps: initial oxidation of uranium at the solid/liquid interface, protonation on the U(IV), Th(IV), U(VI) sites then detachment of the complexes formed at the interface.

## Slide 16
UO2
UO2 + PGM
22oC
Impact of PGM on UO2 dissolution
13
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
UO2 doped with 3% PGM
Rh (10%) – Ru (55%) – Pd (35%)
60oC
40oC
Very strong impact of PGM on RL,0(U)
More important in less acidic media
Associated to reduction of induction period
0.1 – 0.5 – 1 – 2M – 4M HNO3
T : 22oC – 40oC – 60oC
Static conditions
Reduction
Notes: The influence of the uranium mole loading on the normalized dissolution rates was studied for several Th1-xUxO2 solid solutions samples with various chemical compositions in 2 mol.L-1 HNO3 and at 60°C
You can see that after 170 days of leaching test , only 20 percent of the mixed oxide with a uranium mole loading of 0,16 are dissolved….
Conversely to that was observed for Th1-xCexO2 solid solutions, the substitution of thorium by uranium (IV) led to a significant modification of the chemical durability of Th1-xUxO2 solid solutions. Indeed, an increase of the normalized dissolution rates RL,0(U) and RL,0(Th) by three orders of magnitude is observed between Th0.84U0.16O2 and Th0.29U0.71O2. This strong effect is probably due to oxidation of tetravalent uranium into uranyl at the solid/liquid interface, as already described by De Pablo, as you have seen during Nicolas Dacheux talks.
the dissolution could occur in three steps: initial oxidation of uranium at the solid/liquid interface, protonation on the U(IV), Th(IV), U(VI) sites then detachment of the complexes formed at the interface.

## Slide 17
Impact of PGM on UO2 dissolution
0.016 % dissolved U
68 % dissolved U
14
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
0.1 M HNO3 – 22oC
Static conditions
 4000
UO2 + PGM
RL,0 (U) = (1.2 ± 0.2)  10-2 g.m-2.d-1
UO2
RL,0 (U) = (6.7 ± 0.3)  10-4 g.m-2.d-1
RL,0
 200
Strong impact associated to the presence of PGM on RL,0(U)
Same results for individual incorporation (Rh, Ru or Pd)
Solid contribution @ the solid/liquid interface ?
Solution contribution: reduction of HNO3 by PGM then production of autocatalytic species in solution (e.g. HNO2) ?
UO2 doped with 3 mol% PGM
Rh (10%) – Ru (55%) – Pd (35%)
Notes: The influence of the uranium mole loading on the normalized dissolution rates was studied for several Th1-xUxO2 solid solutions samples with various chemical compositions in 2 mol.L-1 HNO3 and at 60°C
You can see that after 170 days of leaching test , only 20 percent of the mixed oxide with a uranium mole loading of 0,16 are dissolved….
Conversely to that was observed for Th1-xCexO2 solid solutions, the substitution of thorium by uranium (IV) led to a significant modification of the chemical durability of Th1-xUxO2 solid solutions. Indeed, an increase of the normalized dissolution rates RL,0(U) and RL,0(Th) by three orders of magnitude is observed between Th0.84U0.16O2 and Th0.29U0.71O2. This strong effect is probably due to oxidation of tetravalent uranium into uranyl at the solid/liquid interface, as already described by De Pablo, as you have seen during Nicolas Dacheux talks.
the dissolution could occur in three steps: initial oxidation of uranium at the solid/liquid interface, protonation on the U(IV), Th(IV), U(VI) sites then detachment of the complexes formed at the interface.

## Slide 18
Catalytic process associated to PGM
15
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
0.1 M HNO3
T : 22oC – 40oC – 60oC
Static conditions
Significant decrease of EA with PGM
Catalytic process
Predominant in less acidic media
Solution + at solid/liquid interface ?
Eapp = 35  12 kJ.mol-1
Eapp = 87  8 kJ.mol-1
Catalytic
predominant
Redox
predominant
Predominant dissolution reaction
UO2 doped with 3 mol% PGM
Rh (10%) – Ru (55%) – Pd (35%)
Notes: The influence of the uranium mole loading on the normalized dissolution rates was studied for several Th1-xUxO2 solid solutions samples with various chemical compositions in 2 mol.L-1 HNO3 and at 60°C
You can see that after 170 days of leaching test , only 20 percent of the mixed oxide with a uranium mole loading of 0,16 are dissolved….
Conversely to that was observed for Th1-xCexO2 solid solutions, the substitution of thorium by uranium (IV) led to a significant modification of the chemical durability of Th1-xUxO2 solid solutions. Indeed, an increase of the normalized dissolution rates RL,0(U) and RL,0(Th) by three orders of magnitude is observed between Th0.84U0.16O2 and Th0.29U0.71O2. This strong effect is probably due to oxidation of tetravalent uranium into uranyl at the solid/liquid interface, as already described by De Pablo, as you have seen during Nicolas Dacheux talks.
the dissolution could occur in three steps: initial oxidation of uranium at the solid/liquid interface, protonation on the U(IV), Th(IV), U(VI) sites then detachment of the complexes formed at the interface.

## Slide 19
Impact of PGM : contribution in solution
Leachate
Dissolution reactor
UO2 Pellet
Magnetic stirrer
Support




PGM metallic powder
16
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
Sintered UO2
+ PGM (in solution)
0.1 HNO3 – 60oC
Static conditions
Increase of RL,0 (U) in the
presence of PGM powders
Rh: RL,0 (U) = (2.3 ± 0.1)  10-1 g.m-2.d-1
Pd: RL,0 (U) = (9.3 ± 0.2)  10-2 g.m-2.d-1
Ru: RL,0 (U) = (1.8 ± 0.1)  10-2 g.m-2.d-1
Pure UO2
RL,0 (U) = (3.3 ± 0.1)  10-3 g.m-2.d-1
Catalytic effect associated
to PGM in solution
RL,0
 70
Notes: The influence of the uranium mole loading on the normalized dissolution rates was studied for several Th1-xUxO2 solid solutions samples with various chemical compositions in 2 mol.L-1 HNO3 and at 60°C
You can see that after 170 days of leaching test , only 20 percent of the mixed oxide with a uranium mole loading of 0,16 are dissolved….
Conversely to that was observed for Th1-xCexO2 solid solutions, the substitution of thorium by uranium (IV) led to a significant modification of the chemical durability of Th1-xUxO2 solid solutions. Indeed, an increase of the normalized dissolution rates RL,0(U) and RL,0(Th) by three orders of magnitude is observed between Th0.84U0.16O2 and Th0.29U0.71O2. This strong effect is probably due to oxidation of tetravalent uranium into uranyl at the solid/liquid interface, as already described by De Pablo, as you have seen during Nicolas Dacheux talks.
the dissolution could occur in three steps: initial oxidation of uranium at the solid/liquid interface, protonation on the U(IV), Th(IV), U(VI) sites then detachment of the complexes formed at the interface.

## Slide 20
Microscopic study
---
Microstructural evolution of solid/solution interface
Notes: 20
20

## Slide 21
Operando study of evolving interface during dissolution
Environmental SEM observations
Dissolution tests
…
17
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017

## Slide 22
T. Cordara, PhD, ICSM/CEA, Univ. Montpellier, Nov 2017
18
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
UO2 pellet with 3 mol.% PGM
0.1 M HNO3 – T = 60oC
Dissolution time : 58 days
Impact of PGM : contribution at the solid/solution
interface
Heterogeneous dissolution
Preferential dissolution zones :
GB, triple junctions, pores
PGM / UO2 / Solution interface
Surface reactions
controlling dissolution
Impact of PGM
@ Solid/Liquid interface
Evolution of NL(U)

## Slide 23
t = 0h
3 µm
3D analysis of the dissolution of UO2 + PGM
645 hours
287 hours
Sintered UO2 doped with 3 mol% Rh-Ru-Pd
0.1 M HNO3 – 60°C
Operando ESEM:
Sequence of stereoscopic images
3D Reconstruction
Zones of interest: Access to dissolved volumes
* T. Cordara, PhD, ICSM/CEA, Univ. Montpellier, Nov. 2017
19
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
t = 96h
3 µm
3 µm
t = 287h
3 µm
t = 645h
3 µm
t = 1392h

## Slide 24
GB1
GB2
GB3
3D analysis of the dissolution of UO2 + PGM
20
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
GB1
RL,0 (global) = 7.4  10-2 g.m-2.d-1
RL,0 (GB) = (6.5 to 8.4 )  10-2 g.m-2.d-1
Starting global dissolution directly linked to the dissolution of GB

## Slide 25
Conclusions & Outlooks
21
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
Strong impact of PGM on RL,0(U)
Impact at
S/L interface
Impact in solution

## Slide 26
CNRS – Univ. Montpellier
METSA
EU: TALISMAN, GENIORS
Financial support
www.icsm.fr
Laboratory of Matter in Environmental Conditions
H.P Brau (MET)
J. Ravaux
(ESEM and X-EDS)
B. Corso (PXRD)
Dr. R. Podor
(ESEM and X-EDS)
Scientific contribution and technical support
CEA & AREVA
Acknowledgements
IT Department
J. Favrichon
A. Delannoy
(SIP2D)
Ph. Moisy
A. Salvatores
X. Machuron Mandard
S. Grandjean
Laboratory of Evolving Interfaces in Materials
GENIORS

## Slide 27
And you for listening…

## Slide 28
Impact of HNO2 on dissolution
F. Tocino, PhD, ICSM/CEA, Univ. Montpellier, Dec. 2015
U0.75Th0.25O2
4 M
2 M
1 M
0.5 M
0.1 M
0.05 M
 HNO3
 H2SO4
 HCl
 HNO3 + hydrazinium
 HCl + NaNO2
Strong increase of the dissolution rate with HNO2
Lower impact of H3O+ et NO3-
T. Dalger, PhD, ICSM/CEA, Univ. Montpellier, 2016–2019
T. Dalger et al., J. Nucl. Mater., To be submitted
NaNO2 3×10-2 M
NaNO2 2×10-2 M
NaNO2 1×10-2 M
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017