## Slide 1
Effect of lanthanide elements on the dissolution of uranium dioxide
INSTITUT DE CHIMIE SEPARATIVE DE MARCOULE
T. Cordara 1, L. Claparede 1, S. Szenknect 1,
Mesbah 1, C. Lavalette 3 , R. Podor 2
N. Dacheux 1
1 ICSM/LIME, UMR 5257, CEA, CNRS, Univ. Montpellier, ENSCM
2 ICSM/L2ME, UMR 5257, CEA, CNRS, Univ. Montpellier, ENSCM
3 AREVA NC / BG aval / DO recyclage / RDP, Paris

## Slide 2
Transverse approach of the material elaboration
Model compounds :
New ways of synthesis
New precursors
Properties in use :
Chemical durability
Long-term behavior
Sintering :
densification
microstructure
Optimized Syntheses
Dissolution of AnO2, (An,Ln)O2-x / Fluorite-type prepared from oxalate precipitation
  Conventional parameters ( chemical composition, temperature, acidity, … )
  Structural parameters ( oxygen vacancies, superstructure, secondary phases, … )
  Microstructural parameters ( crystal defects, crystallite size, densification rate, … )
Dissolution
Leaching
How can sample preparation impact dissolution ?
1
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017

## Slide 3
Distribution of FP in SNF
2
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
Spent Nuclear Fuel
  U (95 wt.%) – Pu (1 wt.%)
  MA (0.1 wt.%) – FP (4 wt.%)
More than 40 FP
4 main types
PGM
(Ru, Rh, Pd)
 0.6 mol.%
Lanthanides
(La, Ce, Pr, Nd)
 1 mol.%
Which impact of FP on UO2 dissolution ?
P. Burns, R.C. Ewing, A. Navrotsky, Science 2012, 335, 1184-1187
PRECCI Report, CEA, 2001, CEA-R-5958E
Next talk …

## Slide 4
Model compounds
Synthesis / Densification
Dissolution experiments
Macroscopic dissolution rates
Monitoring of solid/liquid interface
Evolving structural and microstructural parameters
Macroscopic description of the dissolution
Impact of dissolving solution :
pH, T, redox, composition…
Microscopic description of the evolving interface
Structural and microstructural control of starting materials
Operando analysis (ESEM, X-EDS, G-XRD, XRR, AFM)
 Topography, porosity, chemical composition of interface
RL = k0  e-EA/RT  a(H3O+)n  g(I)   a(i)ni  f (RG (,T) )
Methodology
3
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017

## Slide 5
Samples elaboration
----
Sintering
Notes: 5
5

## Slide 6
R. T.
H2C2O4 : + 50%
Preparation of U1-xLnxO2-x/2
Conversion
Oxalate precipitation
500oC / 4 h
Air
then
Ar / H2
4
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
Washing
( H2O – EtOH )
Drying
( 90oC )
(U1-xLnx)(C2O4)2-x/2 . n H2O (x = 0.1 & 0.2)
Y : 7% - La : 13% - Ce : 26% - Pr : 12% - Nd : 42%
5 µm
U1-xLnxO2-x/2
5 µm
Platelet grains
 5 µm in size
Y | 0.07 | 0.06 ± 0.02 | 99.9 
La | 0.13 | 0.14 ± 0.03 | 93.8 
Ce | 0.26 | 0.31 ± 0.05 | 92.9 
Pr | 0.12 | 0.13 ± 0.08 | 98.7 
Nd | 0.42 | 0.42 ± 0.04 | 95.6 
 | Expected mole ratio | Obtained (Dissolution) | Recovery yield (%)
U | 0.9 | 0.89 ± 0.04 | 99.3 
Ln(III) | 0.1 | 0.11 ± 0.02 | 
Full dissolution
ICP-AES

## Slide 7
Characterization of U1-xLnxO2-x/2 samples
5
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
U0.9Ln0.1O1.95
U0.8Ln0.2O1.9
UO2
Intensity (a.u.)
2q (degrees )
Incorporation of Ln(III) in the UO2
Fluorite-type structure
a = 5.466 Å
J. Tsuji, J. Alloys Compds, 1998, 271, 391
Literature :
a = 5.469 Å
a = 5.438 Å
a = 5.442 Å

## Slide 8
Sintering of U1-xLnxO2-x/2 samples
Uniaxial pressing
RT – 500 MPa
Heating treatment
1550oC / 8h
Ar – 5% H2
Characterization
PXRD, BET, ESEM, Pycnometry
6
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
Grinding step
30 Hz / 30 min
U0.9Ln0.1O1.95
4 µm
4 µm
UO2
Densification rate: 93%
Average grain size: 11.8 µm
SSA: 5  10-3 m2.g-1
Densification rate: 90%
Average grain size: 3.4 µm
SSA: 5  10-2 m2.g-1
Densification rate: 87%
Average grain size: 0.9 µm
SSA: 1  10-2 m2.g-1
U0.8Ln0.2O1.9

## Slide 9
Macroscopic study
---
Multiparametric expression of the dissolution kinetics
A.C. Lasaga, Kinetic Theory in the Earth Sciences, Princeton Univ. Press, 1998
Notes: 9
9

## Slide 10
ICP–AES
ICP-MS
a liquid scintillation
Static conditions
Sintered Pellet
Dissolution test: experimental device
RL(i) ≈ RL(j): congruent dissolution
RL(i) ≠ RL(j): incongruent dissolution
7
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
Leachate
Dissolution reactor
Pellet
Magnetic stirrer
Support
Reactive surface area (m2)
Amount of (i) in solution (g)
Mass ratio of (i) in the solid

## Slide 11
Nature of the dissolution of U1-xLnxO2-x/2
8
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
U0.9Ln0.1O1.95
U0.8Ln0.2O1.9
Strong impact of Ln(III) on RL,0 for low acicity (CHNO3 < 1M)
e.g. increase by a factor up to  20 for U0.9Ln0.1O1.95 vs. UO2
Small impact for higher acid concentrations (CHNO3 > 2M)
Congruent dissolution Ln(III) / U
In agreement with other systems (Th- & Ce-based)
D. Horlait et al., J. Mater. Chem. A 2014, 2, 5193 – J. Nucl. Mater., 2012, 429, 237; S. Szenknect et al., J. Phys. Chem. C 2012, 116, 12027
Notes: The influence of the uranium mole loading on the normalized dissolution rates was studied for several Th1-xUxO2 solid solutions samples with various chemical compositions in 2 mol.L-1 HNO3 and at 60°C
You can see that after 170 days of leaching test , only 20 percent of the mixed oxide with a uranium mole loading of 0,16 are dissolved….
Conversely to that was observed for Th1-xCexO2 solid solutions, the substitution of thorium by uranium (IV) led to a significant modification of the chemical durability of Th1-xUxO2 solid solutions. Indeed, an increase of the normalized dissolution rates RL,0(U) and RL,0(Th) by three orders of magnitude is observed between Th0.84U0.16O2 and Th0.29U0.71O2. This strong effect is probably due to oxidation of tetravalent uranium into uranyl at the solid/liquid interface, as already described by De Pablo, as you have seen during Nicolas Dacheux talks.
the dissolution could occur in three steps: initial oxidation of uranium at the solid/liquid interface, protonation on the U(IV), Th(IV), U(VI) sites then detachment of the complexes formed at the interface.

## Slide 12
0.1 – 0.5 – 1 – 2M – 4M HNO3
T : 22oC – 40oC – 60oC
Static conditions
Sintered U0.9Ln0.1O1.95
CHNO3 < 0.5 M  Eapp  50 kJ.mol-1
  Surface controlling reactions
CHNO3 > 0.5 M  Eapp  100 kJ.mol-1
  Redox controlling reactions
Impact of the acid concentration on the activation energy
9
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
Impact of temperature on U0.9Ln0.1O1.95 dissolution
107  4 kJ.mol-1
99 19 kJ.mol-1
48  10 kJ.mol-1
51  11 kJ.mol-1
Notes: The influence of the uranium mole loading on the normalized dissolution rates was studied for several Th1-xUxO2 solid solutions samples with various chemical compositions in 2 mol.L-1 HNO3 and at 60°C
You can see that after 170 days of leaching test , only 20 percent of the mixed oxide with a uranium mole loading of 0,16 are dissolved….
Conversely to that was observed for Th1-xCexO2 solid solutions, the substitution of thorium by uranium (IV) led to a significant modification of the chemical durability of Th1-xUxO2 solid solutions. Indeed, an increase of the normalized dissolution rates RL,0(U) and RL,0(Th) by three orders of magnitude is observed between Th0.84U0.16O2 and Th0.29U0.71O2. This strong effect is probably due to oxidation of tetravalent uranium into uranyl at the solid/liquid interface, as already described by De Pablo, as you have seen during Nicolas Dacheux talks.
the dissolution could occur in three steps: initial oxidation of uranium at the solid/liquid interface, protonation on the U(IV), Th(IV), U(VI) sites then detachment of the complexes formed at the interface.

## Slide 13
Effect of acid concentration on U0.9Ln0.1O1.95 dissolution
RL = kT’  (CN) n’
10
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
Modification of the preponderant dissolution mechanism with acid concentration
CHNO3 < 0.5 M  Surface controlling reactions
CHNO3 > 0.5 M  Redox controlling reactions
0.1 M
0.5 M
1 M
2 M
4 M
n' = 2.3 – 4.5
0.5 M HNO3
Sintered U0.9Ln0.1O1.95
0.1 – 0.5 – 1 – 2M – 4M HNO3
T : 22oC – 40oC – 60oC
Static conditions
Notes: The influence of the uranium mole loading on the normalized dissolution rates was studied for several Th1-xUxO2 solid solutions samples with various chemical compositions in 2 mol.L-1 HNO3 and at 60°C
You can see that after 170 days of leaching test , only 20 percent of the mixed oxide with a uranium mole loading of 0,16 are dissolved….
Conversely to that was observed for Th1-xCexO2 solid solutions, the substitution of thorium by uranium (IV) led to a significant modification of the chemical durability of Th1-xUxO2 solid solutions. Indeed, an increase of the normalized dissolution rates RL,0(U) and RL,0(Th) by three orders of magnitude is observed between Th0.84U0.16O2 and Th0.29U0.71O2. This strong effect is probably due to oxidation of tetravalent uranium into uranyl at the solid/liquid interface, as already described by De Pablo, as you have seen during Nicolas Dacheux talks.
the dissolution could occur in three steps: initial oxidation of uranium at the solid/liquid interface, protonation on the U(IV), Th(IV), U(VI) sites then detachment of the complexes formed at the interface.

## Slide 14
Microscopic study
---
Microstructural evolution of solid/solution interface
Notes: 14
14

## Slide 15
Operando study of evolving interface during dissolution
Environmental SEM observations
Dissolution tests
…
11
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017

## Slide 16
Preferential dissolution zones (GB)
Ln(III) – enrichment in GB
 Decrease of energy of cohesion
Monitoring of solid/liquid interface during dissolution by ESEM
T. Cordara, PhD, ICSM/CEA, Univ. Montpellier, Nov 2017
12
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
UO2 pellet
1 M HNO3 – T = 60oC
Dissolution time : 3.2 days
U1.9Ln0.1O1.95 pellet
1 M HNO3 – T = 60oC
Dissolution time : 1.6 days
Homogeneous dissolution
Microstructural evolution
Oxidation of U(IV)
D. Horlait et al., J. Nucl. Mater., 2012, 429, 237
S. Szenknect et al., J. Phys. Chem. C 2012, 116, 12027

## Slide 17
Conclusions & Outlooks
13
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
Incorporation of Ln(III) in the UO2
Solid solutions with fluorite-type structure
Well densified pellets
Modification of the preponderant dissolution mechanism with acid concentration ( @ 0.5M HNO3 )
Surface  Redox
controlling reactions
Existence of preferential
dissolution zones
Ln(III) – enrichment in GB
 Decrease of energy of cohesion
Macroscopic description
Microscopic description
Strong impact of lanthanides on the dissolution of UO2 in the lower concentrated acid solution

## Slide 18
CNRS – Univ. Montpellier
METSA
EU: TALISMAN, GENIORS
Financial support
www.icsm.fr
Laboratory of Matter in Environmental Conditions
H.P Brau (MET)
J. Ravaux
(ESEM and X-EDS)
B. Corso (PXRD)
Dr. R. Podor
(ESEM and X-EDS)
Scientific contribution and technical support
CEA & AREVA
Acknowledgements
IT Department
J. Favrichon
A. Delannoy
(SIP2D)
A. Salvatores
X. Machuron Mandard
S. Grandjean
Laboratory of Evolving Interfaces in Materials
GENIORS

## Slide 19
And you for listening…

## Slide 21
General trend of UO2 dissolution in nitric acid
T. Cordara et al., J. Nucl. Mater. 2017, 496, 251-264
N. Dacheux et al. , SBNWM symposium 2017, Sydney, October 29 – November 03, 2017
Kinetics
3 domains
RL.pulse (U)
RL.0 (U)
RL.t (U)
≈ 0.05
≈ 0.5
Dissolved mass, m/m0 (%)
Leaching time (days)
RL,pulse
RL,0
Increase of S
Increase of autocatalytic species
↗↗ of RL(t)
Steady state:
Constant rate
≈ 90



Normalized dissolution rate
RL.0 (U) expressed in g.m-2.d-1
Induction period
Notes: The influence of the uranium mole loading on the normalized dissolution rates was studied for several Th1-xUxO2 solid solutions samples with various chemical compositions in 2 mol.L-1 HNO3 and at 60°C
You can see that after 170 days of leaching test , only 20 percent of the mixed oxide with a uranium mole loading of 0,16 are dissolved….
Conversely to that was observed for Th1-xCexO2 solid solutions, the substitution of thorium by uranium (IV) led to a significant modification of the chemical durability of Th1-xUxO2 solid solutions. Indeed, an increase of the normalized dissolution rates RL,0(U) and RL,0(Th) by three orders of magnitude is observed between Th0.84U0.16O2 and Th0.29U0.71O2. This strong effect is probably due to oxidation of tetravalent uranium into uranyl at the solid/liquid interface, as already described by De Pablo, as you have seen during Nicolas Dacheux talks.
the dissolution could occur in three steps: initial oxidation of uranium at the solid/liquid interface, protonation on the U(IV), Th(IV), U(VI) sites then detachment of the complexes formed at the interface.