## Slide 1: Simplified UK Magnox waste glass alteration layer characterisation using 29Si,17O and 25Mg NMR techniques
Rui Guo & Ian Farnan
Notes: MAGnesium Non-OXdising

## Slide 2: Background
Mixture Windscale (MW) 25 wt% waste load glass: MW25 (borosilicate glass)
Full-component MW25 simulant glass: 23-oxide components
Simplified 6-oxide components glass:
“to study the effect of Mg on glass dissolution as opposed to Ca”
Leached in deionised water;
Leached in 17O enriched (45%) water;
MgEM made using 25Mg enriched (99.7%) MgO as precursor (leached in deionised water).
Cation | Al | B | La (REs) | Mg/Ca | Na (alkalis) | Si
mol% | 4.87 | 27.58 | 1.72 | 6.54 | 15.38 | 43.91
MgEM CaEM
Notes: Simplified 6-oxide component glasses were made to study the effect of magnesium against calcium on dissolution;
The GLASTAB project (European) in Switzerland: MW and SON68 glasses leached in pure water at 90℃ for more than 12 years (1200 m^-1, too).

## Slide 3: Motivation
Chart: Leaching time (days)
| 28 | 112
B | 4.023 | 6.6573
Mg | 0.052735 | 0.00061941
Chart: Leaching time (days)
| 7 | 14 | 28 | 112
B (MgEM) | 4.84 | 6.59 | 7.63 | 7.96
B (CaEM) | 0.426 | 0.601 | 0.667 | 0.928
Mg (MgEM) | 0.00547 | 0.00536 | 0.00411 | 0.00193
“1. Leached in deionised water”
“3. MgEM made using 25Mg enriched (99.7%) MgO as precursor (leached in deionised water)”
4 weeks
Notes: Would the deposit of magnesium back onto the surface contribute to the drastically different dissolution rates;
It is important to understand in what form they have been incorporated;

## Slide 4: XRD
4wk leached
16wk leached
To use multinuclear NMR techniques to characterise the altered layer that results from re-organisation processes and precipitation reactions
Notes: Any proto-crystalline or amorphous phase would be difficult to be seen by XRD;
NMR does not care long range order, it only uses magnetic nuclei as probe for local chemistry and structural environments, therefore could provide insightful information;
The GLASTAB project (European) in Switzerland: MW and SON68 glasses leached in pure water at 90℃ for more than 12 years (1200 m^-1, too).

## Slide 5: Cross polarisation (CP) NMR
Achieved by transferring magnetization (M) from protons to the nuclei of interests:
Contact time (CT): the time during which M is transferred
1H 29Si
1H 17O
1H 25Mg
Benefits: 1. Signal enhancement; 2. selectivity etc.
Chart: Leaching time (days)
| 7 | 14 | 28 | 112
B (MgEM) | 4.84 | 6.59 | 7.63 | 7.96
Mg (MgEM) | 0.00547 | 0.00536 | 0.00411 | 0.00193
~100 m
Experimentally difficult!
~3 m
Notes: To explain and explore CT later;
The diameter of glass particles in question is at the scale of 100 um while the longest leached samples, based on B concentration in solution, only builds up an altered layer with an effective thickness of ~3 um;
The GLASTAB project (European) in Switzerland: MW and SON68 glasses leached in pure water at 90℃ for more than 12 years (1200 m^-1, too).

## Slide 6
Mixture Windscale (MW) 25 wt% waste load glass: MW25
Full-component MW25 simulant glass: 23-oxide components
Simplified 6-oxide components glass:
Leached in deionised water;
Leached in 17O enriched (40%) water;
Made using 25Mg enriched (99.7%) MgO as precursor.
Cation | Al | B | La (REs) | Mg | Na (alkalis) | Si
mol% | 4.87 | 27.58 | 1.72 | 6.54 | 15.38 | 43.91
Notes: The GLASTAB project (European) in Switzerland: MW and SON68 glasses leached in pure water at 90℃ for more than 12 years (1200 m^-1, too).

## Slide 7: 29Si CPMAS: depolymerisation
The position of the primary peak is in the range of -90~-100 ppm, which mainly corresponds Q3 species i.e. Si connected to 3 bridging oxygens (BOs) and 1 non-bridging oxygen (NBO), in this case, Si-OH. As CT increases, Si species that are more electronically shielded get cross polarised i.e. Q4, which locate further from protons.
 | 0.5 ms
 | 5 ms
 | 20 ms
 | 0.5 ms
 | 5 ms
 | 20 ms
~-110 ppm
-90~-100 ppm
 | MgEM leached (5ms)
 | MgEM pristine
 | MgEM leached (5ms)
 | MgEM pristine
~-110 ppm
Notes: Altered layer gets depolymerised due to hydration & hydrolysis, which is also illustrated by comparison with single pulse spectrum of pristine glass;
The GLASTAB project (European) in Switzerland: MW and SON68 glasses leached in pure water at 90℃ for more than 12 years (1200 m^-1, too).

## Slide 8: 29Si CPMAS : other minerals
Aluminous hectorite precipitate on AVM-10 French glass
(B. Thien et al. App. Caly Sci. 49 (2010) 135-141)
 | Simplified MW25
 | Al Hectorite
 | Talc
 | Simplified MW25
 | Al Hectorite
 | Talc
~-90 ppm
~-96 ppm
Notes: If there is any local reorganization that took place with magnesium deposit, what mineral structure would it be similar to;
The XRD identified aluminous hectorite phase found as a result of AVM-10 glass (~6 wt% MgO) dissolution after 2500 days by adding MgCl2 after 114 days;
The GLASTAB project (European) in Switzerland: MW and SON68 glasses leached in pure water at 90℃ for more than 12 years (1200 m^-1, too).

## Slide 9
Mixture Windscale (MW) 25 wt% waste load glass: MW25
Full-component MW25 simulant glass: 23-oxide components
Simplified 6-oxide components glass:
Leached in deionised water;
Leached in 17O enriched (40%) water;
Made using 25Mg enriched (99.7%) MgO as precursor.
Cation | Al | B | La (REs) | Mg | Na (alkalis) | Si
mol% | 4.87 | 27.58 | 1.72 | 6.54 | 15.38 | 43.91
Notes: The GLASTAB project (European) in Switzerland: MW and SON68 glasses leached in pure water at 90℃ for more than 12 years (1200 m^-1, too).

## Slide 10: 17O NMR
Since the natural abundance of 17O is ~0.038%, the NMR signal detected must be selectively from the altered glass surface which “incorporates” the 17O from the enriched water, even without CP!
Line features indicate multiple oxygen sites in the altered layer but could not be resolved
Single-pulse MAS @15 kHz

## Slide 11: Static echo spectra
Since the natural abundance of 17O is ~0.038%, the NMR signal detected must be selectively from the altered glass surface which “incorporates” the 17O from the enriched water, even without CP!
1H decoupled
SiO2
Protonated bridging oxygens (BO) as signal pulled up by 1H decoupling
Notes: Static experiment could disperse the resonance frequencies and yield line features;
Without constraints that are available to known samples, it is difficult to fit the experimental spectra like this;
The GLASTAB project (European) in Switzerland: MW and SON68 glasses leached in pure water at 90℃ for more than 12 years (1200 m^-1, too).

## Slide 12: Static CP
How about CP?
 | CT (ms)
 | 1
 | 0.5
 | 0.1
 | 0.05
 | CT (ms)
 | 1
 | 0.5
 | 0.1
 | 0.05
 | ct 1ms
 | ct 5
 | echo
 | ct 1ms
 | echo
Hydroxyl oxygen signals get accentuated with shorter CT because of shorter O-H distance, which are absent in the echo spectra!
Notes: The signals seen in the static echo spectra must contain BOs that are protonated, which is consistent with the decoupling results;
The GLASTAB project (European) in Switzerland: MW and SON68 glasses leached in pure water at 90℃ for more than 12 years (1200 m^-1, too).

## Slide 13: Calculation and simulation
CASTEP NMR calculation of the hydroxyl oxygen(s) in talc yields
Cq~8.1 MHz and eta~0.01 (
Tentative fitting yields:
iso~28 ppm
Cq~7.9 MHz and eta~0
Notes: CASTEP NMR-DFT theory based code for calculating electronic structures. In this case, NMR parameters;
The lineshape is far too complicated to categorically assign that fitting to talc but similar local –OH structures must exist;

## Slide 14
Mixture Windscale (MW) 25 wt% waste load glass: MW25
Full-component MW25 simulant glass: 23-oxide components
Simplified 6-oxide components glass:
Leached in deionised water;
Leached in 17O enriched (40%) water;
Made using 25Mg enriched (99.7%) MgO as precursor.
Cation | Al | B | La (REs) | Mg | Na (alkalis) | Si
mol% | 4.87 | 27.58 | 1.72 | 6.54 | 15.38 | 43.91
Notes: The GLASTAB project (European) in Switzerland: MW and SON68 glasses leached in pure water at 90℃ for more than 12 years (1200 m^-1, too).

## Slide 15: 25Mg NMR
One of the toughest nuclei to be observed in solid-state NMR:
High magnetic field & isotopic enrichment; long acquisition time & poor resolution!
UK 850 MHz Solid-state NMR facility
14 kHz MAS dfs_spinecho
 | Pristine
 | 16wk
 | Pristine
 | 16wk
 | Aluminous hectorite
 | Talc
 | Aluminous hectorite
 | Talc
Notes: The Mg speciations contribute to the peak shift although the majority signal is still from the pristine glass;

## Slide 16
How about CP?
static cp
 | Talc
 | 16wk
 | Talc
 | 16wk
Mg environment closer to that in talc than Al hectorite consistent with 29Si NMR results
qcpmg
 | Al Hectorite
 | 16wk
 | Al Hectorite
 | 16wk
Notes: Based on CASTEP calculation, two magnesium sites in talc have very similar isotropic chemical shifts; CP at different CT time could result in intensity distortion;
The broadening of Al Hectorite spectrum might be due to paramagnetic effects;

## Slide 17: Summary
Alteration layer of MgEM glass is depolymerized and the local silicon environments similar to that of talc;
Bridging oxygens (BOs) are protonated. Hydroxyl oxygens are only seen in CP conditions with short CT with local oxygen environments resemble that of talc;
Mg environments are closer to that of talc which is consistent with silicon and oxygen results;
Precipitates possess a talc-like structure while other Mg-silicates also need to be “tested”.
Notes: The GLASTAB project (European) in Switzerland: MW and SON68 glasses leached in pure water at 90℃ for more than 12 years (1200 m^-1, too).

## Slide 18: Future work
CPMAS experiments to improve oxygen-17 and magnesium-25 static CP spectra resolutions;
CASTEP NMR calculations on other magnesium silicates such as hectorite & sepiolite etc. where isotopic enrichment is not always viable.
 | CPMAS (20 kHz)
 | Single-pulse MAS (20 kHz)
 | CPMAS (20 kHz)
 | Single-pulse MAS (20 kHz)
Promising results from 17O CPMAS
Notes: The GLASTAB project (European) in Switzerland: MW and SON68 glasses leached in pure water at 90℃ for more than 12 years (1200 m^-1, too).

## Slide 19: Acknowledgements
The UK 850 MHz solid-state NMR Facility used in this research was funded by EPSRC and BBSRC (contract reference PR140003), as well as the University of Warwick including via part funding through Birmingham Science City Advanced Materials Projects 1 and 2 supported by Advantage West Midlands (AWM) and the European Regional Development Fund (ERDF);

## Slide 20: 29Si CPMAS dynamics
Transfer efficiency depends on 1H-29Si spatial distance and in competition with 1H relaxation in RF;
CT (ms)
Overall intensity evolves. How about lineshape?
0.5
1
5
10
15
20
30
40
60
80
Notes: First of all, CT has a huge impact on the line intensity as the build-up of M transfer is in competition with proton relaxation;
The second effect is lineshape as further located nuclei could be excited with increasing CT, which might have different resonance frequency;
The GLASTAB project (European) in Switzerland: MW and SON68 glasses leached in pure water at 90℃ for more than 12 years (1200 m^-1, too).