## Slide 1
Advanced Materials and Processes for Application to the Back-end of the Nuclear Fuel Cycle
Vittorio (Victor) Luca
Comisión Nacional de Energía Atómica
Acknowledgements: The presenter expresses his sincere gratitude to the conference organizers for the kind invitation and the IAEA for financial assistance

## Slide 2
3 NUCLEAR POWER PLANTS
6 RESEARCH REACTORS
2 IRRADIATION PLANTS
1 HEAVY WATER PLANT
2 URANIUM MINING FACILITIES
4 ACCELERATORS
1 URANIUM ENRICHMENT FACILITY
376 INDUSTRIAL APPLICATION FACILITIES
3 NUCLEAR RESEARCH CENTERS
1 TECHNOLOGICAL CENTER
3 NUCLEAR MEDICINE SCHOOLS 68 COBALT THERAPY CENTERS
57 BRAQUITHERAPY CENTERS
309 NUCLEAR MEDICINE CENTERS
45 MEDICAL ACCELERATORS
408 IMMUNE ESSAYS LABS
>60 YEARS of NUCLEAR ACTIVITY IN ARGENTINA
No Repository!

## Slide 3
Priority 1
Priority 2
CNEA Waste Streams

## Slide 4
Collaborators
CNEA: Cerchietti, Custo, Alurralde, Vega, Halac, Vaccaro, Alvarado, Quintana, Cestau, Sobra…
ANSTO: Veliscek-Carolan, Scales, Hanley…
ICSM: Arrachart, Rey
Banchi, Castro, Rodriguez
Civitate
Treatment of gaseous efluentes from IX resin processing
Curi
CST use and immobilization
Tejada
Zr(IV)-organophosphonate coordination polymers for LN3+/AN3+ separations
Manzini, Dos Santos, Talavera-Ramos, Telleria-Narvaiz
Target materials for cleaner 99Mo production
Sansierra, Alvarez
Treatment & Conditioning of spent IX resins
Research Group Activities
Notes: https://www.youtube.com/watch?v=rw9zbeHEXY8

## Slide 5
Cradle-to-Grave Concept for Radioactive Waste Management
Step 1
Utilization and/or development of predominantly inorganic & hybrid adsorbents with tailorable porosity and composition
(e.g. ZrxTi1-xO2).
2 – 10 nm
Step 3
Selective extraction of target species.
Step 2
Funcionalization of adsorbent surfaces to enhanced selectivity for target species
( e.g. Polyphosphonic acids).
Deep underground
repository disposal
Option 1: Cradle-to-Grave
Simple convertion to dense highly insoluble ceramic,
glass or other
∆
Requirements
Transparent to neutrons
Stable in very high radiation fields
Good chemical stability
High thermal conductivity
No phase changes
Recyclable/reprocessable
(i.e. soluble in HNO3)
Ceramic with hierarchical porosity
ZrxTi1-xO2
RF Resin
SdVB Resin
Option 2
Use as recyclable inert matrix e.g. ZrC, SiC, ZrO2, Al2O3…
5 mm Porous Monolith
Transmutation in FR, LWR or ADS
Notes: In the paper by Degueldre and Paratte (Concepts for an inert matrix fuel, an overview. J. Nucl. Mater. 1999,274,1) similar ideas are also articulated.

## Slide 6
Decontaminated
liquid
Sorbent Columns
Contaminated waste
liquid
137Cs-selective Silicotitanate
Cradle-to-Grave
Nyman et al. Mater. Res. Soc. Symp. Proc. 1999, 556, 71
Su et al. Mater. Res. Soc. Symp. Proc. 1999, 556, 77
Tomasberger et al. Radiochim. Acta 2001, 89, 145

CST Sitinakite
Pollucite
CsTiSi2O6.5
Na2Ti2SiO7.H2O
Na+
Cs+
Leach rates several orders of magnitude lower than that of borosilicate glass

## Slide 7
Mesoporous Zr0.33Ti0.66O2
Δ
1 mm
Uncalcined
Calcined 450 oC
Luca et al. Micro. Meso. Mater. 2007, 103, 123
Griffith et al. Langmuir 2008, 24,12312
Sizgek et al. Langmuir 2008, 24, 12323
900 oC
1300 oC
Uniform porosity (monomodal)
Homogenous distribution of Zr and Ti
Very high thermal stability
Conversion to zirconolite possible
Able to be produced directly in column-ready bead form
Notes: Thus bidentate bridging coordination of the carboxylate dominates as the proportion of metal centers increases
Monodentate coordination is usually distinguished by a large ∆ = (sym – asy) whereas for bidentate coordination ∆ is smaller than in the free acid or simple salts

## Slide 8
Treatment and Conditioning of Spent Resins

## Slide 9
Sensitivity Factor
Criteria/Indicators
Down Selection Methodology
Short List
BAT (Best Available Technology) Analysis (IAEA, TECDOC 1744)

## Slide 10
Direct Immobilization
Polymer (e.g. Socodei, France)
Cement (OPC-based, Geopolymer) Bitumen (e.g. Sweden)
Ceramicrete, Duralith, SiAl, Cast Stone
Destructive Treatment
Pyrolisis (e.g. Belgoprocess)
FBSR (e.g. THOR, USA)
Incineration
Vitrification
Thermal Plasma
Microbioligical
Wet Oxidation
Acid Digestion
Molten salt
Catalytic oxidation
Supercritical Water Oxidation
Electrochemical Oxidation
Thermochemical methods
HIP
Pyrolisis (300  50 oC)
Simple process
Volume reduction
Flameless
Versatile
Ultra stable products
Minimal 2º wastes
Processes Considered

## Slide 11
Pirolisis
300-600 oC
Polímero
HIP?
Opción 3
Opción 2
Opción 1
Polymer
Contenidor de Alta Integridad
Pirolisis
300-600 oC
Polímero
Options Considered for Treatment and Conditioning of Spent IX Resins
MERCURE process, Socodei, Francia
500 m3/year

## Slide 12
Treatment and Conditioning of Spent IX Resinas
Is it possible to develop a low temperature pyrolysis process that results in a volume reduction and at the same time confines that entire radionuclide inventory within the matrix that is generated?
What are the relations between process temperature and the structure microstructure and the chemical properties of the products generated?
Traps
Tubular Oven
N2, Ar, CH4 …
Cs, Sr, Co y Ni-saturated resins
Experimental Setup

## Slide 13
Cs
S
Sr
Ni
Co
, N2
Thermal Treatment of Cation Exchange Resins
Cation exchange resin (Lewatit® MonoPlus S100H)
Cs
600 oC/N2
10 oC/min
Luca et al. J. Nucl. Mater. 2012, 424, 1
Cs, Sr, Co & Ni-saturated

## Slide 14
What are the chemical caracteristics of resins pyrolyzed at low temperature?
How can we modify these products in order to improve their performance?
Cs
Fracción lixiviada Instantáneamente

## Slide 15
Leaching as a Function of Loading
[137Cs] of Typical Spent PHWR Resins  0.051 nmol/g
200 oC
300 oC
400 oC

## Slide 16
Anion Exchange Resins (Lewatit® Monoplus M500)
36Cl- T1/2 = 3.01x105 years
129I- T1/2 = 1.57x107 years
14CO32- T1/2 = 5.73x103 years
99TcO4- T1/2 = 2.111x105 years
LCMS Detection of 127I at Reactor Outflow
14C by Scintillation Counting
Anion exchange resins are more complex than their cation exchange resin counterparts since they trap isotopes that have long half lives, are highly volatile and biocompatible.
Upper limit for 14C retention is around 200 oC.
For 129I it would be around 300 oC.
Luca et al. J. Environ. Chem. Eng. 2017, 5, 4165

## Slide 17
Resin Dewatering
Low Temperature
Pyrolysis
High Performance Plasma treatment or Post Combustion System
Radionuclide Capture
in Selective Adsorbents
Polymer Encapsulation
(Epoxy, phenolic resin…)
Interim Storage/Repository
14C,129I…
2H, 3H
Recycle/Disposition
Spent Resin
Simplified Process Flow Sheet
Bench-Scale Demo  Pilot Scale at Kg/h Throughput (cold and then hot)

## Slide 18
The only process that at present meets ANDRA requirements for the disposition of spent IX resins.
Limited exudation of water
Low exothermicity
Confinement of radioactivity
Good compressive strength (>8MPa)
Low leaching
Resistance to thermal cycling
homogeneous
Resistance to radiation
Max packet dose of 2 mSv/h. Ahora <0.75 mSv/h.
Not flammable
The process depends on the polymeric reaction between an epoxide and D7M6 hardner.
57,58,60Co, 110mAg, 134,137Cs…
>400 / año
1.2 m3
Mercure Process - SOCODEI

## Slide 19
Cumulative leached fraction (F) of Cs+, Sr2+, Co2+, Ni2+ -saturated resins
Ultrapure Water
Ultrapure Water
RII
NC-5 + RII
NC-5: 70 % RII (300 oC), 27 % Resol, 3 % SiO2 (fume)
Spent IX Resin Immobilization
Phenolic Resin-SiO2 Nanocomposites
a
b
c
Cumulative leached fraction (F) of Cs+, Sr2+, Co2+, Ni2+ -saturated resin-composites

## Slide 20
HNO3/NaNO3 1M
HNO3/NaNO3 1M
RII
HNO3 1M
HNO3 1M
NC-5: 70 % RII (300 oC), 27 % Resol, 3 % SiO2 (fume)
Spent IX Resin Immobilization
Resol-SiO2 Nanocomposites

## Slide 21
99 Million Years
Natural Analogues
Xing et al. - A mid-Cretaceous enantiornithine (Aves) hatchling preserved in Burmese amber with unusual plumage. Gondwana Research. 2017, 49, 264

## Slide 22
Zirconium Phosphonate Coordination Polymers for LN and AN Separations and Immobilization

## Slide 23
U
Pu
Np
European Reference Process
Chemical similarity of LN and AN elements makes their separation non-trivial
Glass
Am, Cm
LN
Am, Cm
FPs
Cs,Sr,I,Tc
LN
Cm
Am
PUREX
DIAMEX
SANEX
DIAMEX

## Slide 24
Preparation and Adsorption Properties of Zr(IV) – Poliphosphonates
Zr(IV)-based polyphosphonate MOFs are LN and AN selective & are highly insoluble
nZrOCl2.8H2O
NaOH
8 mol/L
+

Amorphous
Precipitate/gel
2.
+
Luca et al. Hydromet.. 2015, 154, 118-128
nZrOCl2.8H2O

nZrCl4
nZr(OPr)4
Poorly Crystalline
+
3.
Luca et al. Inorg. Chem. 2016, 55, 7928-7943
nZrOCl2.8H2O/
ZrCl4/,
NaOH/HNO3
+

1.
+
Veliscek et al. Sep. Pur. Technol. 2014, 129, 150-158
Amorphous
Precipitate/gel
Veliscek et al. MMM 2017, 252, 90-104
ANSTO

## Slide 25
3000 nm
Zr
Coordination Polymers for LN Separations
Chart: % Extraction
| Co | Sr | Cs | La | Ce | Pr | Nd | Gd | Dy | Ho | Th
 | 5.2511 | 3.918 | 19.435 | 14.6318 | 23.3476 | 28.0414 | 24.4288 | 40.9262 | 75.7019 | 75.1105 | 100
Zirconium Thorium Pyrophosphate
(ZrTh)P2O7 Cubic P a -3
800 – 1000 oC
Luca et al. Inorg. Chem. 2016, (in press)

## Slide 26
Chart: AC-19A2 con SL-23 (5 ppm)
| 0 | 4 | 8 | 12 | 16 | 20 | 36 | 52 | 68 | 84 | 100 | 116 | 132 | 148 | 164 | 180 | 196 | 212 | 228 | 244 | 260 | 276 | 292 | 308 | 324 | 340 | 356 | 372 | 388 | 404 | 420 | 436 | 452 | 468 | 484 | 500 | 516 | 532 | 548 | 564 | 580 | 596 | 612 | 628 | 644 | 660 | 676 | 692 | 800
Cs | 0 | 0.193 | 1.902 | 4.663 | 6.03 | 6.66 | 7.494 | 7.596 | 7.922 | 7.138 | 6.736 | 7.207 | 6.97 | 7.234 | 6.546 | 6.715 | 6.672 | 6.947 | 6.569 | 6.802 | 6.856 | 6.571 | 6.674 | 6.287 | 6.929 | 6.667 | 6.542 | 6.376 | 6.687 | 6.242 | 6.828 | 7.051 | 7.045 | 6.786 | 6.146 | 6.832 | 6.609 | 6.574 | 6.417 | 6.518 | 6.477 | 6.452 | 6.392 | 6.833 | 6.352 | 6.466 | 6.305 | 6.383 | 6.1937
Sr | 0 | 0.022 | 0.444 | 1.014 | 1.757 | 2.74 | 4.711 | 5.309 | 4.876 | 5.12 | 4.871 | 5.241 | 5.256 | 4.863 | 4.65 | 5.151 | 4.857 | 4.793 | 4.842 | 5.125 | 4.836 | 4.636 | 4.817 | 4.92 | 4.729 | 5.16 | 4.794 | 4.907 | 4.745 | 4.482 | 5.061 | 5.108 | 5.044 | 4.933 | 4.865 | 4.894 | 5.051 | 4.719 | 4.593 | 4.926 | 5.056 | 4.652 | 4.932 | 4.841 | 4.633 | 4.884 | 4.831 | 4.772 | 4.7255
La | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.174 | 0.488 | 0.78 | 1.301 | 2.082 | 2.647 | 3.547 | 4.19 | 4.836 | 5.364 | 5.797 | 6.353 | 6.457 | 6.609 | 6.759 | 6.799 | 7.027 | 6.887 | 6.879 | 6.865 | 6.638 | 7.009 | 7.118 | 7.318 | 6.947 | 6.77 | 6.957 | 6.976 | 6.994 | 6.773 | 6.867 | 6.771 | 6.673 | 6.86 | 6.892 | 6.654 | 6.852 | 7.186 | 6.763 | 6.634
Ce | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.119 | 0.264 | 0.472 | 0.732 | 1.171 | 1.516 | 2.068 | 2.49 | 3.143 | 3.388 | 4.001 | 4.245 | 4.534 | 4.741 | 4.893 | 4.881 | 5.375 | 5.221 | 5.44 | 5.227 | 5.184 | 5.71 | 5.87 | 5.724 | 5.601 | 5.423 | 5.642 | 5.58 | 5.661 | 5.631 | 5.673 | 5.65 | 5.626 | 5.524 | 5.717 | 5.504 | 5.65 | 5.565 | 5.454 | 5.5225
Pr | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.094 | 0.333 | 0.515 | 0.819 | 1.128 | 1.543 | 1.853 | 2.322 | 2.639 | 3.025 | 3.307 | 3.651 | 3.818 | 3.973 | 4.007 | 4.403 | 4.329 | 4.448 | 4.425 | 4.242 | 4.779 | 4.736 | 4.529 | 4.646 | 4.673 | 4.813 | 4.646 | 4.872 | 4.775 | 4.862 | 4.893 | 4.736 | 4.828 | 4.893 | 4.78 | 4.937 | 4.728 | 4.868 | 4.693
Nd | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.073 | 0.343 | 0.515 | 0.82 | 1.07 | 1.623 | 1.917 | 2.439 | 2.596 | 3.042 | 3.435 | 3.648 | 3.819 | 4.004 | 4.359 | 4.486 | 4.307 | 4.518 | 4.648 | 4.436 | 4.887 | 4.866 | 4.439 | 4.709 | 4.686 | 5.006 | 4.879 | 5.073 | 4.878 | 5.034 | 4.971 | 4.891 | 5.078 | 5.138 | 5 | 5.16 | 4.809 | 5.077 | 4.9793
Gd | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.018 | 0.038 | 0.161 | 0.256 | 0.464 | 0.585 | 0.813 | 0.949 | 1.273 | 1.304 | 1.746 | 1.903 | 2.152 | 2.333 | 2.522 | 2.611 | 2.825 | 2.765 | 3.075 | 3.147 | 3.146 | 3.503 | 3.29 | 3.163 | 3.358 | 3.477 | 3.781 | 3.71 | 3.62 | 3.834 | 3.806 | 3.898 | 3.811 | 3.934 | 3.994 | 3.911 | 4.056 | 3.897 | 4.047 | 4.1457
Dy | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.041 | 0.061 | 0.163 | 0.3 | 0.342 | 0.558 | 0.824 | 0.947 | 1.273 | 1.415 | 1.631 | 1.825 | 2.075 | 2.263 | 2.431 | 2.555 | 2.866 | 2.815 | 3.036 | 2.912 | 3.01 | 3.365 | 3.465 | 3.408 | 3.443 | 3.476 | 3.546 | 3.626 | 3.697 | 3.746 | 3.846 | 3.882 | 3.785 | 3.814 | 3.882 | 3.758 | 3.854 | 3.975 | 3.862 | 4.227
Ho | 0 | 0 | 0 | 0.029 | 0 | 0 | 0.021 | 0.027 | 0.049 | 0.084 | 0.158 | 0.239 | 0.382 | 0.533 | 0.753 | 0.991 | 1.228 | 1.516 | 1.873 | 2.004 | 2.216 | 2.433 | 2.599 | 2.809 | 3.005 | 3.254 | 3.475 | 3.421 | 3.398 | 3.342 | 3.69 | 4.183 | 4.144 | 3.954 | 3.951 | 3.912 | 4.037 | 4.191 | 4.055 | 4.142 | 4.201 | 4.013 | 4.227 | 4.299 | 4.15 | 4.284 | 4.347 | 4.248 | 4.5962
Co | 0 | 0.072 | 0.495 | 1.096 | 1.85 | 2.769 | 4.748 | 5.184 | 5.389 | 5.367 | 5.255 | 5.405 | 5.459 | 5.304 | 5.151 | 5.335 | 5.259 | 5.209 | 5.123 | 5.226 | 5.3 | 5.231 | 5.152 | 5.053 | 5.208 | 5.317 | 5.186 | 5.176 | 5.229 | 4.906 | 5.347 | 5.296 | 5.155 | 5.129 | 4.983 | 5.204 | 5.16 | 5.133 | 5.063 | 5.17 | 5.127 | 5.104 | 5.014 | 5.199 | 5.014 | 5.092 | 5.094 | 4.987 | 5.105
Th | 0 | 0 | 0 | 0 | 0 | 0.018 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0.03 | 0 | 0 | 0 | 0.043 | 0.017 | 0 | 0.04 | 0.043 | 0.024 | 0.019 | 0 | 0.034 | 0.031 | 0.059 | 0.042 | 0.079 | 0.054 | 0.054 | 0.071 | 0.085 | 0.111 | 4.478
900 oC/air
900 oC/N2
Th0.049La0.013Ce0.015Pr0.015Nd0.015Gd0.013Dy0.015Ho0.014Sr0.025Zr0.84P1.84O6.56
Th0.058La0.009Ce0.009Pr0.012Nd0.012Gd0.009Dy0.012Ho0.011Sr0.033Zr0.83O1.93
No Detectable leachable!!

## Slide 27
Zr-ATMP Coordination Polymer
nZrOCl2.8H2O/
ZrCl4/,
NaOH/HNO3
+

1.
+
Amorphous
Precipitate/gel
Radiation Stability of Zr(IV)-polyphosphonate Coordination Polymer Hybrids

## Slide 28
Gd
Lu
Ce
Eu
ATMP-Zr (coordination polymer)
Notes: Each element present at about 1 ppm

## Slide 29
Gd
U
Th
Lu
ATMP-Zr (coordination polymer)

## Slide 30
ATMP-Zr (coordination polymer)
31P MAS NMR

## Slide 31
Cleaner 99Mo Production Methods
99Mo accounts for 30 million diagnostic procedures annually

## Slide 32
- High specific activity (Ci/g)
- Simple & convenient
- No waste!
- Low specific activity
(2 vs 10.000 Ci/g).
- Needs 98Mo.
- Needs targets enriched in 235U.
- Processing complex.
- Generates radwaste.
Advantages
Disadvantages
Mo-99 Production Methods

## Slide 33
3. Radioisotopes for health
99Tc is a derivative of 99Mo which is the most utilized radioisotope in nuclear medicine and is used for the detection of disease and thus contributes to the saving of lives. Globally more than 80.000 procedures utilizing this isotope are undertaken per day. In our country more than 2 million patients are processed per year. The increase in the production of 99Mo will enable Argentina to satisfy the national requires and also help to satisfy an increasing international demand (about 10% of global production). This will enable us to consolidate our leadership position in the provision of radioisotopes for medical applications.
1. Structural necessities
2. Nuclear technology for national development
Objetives
RA-10 Project
https://www.youtube.com/watch?v=qe1jYmStc_4
Notes: Fabbri - Proyecto RA-10.pdf
https://www.cab.cnea.gov.ar/index.php/proyecto-ra-10/61-espanol/proyectos/ra-10/278-objetivos-y-metas
http://www.cnea.gov.ar/RA10-objetivosymetas

## Slide 34
LLLW
1
2
ILLW
Al2O3 column
AG1-X8 column
Chelex columns
Boil-down & pH adjust
Mo-99
CST column
Mo stripped alkaline Na2SO4 soln
VIMo(SCN)43-/H2SO4
Wash H2SO4-KSCN, strip Mo with NaOH
Wash H2SO4-KSCN, strip Mo with NaOH
U-235 recycle
(U-238, Sr-90, LA3+…)
4 M NaOH, 0.4 M Al3+
I-131 retention
Xe-133
~
~
1
2
3
4
5
6
7
8
Simplified CNEA Process Flowsheet
Sameh & Ache, Radiochimica Acta 1987, 41, 65-72.
Notes: A. Sameh & H.J. Ache, Production Techniques of Fission Molybdenum-99, Radiochimica Acta 1987, 41, 65-72.

## Slide 35
Packed Alumina
Column 32 x 120 mm
Flow rate = 5 mL/min
Stage 1
Mo-99
Absorption
Primary
Liquid Waste
80% U Deportment
Secondary
Liquid Waste
Stage 6. Boil down
Ammonia-rich
Condensate
Stage 2. 1M HNO3 wash (800 mL)
Stage 3. Water wash
Stage 4. 0.01M Ammonia wash
Stage 5.
Strip 1M Ammonia
8M HNO3
Mo-99 Product
Bulk MgO
Dissolution
Sieving
Holding Tank
45 g Uranium Dioxide (UO2) 2.2% 235U
Magnesium Oxide (MgO)
8M Nitric Acid
( Minor MgO)
UO2 (Minor MgO)
`Rocket´ can
Irradiated 7 days
ANSTO Mo-99 Production
1965 - 2008
For 6 can run
Produce 850 mL of 1.1 M UO22+ in
0.75 M HNO3 + 12 ppm Mo + ~ 300 FPs
Stage 1. Load
Stage 7.
Purification
C1
C1
C1
C2
Stage 8. Boil down to
specified vol.
Notes: Five production runs per week totaling 675 Ci (25,000 GBq) at EOB. Simple acid-side process that served for 50 years that could be improved with better solid-extractants, i.e. to replace alumina.

## Slide 37
Uranium can be easily recovered from the filter cake using a variety of processes. For instance PUREX, UREX SX processes or using Extraction Chromatography.
TBP
Impregnación
XAD7
Wastestream 2: Filter cake of 235/238UO2.ZH2O
`PUREX in a Column´
Vaccaro et al., Argentina’s Efforts to Recover and Down-blend Irradiated HEU from Mo-99 Production Targets. RERTR 2016

## Slide 38
Target Fabrication
Irradiation
Improve process from
the head-end?
Improve
recovery step?
Traditional versus New Approaches
UAlx dispersion Target
Sublimation
or
Leaching
?
Recovery 235U
13.0 cm
3.5 cm
Dissolution
Recover 99Mo
Adsorption/IX
Acid
Alkaline
LLW/ILW
Nordion (Canada)
IRE (Belgica)
IPPE (Russia)
ANSTO (Australia)
CNEA (Argentina)
NECSA-NTP (S. Africa)
MALLINCKRODT (Holland)
500-1000 L/year ILLW

## Slide 39
Denis Levins et al.
ANSTO's Radioactive Waste Management Policy Preliminary Environmental Review
ANSTO/E728
May 1996
“The present method of molybdenum-99 production should be reassessed from a cleaner production viewpoint. This will involve consideration of modifications to the process to eliminate ammonium salts in the waste and, more radically, assessment of alternative technologies with the aim of reducing liquid waste volumes and/or activities.”
Green Chemistry is the area of chemistry and chemical engineering that focuses on the design of processes that minimize the generation of toxic substances.
Today it is not good enough to just have a process. We need to have the cleanest possible process!

## Slide 40
Methods and apparatus for selective gaseous extraction of molybdenum-99 and other fission product radioisotopes
WO 2011156446A2 filed 8-Jun-2011
WO 2011156446A3
General Atomics
MoO2Cl2
CONCLUSION
The choice of a particular scheme for the production of 99Mo is, as a rule, Primarily governed by availability of the equipment and raw materials. Traditional “wet” processes for the production of fission molybdenum are successfully used up to now. At the same time, the major problem in this field is the utilization of radioactive wastes. Ultimately, waste management may be the most expensive part of any process scheme, taking into account the modern attitude to environmental problems. In this context we believe sublimation procedures to be the most promising for the future, since these procedures yield a high-purity product with minimal wastes.
Methods for Production of 99Mo (Review)
M.P. Zykov* and G.E. Kodina**
* Khlopin Radium Institute, Research and Production Association, St. Petersburb, Russia
** Institute of Biophysics, Russian Academoy of Sciences, Moscow, Russia
Received May 14 1998
Radiochemistry 1999, 41 (3), 193-204

## Slide 41
Kurze Originalmitteilungen
On the Sublimation of 99mTc from Irradiated Molybdenum Trioxide
E. Hallaba, H.A. El-Asray
Environmental Health Studies 1975, 11, 290
99Mo or 99mTc by Sublimation
Zsinka 99mTc Sublimation Generators Radiochimica Acta 41, 91-96 (1987)

## Slide 42
Porous microsphers (500-1000 mm) of ZrCx, SiC, MAX, UCx..
Pore dimaeters 10-100 nm.
400 mm
Actual Microsphere
235U
99Mo
FP
n
Hypothetical Target Parameters
55.0 mm
11 .0 mm
Al or Zr irradiation can (500-800 mm)
Loading of pores with between 0 y 100% UO2, UCx or other
Free space for fission gases
Maximum packing
V ~ 7.3 cm3 x 0.75 ~ 5.475
But microspheres are 50% porous  5.475 * 0.5 ~ 2.74 cm3
Neutron flux
1– 10x1013 ncm-2s-1
n
Van Til, Sphere Irradiation (JRC-IET)
Notes: Van Til - SPHERE irradiation

## Slide 43
235U
n
99Mo
FP
Nanocrystals
Nanopore
Elm et al. ACS Appl. Mater. Inter. 2015, 7, 11792.
R  n  
R = reaction rate
n = no. target nuclei
 = neutron flux
= cross section (600 barns)
37 barns (99Mo) 6.1 %
n
High Resolution SEM of Mesoporous Y-stabilized ZrO2

## Slide 44
11 .0 mm
55.0 mm
f = 1.75-3.5 x 1013 n cm-2 s-1
Flux
U density
Thermo-hydraulic Modeling with Dionisio
Soba & Denis, J. Nucl. Mater. 2008, 374, 32-43

## Slide 45
Microspherical Materials Through Ion Exchange and Polymer Templating
[Zr4(OH)8(H2O)16Cl6]2+
1100 oC/air
Gel-IER
1100 oC/N2
SBET  0 m2/g
SBET ~600 m2/g
Macroporous IER
1350 oC/Ar
Scales et al., MMM 2017, (in press)

## Slide 46
Nitriding ZrO2 using N2-H2(5%)
ZrN + O2 → ZrO2 + 1/2N2
ZrC + O2 → ZrO2 + 1/2CO2
Polyzirconoxane
+
∆
1350 oC
N2-H2 (5%)
Synthesis of Porous Zirconium Oxycarbonitride Micospheres

## Slide 47
Sr
Cs
U
Mo
ZrHC-1
Mo
U
Sr
Cs
Strip Cs+, Sr2+ and UO22+ using mildly acid solution 2 < pH < 3.
Extract MoO4- using mildly alkaline solution pH > 11.
Load uranium as UO22+ at 3 < pH < 11.
Cycle | Ads (%) | Des (%)
1 | > 99 | 86
2 | > 99 | 91
3 | > 99 | 96
4 | > 99 | 83
0.025 mmol/L
ZrC-Carbon Composite Microspheres
Scales et al. MMM 2015, 212, 100-109

## Slide 48
ZrC
G
ZrOCN
96%
ZrOCN
Nano- graphite
ZrOCN-Carbon Composite Microspheres
Notes: ZrC = LD27-20J. Surfaces would need to be functionalized to impart actinide selectivity.

## Slide 49
Ce
98Mo
238U
Experiments in Progress
Ce-143
Ce-141
Pr-143
Carbon
ZrC
ZrOCN
ZrO2
Al2O3
SnO2
UO2
…

## Slide 50
ZrC
ZrO2
Oxidation of Nanocrystalline Zirconium Carbides
+
2O2
CO2
+

## Slide 51
Radiation Response of Nanoporous Materials
If nanoporous/nanostructured materials are going to be use in high radiation fields then:
How do they respond to different kinds of radiation?
Can we use them as targets for the production of fission 99Mo?
Notes: Next generation of nuclear systems will need materials that are stable in extreme environments!
Motivations: (1) to see how nanomaterials respond to radiation, (2) to apply advanced materials as targets.

## Slide 52
Radiation Response of Mesoporous Silicate and Borosilicate Thin Films
meso-Ti0.66Zr0.33O2
Glass
2D Hexagonal
3D Hexagonal
Dourdain et al. J. Nucl. Mater. 2012, 427, 411
First studies of radiation damage of nanoporous silicates
92 MeV Xe+ 1x1014 cm-2
Silicon substrate
q
q
Position of main reflection → cell dimension
Intensity → contrast & order
60-100 nm

## Slide 53
n
B
4He2+
7Li3+
Si
O
10B + 1n  7Li + 4He (2.8 MeV) + g (478 KeV) RA3 Ezeiza
Radiation Response of Mesoporous Silicate and Borosilicate Thin Films

## Slide 54
10B + 1n  7Li + 4He (2.8 MeV) + g (478 KeV) RA3 Ezeiza
d-spacing is maximum for B content of 5 % and then decreases again.
The d-spacing contracts as a function of irradation time for given B content.
Area of main reflection is relatively unaltered as a function of irradiation time for given B content.
Chart: mol % B
| 0 | 2 | 5 | 7 | 10 | 20 | 30 | 40 | 50
1 | 38.141 | 36.3454 | 37.1377 | 36.9011 | 35.9562 | 35.701 | 35.7347 | 37.3068 | 39.4397
35 | 37.5263 | 33.91 | 36.3346 | 35.7166 | 35.0276 | 34.1014 | 33.462 | 34.8189 | 36.3057
200 | 37.0986 | 33.0549 | 35.5952 | 34.7639 | 34.0316 | 32.7419 | 32.7424 | 33.556 | 35.5424
400 | 37.1566 | 33.3082 | 35.7695 | 35.6243 | 34.7629 | 32.7513 | 32.7732 | 33.5534 | 35.9487
Chart: mol % B
| 0 | 2 | 5 | 7 | 10 | 20 | 30 | 40 | 50
not irrad | 37.1566 | 33.3082 | 35.7695 | 35.6243 | 34.7629 | 32.7513 | 32.7732 | 33.5534 | 35.9487
irrad 2 d | 36.7673 | 33.187 | 35.4759 | 33.799 | 33.6428 | 32.4397 | 31.6065 | 33.4315 | 34.458
irrad 30 d | 35.7423 | 31.5489 | 34.2029 | 32.8441 | 31.1646 | 31.162 | 28.891 | 30.5915 | 31.7388
Radiation Response of Mesoporous Silicate and Borosilicate Thin Films
Manzini et al. NIM B 2017, (in press)

## Slide 55
70 MeV
180 keV
Iodine Ion Irradiations of Mesoporous Silicate and Borosilicate Thin Films
TANDAR accelerator

## Slide 56
70 MeV, 1014 cm-2
Poca diferencia en los parámetros de la celda cristalina luego de irradiar a 70 MeV (0.002 dpa) 132 keV (1.73 dpa).
132 keV, 1014 cm-2
70 MeV, 1014 cm-2
No irradiado
Manzini et al. J. Nucl. Mater. 2016, 482, 175
0.002 dpa
1.73 dpa
Radiation Response of Mesoporous and Nanocrystalline Zirconium Oxide Thin Films

## Slide 57
Radiation Tolerance of Mesoporous Nanocrystalline Zirconia
Ce0.10Zr0.90O2
82 dpa
180 keV, 1016 cm-2
82 dpa

## Slide 58
180 keV, 1016 cm-2
82 dpa
200 nm
200 nm
BCZ-350
BCZ-350i
Radiation Tolerance of Mesoporous Nanocrystalline Zirconia

## Slide 59
Main Conclusions
A capability for conducting novel research relevant to the back-end of the nuclear fuel cycle has been established.
Scientific underpinnings have been established for a new low-temperature pyrolysis process for the treatment of spent IX resins that generates highly stable pyropolymers.
New LN and AN selective Zr(IV)-coordination polymers have been developed that lend themselves to facile end-of-life management (cradle-to-grave).
Strategy has been developed for the development for the cleaner production 99Mo from the fission of LEU.
Provided first insights into the radiation response of mesoporous nanocrystalline zirconia and LN-zirconia thin films.

## Slide 60
Direct Containerization in High Integrity Container
Cast from lead
Lined with iron for mechanical strength
Presently used for storing Co-60 (1900 Ci)
30 of the Cs-CST columns have 750 Ci 137Cs
Conditioning of Spent CST Columns - Direct Containerization

## Slide 61
137CsNaTi2SiO7.H2O
In-Situ Immobilization/Conditioning of CST
Phenolic Resin

## Slide 62
a
b
c
1
2
4
3
Nb
Cs
Zr
Ti
Na
Ni
Mn
Fe
C
Cr
Si
200 mm