## Slide 1: Synthesis and Structure of Novel Oxide Compounds Containing RE = Y, Yb, Gd, Sm, and La and M = Zr, Ti, and Sn
R. Newman,1 R.D., Aughterson,2 G.R. Lumpkin3*
1Imperial College, London, UK; 2Nuclear Materials Development and Characterisation, ANSTO-NSTLI; 3Nuclear Fuel Cycle Research, ANSTO-NSTLI

## Slide 2: Introduction
Developmental work following earlier period of research by Russian workers, e.g., Shepelev and Petrova (2008)
Lau et al. (2007, 2008) and Whittle et al. (2011) studied structure of Ho2TiO5 and Y2TiO5 in some detail (radiation effects from Whittle et al.)
Aughterson et al. (2014-2017) focussed on synthesis, structure, radiation effects, and some properties for the RE2TiO5 series and certain solid-solutions
Tracy et al. (2012), Zhang et al. (2013), swift heavy ions, tracks, etc.
Our interest is mainly in finding new candidate materials for IMFs and waste forms, with REE flexibility and radiation tolerance
Possible phase relations in the RE2TiO5 system after Shepelev and Petrova (2008). O = orthorhombic, H = hexagonal, and C = cubic structures

## Slide 3: Summary of Structure Types
Aughterson et al. (2014) J. Solid State Chem. 213, 182-192; Aughterson et al. (2015) J. Solid State Chem. 227, 60-67

## Slide 4: Order-Disorder Observed by TEM
Hexagonal Sm1.6Yb0.4TiO5
Trigonal bipyramid: 60% Ti, 20% Ln, and 20% vacancies
Disorder (dynamic?)
3{111}* & 7{662}* GF ± ½{111}* More diffuse
[001]
[-120]
Cubic Phases
From Y/Ho to Yb
Cation/anion disorder
Modulated structure
Aughterson et al. (2014) J. Solid State Chem. 213, 182-192

## Slide 5: Synthesis of Materials
Bulk polycrystalline samples were synthesized in the conventional oxide route
Milled with 12 mm ZrO2 balls using organic solvents
Pellets were consolidated by 20 MPa uniaxial pressing followed by cold isostatic pressing at 250 MPa
Calcined and then sintered at 1500 °C for 48 hours
Gd2TiO5
Yb2SnO5
Yb2O3

## Slide 6: XRD Results
Target pyrochlore Gd2Sn2O7 ✓
Target (unknown) Gd2SnO5 ✗
Target (unknown) Gd2(SnxTi1-x)O5 ✗
Target orthorhombic Gd2TiO5 ✓
Target defect fluorite Sm2ZrO5 ✓
Target (unknown) Yb2Sn1+xO5+2x
Defect flourite Yb2SnO5 ✗
Defect flourite Yb2Sn1.125O5.25 ✓
Defect flourite Yb2Sn1.25O5.5 ✓
Defect flourite Yb2Sn1.375O5.75 ✓

## Slide 7: TEM Analysis - Nanostructure
HRTEM image of Sm2ZrO5 taken with the JEOL 2200 fs in NMDC at ANSTO
FFT obtained from (a) showing a [110] type zone axis orientation
Inverse FFT obtained from a fluorite (F) subcell diffracted beam in (b).
Inverse FFT obtained from a pyrochlore (P) type modulated beam in (b), showing a “domain” structure on the scale of 2-5 nm.

## Slide 8: Electron Diffraction
[111] Zone Defect flourite Yb2Sn1.125O5.25 [131] Zone
Defect flourite Yb2TO5
[111]
[110]
[131]
Withers (2015) IUCrJ 2, 74-84.

## Slide 9: Radiation Damage Effects
Pellets irradiated at CAS at ANSTO using ANTARES
15 MeV Au ions @ fluences of 1, 2, 5, and 7.5 × 1014 ions cm-2
Previous unpublished work from the IVEM-Tandem at ANL (1 MeV Kr)
GIXRD conducted at NMDC at ANSTO with incident angles of 3 and 5°
Remains crystalline to
7.5 × 1014 ions cm-2
IVEM, no amorphization at 50 K
Sm2ZrO5
Yb2Sn1.25O5.5
Yb2TiO5
Remains crystalline to
7.5 × 1014 ions cm-2
No IVEM data are available
Possibly amorphous*
2 × 1014 ions cm-2
IVEM, Tc = 479 K

## Slide 10: Summary & Conclusions
We conducted an exploratory study of RE2M1+xO5+2x compounds with RE = La, Gd, Sm, and Yb and M = Ti, Zr, and Sn with partial success
New single phase samples were obtained for Sm2ZrO5 and Yb2Sn1+xO5+2x compositions, basic structures determined by XRD, and complex scattering effects studied by TEM
Initial ion irradiations indicate that Sm2ZrO5 and Yb2Sn1.25O5.5 (and possibly other Yb2Sn1+xO5+2x compositions) are radiation tolerant, unlike Yb2TiO5 and other cubic, defect fluorite type Re2TiO5 compounds
Thanks to Mihail Ionescu for arranging the ion irradiations in the CAS at ANSTO. We acknowledge Pete Baldo and Ed Ryan for assistance on the IVEM-Tandem at ANL.