## Slide 1
Ambient-Cured Geopolymers for Nuclear Waste Storage
Isadora de Borba Busch
Supphatuch Ukritnukun, Pramod Koshy, Charles C. Sorrell
School of Materials Science and Engineering, UNSW Sydney
Daniel Gregg, Eric Lou Vance, Gerry Triani
ANSTO

## Slide 2: Outline
Introduction and Background
  Nuclear Waste Categories
  Geopolymers
  Current Technologies
Experimental Plan
Results and Discussion
Conclusions and Future Work
2

## Slide 3
Introduction & Background

## Slide 4: Nuclear Waste Categories - 1
4
  OPC is currently being used for LLW storage
  Geopolymers is the potential candidate for ILW storage
Image reference: IAEA, Classification of Radioactive Waste
Schematic of super-compaction process for LLW/ILW immobilisation
Notes: Co2 emission from cement production incurred through the consumption of fossil fuel, use of electricity and chemical decomposition of lime stone during clinkerisation

## Slide 5
2(3CaO•SiO2) + 6H2O 3CaO•2SiO2•3H2O + 3Ca(OH)2
C-S-H is contributed for compressive strength
IRRADIATION  WATER DISSOCIATION  H2
5
Calcium Silicate Hydrate (C-S-H)
Mn (– (SiO2)z – AlO2)n, wH2O
Nuclear Waste Categories - 2
Ordinary Portland cement (OPC):
Geopolymers :
Lower water content than OPC
2 types of water:
Bound and Unbound
Can be dehydrated without losing its properties
Na2O – Al2O3 – SiO2 – H2O : N-A-S-H
CaO – Al2O3 – SiO2 – H2O : C-A-S-H
Na2O – CaO – Al2O3 – SiO2 – H2O : N-(C)-A-S-H
Source: Development of Geopolymers for Nuclear Waste Immobilisation - ANSTO
Notes: Co2 emission from cement production incurred through the consumption of fossil fuel, use of electricity and chemical decomposition of lime stone during clinkerisation

## Slide 6
6
Utilisation of industrial by-product
40-90% reduction in CO2 emission
Improved compressive and tensile strength
Improved resistance to fire and aggressive acids
Aluminosilicate Materials (FA, GGBFS, MK)
+
Alkaline Activators (NaOH, Na2SiO3)
+
Aggregates
+
H2O
Curing at 25°C or (40° – 80°C)
Geopolymers – General
GGBFS
Geopolymer
Mortar
FA
Aggregates
Alkaline
Activators
H2O
Image source accessed on 27/10/2017: https://theconstructor.org/concrete/geopolymer-concrete-ecofriendly-construction-material/9430/

## Slide 7
7
Compilation of >20 studies (Na-based system)
Majority of the work utilised high temperature curing in order to achieve > 35 MPa
Fly ash and metakaolin based geopolymer generally requires high temperature curing
Geopolymers – Current Technologies
UNSW – Mix Design
Increase applicability for industry (cured at 25°C)
Reproducible mix design
High compressive strength
Appropriate setting time
Appropriate workability

## Slide 8
UNSW – ANSTO Joint Project
Experimental Plan

## Slide 9: Experimental Plan
9

## Slide 10: Experimental Plan
Materials | ID | Binder | Alkaline Activator | Aggregates | Curing Condition (Temp / Time)
UNSW – Paste | UNSW – GP | FA + GGBFS | NaOH + Na2SiO3 | - | 25°C / 50d
UNSW – Mortar | UNSW – GM | FA + GGBFS | NaOH + Na2SiO3 | Fine | 25°C / 28d
ANSTO – Paste | ANSTO – GP | MK | Not Provided | - | 60°C / 48h
Rocla – Concrete | Rocla – GC | FA + GGBFS | NaOH + Na2SiO3 | Fine + Coarse | 80°C / N/A

## Slide 11
Results &
Discussion

## Slide 12: XRF - Chemical Analysis
13
Oxide | UNSW – GP (wt%) | UNSW – GM (wt%) | ANSTO – GP (wt%) | Rocla – GC (wt%)
SiO2 | 42.72 | 65.04 | 47.49 | 69.80
Al2O3 | 12.91 | 6.94 | 18.79 | 12.10
CaO | 11.16 | 7.16 | 0.02 | 4.90
Fe2O3 | 0.00 | 0.76 | 0.32 | 2.80
Na2O | 6.46 | 3.13 | 12.67 | 5.70
K2O | 0.97 | 0.64 | 0.14 | 2.60
MgO | 1.67 | 0.93 | 0.03 | 0.70
TiO2 | 0.55 | 0.32 | 0.34 | 0.60
P2O5 | 0.05 | 0.03 | 0.00 | 0.00
SO3 | 0.33 | 0.17 | 0.00 | 0.40
Mn3O4 | 1.22 | 0.09 | 0.00 | 0.10
SrO | 0.04 | 0.03 | 0.00 | 0.00
ZrO2 | 0.03 | 0.04 | 0.00 | 0.00
LOI | 22.26 | 14.31 | 20.20 | 0.30
Molar Si/Al | 2.84 | 7.71 | 2.14 | 4.90
Molar Na/Al | 0.83 | 0.72 | 1.11 | 0.77

## Slide 13: Compressive Strength
14
Chart: Compressive Strength (MPa)
| UNSW - GP | UNSW - GM | ANSTO - GP | Rocla - GC
 | 104.1 | 104.8 | 56.9 | 49.6
Ambient Curing
AS 3972 - 2010
28 days (minimum)

## Slide 14: Mineralogy
15
Geopolymer
network
Sand
+Ca
-Ca

## Slide 15: Microstructural Analysis
UNSW - GP
UNSW – GM
16
ANSTO – GP
Rocla – GC
Sand
N-(C)-A-S-H
Rock
Sand
N-A-S-H
N-(C)-A-S-H
N-(C)-A-S-H
Unreacted
Slag
Unreacted
FA

## Slide 16: Leaching Test
17
 | OPC | UNSW - GP | UNSW - GM | ANSTO - MK
Na | ~8-9 | 8.6 | 8.7 | 7.7
Al | - | 12.4 | 13.1 | 13.8
OPC PCT has values for Na of > 30 g/L (ie >30 % loss).
ANSTO – MK has PCT values of ~20g/L (ie 20% loss to the leach solution).
UNSW PTC results were not available in time for this presentation.
Preliminary data – ANS test

## Slide 17
Conclusions &
Future Work

## Slide 18: Conclusions
19
New high-strength geopolymers that were cured in ambient temperature have been developed.
UNSW mix design showed better properties than OPC.
Sample irradiated for 15 days did not show any visible damage.
Ambient-cured geopolymers are a potentially interesting OPC substitute for LLW/ILW storage.
Future Work
Retrieve the samples after 1, 3, 6, and 12 months of irradiation.
Analyze the extent of deterioration after irradiation.
Evaluate the potential of using ambient-cured geopolymers for ILW storage.

## Slide 19
Thank you!