## Slide 1: Synthesis and Characterisation of Glass-Ln2Ti2O7 Pyrochlore
Linggen Kong, Yingjie Zhang, Inna Karatchevtseva
ANSTO
MRS2017 Sydney

## Slide 2: Aim of this work
Develop a method to produce glass-Ln2Ti2O7 pyrochlore
Investigate the processing conditions

## Slide 3: Reaction scheme flow chart
Glass powder: Na2AlBSi6O16 heated at 550oC

## Slide 4: Confirmation of pyrochlore internal crystallization
(GdTi)-complex powders calcined for 4 h at (a) 450◦C,(b) 550◦C, (c) 650◦C, (d) 700◦C, (e) 750◦C, (f) 800◦C
A: anatase TiO2, G: Gd2O3,
P: Gd2Ti2O7 pyrochlore
GC50:50 pellets sintered at 1200◦C for 6 h using the mixture of corresponding powders and the glass precursor powder.

## Slide 5: GC weight ratio effect (glass-Y2Ti2O7)
This method
Using oxides
1200◦C
6 h
1200◦C
6 h

## Slide 6: SEM glass-Y2Ti2O7
(a) 50:50 (b) 40:60 (c) 30:70 (d) 20:80 (e) 10:90
(f) 0:100
1200◦C, 6 h

## Slide 7: XRD
Samples were sintered at 1200◦C for 6 h.
Gd2Ti2O7, (b) Tb2Ti2O7, (c) Er2Ti2O7, (d) Yb2Ti2O7, (e) pure glass.
R: rutile TiO2, P: Ln2Ti2O7 pyrochlore.

## Slide 8: SEM of glass-Ln2Ti2O7
(a) Gd2Ti2O7 (b) Tb2Ti2O7 (c) Er2Ti2O7 (d) Yb2Ti2O7
1200◦C
6 h

## Slide 9: Raman
Samples were sintered at 1200◦C for 6 h.
Gd2Ti2O7, (b) Tb2Ti2O7, (c) Er2Ti2O7, (d) Yb2Ti2O7, (e) pure glass.
R: rutile TiO2, A: anatase TiO2, P: Ln2Ti2O7 pyrochlore.

## Slide 10: Conclusion
A new method was developed to produce glass-Ln2Ti2O7 pyrochlore at 1200oC sintering.
Ln2Ti2O7 pyrochlore was internally crystallized in glass.
Pyrochlore was uniformly distributed in glass matrix.
High ceramic to glass weight ratio led to some impurities.

## Slide 11: ?