## Slide 1: Modelling the Corrosion of Spent Nuclear Fuel Inside a Failed Waste Container Fuel Inside a Failed Waste Container
Nazhen Liu, Ziyan Zhu, Linda Wu, Zack Qin, David Shoesmith
Department of Chemistry and Surface Science Western
The University of Western Ontario
London, ON, Canada
This project is funded under a Collaborative Research and Development agreement between NSERC and the Nuclear Waste Management Organization

## Slide 2: OUTLINE
Canadian disposal scenario
Redox conditions inside a failed nuclear waste container
A few key fuel properties
A one dimensional model for fuel corrosion
The need for a two dimensional model
The influence of H2 from alpha radiolysis and steel corrosion
How much H2 is required to completely suppress fuel corrosion?
Can the model be validated ?

## Slide 3: The Canadian Scenario for the Disposal of High Level Nuclear Waste (Used Nuclear Fuel)
~2.5 m
~0.57 m
Cu-coated carbon steel container
Electrodeposited
Cold spray
Notes: I can say that this is potentially the most dangerous failure mode (and that’s why NWMO is investing in researching this)
The motivation behind my research is ensuring the safe long-term management used nuclear fuel. Canada’s proposed long term management method involves placing used fuel bundles in a copper-coated carbon steel container (the Cu coating being either electrodeposited or cold spray), (sealing the containers), and placing them ~500 m below ground in a deep geological repository. In the repository, the containers will eventually come into contact with groundwater and can begin to corrode. This is where my research comes in.
These containers are the primary engineered barrier within the multi-barrier system proposed for the permanent disposal of spent nuclear fuel.

## Slide 4
Redox Conditions Inside a Failed Container
Large redox gradient exists within the container

## Slide 5: The Key Fuel (UO2) Properties which influence its reactivity
In-reactor Fission
Small grains
Residual grain boundary porosity
Grain boundary tunnels
Grain boundary fission bubbles
Rare earth-doped large grains
Noble metal (Ru, Pd, Mo) particles
Residual non-stoichiometry in grain boundaries
In-reactor irradiation produces a network of noble metal particles (potential cathodes?) within a conductive, oxidizable UO2 matrix (reactive anode?)

## Slide 6
X-ray photoelectron spectroscopy used to determine surface composition
Atomic Force Microscopy (AFM) used to detect corrosion damage
MicroRaman spectroscopy used to determine the influence of doping on the UO2 matrix
Current sensing AFM used to relate surface conductivity to composition
Scanning Electrochemical Microscopy (SECM) used to determine lateral variations in reactivity
Extensive Electrochemical/Spectroscopic/Microscopic Studies of Simulated Fuel Properties have been undertaken
Electrochemical methods used to study UO2 reactivity and the kinetics of oxidant reduction reactions
N. Liu et al: Corrosion of Nuclear Fuel Inside a Failed Waste Container; The Encyclopedia of Interfacial Chemistry: Surface Science and Electrochemistry

## Slide 7
Numerical simulations are applied by the commercially available modelling package, COMSOL Multiphysics based on finite element methods.
The diluted species transportation module is used
Diffusion-reaction equation at steady state
diffusion
reaction
One and Two-dimensional Models Developed for Fuel Dissolution/Radionuclide Release inside a Failed Container
Finite element mesh for a fuel fracture
Notes: The simple equations that model these finite elements are then assembled into a larger system of equations that models the entire problem.

## Slide 8
Reactions Inside a Failed Container
Groundwater

## Slide 9
Reactions Inside a Failed Container
Radiation zone
13 μm

## Slide 10
Reactions Inside a Failed Container

## Slide 11
Reactions Inside a Failed Container
ε

## Slide 12
Reactions inside a Failed Container

## Slide 13
Reactions Inside a Failed Container
F.J. Millero, and S. Sotolongo, Geochim. Cosmochim. Acta 53 (1989) 1867.
4

## Slide 14
The Key Reactions Controlling Fuel Corrosion/Dissolution Inside a Failed Container

## Slide 15
Cross section of used CANDU fuel pellets
Due to the fractured nature of the fuel a two dimensional model is required
Fractures allow groundwater access to the internal structure of a pellet

## Slide 16
H2O2, H2
H2O2, H2
H2O2, H2
Diffusion zone
Bulk solution
Radiation zone
Fe2+, H2
Fractured fuel pellet
Effect of Geometry
Bulk [H2]
Critical [H2]
    L. Wu, N. Liu, Z. Qin, and D.W. Shoesmith, J. Electrochem. Soc. 161(8) (2014) E3259-E3266.

## Slide 17
THE INFLUENCE OF HYDROGEN ON THE FUEL CORROSION PROCESS

## Slide 18
The Kinetics of Redox Controlling Reactions
Reactions involving H2
Alpha radiation dose rate
Production of H2 by both radiolysis and steel corrosion
Reaction of H2 with H2O2

## Slide 19
Corrosion Rate Inside a Crack
bulk solution
bulk [H2]
The critical [H2] is defined as the minimum bulk [H2] (from carbon steel corrosion) required to completely suppress fuel corrosion.
The Critical [H2]
As the bulk [H2] increases fuel dissolution becomes progressively more suppressed

## Slide 20
Factors Influencing the Critical [H2]
Crack geometry
The calculated critical [H2] in cracks with different widths and depths, with α dose rate = 9.03 × 105 Gy a−1.
There exists an upper limit (5.7 μmol L−1 indicated by the dashed line) for the critical [H2] for the anticipated range of possible crack geometries.
    L. Wu, N. Liu, Z. Qin, and D.W. Shoesmith, J. Electrochem. Soc. 161(8) (2014) E3259-E3266.

## Slide 21
Separation of Internal and External H2 Effects

## Slide 22
H2O2, H2
H2O2, H2
H2O2, H2
Diffusion zone
Bulk solution
Radiation zone
Fe2+, H2
Fractured fuel pellet
Separation of Internal and External H2 Effects
The effects of radiolytic (internal) H2 and H2 from steel corrosion are separated by calculating the ratio of their concentrations at specific locations

## Slide 23
Separation of Internal and External H2 Effects
600
500
400
300
200
100
0
nmol L-1
99
98
97
96
95
94
nmol L-1
Internal
[H2]
External
[H2]
Internal [H2] / nmol L-1
Distance to crack bottom / mm
Distance to crack bottom / mm
External [H2] / nmol L-1

## Slide 24
Separation of Internal and External H2 Effects
Fraction of internal H2 effect :
internal [H2]
internal [H2] + external [H2]
External [H2] / nmol L-1
Internal [H2] / nmol L-1
Distance to crack bottom / mm
Distance to crack bottom / mm
Distance to crack bottom / mm
Fraction of H2 Effect

## Slide 25
Separation of Internal and External H2 Effects
600
500
400
300
200
100
0
nmol L-1
Internal [H2] inside a crack
0.5 mm
1 mm
3 mm
6 mm
As the crack depth increases with a constant width,
there is an accumulation of radiolytic internal H2.

## Slide 26
Separation of Internal and External H2 Effects
Crack depth
As the fracture depth increases for a constant fracture width, the fraction of UO2 corrosion suppressed by internal H2 increases.
Fraction of H2 Effect
Distance to crack bottom / mm
Fraction of H2 Effect
Distance to crack bottom / mm
Fraction of H2 Effect
Distance to crack bottom / mm
Fraction of H2 Effect
Distance to crack bottom / mm
Bulk [H2] = 10 nM
Depth = 0.5 mm
Width = 0.6 mm
Bulk [H2] = 10 nM
Depth = 1 mm
Width = 0.6 mm
Bulk [H2] = 10 nM
Depth = 3 mm
Width = 0.6 mm
Bulk [H2] = 10 nM
Depth = 6 mm
Width = 0.6 mm

## Slide 27
Separation of Internal and External H2 Effects
900
800
700
600
500
400
300
200
100
0
nmol L-1
0.6 mm
0.3 mm
0.1 mm
Internal [H2] inside a crack
As the crack gets narrower with a constant depth,
there is an accumulation of radiolytic internal H2.

## Slide 28
Separation of Internal and External H2 Effects
Crack width
As the crack gets narrower with a constant fracture depth, the fraction of internal H2 effect on the suppression of UO2 corrosion increases.
Internal H2
External H2
Fraction of H2 Effect
Distance to crack bottom / mm
Liu et al. Roles of radiolytic and externally generated hydrogen …. Environ.Sci.Technol. 59, 12348 (2016)

## Slide 29
Can this Model be Validated by Comparison to Corrosion Rates Measured on Fuel Specimens?

## Slide 30
Corrosion rates of α-doped UO2. non-doped UO2 (0.01 MBq.g-1(UO2), SIMFUEL and some spent fuels
Linear least squares fit used by the Canadian Nuclear Waste Management Organization in safety assessments (A,B.C data not included)
Carbol et al. Swedish Nuclear Fuel and Waste Management Company Report SKB-TR-05-09 (2005)

## Slide 31
Model Reconfigured to Represent the Conditions in the Fuel Experiments

## Slide 32
Model calculation compared to the full measurement set
Model calculation compared only to the data measured on specimens similar to those used in compiling the model data base
Liu et al. Modelling the radiolytic corrosion of α-doped UO2 and spent nuclear fuel,
J.Nucl.Mater, 494, 87 (2017)
The dominant influence on fuel corrosion is the radiolytic dose rate

## Slide 33
On-going and Future Studies
Incorporation of more representative radiolysis model taking into account the alpha radiolysis of chloride containing groundwaters.
The consequences of H2O2 decomposition to produce the less reactive but also less readily scavenged O2
The consequences of corrosion product deposition within fuel fractures.
A more appropriate analysis of the distribution of radionuclides within the fuel.
Extension of the model to a full fuel bundle with different modes of failure.
Incorporate the he α-radiolysis –H2 effect
Modelling the Cigar Lake deposit to validate the model

## Slide 34
Acknowledgements
Michael Wu
This research is funded under the Industrial Research Chair agreement between the Canadian Natural Sciences and Engineering Research Council (NSERC) and NWMO (Nuclear Waste Management Organization), Canada.
Nazhen Liu
Zach Qin
Nazhen
Liu
Ziyan
Zhu
Zach
Qin

## Slide 35
Reactions Inside a Failed Container
    J.C. Wren, D.W. Shoesmith, and S. Sunder, J. Electrochem. Soc. 152 (2005) B470.
    S. Nilsson and M. Jonsson, J. Nucl. Mater. 372 (2008) 160.

## Slide 36: Effect of radiolytic H2
15 μm
15 μm
A. Traboulsi, J. Vandenborre, G. Blain, B. Humbert, J. Barbet, M. Fattahi, J. Phys. Chem. C 118 (2014) 1071-1080.
UO2
UO2
Solution
Solution
α
α
H2
H2
H2O2
H2O2
UO22+
Closed atmosphere
Open atmosphere
Published experiments show radiolytic H2 suppresses fuel corrosion
~ inside a deep crack
15 μm
15 μm

## Slide 37
The Kinetics of Redox Controlling Reactions
Reactions involving H2
Reaction 3 (c)has been shown to be independent of [H2] down to [H2] = 1.17 x 10-3M. This is unlikely to be the case at the lower concentrations anticipated.

## Slide 38
Kinetics of redox reactions involving H2
We assume the reaction will eventually become first order in [H2]
Three kinetic scenarios
Reaction becomes first order for [H2] < 1.17 x 10-6M
Reaction remains independent to a lower [H2] before becoming first order
The rate changes non-linearly with [H2]
The first scenario is adopted yielding a conservatively low rate constant
This procedure is conservative since it minimizes the effect of H2 on fuel corrosion
A similar procedure is adopted for other reactions involving H2

## Slide 39
The influence of H2O2 Decomposition
Experiments show decomposition occurs
The O2 produced reacts much more slowly with UO2 than H2O2
No detailed kinetic analysis has been performed

## Slide 40
Factors Influencing the Critical [H2]
The Critical [H2] / μmol L-1
Time since emplacement in the repository / year
α dose rate
α
β
ϒ
Dose rate at fuel surface (Gy/a)
Time since discharge (a)
1 E +07
1 E +06
1 E +05
1 E +04
1 E +03
1 E +02
1 E +01
1 E +00
10 102 103 104 105 106 107
10 102 103 104 105

## Slide 41
Factors Influencing the critical [H2]
H2O2 decomposition ratio
Fraction of H2O2 going to decomposition
rather than fuel corrosion
R. Pehrman, M. Trummer, C.M. Lousada, M. Jonsson, J. Nucl. Mater. 430 (2012) 6.
L. Wu, D.W. Shoesmith, Electrochim. Acta 137 (2014) 83.
L. Wu, J.S. Goldik, D.W. Shoesmith, J. Electrochem. Soc. 161(6) (2014) C363.
The Critical [H2] / μmol L-1
H2O2 decomposition ratio

## Slide 42: While the groundwater entering the failed container will be anoxic H2O radiolysis due to radioactive decay within the fuel will establish oxidizing conditions
The fuel will corrode and release radionuclides at a rate determined by the radiolytic oxidizing conditions
Corrosion as UVI
Dissolution as UIV
? ?
RN
RN
Only alpha radiation significant
Radiolytic Corrosion and

## Slide 43
Reactions Inside a Failed Container
M.E. Broczkowski, J.J. Noël, D.W. Shoesmith, J. Nucl. Mater. 346 (2005) 16.
M.E. Broczkowski, J.J. Noël, D.W. Shoesmith, J. Electroanal. Chem. 602 (2007) 8.
M.E. Broczkowski, P.G. Keech, J.J. Noël, D.W. Shoesmith, J. Electrochem. Soc. 157 (2010) C275.
4