## Slide 1: Emulsions and Prussian Blue Analogues: Towards new nanomaterials for Cs uptake
Jérémy Causse, CEA Marcoule, Insitut de Chimie Séparative, France
MRS2017, Sydney, November 02nd

## Slide 2
Definitions
EMULSIONS
Oil-in-water (O/W) or water-in-oil dispersions (W/O)
Surfactant needed to stabilise liquid/liquid interface
Droplets size from nm to mm
Template for macro/mesoporous materials
W
O
PRUSSIAN BLUE ANALOGUES
AlkxMy[M’z(CN)6]n …
… but we will stay focused on KxMy[Fe(CN)6]n
Easy to prepare
Cs uptake (nuclear decontamination)

## Slide 3
PBA formation
K+
K+
K+
K+
[Fe(CN)6]4-
M2+
Classical PBA or Metal Hexacyanoferrate (MHCF)
K acts as charge compensator
Exch. K-Cs
PRUSSIAN BLUE ANALOGUES
Liquid Waste treatment
Cs immobilization on solid support
Design of MHCF functionalized silica

## Slide 4
Emulsions
Microemulsion
Transparent
Nanodroplets
Template for nanoparticles (NPs)
HIPE
High-Internal Phase Emulsion
FINNER PHASE >50%
White
5mm < Droplet size < 20mm
Template for porous monoliths
Rdroplets=1.7nm
 Not enough time 

## Slide 5
HIPEs for monolith synthesis

## Slide 6
HIPE for macro/mesoporous monoliths
Si(OH)4
Si(OH)4
Si(OH)4
Si(OH)4
Si(OH)4
Si(OH)4
Si(OH)4
Si(OH)4
Si(OH)4
Si(OH)4
Si(OH)4
Si(OH)4
Si(OH)4
Si(OH)4
Si(OH)4
Si(OH)4
Si(OH)4
Si(OH)4
Foil around 73%vol
Silica precursor in water phase
Oil removal to empty macropores
Materials for continuous processes (not possible with powder)
Interconnected macropores
1-20 mm
Mesopores
2-10 nm
SEM
TEM

## Slide 7
Functionalised monoliths with PBA particles
Premaking of PBA NPs
Use of a colloidal suspension as precursor
Metal ions in the aqueous phase
Use of metal species as nucleation point for PBA particles growth
Design of PBA NPs with O/W interfacial activity
Use of a Pickering emulsion as precursor
3 different functionalisation routes
1
2
3

## Slide 8
1. Colloidal suspension
CuHCF colloidal suspension
CuFC
R
nCN
XRD
FTIR

## Slide 9
1. Colloidal suspension
Sorption capacity of 30-40 mg/g
24 hours contact time with NP 0.2%wt : Afinal=5500Bq/l , DF=7,5
24 hours contact time with NP 1.8%wt : Afinal=600Bq/l , DF=69
Synthetic solution: 41250 Bq/l of Cs137 (1. 10-10M) + 0,5M NaNO3 + SO42- + PO43- + K + Mg + Ca (1,10-3M)

## Slide 10
1. Colloidal suspension: salting-out
21 mai 2014
Oil
Oil
Oil
Oil
Oil
Oil
[NPs] ↑
NPs favours dehydration of P123
P123 « is » more hydrophobic
Hydrophobic core of the micelle is bigger
P123 cmc decreases
More micelles with bigger core for the same concentration of [P123]
[P123] =

## Slide 11
2. Metal Ions
Co2+
Co2+
Co2+
Co2+
Co2+
Co2+
Co2+
Co2+
Co2+
Co2+
Co2+
Co2+
Co2+
Co2+
Co2+
Co2+
Co2+
Co2+
Calcination 500°C
Impregnation with aqueous solution of K4FeCN6
Co-monolith
Zn-monolith
Cu-monolith
Only metal is present during monolith synthesis
Calcination is possible because MHCF is not present yet
Monolith mechanical strength is increased

## Slide 12
2. Metal ions
Co
Zn
Cu
SEM: Cubic particles (from 50nm to 300nm) inside macropores
BET: decrease of specific surface after impregnation
SAXS: decrease of the intensity of mesopores signal
BET+SAXS: presence of some smaller NPs inside mesopores? (no proof with TEM)

## Slide 13
2. Metal ions
7,4%wt CoPBA
7,4%wt ZnPBA
6,9%wt CuPBA
Bulk
Silica Monolith
[Na]/[Cs]=10
≈ 7%wt PBA particles in the monoliths
Cs sorption capacity ≈ 25mg/g for ZnPBA
Same efficiency hierarchy for bulks and monoliths

## Slide 14
3. Pickering emulsions
Surface modification
H
H
H
H
H
H
H
H
H
L
L
L
L
L
L
L
L
L
H = PDDA
L = CH3-(CH2)n-NH2
PBA NPs very hydrophilic
Not active at O/W interface
Surface modification needed
With PDDA: Interfacial activity
With Alkylamines: No interfacial activity
Interest: Location of PBA on the surface of macropores
PDDA

## Slide 15
3. Pickering emulsions
CuHCF NPs covered with PDDA lower water/cyclohexane interfacial tension values

## Slide 16
3. Pickering emulsions
O/W 50/50 mix
Stable emulsions for [NPs]=8g/L
Creaming due to oil buyoancy
Road to functionalised materials
To be continued…
Wet-SEM image

## Slide 17
II – Microemulsion for NPs synthesis

## Slide 18
Core shell nanoparticles PBA@SiO2
Cu2+
[Cu(AOT)2]=0,044M
isooctane
w=5
[Na(AOT)] = 0,1M
isooctane
[K4Fe(CN)6]=0,05M
w=5
Basic condition NH4OH (1,338 M)
h= 4,8
TEOS
2)Growth of a silica shell
1)Synthesis of CuHCF NPs
Very stable µemulsion
Generally, more concentrated system
More variable parameters (w, [K2CuFe(CN)6], pH, [TEOS])
easier to characterize
1) Modification of the surfactant
Ion exchange
Cu(NO3)2
2) Synthesis of core-shell NPs

## Slide 19
Core shell nanoparticles PBA@SiO2
STEM-HAADF images
DNP=20-30 nm
Dcore=2-4nm

## Slide 20
Why those NPs?
To use it as materials precursor
Membranes, gels, monoliths …
HIPEs stabilisation
A model material for separation/conditioning strategy
Before irradiation
After irradiation
Irradiation with heavy ions
Densification of the mesoporous silica1
A possible closure of the material
Troom; Ar:20MeV, 1015 cm-2
Directly a containment material?
1 S. Dourdain, X. Deschanels, G. Toquer, C. Grygiel, I. Monnet, S. Pellet-Rostaing, A. Grandjean J. Nucl. Mat. (2012), 427, 411-414

## Slide 21
Outlook
HIPE - Monoliths
Silica support is controlled
Other inorganic matrices
Reverse W/O HIPE with O=SMP10
SiC monoliths for solar energy
SiCO monoliths with mechanical strength increase with regard to SiO2
SMP10: SiC or SiCO precursor

## Slide 22
Microemulsion - NPs
Directly a containment material?
Before irradiation
After irradiation
Irradiation with heavy ions
Densification of the mesoporous silica1
A possible closure of the material

## Slide 23
Acknowledgements
Alicia Sommer-Marquez
Post-Doc
Martin Mayer
Master Trainee
Clémentine Mansas
Ph-D student
Najat Talha
Technician