## Slide 1: Preparation of Ln1-2xCaxThxPO4.nH2O rhabdophane-type as low precursors to monazite-Cheralite ceramics Danwen Qin, Adel Mesbah, Stéphanie Szenknect, Nicolas Dacheux, Nicolas Clavier
Adel.mesbah@cea.fr
Thorium incorporation in phosphates matrices: the case of xenotime
Adel Mesbah, Nicolas Clavier, Stéphanie Szenknect, Janeth Lozano-Rodriguez, Nicolas Dacheux.

## Slide 2: Long term disposal of nuclear wastes
Conditioning and storage of High level Wastes: Actinides

## Slide 3: Which Matrix?
Different matrices have been considered
  Glass matrices
    Borosilicate (R7T7 in France)
    ATS (Alkaline-Tin-Silicate)
    LaBS: Glass enriched with lanthanides
    Glasses containing high amount of phosphates
  Ceramics
    Pyrocholore (Ln2Ti2O7, CaPuTi2O7)
    Brannerite
    Zirconolite (CaZrTi2O7)
    Perovskite (CaTiO3)
    Silicate : Zircon (ZrSiO4), coffinite (USiO4)
    Phosphate : Monazite, xenotime (LnPO4), Cheralite (CaAn(PO4)2), Apatite, thorium phosphate diphosphate (TPD)
  Glass-ceramics

## Slide 4: REEPO4. nH2O compounds
1- A. Mesbah et al, Cryst. Growth. Des, 14 (10), 5090–5098, 2014, 2- Ni, Y. X. et al, Am. Min. 80, 21-26, 1995 3- Hikichi, Y et al, J. Amer. Ceram Soc, 1989, 72, 1073-1076.
Rhabdophane1: REEPO4, 0.667H2O
Churchite3: REEPO4 2H2O
Monazite2: REEPO4
Xenotime2: REEPO4
Monoclinic, C2
Monoclinic, P21/n
Monoclinic, C2/c
Tetragonal, I41/amd

## Slide 5: Why the REEPO4 compounds?
N. Clavier, R. Podor, N. Dacheux, J. Europ. Ceram. Soc. 31 (2011) 941-976 (REVIEW)
Direct substitution : MIII/MIII :
  La  Gd ; Pu  Es ; Tb & Bi (thermal limitations)  Solid solutions
Single substitution : MI/MIII & MIV/MIII :
  MIMIV2(PO4)3 compounds
Coupled substitution : MII+MIV/MIII :
  (MIII,MII,MIV)(PO4) compounds
Coupled mixed substitution : (MIII+XVO4)/(MIV+YIVO4) or (MIII+XVO4)/(MII+ZVIO4)
  (MIII,MIV)(PO4, SiO4)  LaPO4 – ThSiO4 (huttonite, monoclinic P21/n)
            ErPO4 – ThSiO4 (Zircon, tetragonal I41/amd)
Remarkable chemical flexibility

## Slide 6: Incorporation of thorium in REEPO4
Ak2+ + Th4+ <-> 2 REE3+
AkxThxREE1-2xPO4
Challenge:
Synthesis of homogeneous compounds
Use of wet chemistry methods
Thermal conversion to anhydrous compounds: Monazite-cheralite-xenotime
Avoid grinding steps
solid-state chemistry methods
Th4+ + SiO44- <->
REE3+ + PO43-
Th1-xREEx(PO4)x(SiO4)1-x
Th(IV)

## Slide 7: Light REE (La to Gd)
Thermal conversion
Between 500°C and 900°C
- H2O
REEPO4.nH2O
Monoclinic, C2
REEPO4
Monoclinic, P21/n
Rhabdopane
Monazite

## Slide 8: The crystal structure of the Rhabdophane
R. Mooney, acta Crystallographica, 3 (1950) 337-340, Journal of Chemical Physics (1948), 16, 1003-1003
Hexagonal form*, P3121: a= 7.069(3) Å, 6.443(5) Å
Le-bail refinement in P3121
The hexagonal structure doesn’t match with the Synchrotron data
Problem

## Slide 9: LnPO4. 0.667H2O: the monoclinic form
A. Mesbah et al, Cryst. Growth. Des, 14 (10), 5090–5098, 2014
Monoclinic C2, a = 28.0903(1) Å, b = 6.9466(1) Å,
c= 12.0304(1) Å, β = 115.23(1)° and V = 2123.4 (1) Å3 with Z = 24
SmPO4.0.667 H2O
LnPO4. nH2O

## Slide 10: Thermal behavior: toward the monazite
Swelling of 1%
Pellet of SmPO4. 0.667 H2O
Dilatometry experiment
In situ PXRD
CuKα1,2
TGA Analysis
Stabilization of LnPO4.0.5H2O?
Remember
CaSO4.0.5H2O
?
LnPO4.0.5H2O
LnPO4

## Slide 11: In the pursuit of the crystal structure
Mesbah et al, Crystal Growth & Design 14 (10), 5090-5098, 2014
Mesbah et al, J. Solid. Stat. Chem, 249, 221-227, 2017
Monoclinic, C2
Monoclinic, C2
Hexagonal, P3121
SmPO4.0.667 H2O
SmPO4.0.5 H2O
SmPO4
-0,167H2O
-0,5H2O
80°C
213°C
Synchrotron Soleil

## Slide 12: Synchrotron
CaSO4.0.625 H2O
CaSO4.0.5 H2O
SmPO4.0.667 H2O
SmPO4.0.5 H2O

## Slide 13: LnPO4.nH2O
When you think it’s over it begins again
LnPO4
LnPO4.0.5H2O
LnPO4.0.667H2O
Larger Channels

## Slide 14: Light REE (La to Gd)
Thermal conversion
Between 500°C and 900°C
- H2O
CaxThxREE1-2xPO4.nH2O
Monoclinic, C2
CaxThxREE1-2xPO4
Monoclinic, P21/n
Rhabdopane
Monazite-Cheralite

## Slide 15: CaxThxREE1-2xPO4
Synthesis of the hydrated forms
x CaCl2 + x Th(NO3)4 + 1-2x REECl3 + H3PO4 CaxThxREE1-2xPO4. nH2O + 3H+ + 4xNO3- + 3-4x Cl-
Multiparametric study
What is the trick to stabilize pure and homogeneous compounds ?
CaxThxREE1-2xPO4. nH2O
Rhabdophane structure type
Reactants stoichiometry
Heating time
Temperature of synthesis

## Slide 16: Multiparametric study
Reactants stoichiometry
Heating time
Temperature of synthesis
 |  |  | Ca | Th | Pr | P/( Ca + Th +Pr)
110 | 1 | 4 | 0.069±0.003 | 0.110±0.004 | 0.821±0.026 | 1.038 ± 0.036
110 | 2 | 4 | 0.095±0.005 | 0.100±0.005 | 0.805±0.034 | 0.981 ± 0.071
110 | 5 | 4 | 0.083±0.004 | 0.109±0.004 | 0.808±0.031 | 1.042 ± 0.043
110 | 10 | 4 | 0.111±0.004 | 0.105±0.003 | 0.785±0.024 | 1.031 ± 0.035
Need excess of calcium
Ca:Th =10:1
110°C
4 days
Stoichiometric and Pure rhabdophane
D. Qin, A. Mesbah et al, J. Nucl. Mat, 492, 88–96, 2017

## Slide 17: CaxThxREE1-2xPO4.nH2O
D. Qin, A. Mesbah et al, J. Nucl. Mat, 492, 88–96, 2017
Excess of calcium during the synthesis
Limit of substitution at x = 0.15
1000°C

## Slide 18: What’s about the pH of synthesis

## Slide 19: Impact of pH
pH = 8
Ca0.5Th0.5PO4.nH2O
Ca0.5Th0.5PO4
1100°C
Formation of a complete solid solution
Slight change of slope
Cationic ordering ?

## Slide 20
Th1-xErx(SiO4)1-x(PO4)x
From silicates to phosphates

## Slide 21: Th1-xErx(SiO4)1-x(PO4)x
1- Mesbah et al, Inorg. Chem, 2015, 54 (14), pp 6687–6696
Synthesis
Synthesis of pure Th1-xErx(SiO4)1-x(PO4)x in application of the previous protocol1 used to synthesize Coffinite USiO4
250°C for 7 days
Th1-xErx(SiO4)1-x(PO4)x
Huttonite, monoclinic P21/n
Zircon, tetragonal, I41/amd
Attempts by mixing the reactants in acidic conditions led to the formation of amorphous powders

## Slide 22: Coffinite ?
Mesbah et al, Inorg. Chem, 54 (14), 6687-6696, 2015.
250°C, 45 bars, 30 d
[CO32-] = 0.5 M
1 mmol UCl4 + 1mmol Na2SiO3
All syntheses performed in an inert glove box (Ar) to prevent U4+ oxidation
Stoichiometric mixture of reactants in hydrochloric media
Basification up to 8.5 (NaOH)
pH buffering (NaHCO3)
Hydrothermal treatment
×
11.3

## Slide 23: Th1-xErx(SiO4)1-x(PO4)x
1- A.Mesbah et al, Inorg. Chem, 55 (21), 11273-11282, 2016
Stabilization of a synthetic
Th1-xErx(SiO4)1-x(PO4)x
solid solution
Si4+
0.4 Å
Th4+
1.19 Å
P5+
0.31 Å
Er3+
1.14 Å
Formation of solid solution
in agreement with the Vegard’s law

## Slide 24: Local structure: EXAFS
Stability of the Th-O distances
Evolution of the Er-O distances

## Slide 25: Spectroscopy

## Slide 26: Conclusion and Perspectives
Incorporation of An4+
CaxThxREE1-2xPO4.nH2O
Wet chemistry methods
Th1-xErx(SiO4)1-x(PO4)x
Th1-xErx(SiO4)1-x(PO4)x
CaxThxREE1-2xPO4
Chemical durability : dissolution kinetics and thermodynamics
Thermal treatment: conversion
Sintering capability
Pure and homogeneous compounds

## Slide 27: Acknowledgments
26
Laboratory of Evolving Interfaces in Materials
Thank you for your attention !
www.icsm.fr
Alexandra Navrotsky
Rod Ewing