## Slide 1: Synthesis and characterization of brannerite UTi2O6
Adel Mesbah, Stéphanie Szenknect, Nicolas Dacheux
Adel.mesbah@cea.fr
Julien Marcadier, Daniel Beauffort, Anne-Magali Seydoux, Virginie Chapon, Aurelien Eglinger, Phillipe Gonclaves, Yann Batonneau, Maurice Pagel

## Slide 2: Why Brannerite ?
1. Bowell, R. J.; Grogan, J.; Hutton-Ashkenny, M.; Brough, C.; Penman, K.; Sapsford, D. J. Minerals Engineering 2011, 24, 1305. 2. Guilligan.R, Nikoloski. A.N, Minerals Engeneering, 2015, 71, 34-48, 3. S.V.Yudintsev et al, Radiochemstry, 333-348, 2016
Phases identified in different places:2
Elliot Lake (Canada), Mount Isa (Australia), Kirovograd (Ukraine), Crocker Well (Australia), Witwatersrand (South Africa)…
(U, Ca, Y, Ce, La, Pb, Th)(Ti, Si, Al Fe)2O61
Third source of U4+ on earth: UTi2O6
Front-End
Back-End
Possible host ceramic for actinides3
Enter in the composition of the Synroc
Exhausting of U-resources
Ceramics for the specific conditioning of HLW

## Slide 3: How it looks
1. Bowell, R. J.; Grogan, J.; Hutton-Ashkenny, M.; Brough, C.; Penman, K.; Sapsford, D. J. Minerals Engineering 2011, 24, 1305. 2. Guilligan.R, Nikoloski. A.N, Minerals Engeneering, 2015, 71, 34-48, 4. KB Helean et al, J. Nucl. Mater, 231-244, 2003
Crystal structure
Phases identified in different places2:
Elliot Lake (Canada), Mount Isa (Australia), Kirovograd (Ukraine), Crocker Well (Australia), Witwatersrand (South Africa)…
Natural mineral is metamict
UTi2O6: Monoclinic C2/m
a = 9.822 Å, b = 3.824 Å, c 7.036 Å et β = 118.84°
(U, Ca, Y, Ce, La, Pb, Th)(Ti, Si, Al Fe)2O61
Requires heating at 1000°C in order to recover the crystallinity
Thermal treatment
Precedent works: More dedicated to the extraction of U under aggressive conditions
Brannerite: refractory phase to dissolution
Only few thermodynamic data4

## Slide 4: Challenges
Pure Brannerite
Multiparametric dissolution experiments
Free from TiO2 and UO2
Acid concentration, T, complexing agent, Redox

## Slide 5: How to prepare brannerite
1 –F.A. Charalambous et al, Hydrometallurgy, 139, 1-8, 2013
2 – A.E. Ringwood, et. Al, in W. Lutze and R.C. Ewing (Eds), Radioactive Waste Forms for the future “SynRoc”, 223-334, 1988
Alkoxyde/nitrate route2
Titanium Isopropoxyde (IV) + uranyl nitrate solution
Wet milling 16 h, thermal treatment at 1400 °C for 14h
Solid state synthesis
UO2 + TiO2
Uranium oxide (UO2) et de titanium (TiO2) under the form of powders
Different methods: Synthesis of precursors
Acetate method1
uranium acetate + TiOSO4.2H2O in oxalic solution
Evaporation of the solution at 200°C, calcination at 600°C
Milling and thermal heating at 1200°C for 96h

## Slide 6: Which atmosphere?
E.R Vance, et al, J. Amer. Cerm. Soc, 141–144, 2001
Ar/H2
Ti3O5 + UO2
Air
TiO2 + U3O8
Ar or N2
UTi2O6 + UO2
Agrees with what was already reported in the literature

## Slide 7: Synthesis under Argon at 1300°C
Calcination (Ar/H2, 600°C, 5h) + Milling (12h, 30.0 s-1) + pelletizing (~1,5 bar) + thermal treatment (Ar, 1300°C, 72h)
Molar % of UTi2O6 vs UO2
Acetate
Alkoxyde
UO2 + TiO2
Mixing UO2 + TiO2 offers better results
Introduction of the accurate amount of reactants
Long time of Grinding

## Slide 8: Hydroxide method
Evaporation under vacuum: High specific surface area
Direct thermal treatment at 1300°C during three days under Ar (Low Oxygen content)
Eliminate the grinding step
U(IV) + Ti
HCl
msynthesised ≤ 1 g
J. Martinez, Patent FR3016360 – WO2015/107086, 2015
Room temperature
Excess of NH4OH
Washing
(water + ethanol)
Precipitate
+
EtOH
Drying under vacuum
T = 40oC

## Slide 9: Synthèse par voie hydroxyde
One step synthesis
Free from TiO2
Free from UO2
Pure brannerite in a couple of days

## Slide 10: Thermal behavior

## Slide 11: In Situ PXRD under N2
5°C/min
3h
1h
1100°C
1h for each PXRD pattern
collection
Use of UO2 and TiO2 after 6 hours of mechanical grinding

## Slide 12: In Situ PXRD under N2
Crystallization of U3O8 + TiO2
40 °C
100 °C
200 °C
300 °C
400 °C
500 °C
600 °C
700 °C
800 °C
900 °C
grinding of UO2 + TiO2 during 12h
U3O8 + TiO2 nanometric
Crystallization U3O8 + TiO2
500°C
Oxidation of uranium

## Slide 13: In Situ PXRD under N2
600 °C
700 °C
800 °C
900 °C
1000 °C
1100 °C
1100 °C
1100 °C
1100 °C
Crystallization U3O8 + TiO2
1000°C: reduction U3O8
UO2

## Slide 14: In Situ PXRD under N2
Formation of brannerite at 1100°C after 5 hours
Direct synthesis of brannerite from U3O8 + TiO2

## Slide 15
Summary
One step and rapid synthesis of pure brannerite by following the hydroxide method (Ar or N2)
Highly reactive particles
large specific surface area
Pure brannerite
Under inert atmosphere (Argon or Nitrogen) with low oxygen content
UO2
U3O8
Ti - source
Brannerite (UTi2O6)
Improved homogeneity
Lower time of synthesis

## Slide 16: What’s next: dissolution
1- F.A. Charalambous et al, Hydrometallurgy, 139, 1-8, 2013, 2. Guilligan.R, Nikoloski. A.N, Minerals Engeneering, 71, 34-48, 2015 (Review) and multiple research works in hydrometallurgy.
Multiparametric dissolution experiments: determination of the kinetic parameters
Literature
H2SO4 (2M, 70-90°C) in presence of Fe
UTi2O6 + Fe2(SO4)3  2FeSO4 + UO2SO4 + 2TiO2
TiO2 + H2SO4  TiOSO4 + H2O
2Fe2+ + MnO2 + 4H+  2Fe3+ + Mn2+ + 2H2O
Acid concentration, T, complexing agent, Redox
Role of silicate ?
Coffinite (USiO4) was usually found as alteration product in some places
Extraction of uranium
Mostly focused on natural samples

## Slide 17: Leaching/dissolution
0.1 M H2SO4
0.1 M H2SO4+ Si
0.1 M H2SO4+ Fe
% Dissolved U : x 2 with presence of silicate
X 2
X 20
Detailed results coming soon (NEXT Year in Boston)

## Slide 18: Acknowledgments
17
Laboratory of Evolving Interfaces in Materials
Thank you for your attention !
www.icsm.fr
Ressources
Julien Marcadier, Daniel Beauffort, Anne-Magali Seydoux, Virginie Chapon, Aurelien Eglinger, Phillipe Gonclaves, Yann Batonneau, Maurice Pagel