## Slide 1
Effect of Carbonate on Lanthanides Migration Behavior in Compacted Bentonite
Kazuya Idemitsu, Kazuyuki Fujii, Yuki Kakoi, Noriya Okubo, Yaohiro Inagaki, Tatsumi Arima
Dept. of Applied Quantum Physics and Nuclear Engineering, Kyushu Univ., 744 Motooka, Nishi-ku, Fukuoka, Japan

## Slide 2
Objective
To investigate the effect of carbonate ion
for diffusion of lanthanides in compacted bentonite
Lanthanide Atomic No. | La 57 | Ce 58 | Pr 59 | Nd 60 | Pm 61 | Sm 62 | Eu 63 | Gd 64 | Tb 65 | Dy 66 | Ho 67 | Er 68 | Tm 69 | Yb 70 | Lu 71
Actinide Atomic No. | Ac 89 | Th 90 | Pa 91 | U 92 | Np 93 | Pu 94 | Am 95 | Cm 96 | Bk 97 | Cf 98 | Es 99 | Fm 100 | Md 101 | No 102 | Lr 103
Ln3+ + 2CO32-
Ln(CO3)2-
Ln3+ + CO32-
LnCO3+

## Slide 3
Diffusion Experiment
Compacted bentonite
Saturate with
carbonated water
Spike tracer
Diffusion test
analysis
Tracer solution
Ln(NO3)3
Porous filter
Carbonated
water
Bentonite specimen
Ø:10 mm H: 10mm
Acrylic plate

## Slide 4
Experimental conditions
Bentonite | Kunipia F® (Mont.>99%)
Size | 
Dry density | 1.0, 1.2, 1.4 Mg/m3
NaHCO3 | 0.01～1.0 M
Temp. | 25°C
Tracer | Ln(NO3)3 , 10μM, 5µL
Diffusion period | 1～4 weeks

## Slide 5
Measurement
Knife
Bentonite specimen
1N HNO3
(1) Slice
(3) Centrifugation
and
sampling
(2) Extract ions
(4) Ln concentration measurement
with ICP-MS (Agilent 7500)

## Slide 6
Result Er Profile (1.0M, 1.2 Mg/m3)

## Slide 7
Analysis (instantaneous planar source)
・Initial and boundary conditions
・Diffusion equation
・Solution
Da : Apparent diffusion coefficient
[m2/s]

## Slide 8
Analysis (1.0M, 1.2 Mg/m3)
Da=(3.9±0.2)×10-13 [m2/s]

## Slide 9
Dry density dependence
NaHCO3 1.0 M
Da decreased with dry density.

## Slide 10
Carbonate concentrasion dependence
La, Nd
Da decreased.
Eu
Da decreased then increased.
Dy, Er, Lu
Da increased.
0.25
Dry density1.0 Mg/m3

## Slide 11
Carbonate concentration dependence
Dry density1.0 Mg/m3
0.25
La, Nd
Da decreased.
Eu
Da decreased then increased.
Dy, Er, Lu
Da increased.

## Slide 12
pH measurement on and in bentonite
pH electrode (H260GNP, LMS Co., Ltd.)
Pore solution
Upper solution

## Slide 13
Upper solution
 | 1.2 Mg/m3 | 1.4 Mg/m3 | 1.6 Mg/m3
0.1M | 9.4 | 9.3 | 9.4
0.5M | 11.0? | 9.6 | 9.9
1.0M | 9.6 | 9.5 | 9.5
Pore solution
 | 1.2 Mg/m3 | 1.4 Mg/m3 | 1.6 Mg/m3
0.1M | 8.9 | 9.0 | 8.4
0.5M | 10.2? | 9.8 | 10.3
1.0M | 9.3 | 10.0 | 10.0
pH measurement on and in bentonite

## Slide 14
Complexation constant of lanthanides
Lanthanide Carbonate in sea water
Kirk J. Cantrell and Robert H. Byrne, Geochimica et Cosmochimica Acta Vol.51 ,1987
La Nd Eu Dy Er Lu
La Nd Eu Dy Er Lu
b1
b2
GeoChemistWB
GeoChemistWB
K. Spahiu, J. Bruno, TR95-35, A selected thermodynamic database for REE to be used in HLNW performance assessment exercises, 1995.
W. Hummel, et.al., Nagra/PSI Chemical Thermodynamic Data Base 01/01, 2002

## Slide 15
[Ln(CO3)2-], [LnCO3+] fraction
La
Lu
Upper solution
Pore solution ?
LnCO3+ Ln(CO3)2-

## Slide 16
[Ln(CO3)2-], [LnCO3+], Ln2(CO3)3
Ln2(CO3)3 (s)
Ln (CO3)2-
LnCO3+
La
Nd
Eu
Dy
Er
Lu
Ln2(CO3)3 (s)
2Ln3+ + 3CO32-
 | pKsp
Lu | 33.0
Er | 33.6
Dy | 34
Eu | 35
Nd | 34.65
La | 35.3
K. Spahiu et.al. 1985

## Slide 17
Conclusion
In the lower bicarbonate conditions than 0.25 M La had the largest Da of ca. 10-13 m2/s at 1.0 Mg/m3 and Da was small as atomic No. becomes big.
In the higher bicarbonate conditions than 0.25 M Lu had the largest Da and Da was small as atomic No. becomes small.
Especially La and Nd had smaller diffusion coefficient than 10-14 m2/s even at 1.0 Mg/m3. This could be caused by precipitation of carbonate.
Da of Lu increased from 2 x 10-14 to 10-12 m2/s with bicarbonate concentration up to 1.0 M.
[CO32-] in pore water would be much lower than that in contact solution.