## Slide 1: Effects of Li, Ca, Fe, and B on NaAlSiO4 nepheline crystallization in high level waste glasses
John S. McCloy, José Marcial, Mostafa Ahmadzadeh, Yaqoot Shaharyar, Ambar Deshkar, Ashutosh Goel
Glass Wasteforms
Sydney, Australia
Oct 31, 2017
http://labs.wsu.edu/mccloy/
Notes: Effects of Li, Ca, Fe, and B on NaAlSiO4 nepheline crystallization in high level waste glasses
John McCloy, José Marcial, Mostafa Ahmadzadeh, Yaqoot Shaharyar, Ambar Deshkar, Ashutosh Goel (+ others in acknowledgements)
Owing to high concentrations of Al2O3 from dissolved fuel cladding and Na2O from basification of the waste, about half of the high-level waste by volume at Hanford, Washington, USA is rich in both Na and Al. Formulations of high waste-loading glasses result in lower amounts of SiO2, which often leads to undesirable precipitation of nepheline (NaAlSiO4). Nepheline crystallization can be affected by modifiers (Li, Ca) added to lower viscosity and improve electrical conductivity of the melt. Also, B is frequently added to reduce viscosity, and Fe is present in varying amounts from steel tank corrosion. Given the existence of various natural minerals of the stoichiometries (Na,Li,Ca0.5)(Al,Fe,B)SiO4, we sought to study the effects of substitution in the stoichiometric nepheline glass on the resulting crystallization. We summarize here several years of work, including characterization by nuclear magnetic resonance, vibrating sample magnetometry, Raman spectroscopy, thermal analysis, x-ray diffraction, electron microscopy, and electron microprobe.

## Slide 2: Motivation
US HLW
Hanford site
Notes: Of >100 US nuclear waste sites, Hanford, WA is the largest
  177 tanks of >56 million gallons from Pu-production
Much of the High-level waste (HLW) is high in Al & Na
HLW will be mixed with glass-forming additives and vitrified
Desired result: permanent disposal in a geological repository

## Slide 3: The Nepheline problem
Large crystals in some cases
Marcial et al, Proc MRS 1744, 85 (2015)
Canister centerline cooling
Kroll et al, Ceram Trans 260, 159 (2016)
Increased leach rate
Notes: HLW glasses will be poured into canisters and cooled
HLW glass composition may result in nepheline (NaAlSiO4) crystallization
Primary concern: Nepheline extracts Al2O3 and SiO2 from glass
  Increases susceptibility of HLW glass to chemical attack
  Challenge to understand crystallization with many components
  Seek to understand similarities between mid-range order and crystalline structures.
==
Riley, B.J., B.T. Rieck, J.S. McCloy, J.V. Crum, S.K. Sundaram, and J.D. Vienna, "Tellurite glass as a waste form for mixed alkali–chloride waste streams: Candidate materials selection and initial testing," Journal of Nuclear Materials, 424(1–3), 29-37 (2012).
Kroll, J.O., J.D. Vienna, and M.J. Schweiger, "Effects of Al2O3, B2O3, Li2O, Na2O, and SiO2 on Nepheline Crystallization in Hanford High Level Waste Glasses," In Ceramics Transactions 260: Advances in Materials Science for Environmental and Energy Technologies V, John Wiley & Sons, Inc., 159-169 (2016).

## Slide 4: Previous work on nepheline formation
Li et al, Cer Trans 87, 279 (1998)
  ND = SiO2/(SiO2+Al2O3+Na2O) > 0.62
~0.62
Normalized ternary and SiO2
Vienna et al, IJAGS 8, 143 (2016)
Neural network and quantification
Utlak & Besmann, JACERS in press (2017)
Thermodynamic
McCloy et al, IJAGS 2, 201 (2011)
Optical Basicity
Notes: Li, H., B. Jones, P. Hrma, and J.D. Vienna, "Compositional effects on liquidus temperature of Hanford simulated high-level waste glasses precipitating nepheline (NaAlSiO4)," In Ceramic Transactions, D.K. Peeler and J.C. Marra, ed., 87, Environmental Issues and Waste Management Technologies in the Ceramic and Nuclear Industries III, American Ceramic Society, Westerville, OH, 279-288 (1998).
McCloy, J.S., M.J. Schweiger, C.P. Rodriguez, and J.D. Vienna, "Nepheline Crystallization in Nuclear Waste Glasses: Progress Toward Acceptance of High-Alumina Formulations," International Journal of Applied Glass Science, 2(3), 201-214 (2011).
Vienna, J.D., J.O. Kroll, P.R. Hrma, J.B. Lang, and J.V. Crum, "Submixture Model to Predict Nepheline Precipitation in Waste Glasses," International Journal of Applied Glass Science, 8(2), 143-157 (2016).
Utlak, S.A. and T.M. Besmann, "Thermodynamic assessment of the pseudoternary Na2O–Al2O3–SiO2 system," Journal of the American Ceramic Society, n/a-n/a).

## Slide 5: Overview
Crystallography – nepheline & related minerals
Composition from complex waste glasses
Effect of different cooling conditions
Glass composition effects
  Al/B
  Al/Fe
  Na/Ca
  Na/Li

## Slide 6: Crystallography: (A,AE)(Al,B,Fe)SiO4
Malinkoite (MA)
NaBSiO4
Hex P63
Eucryptite (EU)
LiAlSiO4
Hex P6422
Nepheline (NE) NaAlSiO4
Hex P63
Na, Fe: no mineral
Li, Fe: no mineral
Ca, Al: Anorthite
Ca, B: Danburite
  NEPHELINE: (Na,Ca,Mg,□)0.75oval(K,Na,Ca,□)0.25hex(Al,Fe)SiO4

## Slide 7: Nepheline in complex HLW glasses
Nepheline crystal composition (WDS)
Compositional maps, NP-K-2 CCC
Compositional maps, A4 CCC
Marcial et al., Amer. Min., 101(2), 266-276 (2015).
Marcial et al, Proc MRS 1744, 85 (2015)
Selective partitioning
Notes:   Crystallize nephelines of varying composition
    Depends on starting melt comp.
  Crystals partition components
  Microstructures depend on composition

## Slide 8: Effect of heat treatments
Sp
Sp,Ne
CCC: Sp, Ne, ß-Eu
Nepheline = NaAlSiO4
Spinel = Fe3O4
Eucryptite = LiAlSiO4
Apatite = Ca5(PO4)3(OH)
ɣ-Eu, Ne, Sp
β-Eu, Ap
Time-Temperature-Transformation
SRL-131
Jantzen et al., Proc. Mat. Res. Soc., 44 (1985).
Billings et al, Adv Mat Sci ENT 222, 51 (2010)
SB3-Frit 418
A4 glass (high Li)
Nepheline morphology but NOT composition changes
825°C
30hr
Euhedral
nepheline
Marcial et al., Proc. Mat. Res. Soc., 1744 (2015).
Notes: Varying HT schedule of HLW glasses:
  Affects phases
  Affects microstructure
  Does not affect nepheline comp
Billings, A.L., C.M. Jantzen, C.C. Herman, and S.L. Marra, "Phase Stability of Defense Waste Processing Facility (DWPF) Type High Level Nuclear Waste Glasses," In Advances in Materials Science for Environmental and Nuclear Technology, K. Fox, et al., ed., 222, John Wiley & Sons, Inc., Hoboken, NJ, 51-61 (2010).

## Slide 9: Effect of Al/Fe: NaAl1-xFexSiO4
Fe favors bulk nucleation of Neph over surface nucleation of Carneg
Ne and Fe-oxides
Magnetic Meas.
Fe substitutes on Al site at least x=0.37
Highest Fe: no Neph
Shaharyar et al., JACERS 99, 2306 (2016)
Ahmadzadeh et al., J Geophys Res Sol Ear 122, 2504 (2017)
Notes: Along the Na(Al,Fe)SiO4 join:
  Fe influences nepheline crystallization in Na(Al1-xFex)SiO4, leading to highest nepheline fractions when 0.2<x<0.6.
  EPMA measurements determine maximum Fe incorporation of x=0.37 in nepheline
  Mossbauer spectroscopy indicates that Fe redox state (Fe3+/Fetotal) increases by adding more Fe to the glasses.
---
Ahmadzadeh, M., J. Marcial, and J. McCloy, "Crystallization of iron-containing sodium aluminosilicate glasses in the NaAlSiO4-NaFeSiO4 join," Journal of Geophysical Research: Solid Earth, 122(4), 2504-2524 (2017).
Shaharyar, Y., J.Y. Cheng, E. Han, A. Maron, J. Weaver, J. Marcial, J.S. McCloy, and A. Goel, "Elucidating the Effect of Iron Speciation (Fe2+/Fe3+) on Crystallization Kinetics of Sodium Aluminosilicate Glasses," Journal of the American Ceramic Society, 99(7), 2306-2315 (2016).

## Slide 10: Effect of Al/B: NaAl1-xBxSiO4 glass structure
Lee, MS thesis, Seoul Natl Univ, 2017
↑B → ordered around Al
Al-27
↑B → Na-O-Si (NBO on Si) formed not Na-O-B (NBO on B)
O-17
↑B → (Malink or B-albite) B4↑ & B3↓
B-11
B4
B3
Na-O-Si
B-Ø-B
Nepheline
Malinkoite

## Slide 11: Effect of Al/B: Nepheline crystallization
Quenched
Heat treated
B/Al
B-11 MAS NMR
Marcial et al., unpublished data
Change in B4/B3 when Nepheline crystallizes
Some compositions with Si~B~Al (molar) crystallize a lot of Nepheline; changes ring to chain metaborates
Low B in NaAl1-xBxSiO4 allows Nepheline to form
Marcial et al., Proc WM 1632 (2016)
McCloy et al, JNCS 409, 149 (2015)
XRD Rietveld
15-19 wt% B2O3
Notes: Various experiments have studied the effect of Al/B in Na(Al,B)SiO4 and Na(Al,B)Si3O8:
  Increasing B/(Al+B) increases [4]B/[3]B
  All B species are believed to be non-ring
  Trends in dissolution behavior & density caused by residual Na forming Si-NBO, weak B-O-B bonds
    Evidenced by [3]B when Na/(Al+B)=1, Na-O-[4]Si and B-O-B in 17O 3Q MAS
Strong nepheline bands for highly crystallized glasses
Important bands not due to nepheline
  ~685 cm-1 (Q glass)
    Ring metaborates
  ~705 – 710 cm-1 (CCC glass)
    Chain metaborates
---
McCloy, J., N. Washton, P. Gassman, J. Marcial, J. Weaver, and R. Kukkadapu, "Nepheline crystallization in boron-rich alumino-silicate glasses as investigated by multi-nuclear NMR, Raman, & Mössbauer spectroscopies," Journal of Non-Crystalline Solids, 409, 149-165 (2015).
Marcial, J., J. Kabel, M. Saleh, Y. Shaharyar, A. Goel, and J. McCloy, "Effect of B on Crystallization of Li and Na aluminosilicates," Proc. Waste Management WM2016, 16323 (2016).

## Slide 12: Effect of Na/Ca: Nepheline crystallization
Deshkar et al, JACERS 100, 2859 (2017)
Ca for Na →
Na0.3Ca0.7AlSiO4
Na-23 in Na1-xCaxAlSiO4;
↑Ca, Na-O bond lengthen;
Ca goes into Neph Hex channel
oval
hex
Large amounts of Neph after HT when Ca added
XRD Rietv. of HT
NEPH.
Ca
Notes: Along the (Na,Ca0.5)AlSiO4 join:
  [4]Al-O and [4]Si-O tetrahedra are preferred in glass & crystal
  Increasing additions of Ca/Na deshields Na
  Small Ca additions favor nepheline crystallization over Carnegieite
  Near endmembers; Ca may enters nepheline
23Na peak position shifts towards lower frequencies with increasing CaO/Na2O ratio implying towards increase in average Na–O bond length (dNa–O increases from 2.80 Å to 2.90 Å with increasing CaO content) – since the cationic field strength of Ca2+ is higher than Na+, calcium can draw oxygen bonds towards itself, thus forcing sodium site to become bigger.
--
Deshkar, A., J. Marcial, S.A. Southern, L. Kobera, D.L. Bryce, J.S. McCloy, and A. Goel, "Understanding the structural origin of crystalline phase transformations in nepheline (NaAlSiO4)-based glass-ceramics," Journal of the American Ceramic Society, 100(7), 2859-2878 (2017).

## Slide 13: Effect of Na/Li: Nepheline crystallization
Marcial et al., submitted
Li-7
Neph max at low Li
Eucr phases at mid/high Li
XRD Rietv. of HT
No Li: Na→Orth Carneg
Low Li: Li→Neph; complex Li environ.
Mid Li: Na env ~ Neph; Li env ~ γ Eucr
High Li: Na→Eucr; complex Na environ.
NEPH.
Na1-xLixAlSiO4
Na-23
Notes: Along the (Na,Li)AlSiO4 join:
  [4]Al-O and [4]Si-O tetrahedra are preferred in glass & crystal
  Small Li additions favor nepheline crystallization over Carnegieite
  Near endmembers; Li may enter nepheline & Na may enter eucryptite
  Na0.375Li0.625SiO4 highest amorphous fraction after HT through Rietveld

## Slide 14: Implications
Glasses & crystallized glasses should be studied
  NMR, Raman, EPMA, XRD, magnetic methods, Mössbauer
Cooling conditions strongly influence amounts of nepheline, in some cases phases and/or compositions
Fe, Ca, and likely Li go into nepheline; B does NOT go in
High Fe and B generally suppress nepheline
Li and Ca have more complex effects
Future
Quantify amount of Ca that can go into nepheline
Further defined the change in B with crystallization
Explore any role of Ti and of combined effects
Role of alkali/AE coordination on crystallization tendency
Recommend composition adjustments to avoid crystallization
In-situ synchrotron crystallization experiments
Notes: NMR on crystallized glasses aids understanding of environments in glass
offered insight into early vibrational spectroscopy:
  Influences on chemical durability from B are believed to be due to network breaking and NBOs
  Gained insight on influence of mixed cations which promote nepheline over Carnegieite
Determined that the major influence in total suppression of crystallization is the addition of B and Fe in simple glasses

## Slide 15: Collaborators
Funding
Notes: DON’T HAVE A PIC OF PAUL GASSMAN (PNNL) or JAKE AMOROSO (SRNL)

## Slide 16: Thanks!