## Slide 1
~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~ Dr. Hugo L. Bianchi Comisión Nacional de Energía Atómica Química, Centro Atómico Constituyentes, Av. General Paz 1499, (1650) San Martín, Pcia de Buenos Aires ARGENTINA Phone:(54)11 6772 7195 FAX:(54)11 6772 7886
Mobile: (54) 911 4078 8239 bianchi@cnea.gov.ar bianchi.hugo@gmail.com ~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~~
Gerencia de Área
Seguridad y Medio Ambiente
Gerencia de Química
Departamento de Aplicaciones y
Fundamentos de la Química
Laboratorio de Fisicoquímica

## Slide 2: Pyrolysis and Plasma applied to Nuclear ion Exchange Resins Treatment Hugo L. Bianchi, Vittorio Luca, Hernán Castro and Raúl Ariel Rodriguez Constituyentes Atomic Center, CNEA Sydney, Nov. 2, 2017

## Slide 3: Argentinean Nuclear Waste Streams (Set 2016)
Nuclear waste Input to AGE (Ezeiza Atomic Center Area)

## Slide 4: Argentinean Nuclear Waste Streams (Set 2016)
Nuclear waste stock at the nuclear power facilities

## Slide 5
Ion Exchange resins as a problematic waste
Need of a low scale process for Argentina (10 m3 per year generation)
Low temperature pyrolysis as good alternative
Plasma treatment for gas conditioning

## Slide 6: Optimal process requierements
Product stability
Adecuate economic scale
Safety
Environmental Safety
Radiological Safety

## Slide 7: Low Temperature Pyrolisis
Volume Reduction
Low mass transfer to gas phase
The product is the confinement of the mayor fraction of the radionucleides inventory
Stable Product (carbon)
High Safety profile process

## Slide 8: Low Temperature Pyrolysis Process
Interim
Storage
Low Temperature Pyrolysis
Solid Product
Plasma (HPPT)
Selective Sorbents
Filters and Scrubber
Solid Product

## Slide 10
Research advances

## Slide 11: Low Temperature Pyrolysis Process
Interim
Storage
Low Temperature Pyrolysis
Solid Product
Plasma (HPPT)
Selective Sorbents
Filters and Scrubber
Solid Product

## Slide 12
Cation Exchange Resins

## Slide 18
Anion Exchange Resins

## Slide 20: Anionic resins water reabsortion

## Slide 21: Low Temperature Pyrolysis Process
Interim
Storage
Low Temperature Pyrolysis
Solid Product
Plasma (HPPT)
Selective Sorbents
Filters and Scrubber
Solid Product

## Slide 22
Complex Gas Mixture from anionic spent resin

## Slide 23: Anionic funtional group loss start at 125C
Chart: 
Chart: 

## Slide 24: Anion resin C14 behavior
Colaboración con Vaccaro y Alvarado

## Slide 25
Complex Gas Mixture from anionic spent resin
Chart: 127

## Slide 26
Complex Gas Mixture from anionic spent resin
Chart: I-CH3
Chart: I-CH2-CH3

## Slide 27
Complex Gas Mixture from anionic spent resin
Chart: 

## Slide 28
Complex Gas Mixture from anionic spent resin
Chart: Cl-CH3

## Slide 29
Why to use Plasma as gas treatment process?

## Slide 30
Plasma is a promising technology on nuclear aplications
Plasma is a well known technology for gas treatment
No dilution
Flame less
Safe and controllable
Smaller filtering and gas cleaning

## Slide 31
High Safety Profile
High efficiency reaction media
Subatmosferic operation
No dilution of reaction products
If ICP is used, no electrodes needed
Low temperature process
NOx control
High Performance Plasma Treatment advantages

## Slide 32
Chemical reactions in plasma conditions

## Slide 33
Experimental arrangement: inductively coupled plasma laboratory scale flow reactor operating under sub-atmospheric conditions
1. Sample, 2. Injection heater, 3. Quartz reactor, 4. Cold trap,
5. Chemical resistant vacuum pump, 6. High resolution spectrometer, 7. Multi-gas analyzer, 8. Gas mass spectrometer, 9. Scrubber,
10. PC, MFC: Mass Flow Controllers,
HF y Tune: RF generator and matching network.
Ne ≈ 1019 m-3
Te ≈ 7000 K Tg ≈ 350 K

## Slide 34
Destruction and removal ratio with water
Compuesto | m/z | DRE (%)
ETILENDIAMINA | 61 (+) / 121 (+) | 99,9214
N-PROPILAMINA | 60 (+) | 99,9916
N-BUTILAMINA | 74 (+) | 99,0834

## Slide 37
We got a reasonable anhydrous product.
The off gas treatment is simple safe and compact.
The off gas can trap all the C14 emissions if necessary.
A bench scale is needed to validate the concept.
Conclusion

## Slide 38
Thank you

## Slide 40: Setup experimental instrumentado con MS, OES y análisis de gases

## Slide 41
Facilidad de estudio de reacciones químicas en condiciones de plasma

## Slide 43
NUCLEAR FIELD IN ARGENTINA COMISIÓN NACIONAL DE ENERGÍA ATÓMICA
CNEA Headquarters
Bariloche Nuclear Research Center
Constituyentes Nuclear Research Center
Ezeiza Nuclear Research Center
Pilcaniyeu Technological Center
(Río Negro)
Uranium mining and milling (San Rafael - Mendoza)

## Slide 44
DIOXITEK UO2 Production Plant
NASA Nuclear Energy
CONUAR Fuel elements production
FUESMEN Nuclear Medicine
FAE Special alloys production
ENSI D2O Production Plant
NUCLEAR ENTITIES IN ARGENTINA
INVAP Technological development

## Slide 45
2 NUCLEAR POWER PLANTS
1 NUCLEAR POWER PLANT UNDER CONSTRUCTION
6 RESEARCH REACTORS
2 IRRADIATION PLANTS
1 HEAVY WATER PLANT
2 URANIUM MINING FACILITIES
4 ACCELERATORS
1 URANIUM ENRICHMENT FACILITY
376 INDUSTRIAL APPLICATION FACILITIES
3 NUCLEAR RESEARCH CENTERS
1 TECHNOLOGICAL CENTER
3 NUCLEAR MEDICINE SCHOOLS 68 COBALT THERAPY CENTERS
57 BRAQUITHERAPY CENTERS
309 NUCLEAR MEDICINE CENTERS
45 MEDICAL ACCELERATORS
408 IMMUNE ESSAYS LABS
NUCLEAR ACTIVITIES

## Slide 46
NUCLEAR POWER PLANTS
• Atucha I (350 MWe)
• Embalse (650 MWe)
• Atucha II (750 Mwe), to be started
RESEARCH AND PRODUCTION REACTORS
 MEDICAL AND INDUSTRIAL APPLICATIONS
Radioisotopes for medicine and industry, produced in:
• One research/production reactor: 99Mo, 131I, 32P, 153Sm, 51Cr, 177Lu, 192Ir
• Two cyclotrons: 201Tl, 18F, 67Ga, 111In
• Embalse NPP: 60Co
NUCLEAR INDUSTRY
• Uranium mines and UO2 conversion plant
• Fuel elements fabrication for the NPP’s and RR’s
• Zy tubes manufacturing for fuel cladding
• Heavy water production
RADWASTE IS GENERATED DURING OPERATION, MAINTENANCE & FUTURE
DECOMMISSIONING
MAIN PLANTS AND FACILITIES

## Slide 47
NUCLEAR POWER PLANTS
NPP | REACTOR TYPE | POWER [MW] | START UP | EOL (foreseen)
ATUCHA-I | HWR Pressure vessel (Siemens design) | 350 | 1974 | 2019 (extension to 2027)
EMBALSE | HWR-CANDU Pressure tubes (AECL design) | 650 | 1984 | 2012 (extension to 2039)
ATUCHA-II | HWR Pressure vessel (Siemens design) | 750 |  Construction started in 1981  Interrupted in 1994 Re-started in 2006 Start up 2012-2013 |