## Slide 1
Atomisitc simulation
of interfaces in glass/crystal composites
for nuclear wasteforms
p.fossati@imperial.ac.uk
Paul C. M. Fossati, Michael J. D. Rushton & William E. Lee

## Slide 2: Context
From an atomistic point of view
Durability of GCC wasteforms
RuO2 crystals in borosilicate glass
Common crystallite in glass waste forms
Simple structure
Crystal picture: Rose et al., 2011
Effect of secondary phases
in glassy wasteforms
Change melt and glass thermophysical properties
Change radiation resistance?
Change long-term behaviour?

## Slide 3: Modelling approach: material
Simplified material
Sodium silicate glass (Na2O)x(SiO2)1-x
Rutile TiO2, isomorphous with RuO2
Parameter 1: Na concentration (glass polymerisation)
Parameter 2: crystal orientation (interface topology)
Si
Na
O

## Slide 4: Molecular Dynamics model
Empirical potentials
Rigid-ion
Pair interactions (simple and efficient)
Wide range of compounds
Simulation parameters
~ 300 000 atoms
~ 130x130x180 Å
Quench rate: 2.5 K/ps
Potential: Pedone et al., 2006
Scalable
~ ns simulation time, necessary for diffusion
million+ atoms, necessary for fracture
Atomistic model
Empirical (classical) force fields
Calculate atomic trajectories

## Slide 5: Glass/Crystal Composite (GCC) creation
Relaxation
1
Relaxation
2
Quenching
Final relaxation
+ production
Time
Temperature
Ṫ
Quench rate Ṫ
as small as practically possible (but still very high)
needs to be consistent across simulations
Crystal
Frozen during quenching
Glass
Variations considered
crystal orientation (12 interfaces with indices lower than 3)
glass composition (0%, 10% and 20% Na2O)
Glass density
fixed to experimental room-temperature values
volume kept constant during quenching

## Slide 6: Interfaces
Interface orientations
All planes with indices ≤ 2 tested
Examples shown here: (100) and (121)
(100) rutile surface
(121) rutile surface

## Slide 7: Composition of GCC interfaces
Si
O
Ti
Colour code:
z-density plots
show concentration of each species as a function to distance from interface
peaks correspond to enriched layers
on the crystal side: clear, well-defined peaks for most interfaces
Pure SiO2 glass:
➔ Some interfaces show layers in the glass, e.g. (111)
➔ Some don’t, e.g. (121)
➔ Layering up to ~5–8 Å into glass phase
(100) interface; SiO2 glass
(121) interface; SiO2 glass

## Slide 8: Composition of GCC interfaces
(100) interface; 10% Na2O
(121) interface; 10% Na2O
(100) interface; 20% Na2O
(121) interface; 20% Na2O
Si
Na
O
Ti
Colour code:
Effect of sodium:
➔ Does not change interfaces without layers much
➔ At first increases layering
➔ Then reduce it
➔ No real segregation in any case

## Slide 9: Interface layer structure
➔ More aligned tetrahedra for layered interfaces (100)
Orientation distribution of SiO4 in first interface layers
α
SiO4 tetrahedron orientation:
Interface

## Slide 10: Interface layer: (100)
10% Na2O: most tetrahedra are face-connected
20% Na2O: Na compete with tetrahedra
Sodium effect
Na promotes ordering initially
But then limits population of aligned SiO4
Higher Na concentration: Na lines
With Na: most tetrahedra connected to the crystal by 3 O (face-connected)
SiO4 tetrahedra
Na ions
Colour code:
TiO6 octahedra not shown
0% Na2O
Representation of the first silicate layer

## Slide 11: Interface layer: (121)
Sodium effect
Na-rich channels
Na concentration does not seem to change SiO4 ordering
Face-connected tetrahedra not dominant
SiO4 tetrahedra
Na ions
Colour code:
TiO6 octahedra not shown
Representation of the first silicate layer
10% Na2O
20% Na2O: aligned Na
0% Na2O

## Slide 12: Ordering beyond the first glass layer: (100) interface
Arches: successive rings with 4 Si and 1 Ti
Face-connected SiO4
TiO2 crystal
Face-connected tetrahedra
Constrain the glass network
Cause layering in the glass phase
Open possible diffusion channels

## Slide 13: Radiation damage
Ordering perturbations
Ti-rich regions in the silicate layer
Ti coordination environments
  4 (tetrahedra)
  5 (truncated octahedra)
  6 (octahedra)
Core poor in Na
10 keV cascade on (100) interface (x=0.1)

## Slide 14: Radiation damage: density
On the glass side
Low-density core, high-density shell
On the crystal side
Much better reconstruction (smaller low-density core)
No high-density shell
Colour code:
local density
3 g/cm³
1.5 g/cm³
Slice of a 10 keV thermal spike on a (100) interface

## Slide 15: Interfaces: defect energies
Driving force for Tii to move to the glass once they have formed
Si tends to be substitutional
Na tends to be interstitial
Defect | ∆E
Tiglass | 0.5 eV
Tii | 3.5 eV
Nai | 0.7 eV
SiTi | 1 eV
Estimates from simulations with x=0.1

## Slide 16: Acknowledgments
Computing facilities
Imperial College HPC cluster
Thomas (Materials and Molecular Modelling Hub)
Robin Grimes
Erik Hansen

## Slide 17
Atomisitc simulation
of interfaces in glass/crystal composites
for nuclear wasteforms
p.fossati@imperial.ac.uk
Paul C. M. Fossati, Michael J. D. Rushton & William E. Lee