## Slide 1: Hierarchical biomimetic porous tantalum fabricated by liquid metal dealloying
Sanka Mendis
VASSCAA Conference 2018
Supervisors:
Prof. Ma Qian Dr. Wei Xu Dr. Daniel Liang (CSIRO)

## Slide 2
Outline
Fundamentals of Nanoporous Metals Fabricated via liquid metal dealloying
  - Kinetics of Liquid Metal Dealloying
  - Morphology evolution
Mechanical Properties
- Uniaxial micro-compression
- Pico-indentation
- Superelastic Response
Mineralisation
  Wettability
  CaP deposition

## Slide 3
Background
The human bone is a complex natural composite consisted of multi-scale hierarchical structure.
Architecture of typical human bone [Wang, X, et, al. Biomat 2016].
Human bone can be classified as compact cortical bone, and trabecular/cancellous bone.
Cortical bone is a compact soild with ~3-5% porosity
Trabecular bone is a highly porous sponge-like structure with 50 – 90% porosity

## Slide 4: Hierarchical ‘bone-like’ structure
Background
Developing a hierarchical bone structure with a multi-scale interconnected pore structure is essential for bone healing and longevity of the implant.
Macroscale
Microscale
Nanoscale
Bone
Implant
Bone Cells
Integrins
Collagen, proteins and filopodias
Adopted from Gittens RA, et al. Biomaterials 2011.

## Slide 5
Nanoporous surface modification via liquid metal dealloying to create a bicontinuous surface structure
  Nanoporous Surface Modification of Ti-Ta alloys using Selective Dealloying
Macro-porous structure
Micro-porous structure
Nanoporous Surface structure
Selective dealloying will produce a Tantalum rich nano-scale interconnected porous structure

## Slide 6
Liquid Metal Dealloying Process
Schematic of the dealloying method using a metallic melt,
Atom B (orange) dissolves into a melt composed of C atoms (pink)
Remaining atom A (green)
self-organizes into a porous structure by surface diffusion
Miscible, ΔHMix < 0
Immiscible, ΔHMix > 0

## Slide 7
Dealloyed Composite
Bicontinuous Ta/Bi composite is formed once dealloying is finished
Continuous Tantalum ligaments
Interpenetrating Bi-phase
Element | wt%
Bi | 49.9
Ta | 48.0
Ti | 2.1

## Slide 8
Interconnected Nanoporous Structures
Morphology of engineered nanoporous Tantalum surface structures

## Slide 9
Nanoporous Surface
Producing mechanically stable “Monolithic” nanoporous surface on Ti-Ta alloys

## Slide 10
Kinetics of Porosity Evolution
Porosity & Interface evolution during liquid metal dealloying – “Monolithic”
T (°K) | n | k, m
873 | 0.6304 | 1.51610-6
973 | 0.5594 | 3.40010-6
1073 | 0.5420 | 4.88110-6
1273 | 0.4966 | 1.17110-5

## Slide 11
Kinetics of porosity evolution
Underlying dealloying mechanism: activation energy for the growth of dealloying interface
The activation required for interface evolution is ≈ 46.1 kJ/mol
Similar to activation energy required for dealloying in Cu melt [1]

## Slide 12
Kinetics of ligament coarsening
Time dependent ligament coarsening
Type equation here.
Ligament coarsening expressed as a power function
Activation required for Ligament Coarsening: ~71.7 kJ/mol
Mendis, S, et al. materials characterization 2018 (submitted)

## Slide 13
Nanoporous Surface Characterisation
Interconnected Ta ligaments and evolution of grain boundaries using FIB
Estimated volume fraction of porosity is: ~ 70% ± 4.72

## Slide 14
Ligament Structure Characterisation
High Resolution-TEM characterization of “Monolithic” Tantalum ligaments

## Slide 15
Ligament Structure Characterisation
TEM selective area diffraction of “Monolithic” Tantalum ligaments
Single crystal Tantalum ligaments
Z =[111]/ BCC

## Slide 16
Micromechanical Testing
Uniaxial compression testing of nanoporous Ta micro-pillars
Before Compression
After Compression
Densification

## Slide 17
Micromechanical Testing
Phenomelogical model explaining compression modulus
Cell Geometry: single node tetrahedron [2]
lx = 120nm
lx = 92nm
lx = 74nm
2

## Slide 18
Micromechanical Testing
In situ pico-indentation of “Monolithic” Ta Surfaces
Reduced Modulus, ER (GPa) | Hardness (MPa)
3.783 ± 3.46 | 260 ± 49.68

## Slide 19
Superelastic Mechanical Response
Cyclic compression testing of nanoporous Ta micro-pillars
Plastic deformation after 10 cycles of loading
Mendis, S, et al. material research, 2018 (submitted)

## Slide 20
Mineralisation, CaP Formation and Composites
Evaluating the ‘bone-like’ CaP mineralisation on nanoporous Ta and forming osteo-inductive composite surfaces
Bio-activation with HNO3
Calcium Phosphate mineralization
Bone-like CaP precipitation on the nanoporous surface after only 2 days of immersion in simulated human blood plasma solution.

## Slide 21
Wettability of Nanoporous Ta
Surface wettability of nanoporous Ta compared to polished Ti-Ta alloy
(A)
(B)
(c) = Polished Ti-Ta alloy surface

## Slide 22
Bimodal Porosity
Porosity evolution on Ti-Ta surfaces with -phase precipitation
Selective dealloying of the  phase resulting in larger scale pores with various morphologies
Precursor
Dealloyed Surface

## Slide 23
Nanoporous Ta Surfaces
Effect of precursor microstructure on the dealloying and porosity evolution
Lamellar channels
Channel walls consist of open, 3D nanoporous structure with pores and ligaments sizes of 20 ~ 60 nm

## Slide 24
Multi-modal porousity
Multi-scale interconnected porosity by adding Oxygen
Dealloyed pore morphology of acicular -precipitates

## Slide 25
Multi-modal porous Ta Surfaces
Multi-scale interconnected porosity
Nanoporous voids found on the macro-scale porosity walls

## Slide 26
Current & Future Plans
Biocompatibility & Cell attachment on nanoporous Ta surfaces
    In Vitro Cell compatibility
    Cell Proliferation and Differentiation
Bulk Nanoporous Tantalum fabrication
- Bulk Mechanical Properties

## Slide 27
Summary
Establishing liquid metal dealloying parameters for Ti-Ta alloy system in low temperature (Tdealloy< 1000°C) metallic melts
  Characterization of dealloying kinetics: Interface evolution and ligament coarsening
  Characterization of porosity evolution and ligament crystal structure
  Developing mechanically stable surface coatings with multi-scale porosity and ligament morphology
Characterization of micro-mechanical properties of nanoporous Ta fabricated using liquid metal dealloying
  Evaluate scaling laws and mechanical behaviour of the nanoporous Ta ligaments
Evaluation of the mineralization is currently being conducted at various different immersion times
  Vacuum impregnation to create bicontinuous CaP/Ta composite is being explored to improve bioactivity
  Wetting

## Slide 28
References
[1] McCue I, Gaskey B, Geslin P-A, Karma A, Erlebacher J. Kinetics and morphological evolution of liquid metal dealloying. Acta Materialia 2016;115:10-23.
[2] Huber N, Viswanath RN, Mameka N, Markmann J, Weißmüller J. Scaling laws of nanoporous metals under uniaxial compression. Acta Materialia 2014;67:252-65.
[3] Miyazaki T, Kim H-M, Kokubo T, Ohtsuki C, Kato H, Nakamura T. Mechanism of bonelike apatite formation on bioactive tantalum metal in a simulated body fluid. Biomaterials 2002;23:827-32.

## Slide 29
Acknowledgements
Supervisors
- Prof Ma Qian (RMIT University)
- Dr. Wei Xu (Deakin University)
- Dr. Daniel Liang (CSIRO)
RMIT Microscopy and Microanalysis Facility (RMMF)
    Dr. Matthew Field
    Dr. Edwin Mayes
CSIRO Manufacturing (Technical Staff)
    Michael Kellam
    David Renshaw
Ali Ramezan-Nejad & Jackson Smith (Research Colleagues)

## Slide 30
THANK YOU
Questions?