## Slide 1: Surface defect engineering in semiconducting photocatalyst and electrocatalyst
Haifeng Feng
24-07 2018

## Slide 2
Outlines
1. Background
2. Rutile TiO2(110) surface: OV point defects
3. BiOBr nanosheets: lateral pseudo-heterojunctions

## Slide 3
Surface defect in catalysis
Background
G. Li, et al. Chem. Soc. Rev. 2017, 46, 1693
Vacancy
Boundaries
Stacking fault
Adatom
Substitution
Dislocation
Hetero-structure
……
Chemical and physical properties
Active sites
Catalytic activity and selectivity

## Slide 4
*Scanning tunneling microscopes: high resolution > 1 Å
*Molecular beam epitaxial (MBE) deposition: UHV < 5 × 10-11 Torr
*Low temperature: 4 K to 300 K
*In-situ annealing (up to 1200 oC)
*High purity oxygen and water source
*SNOM: ex/in-situ Raman system (TERS and confocal Raman)
Background
AFM System
*Atomic force microscope:
high resolution > 1 Å in Z, > 30 nm
*Kelvin probe force microscope:
surface potential measurement
*Force curves and mapping
* Conductive AFM
IV curves and conductivity mapping

## Slide 5
STM image
A
B
1 × 1 600 oC
1 × 2 900 oC
surface with OVs
C
400 oC
900 oC
600 oC
surface with cross-links
Rutile TiO2(110) surface: OV point defects
Oxygen vacancy (OV)

## Slide 6
Rutile TiO2(110) surface: OV point defects
SEM image of reduced TiO2 single crystal sample cut by a focused ion beam (FIB); inset is an enlarged image of the selected area.
(a) Cross-sectional STEM in ABF (b) Cross-sectional STEM HAADF mode (c) and (d) In-situ EELS Ti-L edge and low-level spectra
Scanning transparent electron microscopy (STEM)

## Slide 7
Rutile TiO2(110) surface: OV point defects
Hydrogen evolution reaction (HER) in alkaline media
(a) LSV data, red solid and green dashed lines are LVS curves before and after cycling1000 cycles, respectively. (b) Cycling stability over 18 h. (c) Tafel plot of the OV-high TiO2. (d) Cdl determined from the linear fitting of the capacitive current vs. scan rate, measured from the cyclic voltammetry (CV) curves.
H. Feng, et al. ACS Catal. 2018, 8, 4288

## Slide 8
Rutile TiO2(110) surface: OV point defects
Height difference
Behaviours under tip plus

## Slide 9
Rutile TiO2(110) surface: OV point defects
In-situ STM studies on electrocatalytic dynamics occurring on TiO2(110) surface associated with oxygen vacancies
In-situ STM observation of dissociation of H2O and OH

## Slide 10
Rutile TiO2(110) surface: OV point defects
(c)
Surface OV
Sublayer OV
Overall Pathways
In summary, sublayer OVs are most important in the electrocatalytic activity!

## Slide 11
BiOBr nanosheets: lateral pseudo-heterojunctions
Close collaboration with Prof. Weichang Hao group in Beihang University:
J. Mater. Chem. A 2018, 6, 2193
2D Mater. 2017, 4, 025102
Dalton Trans. 2017, 46, 15582
J. Phys. Chem. C 2016, 120, 8589
J. Mater. Chem. A 2016, 4, 10992
ACS Appl. Mater. Interfaces 2015, 7, 27592
J. Phys. Chem. C 2015, 119: 14094
Scientific Reports 2014,4:7384
ACS Catal. 2014,4:954-961
D. S. Bhachu, et al. Chem. Sci. 2016, 7, 4832.
H. An, et al. Rare Metal 2008, 27, 243.
H. Feng, et al. 2D Mater. 2017, 4, 025102.
AFM images of BiOBr nanosheets. Scale bars are 1μm.
(a)
(b)
(c)

## Slide 12
SEM, TEM and cross-sectional images of BiOBr nanosheets.
BiOBr nanosheets: lateral pseudo-heterojunctions
(a)
(b)
(c)
(d)
(e)
(f)
(g)
(h)
(i)
(g)
H. Feng, et al. 2D Mater. 2017, 4, 025102

## Slide 13
KPFM can measure the surface potential distribution
BiOBr nanosheets: lateral pseudo-heterojunctions
Confocal Raman mapping

## Slide 14
Photocurrent of individual BiOBr nanosheets.
Proposed diagram of the band alignment at the pseudo-heterointerface in BiOBr-circle nanosheets.
BiOBr nanosheets: lateral pseudo-heterojunctions
In summary, the lateral pseudo-heterojunctions can promote the charge separation and photo-response.

## Slide 15
Acknowledgement
Research Grants
These works were supported by the Australian Research Council (ARC) through LIEF grants (LE100100081 and LE110100099), Discovery Projects (DP140102581, DP160102627, and DP170101467), BUAA-UOW Joint Research Centre Research Grants, aUniversity of Wollongong Research Council (URC) Small Grantnd two.
Colleagues and Collaborators
University of Wollongong: Prof. Shi Xue Dou, Dr. Yi Du, Dr. Xun Xu, Dr. Jincheng Zhuang, Mr. Long Ren, Mr. Liang Wang, A/Prof. Michael Higgins, Dr. David Mitchell in electron microscope centre (EMC) in UOW
Collaborators: Prof. Weichang Hao’s group (Beihang Uni), A/Prof. Zhenpeng Hu (Nankai Uni), Dr. Dr. Jiaou Wang’s group (IHEP, CAS), Dr. Ashley D Slattery (Uni of Adelaide)
STM Team @ UOW

## Slide 16: Closer Title