## Slide 1: Interface-induced Magnetic Polar Metals in Complex Oxides
Meng Meng, Institute of Physics, CAS
mengm@iphy.ac.cn
VASSCAA-9, Sydney, August. 13th, 2018
Funded by U.S. DOE under Grant No. DOE DE-SC0002136.

## Slide 3
Oxide Polar Metals
Can ferroelectrics marry metallicity?
The net electric field inside a conductor is zero by effective charge screening.
Simple answer: No!
dipole
Perovskites with octahedral tilt tend not polar or ferroelectric.
Off-centering polar distortions are driven by B-site bonding preference, but result in insulating phase. (zero electron in d orbitals)

## Slide 4
Criteria: Coexistence of polar structural displacement & metallicity.
Material survey: Oxide polar metals are extremely scarce.
Few oxide examples: BaTiO3-δ, PbTi1-xNbxO3 films, LiOsO3, NdNiO3 films, BaTiO3/SrTiO3/LaTiO3 superlattice
No magnetism
Oxide Polar Metals
Criteria: Coexistence of polar structural displacement & metallicity.
Material survey: Oxide polar metals are extremely scarce.
Few oxide examples: BaTiO3-δ, PbTi1-xNbxO3 films, LiOsO3, NdNiO3 films, BaTiO3/SrTiO3/LaTiO3 superlattice
No magnetism
Polar Metals
Upon electron doping, conduction electrons can be induced.
the amplitude of polar distortion suppressed rapidly
PHYSICAL REVIEW B 96, 165206 (2017)

## Slide 5
Bulk Polar Metal
A centrosymmetric (R3c) to non-centrosymmetric (R3c)
transition in metallic LiOsO3
-
Exhibit a polar distortion by a continuous shift of Li+ ions below 140 K

## Slide 6
Criteria: Coexistence of polar structural displacement & metallicity.
Material survey: Oxide polar metals are extremely scarce.
Few oxide examples: PbTi1-xNbxO3 films, BaTiO3-δ, LiOsO3, NdNiO3 films, BaTiO3/SrTiO3/LaTiO3 superlattice
No magnetism
A site ions displacement: Polar Structure
B site (B-O-B bond): Metallicity
Charge
Polar Metals
Lattice
de-coupled
weak electron-lattice coupling principle
Oxide Polar Metals

## Slide 7
Designing Oxide Polar Metals
?
Polar Metals
?
Coupling?
Coupling?
Magnetic
Lattice
Spin
Coupled
Coupling?
Charge
STO substrate
N*BTO
M*SRO
(N+1)*BTO
Interface
SrRuO3
Itinerant ferromagnetic metal with Tc~160 K
Nonmagnetic Insulator below 4 u.c.
Substrate (SrTiO3)
film

## Slide 8
STEM Structure Characterization
STO substrate
9*BTO
3*SRO
10*BTO
STO
BTO
BTO
SRO
ABF
HAADF
ABO3
Ti
O
Ru
O
O
Ti
O
Growth direction
Image along [110] direction
STO
BTO
BTO
SRO
cSTO = 3.905 Å
4.036 Å
3.92 Å
Polar Displacement from Ru-O-Ru Bonds
B
O
Growth direction

## Slide 9
Electric Transport Properties
Behave ferromagnetic metal in 3 uc sandwiched SrRuO3
STO
3*SRO
Re-emergent Metallicity
STO
3*SRO
STO
9*BTO
3*SRO
10*BTO
STO
9*BTO
3*SRO
10*BTO
Magneto-Resistance

## Slide 10
Magnetic Properties
Emergent Ferromagnetism
High Spin State
t2g
eg
t2g
eg
STO
9*BTO
3*SRO
10*BTO
STO
9*BTO
3*SRO
10*BTO
60*SRO
Ru 4d:
Show strong enhancement of ferromagnetism in SrRuO3

## Slide 11
Density Functional Theory
Polar
Magnetic
Metal
Ru-O
Structure & Magnetic Property
as function of on-site Coulomb U
As function of on-site coulomb U:
Emergence of polar mode
Total suppression of tilt mode
Low-spin to High-spin crossover
Large Spin-Lattice Coupling

## Slide 12
Role of Spin-Lattice Coupling
bulk=7.65
Ferroelectric-like distortion can drive a spin-crossover intermediate spin to high spin state
Qpolexp. ~ 0.1 Å
Figure 4 (b): Variation of the average magnetic moment on Ru (in μB) as a function of magnitude of polar distortion Qpol ( in Å) for different tilt angle Qtilt (in degree °) for U= 3.5 eV

## Slide 13
Magnetic Polar Metal Phase at Interface
We did create magnetic polar metal phase through designing oxide heterostructure
Ru
O
O
Ru

## Slide 14
Thank you!

## Slide 15: Experiments: Growth & XRD
STO substrate
N*BTO
M*SRO
(N+1)*BTO
Trilayer system
Many BTO(N+1)/SRO(M)/BTO(N) on STO with combination of N, M are grown, typical samples includes BTO11/SRO4/BTO10, BTO10/SRO3/BTO9, BTO7/SRO3/BTO6, BTO5/SRO2/BTO4 etc.
The reason of one more layer on surface is that the surface layer of BTO is usually gone during STEM sample preparation
Below shows XRD of BTO11/SRO4/BTO10, there are several features:
  1) Film quality is very good (FWHM = 0.025 is very small for BTO on STO)
  2) Trilayer is fully strained on STO from RLM plot

## Slide 16
STEM EELS Characterization
STO substrate
9*BTO
3*SRO
10*BTO
EELS elemental maps for BTO/SRO/BTO/STO film
STO substrate terminates with TiO2 layer
BTO terminates with TiO2 layer and SRO starts with SrO layer
SRO terminates with SrO layer.
The SRO/BTO interface near substrate side is very sharp with almost no intermixing, the other SRO/BTO interface close to surface has some Ba/Sr intermixing . This is interesting.
Ti
Ru
Ba
Sr
ADF
HAADF
Sr
Sr
STO
BTO
BTO
SRO
Growth direction

## Slide 17
Electric Transport Properties
Behave ferromagnetic metal in SrRuO3
STO
3*SRO
Re-emergent Metallicity
STO
3*SRO
STO
9*BTO
3*SRO
10*BTO
STO
9*STO
3*SRO
10*STO
Magneto-Resistance
STO
60*SRO

## Slide 18
Electric Transport Properties
Thickness dependence of resistivity
The metallicity should not just from the interface

## Slide 19
Geometric Designed Oxide Polar Metals
NdNiO3 on LaAlO3 (111)
BUT the films are not metallic!!
The films are non-centrosymmetric

## Slide 20
Geometric Designed Oxide Polar Metals
BaTiO3/SrTiO3/LaTiO3 “tri-color” superlattice
Nat. Com. 9, 1547 (2018)
HAADF image
Exhibit non-centrosymmetric quasi-two-dimensional metal
Ti
Sr
O
Ba
ABF image
La

## Slide 21
Main Issue: Understanding Interface
the role of octahedral rotations in suppressing ferroelectricity in these materials and show that, as the tolerance factor decreases, rotations alone cannot fully suppress ferroelectricity. Our results show that it is cation displacements (“hidden” in Glazer notation) that accompany the rotations, rather than the rotations themselves, that play the decisive role in suppressing ferroelectricity in these cases.
Charge
Polar Metals
Lattice
de-coupled

## Slide 22
Martenstic transitions
It is a first order solid-solid phase transition with displacive nature (without atomic diffusion) consisting of a homogeneous lattice deformation leading to the new crystal structure.
The Middle Age Knights used to heat their swords in fire and quench them in cold water; after that, the swords became much harder. This method has long been used in the steel industry. The hardening comes from a characteristic microstructure formed by quenching, which is denoted by the term martensite in honour of the German metallographer A. Martens. Initially, the term was ambiguously adopted to denote the microstructure of quenched steels, but, as the nature of this microstructure became better known, the meaning of the word has been gradually clarified and extended to other alloys. The process (a phase transformation) by which the martensite is obtained is a martensitic transformation (MT).

## Slide 23
Zhen
Wang
Ward
Plummer
LSU
Mohammad
Saghayezhian
Hangwen
Guo
Rongying
Jin
Jiandi
Zhang
Yimei Zhu
Sokrates
Pantelides
Vanderbilt
BNL
Saurabh Ghosh
Collaborators
Jiandong
Guo
IOP