## Slide 1
VASSCAA-9 meeting, Sydney, Australia. August 13th-16th, 2018
Dye Giant Absorption and Light Confinement Effects in Porous Microcavities
M. Oliva-Ramírez, J. Gil-Rostra, Adam C. Simonsen, F. Yubero, A.R. González-Elipe,
Institute of Materials Science of Seville, Spain
yubero@icmse.csic.es
Notes: Good morning. Thanks for coming to my contribution to this conference.
My name is Francisco Yubero and the title of my talk is
“Dye Giant Absorption and Light Confinement effects in Porous Microcavities”
This work has been done at the Institute of Materials Science of Seville in Spain

## Slide 2
VASSCAA-9 meeting, Sydney, Australia. August 13th-16th, 2018
Dye Giant Absorption and Light Confinement Effects in Porous Microcavities
M. Oliva-Ramírez, J. Gil-Rostra, Adam C. Simonsen, F. Yubero, A.R. González-Elipe,
Institute of Materials Science of Seville, Spain
yubero@icmse.csic.es
Porous Bragg microcavities as sensing transductors for condensed vapors, transparent fluids and dye solutions
Notes: Good morning. Thanks for coming to my contribution to this conference.
My name is Francisco Yubero and the title of my talk is
“Dye Giant Absorption and Light Confinement effects in Porous Microcavities”
This work has been done at the Institute of Materials Science of Seville in Spain

## Slide 3
Institute of Materials Science of Seville (CSIC-US), Spain
http://www.icmse.cartuja.csic.es/
Size: (45 senior scientists, 55 PhD, post-docs, 30 technicians, administration)
Research units:
Engineered Ceramics for Extreme Environments
Catalysis for Environment and Energy
Mechanochemistry and Reactivity of Materials
Tailored Nanomaterials and Microstructure
Nanostructured Functional Materials
  Nanotechnology on Surfaces research group
  http://sincaf.icms.us-csic.es/
  (7 senior scientists, 5 PhD/post-docs)
Applied/fundamental activity on:
Functional thin films (PVD, plasma-CVD)
Sensors (microfluidic, optical, …)
Fuel cells, solar cells,
Photocatalysis, plasma catalysis,
Dichroic mirrors, luminescent films
1D nanostructures, plasma polymers,
Wetting
…

## Slide 4
OUTLINE OF THE TALK
  Scientific context
  Birefringent Sculptured Bragg Microcavities (SBM): microstructure and optical response
  Application for vapor monitoring
  Application for liquid monitoring
  Light Confinement Effects in SBM
  Summary
Porous Bragg microcavities as sensing transductors for condensed vapors, transparent fluids and dye solutions

## Slide 5
Scientific context: optofluidics & porous thin films
Optofluidics: Integration of photonics and microfluidics
Pores within a thin film: Extremely small detection volumes: femto to nanolitres
Maximize light-analyte interaction (biological/chemical analysis)
Lab-on-a-chip concept
In situ during process reaction (i.e., operando) analysis
Label-free analysis
Liquid analysis: RI
Challenge:
Exploring the opportunities of porous birefringent multilayer structures as optofluidic sensors within a lab-on-a-chip approach
Plasmonics
Photonic crystals
PC Fibers
Nano Lett. 8, 2718–2724 (2008)
Opt. Express 15, 4530–4535 (2007)
Opt. Express 14, 8224–8231 (2006)
Many possibilities based on 2D structures

## Slide 6
Scientific context: fluid/vapor optical sensing with porous films
(SiO2 or TiO2)/H3Sb3P2O14 Bragg stacks
Szendrei et al. Adv. Mater. 27 2015 6341
Infiltration + swelling
  Reflection band position depends on layer(multilayer) thickness and refractive index (RI)
  Individual layer effective RI varies with the amount of condensed vapor and the RI of infiltrated liquid (effective medium theories)
touchless positioning interfaces

## Slide 7
Scientific context: fluid/vapor optical sensing
(SiO2 or TiO2)/H3Sb3P2O14 Bragg stacks
Szendrei et al., Adv. Mater. 27 (2015) 6341
Infiltration + swelling
Liu et al. Optics Express 17 (2009) 16184
Beetles Tmesisternus isabellae
Sensing/reaction based on color change

## Slide 8
Hawkeye et al. Adv. Funct. Mater. 21 2011 3652
Scientific context: optical fluid/vapor sensing
TiO2 STF (distributed Bragg mirror)
color based humidity vapor sensing
L. González-García et al. J. Mater. Chem. 20 2010 6408
SiO2/TiO2 sculptured zig-zag DBM
color based liquid sensing

## Slide 9
Bragg microcavity basic sensing architecture
Bragg microcavity (simple photonic structure) is made incorporating a ”defect” in a Bragg reflector
  Resonant peak RP (narrow pass-band within the photonic band gap) appears
  RP position depends on layer(multilayer) refractive index (RI)
  Individual layers with high open porosity (about 50% void fraction)
  Individual layers effective RI varies with RI of infiltrated liquid (effective medium theories)
    RP position monitors RI of infiltrated phase (well-known)
TiO2
SiO2

## Slide 10
Multilayer preparation:
Technology: PVD-GLAD (EBE)
Materials: TiO2/SiO2
Process pressure 2-3x10-4 mbar
Crucible-substrate distance 50 cm
Deposition rate 6nm/min
φ
α

## Slide 11
Sample preparation: GLAD-PVD technology
Shadowing induces porosity at macro (in-between columns), meso, and micro (inside columns) levels and anisotropic growth
GLAD-PVD film
substrate
0.5 µm
Initial nucleation centers act as “barriers” for the following arriving particles
substrate
source
α
β
shadowed area
Plane of incidence

## Slide 12
Sample preparation: GLAD-PVD technology
substrate
No-shadowing in the direction perpendicular to the plane of incidence
 Column bundling may take place (column fan out)
Kranenburg 1993

## Slide 13
SBM with slanted, zig-zag , vertical architectures
At the surface: Slanted and zig-zag show preferential arrangement of material along the direction perpendicular to the vapor flux
→ bundling phenomena
SiO2
TiO2

## Slide 14
500nm
Slanted p
Within the BM thickness:
Mesoporous extend the whole BM thickness
Self-association of columns (along s direction) even with material change  Fence-bundling
500nm
Slanted s
slanted SBM (FIB-SEM)
p
s

## Slide 15
zig-zag SBM (FIB-SEM)
Δ
π
←Fence-bundling
s
p

## Slide 16
Sample preparation: GLAD-PVD technology
Column bundling modulated by
Process pressure
Initial surface patterning
Temperature
Geometry of deposition
Anisotropic microstructure  Anisotropic optical performance
Higher material connectivity (i.e., polarizability, RI) along s than p direction
Two optical axis (p,s) for normal incidence optical analysis

## Slide 17
BMs with fence-bundling
→ double resonant peak
Optical response of SBM
BMs without fence-bundling
→ single resonant peak
Analysis with unpolarized light

## Slide 18
Fence-bundling induces strong optical polarization activity
Optical activity of BMs
=0⁰ → fence-bundling
=90⁰ →  fence-bundling

=90⁰ (p)
=0⁰ (s)
Analysis with polarized light

## Slide 19
Fast optical axis (low n)
 fence-bundling
Simulated as
uniaxial birefringent BM stack
∆n=(ne-no)=nb-nb
TiO2 ∆n=-0.150
SiO2 ∆n=-0.043
∆ncalcite =-0.172
∆nquartz =+0.009
Slow optical axis (high n) fence-bundling
Optical activity of SBMs

## Slide 20
Optical retarder
Slanted and zig-zag SBMs act as strong wavelength dependent optical retarders
SBMs as optical retarders

## Slide 21
If TII = TX →
SBM behaves as quarter waveplate
SBMs as wavelength dependent retarders (empty)

## Slide 22
Vapor sensing with SBM

## Slide 23
Vapor sensing with SBM
Initial peak shift (pore filling) without loss of birefringence
After a while, birefringence start to diminishes

## Slide 24
Vapor sensing with SBM
Hysteresis as in typical isotherms of mesoporous materials
Gonzalez-Garcia et al.
Nanotechnology 23 (2012) 205701
GLAD TiO2

## Slide 25
Vapor sensing with SBM
Hysteresis loop as in typical Type IV-V isotherm of mesoporous materials:
  First, monolayer/multilayer adsorption (mainly filling the micropores)
  Then, capillarity condensation in mesopores
Birefringence change (note it varies by a factor 5 !!!) monitors site dependent vapor adsorption

## Slide 26
Vapor sensing with SBM
Fill/empty
mesopores
Fill/empty
micropores
Birefringence change monitors site-dependent vapor adsorption (varies by a factor 5)!!!

## Slide 27
Liquid sensing within a microfluidic device
Flow of liquids through the BM
Infiltration is fast, reproducible and robust
Small volumes analyzed (1mm2  1nl)
Lab on a chip

## Slide 28
Linear wavelength dependence of the RP position with the liquid refractive index (200nm/RIU)
ethanol
water
toluene
Cl-benzene
ethanol
water
toluene
Cl-benzene
Resonant peak (RP) positions
air
air
basic optofluidic response of SBM
Oliva-Ramirez et al. ACS Appl. Mater. Interfaces (2013)
(i.e., if RP=0.2nm then RI=0.001 )
Unpolarized light
Vertical SBM

## Slide 29
Optofluidic modulation of BM polarization optical activity
Optofluidic monitoring of glucose in water in a microfluidic device
The ratio A‖/A× can be used as a calibration curve for optofluidic RI determination of liquids
Sensitivity: if A‖/A× varies 0.5%  RI varies 0.0003 RIU (0.2 brix units)
No hysteresis effects !!!

## Slide 30
Microfluidic liquid sensing with SBM
Glucose alcoholic fermentation:
C6H12O6 (glucose 180g) → 2 C2H5OH (ethanol 92g) + 2 CO2 (88g).
nD (@587nm, 25ºC) = 1.333 water, 1.362 ethanol
Jimenez-Marquez et al.
Sensors and Actuators B 225 (2016) 121
Fermentation kinetics

## Slide 31
Microfluidic liquid sensing with SBM
1
3
4
6
5
7
7
Iux
Iuu
2
Patent claimed: “Sensor, apparatus, and method for determining a concentration of solute in a solution” PCT/ES2016/070764
Led light source
Photodiodes as sensors
1 microfluidic chip, 2 SBM transductor, 3 polarizing beam splitter, 4 polarized light, 7 photodiodos

## Slide 32
Motivation: to study light trapping in photonic structures due to electric field confinement
A. Jimenez-Solano et al. Small 11 (2015) 2727)
Colodrero et al. Adv. Mat. 21 (2009) 764
2. To enhance efficiency in dye-sentitised solar cells
1. To enhance luminescence
3. To enhance photocatalytic activity
X. Zheng et al. J. Phys. Chem. C 117 (2013) 21263
The tools needed to make this study
  Porous thin films
  Photonic structure
  Fluidic devices
  Dye solutions
We now focus on:
  Effects of electric field confinement on absorption
Light confinement effects in SBM
Notes: The motivation of this work is in the line of studying light trapping effects in photonic structures due to electric field confinement.
When light propagates in ordered photonic structures, standing waves established, and maxima and minima of the light electric field can be identified at specific locations within the photonic structure
This phenomenon is not new. It is the basis of many research works as these 3 I illustrate here.
1. To enhance the luminescence of dyes incorporated in photonic structures as the one shown here where these authors tune intensity of the luminescence of the dye by placing it at different location within a photonic structure
2. To enhance the efficiency of dye-sentitized solar cells.
3. Or to enhance the photocatalytic activity of 3D inverse opal of titania decorated with dyes
Previous 3 examples show evidences of the light trapping effects in final performance of the developed photonic structure (either luminescence, solar cell efficiency, or photocatalytic activity). Note that previous examples have in common that light absorption has to take place.
In our work we focus on how light absorption of dye solutions infiltrated within porous photonic structures (in particular in the so-called Bragg microcavities) is affected by the electric field localization within the photonic structure.
In the following I am going to introduce the tools we need to make this study:
Basically the porous thin films, photonic structure , the fluidic devices, the dye solutions and the optical characterization set-up

## Slide 33
Photonic architecture: Bragg microcavity optical response
Bragg microcavity is a photonic structure with a central layer (defect) in-between two Bragg reflectors
  Resonant peaks RP appears (narrow pass-band within the photonic band gap)
  RP position depends on layer(multilayer) refractive index (RI)
  Number of RP depends on thickness of central layer
  Note that individual layers are very porous (about 50% void fraction)
  Layer effective RI varies with RI of infiltrated liquid (effective medium theories)
TiO2
SiO2
Notes: The photonic structure we have considered in our experiments is a Bragg microcavity with a large central layer (made using TiO2/SiO2 porous layer) .
For those of you that are not familiar with this type of multilayer designs
A Bragg reflector is just a periodic multilayer with alternate layers with refractive index contrast. It shows a photonic band gap (a reflection band)
A Bragg microcavity consist of a central layer (defect) in between two Bragg reflectors. In these conditions and the appropriate layer refractive index and thicknesses, a resonant peak (a narrow pass-band) appears within the Bragg reflector band.
If the thickness of the central layer is increased, several resonant peaks will appear within the reflection band of the Bragg reflectors. We are interested in these particular type of Bragg microcavities to get simultaneously resonant peaks at the absorption and transparent regions of a dye solution.
Note again that the individual layers of this photonic architectures are porous with open porosity and about 50% voids

## Slide 34
Experimental set-up: microfluidic device including porous BM
Flow of liquids through the BM
Infiltration is fast, reproducible, and robust
Small volumes analyzed (1mm2  1nl)
Lab on a chip
Microfluidic Bragg microcavity including zig-zag architecture
150μm
BM
Spacers
Type 2
BM-Cuvette with Bragg microcavity including slanted architecture
Notes: And these are our fluidic devices. We encapsulate the zigzag porous multilayer described before within a fluidic device that allow to flow of liquids through its open porosity
The liquid infiltration is fast, and reproducible. The volume analyze is about 1nl (remember thickness of multilayer is about 2 micron
We have also for convenience fabricate a homemade BM-cuvette with our slanted porous BM deposited in the inner side of one of its walls.
We have interrogated optically our fluidic devices with this lab-on-a-chip concept

## Slide 35
Why a BM ?
Because there is strong electric field localization at the RP wavelength
Why a porous BM ?
To let liquid flowing through its open pore structure
Why a porous BM with a large defect ?
To allow two resonant peaks RP within the photonic gap so
a RP tuned at the dye absorption (Rhodamine101)
another RP out of the dye absorption
Notes: Summarizing:
We are using a Bragg microcavity because this photonic structure present strong electric field localization at the resonant peak wavelengths.
We need this microcavity to be porous to allow fluid to circulate through its open porosity
And we need a microcavity with a large defect within the photonic gap to get two resonant peaks within the reflection band of the microcavity, to tune one of them to the absorption of a dye solution (in our case Rhodamine 101 – ethanol solutions) and to leave the other in the transparent region of the solution.

## Slide 36
Photonic response of porous Bragg microcavity
BM
Tubes
Type 1
Notes: How are we going to tune the dye absorption and the resonant peak of the microcavity?.
Two strategies:
1. By tilting the angle of incidence of the light with respect to the surface normal of the fluidic device, we can blue shift the resonant peak positions.
Thus, this trick allows to follow the relative differences in response between the two resonant peaks of our microcavity

## Slide 37
150μm
BM
Spacers
Type 2
Photonic response of porous Bragg microcavity: BM-cuvette
x3
x1
Notes: 2. The second strategy is to get profit of the thickness inhomogeneity of the slanted microcavity.
By doing analysis at normal incidence at different point of the BM-cuvette , when lower the total thickness of the microcavity are considered , the resonant peaks shift to lower wavelengths

## Slide 38
Photonic response of Rh101-dye Et-OH solutions infiltrated within BM
P2
P1
P1
P2
Notes: In both cases, the first idea is to scan the position of the lower wavelength resonant peak across the absorption band of the dye solution and to follow the relative evolution of the resonant peak wavelength of the microcavity infiltrated with dye-solutions. And we do that for several dye concentrations
In this figures you can see , first the absorption of the dye-ethanol solution (dotted lines) free (i.e., out of the BM),
Besides, the evolution of the measured transmitted spectra at different spots taken across the BM-cuvette for two dye concentrations. Note that different spots of analysis in the cuvette correspond to microcavities with different total thickness
In the other figure, we can see the wavelength separation of the two resonant peaks for ethanol infiltrated within the microcavity and two dye solutions.
If the infiltrated solution has no absorption (i.e., infiltration of pure ethanol), the separation between the two resonant peaks varies linearly (by changing the total thickness of the BM) , but if the infiltrated liquid has some absorption there is a certain deviation of this linear behavior . The strength of the deviation of this linear response increases with the concentration of the dye solution

## Slide 39
Photonic response of Rh101-dye Et-OH solutions infiltrated within BM
Note dashed lines optical simulations using BM multilayer model, porous EMA layer components, and refractive index and extinction coefficient of solution as fitting parameters
Notes: In this slide, figures a) and b) we show the corresponding transmission measurements as a function of the tilting angle of the device with respect to incident light beam to tune the absorption of the dye solution with one of the resonant peaks.
In figure c) is shown the comparison of the separation between resonant peaks vs tilting angle of the device for ethanol and three Rh101 dye solutions. Again, we observe a deviation of the behaviour of non-absorbing ethanol when one of the resonant peaks is tuned to the absorption of the dye.
Figure d) shows, for comparison, the absorption of free dye solutions
Note also that in figure b) we include dashed lines with optical simulations of our porous microcavities infiltrated with absorbing solutions

## Slide 40
Optical simulations using BM multilayer model, porous EMA layer components, and refractive index and extinction coefficient of solution as fitting parameters
Optical model using WVASE software
Photonic response of Rh101-dye Et-OH solutions infiltrated within BM
Notes: In this slide I give some details about the optical simulation of the BM infiltrated with absorbing solution
We have evaluated the optical characteristics (refractive index and the absorption coefficient) of the dye solution when infiltrated within the Bragg microcavity
For that we have developed optical model (using WVASE software) that take into account the optical characteristics of our system (transparent anisotropic multilayer porous structure infiltrated with absorbing solutions
And we have compared the results to the optical characteristics of the free dye solution (i.e., out of the Bragg microcavities i.e., in a simple cuvette).

## Slide 41
Comparison of photonic response of dye solutions free and infiltrated within BM
When dye-solution infiltrated within BM:
Giant (x20 !!!) dye absorption
Enhanced anomalous dispersion of refractive index
Modified (red shifted) absorption
Notes: The results of the optical analysis of infiltrated microcavities and free dye solutions are shown in these figures.
Above the refractive index and absorption of free dye solutions . Note the scales of the absorption and the effect of this absorption in the anomalous dispersion of the refractive index (about a change of about 0.001 refractive units for dye solution of 10-3 M.
When the dye-solutions are analysed infiltrated within the microcavity, the effect on the strength of the anomalous dispersion of the refractive index is about 0.03 refractive index units, and there is an increase of about a factor 20 in the absorption coefficient with respect to that of the corresponding free dye solution.
Thus we clearly show that when Rh101-ethanol dye solutions are infiltrated in our cavities, a giant absorption of the dye and an strong enhancement of anomalous dispersion of the refractive index take place.
Besides, we observe a red shift of the absorption of the dye when infiltrated within the microcavity.

## Slide 42
Electric field localization/confinement within BM
Notes: The only explanation for this enhanced anomalous dispersion of the refractive index and giant absorption of the dye solutions is that when the dye solution is infiltrated within the microcavity, absorption takes place in an special environment with strongly localised electric field.

## Slide 43
Applications: to enhance sensing (biosensing) capabilities of dye molecules
Note that similar principle applies for enhanced sensitivity of dye molecules nearby plasmonic nanoparticles due to local field enhancement
Design microfluidic devices with photonic crystals with resonant peaks both at dye-absorption and dye-emission wavelengths
500
600
700
absorption
emission
Wavelength (nm)
Electric field confinement within photonic crystal
Notes: This result is not qualitative different than the enhance sensitivity reported of dye molecules nearby plasmonic nanoparticles (also due to the fact that the absorption takes place in an environment of enhanced localised electric fields nearby the surface of these plasmonic nanoparticles).
The most significant result of the analysis we have performed is not the effect itself but the strength of the effect. A factor 20 enhancement in absorption in a photonic structure had not been reported so far.
A possible application of the observed phenomenon might be to develop microfluidic devices including photonic crystals design to have resonant peaks tuned at both absorption and emission bands, in order to get strong enhanced sensitivity to dye molecules in a similar manner than plasmonic nanoparticles.

## Slide 44
Summary
Oliva-Ramírez et al. Sensors and Actuators B 256 (2018) 590; J. Nanophotonics 11 (2017) 046009; ACS Photonics 5 (2018) 984
Fence-bundling in SBM has been identified
Optical activity of SBM is modulated by vapour/liquid infiltration
Site dependent adsorption isotherms
Optofluidic monitoring of RI water-glucose solutions probed
Implementation in prototype to follow alcoholic fermentation kinetics
Electric field localization in porous BM show up as giant absorption and enhanced anomalous refractive index dispersion of infiltrated dye-solutions
Thanks for your attention
Lab on a chip
Notes: Thanks