## Slide 1
On-surface Bottom-up coupling of azine derivatives displaying strong acceptor behaviour
http://www.icmm.csic.es/esisna/
Jose A. Martin-Gago
gago@icmm.csic.es

## Slide 2
b
a
A. P. Côté, et al. , Science, 2005, 310, 1166
On-surface synthesis: from building blocks to networks, supramolecular structures, new molecules or nanostructures
Three pioneering examples

## Slide 3
Three pioneering examples
c
b
a
f
e
d
l
k
j
i
h
g
L. Grill, et al. Nature Nanotechnology, 2007, 2, 687
On-surface synthesis: from building blocks to networks, supramolecular structures, new molecules or nanostructures

## Slide 4
Nature 466, 470-473 (2010)
ULLMANN COUPLING

## Slide 5
Three pioneering examples
G.Otero et al Nature 454, 865-868 (2008))
On-surface synthesis: from building blocks to networks, supramolecular structures, new molecules or nanostructures

## Slide 6
General process
    J. Mendez, M.F. López, J.A. Martin-Gago, Chem. Soc. Rev. 40, 4578–4590 (2011)
Protecting group
v

## Slide 7
On-surface synthesis: Figure of Merits
Formation of new species not available by conventional techniques
Stable structures with efficient electron transfer
UHV- compatible: surface science techniques for a controlled growth and characterization, mainly STM
J.A. Martín-Gago, Nat. Chem. (2011), 3, 11-NEWS AND VIEWS
Protecting
group

## Slide 8
p-aminophenol
two groups (–NH2 and OH), which may be oxidized
Amino
hydroxyl
Presence of two kinds of functional groups with different reactivity, which enables selective reaction.
Which is the group that is more susceptible to be dehydrogenated on surfaces:
amino or hydroxyl?
Can we polymerize aminophenol to form a conductive polymer?
depend on the surface and on face: Cu(110) Pt(111) Cu(111)
Notes: Motivation for studying this simple molecule

## Slide 9
Spheres
Size ≈ 1PAP
54eV
RT
(4X4)
(12 nm x 12 nm), I = 1.1 nA, V = 850 mV
STM
LEED
1 PAP
250°C
(12.2 nm x 12.2 nm), I = 0.31 nA, V = 1035 mV
Elliptical shape
Size ≈ 2PAP
STM
LEED
2 PAP
5 1
-1 2
STM and LEED
Notes: The starting point of our method is the evaporation in ultra-high vacuum (UHV) of p-Ap molecules on an atomically clean Cu(110) surface.
the surface molecular species observed are larger and elliptical in shape and of uniform size, with a bright feature in the center. Further, they are well-organized into
precisely aligned linear rows oriented at an angle of 208 with.
The LEED pattern (see inset) indicates that the molecular arrangement is commensurate with the substrate

## Slide 10
Polymeric 1D chains covering the whole surface!!!!.
4-Aminophenol: adsorption and coupling on Cu(110)

## Slide 11
Which is the structure?

## Slide 12
4nm X 4nm
Δf
Δf
3nm X 3nm
RT
HT
CO-functionalized tip→ intramolecular resolution
Dimers
NC-AFM/STM
Notes: and the nc-AFM image (in the inset) clearly shows the hexagonal carbon rings confirming the presence of single isolated molecules.
The nc-AFM images of the HT phase (Figure 3b) show intramolecular features with two bright protrusions that can be assigned to two equivalent ring structures linked together as a covalent dimer.

## Slide 13
N1s
O1s
hν=650 eV
hν=500 eV
HT
ML
RT
XPS Analysis

## Slide 14
- O1s : No changes
- N1s : iminic (-N=)
reaction takes place through N
- O1s : dehydrogenated
substrate stabilization
- N1s : partially dehydrogenated
Hydrogen bond
Ratio presrves_No disappearance of any of the elements in p-AP
N1s
O1s
hν=650 eV
hν=500 eV
HT
ML
RT
: - Pristine molecule
XPS Analysis

## Slide 15
hν=400 eV
ML and RT : No BE shifts
HT : Shift toward ↓ BE ~ 0.3 eV
Charge
transfer
XPS Analysis

## Slide 16
XPS: -reaction takes place through N
    - O,N dehydrogenated
Konrad Boom et Al.
J. Am. Chem. Soc. 2013, 135, 11501
PAP/Cu(110)
STM images
Nc-AFM: Dimers
No metalorganic
HT PHASE
XPS + STM + NC-AFM
Notes: the STM images show a bright protrusion in the center of the dimer, that is, at the NN position, which can be qualitatively attributed to a charge density increase due to the formation of the covalent bond in the QAz molecule. In an azo-coupled molecule, such as azobenzene, two independent lobes are observed at the rings
with a depression in the center of the molecule.[

## Slide 17
T= 293K = 5.6 ⁰
T= 523 K = 5.4 ⁰
p-polarization
s-polarization
FLAT LYING
Ipol"s"
Ipol“p"
≈ α tan ϒ
C
NEXAFS Analysis
Notes: To obtain further insights into the structure of the HT phase and the role of the surface, we used NEXAFS spectroscopy. By varying the surface orientation with respect
to the linear polarization of the incident light in NEXAFS, the spectral response corresponding to the p*-symmetry components shows dichroic anisotropy (Figure 2 d).[23] The curve that corresponds to the multilayer p-Ap presents no important variations with polarization. However, both RT and HT phases show a strong enhancement of the p* part of the spectra in p-polarization and quenching in s-polarization. This dichroic behavior indicates that the carbon ring is oriented
parallel to the metal surface, with an average tilt of 58,

## Slide 18
C
Molecules present some aromaticity
C K-edge
  Similar electronic
  structure
LT → RT
π* (C=N)
NEXAFS Analysis

## Slide 19
XPS: -reaction takes place through N
    - O,N dehydrogenated
Nc-AFM: Dimers
Electronic structure
Theory
STM images
HT PHASE
XPS + STM + NC-AFM + NEXAFS
?

## Slide 20
EXPERIMENTAL
THEORY
Theory in agreement with experiments for azine structure
Simulations DFT Calculations

## Slide 21
CHARGE TRANSFER : 1,21 e/molecule
AZO (g)
AZINE (g)
AZINE/Cu(110)
Partial conjugation
Azo character
Simulations DFT Calculations
  Intramolecular charge distribution:
TTF on Cu: 0.7 eV

## Slide 22
Bond order analysis

## Slide 23
Strong surface-molecule interaction, the quinoneazine molecule accommodates 1.2 electrons at its carbonyl ends, inducing an intramolecular charge redistribution and leading to partial conjugation of the rings, conferring azo-character at the nitrogen sites.
Organic electronic devices:Molecular electronics → alternative silicon technology → conductive polymers, donor-acceptor compounds improving the interphase between donor-acceptor.
Conclusions
MORE DETAILS : N. Ruiz del Arbol et al. Angew. Chem. Int. Ed. June, 2018

## Slide 24
Oleksander Stetsovych, María Moro-Lagares, Pingo Mutombo, Martin Svec, Pavel Jelínek.
Luca floreano, Albano Cossaro.
Gary J. Ellis.
Irene Palacio, Gonzalo Otero-Irurueta, José I. Martínez, Pedro L. de Andrés, María F. López, José A. Martín-Gago.
ESISNA

## Slide 26
AZINES
Important intermediate molecule in bio –proceses
- important for redox- apications
LT STM/NC-AFM
XPS
NEXAFS
THEORY
Safari et Al.,
RSC Adv., 2014, 4, 46224.
Experiment
Pathway reaction
Quinoneazine
Notes: on-surface chemistry route has now been used to synthesize the strong electron-acceptor organic molecule quinoneazine directly on a Cu(110) surface, via thermally
activated covalent coupling of para-aminophenol precursors.The mechanism is described using a combination of in situ surface characterization techniques and theoretical methods
This molecule has been theoretically proposed for
organic electrodes owing to their extreme redox voltages, and
it can also be employed as an intermediate in the preparation
of several chemically and biologically active compounds.[

## Slide 27
Strong surface-molecule interaction, the quinoneazine molecule accommodates 1.2 electrons at its carbonyl ends, inducing an intramolecular charge redistribution and leading to partial conjugation of the rings, conferring azo-character at the nitrogen sites.
Organic electronic devices:Molecular electronics → alternative silicon technology → conductive polymers, donor-acceptor compounds improving the interphase between donor-acceptor.
Conclusions
MORE DETAILS : N. Ruiz del Arbol et al. Angew. Chem. Int. Ed. June, 2018

## Slide 28
Cu(110)
Pt(111)
?
?
EXPERIMENTS
Molecular electronics → alternative silicon technology → conductive polymers
Role of the surface
5,57 Å
P-aminophenol (PAP)

## Slide 29
STM and XPS : PAP/Pt (111)
Molecules + chains
Molecules
Chains
150 ᴼC
RT
250 ᴼC
At 250°C → Oxygen undergoes a reduction reaction.
N 1S presents two different chemical states
Temperature

## Slide 30
No oxygen @ 250ºC
Leucoemeraldine
Emeraldine
Pernigraniline
XPS Analysis : PAP/Pt (111)
Amine and imine bonds @ 250ºC
0.37
0.63

## Slide 31
Theoretical details
* Density Functional Theory was used effectively combining the localized-basis- set and plane-wave schemes as implemented in the Fireball and Quantum Espresso
(PwScf) Simulation packages. * Inclusion of Van der Waals corrections in a perturbative framework (Grimme Aprox.). * The exchange-correlation effects have been accounted by using the PW91 parametrization, and norm-­conserving scalar­‐relativistic pseudopotentials have been considered to model the ion-­electron interaction.
Theoretical STM Imaging * Tunnelling currents calculated using a Keldysh–Green function formalism, together with the first-­principles tight‐binding Hamiltonian obtained from the local-orbital DFT‐Fireball method. * Pyramidal-terminated clean W-tip. * Constant-current conditions (I=0.2 nA & V=+0.2V).

## Slide 32
Cu(110)
Pt(111)
0.37
0.63
The role of the surface
CONCLUSIONS
P-aminophenol
(PAP)
- Different dimensionality
Different reactivity regarding other methodologies
OSS : discover new materials for innovation
OD
1D