## Slide 1: Capturing interface processes at the atomic scale by high-speed surface X-ray diffraction
National Institute of Advanced Industrial Science and Technology (AIST)
Tetsuroh Shirasawa
Tokyo Gakugei Univ.
Wolfgang Voegeli, Etsuo Arakawa, Toshio Takahashi
National Institute for Materials Science (NIMS)
Takuya Masuda, Kohei Uosaki
Photon Factory, KEK
Tadashi Matsushita
Notes: Thank you chairman for the kind introduction.
My talk is about a high speed surface x-ray diffraction.
We show its capability of capturing interface phenomena.

## Slide 2
Surface X-ray Diffraction
Ideal Surface
Roughness
Displacement
0.1Å
ー Ideal
--- Displacement
-・- Roughness
Substrate
Bragg peak
The most reliable tool for the surface structure analysis
Elements of Modern X-ray Physics (2nd ed., Wiley)
Crystal
Surface
CTR
(Crystal Truncation Rod)
L [r.l.u.]
CTR Intensity [a.u.]
Bragg peak
Notes: Surface x-ray diffraction is probably the most reliable method for the determination of surface and interface structure.
When the electron density of crystal is truncated at the surface, the rod-shaped x-ray scattering appears along the direction perpendicular the surface, it is called CTR.
The CTR profile is very sensitive to the surface structure.
As shown in the example, only a small amount of displacement of the surface atomic layer and surface roughness results in the big change in the CTR profile,
So we can analyze such structures by measuring CTR profile.

## Slide 3
CTR Intensity
Qz
CTR
E-dispersive X-rays
CTR
White SR
Curved crystal
2D detector
Surface
Rainbow SXRD
CTR Intensity
Qz
Surface
Monochro.
X-rays
Conventional method
CTR at once
t 〜 1 s
Point det: t > tens of min.
2D det: t > mins.
Data acquisition time (t)
Point by point
High-speed SXRD
Operando observation
CTR Intensity
Notes: For the quantitative analysis we have to measure the CTR profile.
One drawback of the method is the measurement is time consuming. So we have developed a high speed method.
Commonly for the CTR measurement, a monochromatic x-ray is used and the profile is measured point-by-point by rotating the sample and detector.
The measurement is rather lengthy: typical data acquisition time is more than tens of minutes when a point detector is used and it is more than several minutes when a two-dimensional detector is used.
Our method uses an energy dispersive convergent x-rays which is produced by the curved crystal polychromator, and the scattering distribution is simultaneously recorded by the two-dimensional detector, so that a range of CTR profile is recorded as a function of x-ray energy without moving anything.
The typical data acquisition time is 1s, which allows in operando observation of irreversible surface phenomena.

## Slide 4
Bender
(r = 425mm)
Si(110)
0.2mmt
Polychromator
X-ray window
16 – 23 keV
108 ph/s/eV
Diffractometer
KEK, PF-AR NW2A
Detector
(PILATUS-100K)
χ circle
Polychro.
Gonio. table
Sample stage
X-rays
Detector arm
Detector
Sample stage
(x, y, z, f, tilt)
Gonio. table
q
Polychro. stage
(x, y, z, q, tilt)
χ circle
White SR
Detector arm
Detector stage (d, g)
Polychromator
500–1000mm
~200mm
Tapered undulator
(Side view for clarity)
S
N
S
N
S
N
S
S
N
S
N
S
N
N
Top view
Notes: Here we show the experimental layout.
The experiments were done at KEK PF-AR, and we used a tapered undulator to produce a high-flux white X-ray beam with a smooth spectrum
The typical energy range was 16-23 keV. The x-ray flux is somehow sufficient for CTR measurements.
Whole the goniometer is mounted on the rotatable table to be aligned with respect to the polychromatic x-rays..
The polychromator is a single crystal Si water. It was elastically bent in a solid bender.

## Slide 5
GaAs(001)
GaAs 12 layer
AlAs 8 layer
GaAs 12 layer
AlAs 8 layer
50 reps.
・・・
GaAs/AlAs superlattice
10s
Qz (Q//=0)
4th
3rd
2nd
1st
ー Angle scan (3 hours)
● E-dispersive (10 s)
002
4th
3rd
2nd
1st
Fast CTR measurement
High-speed
Quantitative
Notes: We show an example of the CTR measurement.
The reference sample is the aluminum arsenide and gallium arsenide superlattice.
This is a detector image taken with an exposure time of 10 s.
You see the four superlattice reflections.
The oblique distribution is a diffuse scattering,
This is the intensity plot along CTR. Whole the profile was obtained in the single acquisition and it is identical to the profile obtained by the angle scan method.

## Slide 6
1st
2nd
-3 -4 -5 -6 -7 -8
Log intensity
θ
2θ
kin
kout
qx
qy
qz
qyqz
plane
002
1st
2nd
3rd
4th
qy
Angle scan
(point detector)
104 s
1 s
1s
4th
3rd
2nd
1st
Conversion
Quick characterization of thinfilm structure
Orientation
Domain shape
Strain
Fast Reciprocal Space Mapping
Notes: We can also construct the reciprocal space map from the single image by converting the diffuse scattering distribution to the q space, which is much faster than the angle scan method.
This would be very useful for the study of thin film structures.

## Slide 7
Electrochemical reaction
Thin film growth
Real time monitoring
Notes: We would like to show the examples of real time monitoring of interface phenomena.

## Slide 8
0.5M CH3OH
0.1M HClO4
6H+
CH3OH
+
H2O
CO2
+
6H+ + 6e-
3H2O
2/3O2
+
6e- + 6H+
6e-
Air
Water
Methanol
/Water
CO2
Anode
Cathode
PEM
Direct Methanol
Fuel Cell
H
O
CO2
COad + OHad → CO2 + H+ + e-
O
C
CH3OH → COad+4H+ + 4e-
CO stripping kinetics
Portable DMFC (TOSHIBA)
Methanol electrochemical decomposition on Pt(111)
Notes: The system is the electrochemical decomposition of methanol on Pt single crystal electrode.
This reaction is technologically important due to the fuel cell application.
On the anode surface, the methanol is catalytically reacted with water and finally oxidized to CO2, emitting six protons and six electrons.
The problem of the catalytic reaction is the so-called CO poisoning.
The methanol is immediately decomposed to CO, and the CO covers most part of the surface and catalytic activity is lost.
With increasing potential, OH adsorption occurs and the CO reacts with the surface OH and desorbs from the surface, at the same time the methanol decomposition is activated.
We studied the kinetics of CO poisoning layer to show the capability of the high-speed method.

## Slide 9
5 mV/s
0.5M CH3OH
0.1M HClO4
Dz / Å
O
C
CO2
H
O
50 mV/s
Larger hysteresis
→ CO desorption is rds.
Pt electrode surface structure change during reaction
Displacement
Pt
Shirasawa et al.,
JPC C 121, 24726 (2017)
Δt = 1s
Notes: We measured CTR profile during potential scan with the time resolution of 1 s.
The upper panel shows the vertical displacement of the Pt surface layer obtained by the structure analysis and the lower panel shows the reaction current.
We can see a clear correlation between the displacement and the reaction current,
In the potential region of 0.0–0.4 V the surface is covered with the CO, and the surface layer is lifted up due to the strong interaction with CO.
In the higher potential region, the Dz1 decreases abruptly around 0.6 V due to the desorption of CO. At the same time the reaction current increases steeply.
The point is that in the negative going potential scan, the delta z stats to increase due to the re-adsorption of CO, and it displays the hysteresis which is well correlated with the current hysteresis.
By increasing the potential scan rate, the hysteresis becomes larger, clearly demonstrating that the CO stripping is the rate determining step for the methanol decomposition.
Such a non equilibrium state is observed not be observed in static measurement

## Slide 10
①
②
0.5M CH3OH/0.1M HClO4
0.0V
Dz / Å
O
C
｜
O
C
｜
O
C
｜
O
C
｜
O
C
｜
O
C
｜
H
O
｜
step
edge
O
C
｜
O
C
｜
O
C
｜
O
C
｜
CO2
H
O
｜
・ OH adsorption at step edges
・ CO oxidation at step edges
・ CO diffusion toward step edges
・ Strongly adsorbed less-dense CO layer
CO stripping process
O
C
｜
O
C
｜
O
C
｜
CO2
H
O
｜
H
O
｜
CO2
・ OH adsorption and CO oxidation at terrace
0.8V
Notes: We also studied the behavior of CO stripping by using potential step experiments.
After the potential step from 0.0 V to 0.8 V delta z decreases due to the CO stripping.
Take a close look at the initial region, in the first several seconds delta z does not decrease, instead rather increases from the initial position, and after that it decreases.
This behavior can not be explained by a simple reduction of CO-covered area, because in this model the delta z should decrease from the beginning.
So we propose a model like this,
It is know that OH are preferably adsorbs at defect sites such as step edges, so the CO oxidation would occur at the active sites first.
So, the CO molecules at terrace diffuses toward the active sites in order to compensate the concentration gradient. At the same time, less-dense CO layer is formed.
According to first principles calculations the CO-Pt interaction becomes strong when the CO density is reduced, because of the relaxation of CO-CO repulsive interaction.
Therefore, in such a less-dense CO layer Pt displacement becomes larger due to the stronger interaction.
When OH adsorption occurs on the terrace, the CO stripping is accelerated.
Of course this scenario is speculation. In order to make a firm conclusion we have to perform a systematic study using stepped surfaces.

## Slide 11
Thin film growth
Bi
Bi2Te3
Notes: In the rest of the time we show the thin film growth process of bismuth and bismuth telluride topological insulator very briefly.

## Slide 12
< 1 x 10-8 Pa
70 mm
Be
Baby MBE
Notes: The film was grown in the baby molecular beam epitaxy chamber, which is equipped with a evaporator and ion and non evaporation getter pump.

## Slide 13
Bi thin film growth
Bi wetting layer
Black Phosphorus (BP)
Si(111)-7x7
Si 111
Bi wetting layer
BP(012)
Bulk Bi(001)
Bi(001)
1.3 Å-1
3.4 Å-1
Δt = 1s
Nagao et al., PRL 93, 105501 (2004).
BP → Bulk Bi at surface region
by LEED (λL ~ 1nm）
BP → Bulk Bi whole the film
Notes: The first example is bismuth.
We show the movie of the detector images taken with a time resolution of 1 s.
For each image we can analyze the whole thin film structure from the top to bottom.
In the beginning, the elongation of CTR represents a formation of wetting layer, and then the black Phosphorus structure is formed.
Above a critical thickness of 2 nm, the structure is completely transformed at the bulk Bi structure.
The phase transition was previously observed by LEED, but the penetration depth is about 1 nm.
The present analysis confirms that the structure transition occurs whole the film.

## Slide 14
Bi2Te3 thin film growth
Si(111)-7x7
Si 222
Si 111
Wetting layer
Bi2Te3
Wetting layer
Deformed Bi2Te3
Bulk Bi2Te3
2.0 Å-1
4.0 Å-1
Δt = 1s
Li et al., Adv. Mater. 22, 4002 (2010).
Thinness limit of TI is 2~3 QL
The wetting layer and deformed Bi2Te3 buffer the substrate potential
Notes: The next example is the bismuth telluride topological insulator.
In the beginning the wetting layer is formed, and the fist Bi2Te3 quintuple layer is strongly deformed, and then the bulk like structure is grown on it.
The deformed structure is remained at the interface.
The interface structures would be strongly related to the thinness limit of topological state.
It was shown that the topological surface states disappears below the 2 quintuple layers.
We think the wetting layer and the deformed first quintuple layer play a critical role for the decoupling of the upper layer from the substrate potential and the formation of the topological surface state.

## Slide 15
Operando observation
CTR intensity
Qz
Energy-dispersive SXRD for the high-speed measurement
Electro-decomposition of methanol on Pt(111) electrode.
Thin film growth of Bi and Bi2Te3
Thank you
for your attention!
Summary
White SR
Curved crystal
2D det.
Real-time monitoring of sol.-liq. and sol.-sol. interfaces (Δt = 1s)
Notes: In summary, we have developed an energy dispersive surface x-ray diffraction for the high-speed measurement.
We show examples of the real-time monitoring of the solid-liquid and solid-solid interface systems, demonstrating the capability of the in operando observation.
Thank you for the attention.